Supplementary Information

Graphene Quantum Dot Mediated Atom-Layer Semiconductor Electrocatalyst for Hydrogen Evolution

Bingjie Hu1†, Kai Huang2†, Bijun Tang3, Zhendong Lei3*, Zeming Wang1, Huazhang Guo1, Cheng Lian2*, Zheng Liu3*, Liang Wang1,3*

1Institute of Nanochemistry and Nanobiology, School of Environmental and Chemical Engineering, Shanghai University, 99 Shangda Road, BaoShan District, Shanghai 200444, P. R. China

2State Key Laboratory of Chemical Engineering, Shanghai Engineering Research Center of Hierarchical Nanomaterials, and School of Chemistry and Molecular Engineering, East China University of Science and Technology, Shanghai 200237, P. R. China

3School of Materials Science and Engineering, Nanyang Technological University, 50 Nanyang Avenue, Singapore 639798, Singapore

*Correspondence to: zhendong.lei@ntu.edu.sg (Z. Lei); liancheng@ecust.edu.cn (C. Lian); z.Liu@ntu.edu.sg (Z. Liu); wangl@shu.edu.cn (L. Wang).

†These authors contributed equally to this work

This PDF file includes:

Supplementary Figures. 1-36

Supplementary Tables 1-3

Fig. S1 Difference charge density and bader charge of C atom connected to the -COOH and -OH. The green and red isosurface denote the decrease and increase of electron density, respectively, and the value is ±3 × 10-4 e Bohr-3.

Fig. S2 Gibbs free energy change (ΔG*H) of HER process on four sites of ALQD-SO3.

Fig. S3 Gibbs free energy change (ΔG*H) of HER process on four sites of ALQD-COOH.

Fig. S4 Gibbs free energy change (ΔG*H) of HER process on four sites of ALQD-NH2.

Fig. S5 Gibbs free energy change (ΔG*H) of HER process on four sites of ALQD-OH.

Fig. S6 Bader charge of C atoms near the functional group and C atoms connecting functional group for ALQD-NH2.

Fig. S7 Gibbs free energy change (ΔG*H) of HER process on the C sites connected to the functional group of medium size ALQD.

Fig. S8 Gibbs free energy change (ΔG*H) of HER process on the C sites connected to the functional group of small size ALQD.

Fig. S9 The net weight of ALQD-SO3 which obtained in one-time synthesis.

Fig. S10 TEM image of bulk MoS2.

Fig. S11 AFM image of bulk MoS2.

Fig. S12 (a) XPS survey spectra and High-resolution XPS, Mo 3d (b) and S 2p (c) spectra of ALQD-SO3 before and after 6 months on standing.

Fig. S13 Contact angle of water droplets on the surface of ALQD-SO3 (a) and bulk MoS2 (b).

Fig. S14 TEM images and corresponding lateral size distributions of SO3-GQDs (a), SO3-GQDs-1 (b), SO3-GQDs-2 (c), and SO3-GQDs-3 (d).

Fig. S15 (a) XRD pattern of SO3-GQDs, (b) XRD patterns of SO3-GQDs-1, SO3-GQDs-2 and SO3-GQDs-3.

Fig. S16 (a) FTIR spectrum of SO3-GQDs. (b) FTIR spectra of SO3-GQDs-1, SO3-GQDs-2 and SO3-GQDs-3.

Fig. S17 XPS survey spectra (a) and high-resolution XPS, C 1s (b), N 1s (c), O 1s (d) and S 2p (e) spectra of SO3-GQDs, SO3-GQDs-1, SO3-GQDs-2 and SO3-GQDs-3.

Fig. S18 TEM images of ALQD-SO3-1 (a), ALQD-SO3-2 (b) and ALQD-SO3-3 (c).

Fig. S19 AFM images of ALQD-SO3-1 (a), ALQD-SO3-2 (b) and ALQD-SO3-3 (c).

Fig. S20 XPS survey (a), and high-resolution XPS Mo 3d (b), S 2p (c), C 1s (d) and O 1s (e) spectra of ALQD-SO3-1, ALQD-SO3-2, and ALQD-SO3-3.

Fig. S21 Raman spectra of ALQD-SO3-1, ALQD-SO3-2 and ALQD-SO3-3.

Fig. S22 XRD patterns of ALQD-SO3-1, ALQD-SO3-2 and ALQD-SO3-3.

Fig. S23 Contact angle of water droplets on the surface of ALQD-SO3-1 (a), ALQD-SO3-2 (b) and ALQD-SO3-3 (c).

Fig. S24 LSV curve (a) and corresponding Tafel plots (b) for glassy carbon electrodes deposited with functionalized, ALQD-SO3-1, ALQD-SO3-2 and ALQD-SO3-3. LSVs are taken at 10 mV/s in 0.5 M H2SO4 with a Hg/Hg2Cl2 reference electrode and vitreous carbon counter electrode. Pt and glassy carbon electrodes for HER are included in (a) as a reference.

Fig. S25 TEM images and corresponding lateral size distributions of GQDs-COOH (a) and GQDs-OH (b).

Fig. S26 XRD patterns of GQDs-COOH and GQDs-OH.

Fig. S27 XPS survey spectra (a) and high-resolution XPS, C 1s (b), N 1s (c) and O 1s (d) spectra of GQDs-COOH and GQDs-OH.

Fig. S28 XRD patterns of ALQD-COOH and ALQD-OH.

Fig. S29 Raman spectra of ALQD-COOH and ALQD-OH.

Fig. S30 XPS survey (a), and high-resolution XPS Mo 3d (b), S 2p (c), C 1s (d) and O 1s (e) spectra of ALQD-COOH and ALQD-OH.

Fig. S31 Contact angle of water droplets on the surface of ALQD-COOH (a) and ALQD-OH (b).

Fig. S32 XPS survey spectra (a) and high-resolution XPS, C 1s (b), N 1s (c) and O 1s (d) spectra of GQDs-NH2, XPS survey (e), and high-resolution XPS Mo 3d (f) and S 2p (g) spectra of ALQD-NH2 and bulk MoS2.

Fig. S33 XRD patterns of GQDs-NH2 (a) and ALQD-NH2 (b).

Fig. S34 (a) TEM image and corresponding lateral size distribution of GQDs-NH2. (b) TEM image of ALQD-NH2.

Fig. S35 AFM image of ALQD-NH2.

Fig. S36 LSV curve (a) and corresponding Tafel slope (b) of ALQD-NH2. LSVs are taken at 10 mV/s in 0.5 M H2SO4 with a Hg/Hg2Cl2 reference electrode and vitreous carbon counter electrode. Pt and glassy carbon electrodes for HER are included in (a) as a reference.

Table S1 Element content of ALQD-SO3, ALQD-SO3-1, ALQD-SO3-2, ALQD-SO3-3, ALQD-COOH, ALQD-OH, ALQD-NH2 and bulk MoS2.

|  | Mo 3d (at.%) | S 2p (at.%) | -SO3H (at.%) | C 1s (at.%) | N 1s (at.%) | -NH2 (at.%) | O 1s (at.%) | C=O (at.%) | C-O (at.%) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ALQD-SO3 | 19.35 | 26.17 | 3.8 | 31.74 | 2.81 | - | 19.94 | - | - |
| ALQD-SO3-1 | 16.91 | 23.62 | 3.56 | 35.97 | 4.56 | 0.88 | 18.94 | - | - |
| ALQD-SO3-2 | 17.17 | 28.03 | 3.11 | 32.82 | 3.72 | 0.72 | 18.26 | - | - |
| ALQD-SO3-3 | 16.5 | 27.54 | 2.65 | 33.4 | 2.08 | 0.51 | 20.48 | - | - |
| ALQD-COOH | 14.77 | 28.2 | - | 25.78 | 5.0 | - | 26.23 | 23.0 | 3.22 |
| ALQD-OH | 19.35 | 36.3 | - | 21.27 | 6.43 | - | 16.65 | 0.64 | 16.01 |
| ALQD-NH2 | 17.29 | 32.34 | - | 24.8 | 4.95 | 0.66 | 20.62 | - | - |
| bulk MoS2 | 38.59 | 61.41 | - | - | - | - | - | - | - |

Table S2 Element content of SO3-GQDs, SO3-GQDs-1, SO3-GQDs-2, SO3-GQDs-3.

|  | C 1s (at.%) | N 1s (at.%) | O 1s (at.%) | S 2p (at.%) | -SO3H (at.%) |
| --- | --- | --- | --- | --- | --- |
| SO3-GQDs | 52.2 | 3.84 | 36.47 | 7.49 | 7.49 |
| SO3-GQDs-1 | 70.64 | 5.41 | 19.56 | 4.39 | 4.39 |
| SO3-GQDs-2 | 66.14 | 8.93 | 20.83 | 4.1 | 4.1 |
| SO3-GQDs-3 | 72.52 | 4.15 | 21.18 | 2.15 | 2.15 |

Table S3 Element content of COOH-GQDs, OH-GQDs, NH2-GQDs.

|  | C 1s (at.%) | N 1s (at.%) | O 1s (at.%) | C=O (at.%) | C-O (at.%) |
| --- | --- | --- | --- | --- | --- |
| COOH-GQDs | 69.35 | 3.64 | 27.01 | 22.69 | 4.31 |
| OH-GQDs | 75.73 | 6.96 | 17.31 | 7.42 | 9.89 |
| NH2-GQDs | 65.82 | 8.55 | 25.63 | - | - |