Supporting Information

Understanding Bridging Sites and Accelerating Quantum Efficiency for Photocatalytic CO2 Reduction

Kangwang Wang1, Zhuofeng Hu2, Peifeng Yu1, Alina M. Balu3, Kuan Li1, Longfu Li1, Lingyong Zeng1, Chao Zhang1, Rafael Luque4,5, Kai Yan2*, Huixia Luo1, *

1 School of Materials Science and Engineering, State Key Laboratory of Optoelectronic Materials and Technologies, Guangdong Provincial Key Laboratory of Magnetoelectric Physics and Devices, Key Lab of Polymer Composite & Functional Materials, Sun Yat-Sen University, No. 135, Xingang Xi Road, Guangzhou, 510275, P. R. China

2 School of Environmental Science and Engineering, Sun Yat-Sen University, No. 135, Xingang Xi Road, Guangzhou 510275, P. R. China

3 Departamento de Química Orgánica, Universidad de Córdoba, Campus Universitario de Rabanales, Edificio Marie Curie (C3), Córdoba E-14014, Spain

4 Center for Refining and Advanced Chemicals, King Fahd University of Petroleum and Minerals, Dhahran 31261, Saudi Arabia

5 Universidad ECOTEC, Km 13.5 Samborondón, Samborondón EC092302, Ecuador

*Corresponding author. E-mail: luohx7@mail.sysu.edu.cn (Huixia Luo); yank9@mail.sysu.edu.cn (Kai Yan)

Section I: Experiment section

Synthesis

Preparation of Cu2O nanocubes (NCs):

Cu2O NCs were prepared by adapted from known literature procedure [,]. Specifically, CuSO4∙5H2O (1.5 mmol) and sodium citrate (0.5 mmol) were dissolved into 80 mL of deionized water (DW). Then, 20 mL NaOH (1.25 M) was added to the above solution under stirring. Afterward, 50 mL ascorbic acid (0.03 M) was added to the suspension under stirring for 5 min. The obtained mixed solution was stood for 1 h at room temperature. The precipitate was collected by centrifugation and washed with DW and ethanol several times.

Preparation of Cu2O@In(OH)3 core-shell nanocubes (CSNCs):

A quarter of the as-prepared Cu2O NCs and 11 mg of InCl3 were first dispersed into 40 mL of ethanol/H2O solvent (volume ratio = 1:1) in the presence of 1.33 g of PVP by sonication for 10 min. Then, a Na2S2O3 aqueous solution (1.0 M, 16 mL) was added to the above mixture under stirring. After 1.5 (4.0, 6.0, 8.0, and 10.0) min of reaction, the precipitate was collected by centrifugation and washed with DW and ethanol several times, respectively.

Preparation of In(OH)3 single-shelled nanoboxes (SSNBs):

The as-prepared Cu2O@In(OH)3 CSNCs were dispersed into 20 mL of ethanol/H2O solvent (volume ratio = 1:1). Then, a Na2S2O3 aqueous solution (1.0 M, 8 mL) was added to the above mixture under stirring. After 30 min reaction, the precipitate was collected by centrifugation and washed with DW and ethanol several times.

X-ray Absorbtion Spectra (XAS). The X-ray absorption fine structure (XAFS) spectroscopy of Mo K-edge was collected at the X-ray absorption fine structure for catalysis (XAFCA) beamline of the Singapore Synchrotron Light Source, Singapore. Extended X-ray absorption fine structure (EXAFS) fitting was applied through Athena and Artemis software []. Wavelet transformation (WT) was also employed using the software package developed by Funke and Chukalina using Morlet wavelet with κ = 10, σ = 1 [,]. S02 was obtained from Mo foil and fixed as 0.92. ΔE0 was returned a value of 2.2206 ± 0.4129 eV (3.0 ≤ k ≤ 12.0 Å−1, 1.3 ≤ R ≤ 2.8 Å). The number of variable parameters was 3 out of a total of 8.3906 independent data points, and the R factor for this fit was 1.06%. The Debye-Waller factors were obtained based on the guessing parameters and constrained as 0.004 and 0.002 for Mo−S and Mo−Te, respectively. The delta Rs was based on guessing parameters and fixed as −0.003 and −0.02 for Mo−S and Mo−Te, respectively.

UPS spectra. The work function (Φ) of samples can be obtained by subtracting the cutoff binding energy (ECutoff) from the radiation photon energy (He I α at 21.2 eV), while the valence band (VB) edge and Φ have the following relationship:

|  | ES1 |
| --- | --- |
|  | ES2 |

The bandgaps energy of In2S3, Sv-In2S3, 2H-MoTe2, and Sv-In2S3@2H-MoTe2(5) were calculated by the following equation (Kubelka-Munk (KM) equation):

|  | ES3 |
| --- | --- |

in which α, h, υ, A, and Eg represent the absorption coefficient, Planck constant, light frequency, proportionality, and bandgaps energy, respectively. Combining the Eg values from the UV-Vis absorption spectrum, the conduction band (CB) edge of the nanofiber films was related to VB as follows:

|  | ES4 |
| --- | --- |

TRPL analysis. In terms of TRPL, the decay curves can be well fitted by the following biexponential equations [,]:

|  | ES5 |
| --- | --- |
|  | ES6 |

where I0 represents the baseline correction value, A1 and A2 are the pre-exponential factors. τ1, τ2, and τa represent the lifetime (ns) in different processes, and average lifetime.

Bleach decay kinetics fitting. The bleach decay kinetics in Fig. 4g (320 nm excitation) were fitted with the following equations:

|  | ES7 |
| --- | --- |
|  | ES8 |

Carrier concentration and carrier diffusion lengths (Ld):

|  | ES9 |
| --- | --- |
|  | ES10 |

where U is the Hall voltage, expressed in mv; d is the thickness of the Hall element, expressed in μm; I is the working current, expressed in mA; and B is the magnetic field strength, expressed in T. kB is the Boltzmann’s constant, T is the absolute temperature, μ is the carrier mobility, and τ is the carrier lifetime (Table 1).

CO2 temperature programmed desorption (CO2-TPD) measurements. Typically, Sv-In2S3, 2H-MoTe2, and Sv-In2S3@2H-MoTe2(5) were maintained at 150 ℃ for 1 h in a vacuum environment. Subsequently, the samples were cooled down to room temperature, followed by the exposure of CO2 under 1.0 mbar. After pumping excess CO2 gas, the samples were heated up to 350 ℃ at the rate of 2 ℃·min−1 to measure the desorption spectra during the detection process [].

Incident photon-to-current efficiency (IPCE) and corresponding internal quantum efficiency (IQEpc). The remarkable photoelectric conversion capacity of In2S3, Sv-In2S3, 2H-MoTe2, and Sv-In2S3@2H-MoTe2(5) was also revealed in IPCE profile (Fig. S15c). The detailed IPCE and corresponding IQEpc calculation process via photocurrent measurement is based on equations:

|  | ES11 |
| --- | --- |
|  | ES12 |

where Jp is the photocurrent density, λ represents the wavelength of the monochromatic light, Ilight refer to the incident light power density. The A is the absorbance of the photocatalysts layer on the surface of sample.

Apparent quantum efficiency (AQE) and corresponding IQE (IQEcr). The AQE was determined under above photocatalytic reaction conditions except that five LEDs (420 nm, 3 W) were used as irradiation source. The wavelength-dependent apparent quantum efficiency was measured under the same photocatalytic reaction condition, except for the monochromatic light wavelengths (380, 400, 420, 440, 460, 480, 500, and 520 nm). All the experiments were repeated at least 3 times in parallel to obtain an average value. At the same time, AQE and IQEcr was roughly calculated from the equation []:

|  | ES13 |
| --- | --- |
|  | ES14 |

where A is the absorption of sample solution.

Evaluation of Catalytic Performance. CO2 conversion was calculated according to the following equation:

|  | ES15 |
| --- | --- |

Product selectivity was calculated on a molar carbon basis. Product selectivity was calculated according to the following equation:

|  | ES16 |
| --- | --- |

where Ci indicates the molar fraction of product i and ni is the carbon number of products i.

d-band center. To get the individual orbital components, we employed the code-named “splitdos.dos” to process the output file of the density of states (DOS). The average d-band (d band center) shifts are calculated for the surface metal atoms for both the total d partial DOS and the orbital-resolved d partial DOS. The d band center (𝜀d) is calculated as:

|  | ES17 |
| --- | --- |

where 𝜀 is the electronic energy of states, and 𝑛d(𝜀) is the electronic density of states [].

Work function. The following equation can calculate the work function (Φ) of a material: Φ = Evac−EF, Evac and EF are the vacuum energy and fermi level energy, respectively. In addition, the band structures and DOS of Sv-In2S3, 2H-MoTe2, and Sv-In2S3@2H-MoTe2(5) interface were calculated.

Section Ⅱ: Figures and tables

Fig. S1 a Schematic diagram of preparation process of Sv-In2S3@2H-MoTe2(5). b XRD pattern, c TEM images, d HAADF-STEM and e EDX mapping images (Scale bar = 50 nm), f HRTEM images and SAED pattern of In2S3.

Fig. S2 a TEM, b HRTEM, c HAADF-STEM and EDX mapping images (Scale bar = 50 nm), and d EDX spectrum of Sv-In2S3.

Fig. S3 a TEM, b HRTEM and SEAD pattern, c HAADF-STEM and EDX mapping images (Scale bar = 100 nm), and d EDX spectrum of 2H-MoTe2.

Table S1 Elemental analysis of Sv-In2S3@2H-MoTe2(5) by EDX spectrum.

| Element | Atomic (%) | Molecular formula |
| --- | --- | --- |
| In | 22.15 | In1.00S1.48 |
| S | 32.85 |  |
| Mo | 14.74 | Mo1.00Te2.05 |
| Te | 30.16 |  |

Fig. S4 a EPR spectra of In2S3, Sv-In2S3, and Sv-In2S3@2H-MoTe2(5), respectively. b XPS full-scan survey spectra of 2H-MoTe2, In2S3, Sv-In2S3, and Sv-In2S3@2H-MoTe2(5), respectively. The high-resolution XPS spectra of c Te 3d, d In 3d, e Mo 3d, and f S 2p in 2H-MoTe2, In2S3, Sv-In2S3, and Sv-In2S3@2H-MoTe2(5), respectively.

Table S2 Elemental analysis of as-prepared photocatalysts via XPS spectra.

| Samples | Sv-In2S3@2H-MoTe2(5) | Sv-In2S3 | In2S3 | 2H-MoTe2 |
| --- | --- | --- | --- | --- |
| Method | In/% | S/% | Mo/% | Te/% | In/% | S/% | In/% | S/% | Mo/% | Te/% |
| XPS | 12.65 | 19.1 | 3.07 | 5.45 | 20.64 | 30.61 | 21.7 | 28.29 | 15.43 | 36.13 |

Fig. S5 a Nitrogen adsorption-desorption isotherms, b cumulative intrusion curves, and c BJH pore-size distribution of Sv-In2S3, 2H-MoTe2, and Sv-In2S3@2H-MoTe2(5), respectively.

Table S3 Surface area, pore diameter, and pore volume for 2H-MoTe2, Sv-In2S3, and Sv-In2S3@2H-MoTe2(5), respectively.

| Samples | BET surface area (m2·g−1) | Pore volume (cm3·g−1) | Pore diameters (nm) |
| --- | --- | --- | --- |
| 2H-MoTe2 | 395.46 | 0.175 | 8.20 |
| Sv-In2S3 | 465.95 | 0.127 | 5.93 |
| Sv-In2S3@2H-MoTe2(5) | 495.44 | 0.526 | 4.51 |

Fig. S6 a Mo and b K-edge EXAFS (points) and fit (line) for Sv-In2S3@2H-MoTe2(5), shown in k2 weighted R-space. c WT for the k3 weighted EXAFS contour plots of MoS2.

Table S4 Fitting parameters for Mo K-edge EXAFS for Sv-In2S3@2H-MoTe2(5).

| Paths | CN | R (Å) | σ2 (10−3 Å2) | ΔE0 |
| --- | --- | --- | --- | --- |
| Mo−S | 1.4±0.3 | 2.41 | 0.004 | 2.2206 ± 0.4129 |
| Mo−Te | 4.1±0.2 | 2.72 | 0.002 |  |

Fig. S7 The photos for reaction device of photocatalytic CO2RR test.

Fig. S8 a Photocatalytic CH4 evolution as a function of light irradiation time (KHCO3 solution). b AQE values of CO2 photoreduction to CH4 (KHCO3 solution). c Photocatalytic performance of Sv-In2S3@2H-MoTe2(5) under monochromatic light irradiation (KHCO3 solution). d Comparison of photocatalytic CO2RR performance with visible-light irradiation [−,,,,,,,,,,,,,].

Fig. S9 GC-MS analysis of product after 13CO2 photoreduction at hν = 14.3 eV with Sv-In2S3@2H-MoTe2(5), Sv-In2S3, and 2H-MoTe2, respectively (KHCO3 solution).

Fig. S10 a Yields of CO, CH4, and H2 for photocatalysts (pure H2O solution). b Photocatalytic CH4 evolution as a function of light irradiation time (KHCO3 solution).

Fig. S11 a TEM and b HRTEM images of Sv-In2S3@2H-MoTe2(5) after photocatalytic CO2RR (6 cycles). c XRD patterns of Sv-In2S3@2H-MoTe2(5) after photocatalytic CO2RR (6 cycles), respectively. d S 2p and e Mo 3d XPS spectra of Sv-In2S3@2H-MoTe2(5) after CO2RR test (6 cycles), respectively.

Fig. S12 a The comparison of Mo K-edge XANES spectra. b k3-weighted FT-EXAFS spectra of Mo at R space (the data of reference sample MoS2 come from Fig. 2c). c Mo K-edge EXAFS (points) and fit (line) for sample, shown in k2 weighted R-space after CO2RR test. d The comparison of Mo and In K-edge XANES spectra after photocatalytic CO2RR (6 cycles).

Fig. S13 a Ultraviolet-visible (UV-vis) diffuse reflectance spectra (DRS) and b (αhv)2 versus energy curves of samples. c Ultraviolet photoelectron spectroscopy (UPS) of Sv-In2S3 and 2H-MoTe2, respectively. d Electronic structure and proposed charge transfer mechanism (“S”-scheme charge transfer mechanism).

As presented in Fig. S13a, Sv-In2S3 and In2S3 mainly adsorb visible-light with adsorption edges at around 450 nm. After incorporation with 2H-MoTe2, the optical absorption curve of Sv-In2S3@2H-MoTe2(5) shows a significant red shift, which is mainly owing to the strong light response of 2H-MoTe2 with an absorption edge of about 550 nm. Beyond that, the multiple light absorption effect produced by double shelled nanoboxes structure of Sv-In2S3@2H-MoTe2(5) can effectively extend the light range and increase utilization of visible-light [,].

Fig. S14 Electrostatic potential of a Sv-In2S3, b 2H-MoTe2, and c Sv-In2S3@2H-MoTe2(5), insets are models of In2S3, 2H-MoTe2, and Sv-In2S3@2H-MoTe2(5), respectively. d Average charge density difference of Sv-In2S3@2H-MoTe2(5) along Z axis direction (The magenta area (positive value) and cyan area (negative value) represent accumulation and consumption of electrons, respectively).

Table S5 Work function value under vacuum environment and solvent effect.

| Slab | Evac (eV) | EF (eV) | Φ (eV) |
| --- | --- | --- | --- |
| 2H-MoTe2 | 4.26 | −0.79 | 5.05 |
| Sv-In2S3 | 3.69 | −0.84 | 4.53 |
| Sv-In2S3@2H-MoTe2(5) | 5.06 | 0.45 | 4.61 |

Due to different EF and WF between Sv-In2S3 and 2H-MoTe2, electrons in 2H-MoTe2 are transferred to Sv-In2S3 as a way to equilibrate the EF at the interface between two materials. After that, the photogenerated electrons on CB of 2H-MoTe2 are transferred to VB of Sv-In2S3 by the induction of electrostatic potential and IEF effect, and then recombine with their photogenerated holes, namely “S”-scheme carrier mechanism [−,,].

Fig. S15 a The excitons transport process of Sv-In2S3@2H-MoTe2(5). b TRPL spectra and  c IPCE profile (measured at an open circuit potential) of samples, respectively.

The exciton transport process of Sv-In2S3@2H-MoTe2(5) can be divided into three parts as shown in Fig. S15a. S1 represents the exciton excited by high-energy photon. The competition between the Auger recombination process (S2) and interfacial charge transport process (S3) determine the lifetime of excitons and the density of photogenerated electrons and holes for participating photocatalytic overall water splitting reaction. The lifetime of excitons was evaluated through fs-TA spectra. The fast decay of fs-TA spectrum fitted via bi-exponential decay represents the nonradiative recombination (such as Auger process, insert in Fig. 4g) of samples. The Sv-In2S3@2H-MoTe2(5) exhibits a longer excitons lifetime of 72.54 ps than Sv-In2S3 (24.32 ps) and 2H-MoTe2 (7.23 ps), implying exciton extracting force by interfacial IEF (Fig. S13d) of Sv-In2S3@2H-MoTe2(5) significantly suppresses the Auger recombination of 2H-MoTe2 (Fig. S15a).

Table S6 The average fluorescence lifetime of samples.

| Samples | τ1(ns) | A1 (%) | τ2 (ns) | A2 (%) | Ave. τ(ns) |
| --- | --- | --- | --- | --- | --- |
| 2H-MoTe2 | 0.98 | 17 | 4.4 | 83 | 4.25 |
| In2S3 | 1.6 | 34 | 9.8 | 66 | 9.2 |
| Sv-In2S3 | 11 | 22 | 15 | 78 | 14.3 |
| Sv-In2S3@2H-MoTe2(5) | 12.3 | 28 | 22.6 | 72 | 20.8 |

* : A1+A2 =1

Table S7 AQE and IQEcr value of the Sv-In2S3@2H-MoTe2(5), Sv-In2S3, In2S3, and 2H-MoTe2 under different wavelength irradiation, respectively.

| Wavelength (nm) | Sv-In2S3@2H-MoTe2(5) | Sv-In2S3 | In2S3 | 2H-MoTe2 |
| --- | --- | --- | --- | --- |
|  | AQE (%) | Absorption | IQEcr (%) | AQE (%) | Absorption | IQEcr (%) | AQE (%) | Absorption | IQEcr (%) | AQE (%) | Absorption | IQEcr (%) |
| 380 | 65.29 | 0.6945 | 94.01 | 7.71 | 0.5985 | 12.88 | 7.07 | 0.6011 | 11.76 | 7.42 | 0.7060 | 10.51 |
| 400 | 18.45 | 0.6533 | 28.24 | 5.62 | 0.5819 | 9.66 | 5.05 | 0.5925 | 8.52 | 5.47 | 0.7008 | 7.81 |
| 420 | 16.46 | 0.6465 | 25.46 | 3.65 | 0.5691 | 6.41 | 3.09 | 0.5872 | 5.26 | 4.15 | 0.6947 | 5.97 |
| 440 | 14.3 | 0.6363 | 22.47 | 2.39 | 0.5580 | 4.28 | 1.54 | 0.5841 | 2.64 | 1.50 | 0.6941 | 2.16 |
| 460 | 12.48 | 0.6238 | 20 | 2.18 | 0.5527 | 3.94 | 1.40 | 0.5835 | 2.40 | 1.07 | 0.6952 | 1.54 |
| 480 | 5.91 | 0.6187 | 9.55 | 1.52 | 0.5489 | 2.77 | 0.54 | 0.5832 | 0.93 | 0.46 | 0.6967 | 0.66 |
| 500 | 4.6 | 0.6005 | 7.66 | 1.10 | 0.5469 | 2.01 | 0.38 | 0.5822 | 0.653 | 0.21 | 0.6979 | 0.30 |
| 520 | 2.42 | 0.5967 | 4.06 | 0.73 | 0.5445 | 1.34 | 0.22 | 0.5789 | 0.383 | 0.11 | 0.7021 | 0.16 |

Fig. S16 The optimized atomic models of a,b 2H-MoTe2, c,d Sv-In2S3, and e Sv-In2S3@2H-MoTe2(5) in theoretical calculations, respectively.

Fig. S17 a The schematic illustration of adsorption atomic structures during CO2RR process over Sv-In2S3@2H-MoTe2(5) interfaces (Path 1). b Free energy diagrams for CO2 reduction to CH4 at 1.23 V bias over Sv-In2S3@2H-MoTe2(5) interfaces with the maximum energy barrier (Path 1). c The search process for the minimum energy reaction pathways of CO2RR on Sv-In2S3@2H-MoTe2(5) interfaces. The red arrows denote disallowed reaction paths, while green arrows stand for enabled ones.

All the CO2RR (R1 ~ R16) considered in the search process for the minimum energy reaction pathways of the CO2RR (Fig. S17c) can be written as:

|  | R1 |
| --- | --- |
|  | R2 |
|  | R3 |
|  | R4 |
|  | R5 |
|  | R6 |
|  | R7 |
|  | R8 |
|  | R9 |
|  | R10 |
|  | R11 |
|  | R12 |
|  | R13 |
|  | R14 |
|  | R15 |
|  | R16 |

The hydrogenation reactions (R17 ~ R18) for HER can be written as:

|  | R17 |
| --- | --- |
|  | R18 |

where * denotes the adsorption active site on the substrate.

We treated the charge of the system to refer to the widely-recognized computational hydrogen electrode (CHE) mode [10], in which each reaction step was regarded as a simultaneous transfer of the proton-electron pair as a function of the applied potential. Thus, free energy changes relative to an initial state of gaseous CO2 free above an empty surface can be rewritten as (U = 1.23 V and pH = 0) (R1 ~ R18):

|  | ES18 |
| --- | --- |
|  | ES19 |
|  | ES20 |
|  | ES21 |
|  | ES22 |
|  | ES23 |
|  | ES24 |
|  | ES25 |
|  | ES26 |
|  | ES27 |
|  | ES28 |
|  | ES29 |
|  | ES30 |
|  | ES31 |
|  | ES32 |
|  | ES33 |
|  | ES34 |
|  | ES35 |

The intermediates adsorption energy Eads for H*, OH*, CO*, OCH2O*, CH3O*, COH*, and OCH2O*, etc. can be used as DFT ground state energy calculated as:

|  | ES36 |
| --- | --- |
|  | ES37 |
|  | ES38 |
|  | ES39 |
|  | ES40 |
|  | ES41 |
|  | ES42 |
|  | ES43 |
|  | ES44 |
|  | ES45 |
|  | ES46 |
|  | ES47 |
|  | ES48 |
|  | ES49 |
|  | ES50 |

The evolution of CO2 to CO over Sv-In2S3@2H-MoTe2(5) is a multistep proton-coupled electron transfer process as elucidated below:

|  | ES51 |
| --- | --- |
|  | ES52 |
|  | ES53 |
|  | ES54 |
|  | ES55 |

Fig. S18 a The adsorption configuration of H2O* and H* intermediates on Sv-In2S3@2H-MoTe2(5). The free energy diagrams for b CO2 reduction to CH4 at 1.23 V bias and c alkaline HER on over samples with the maximum energy barrier.

Table S8 The Zero-pint energy correction (EZPE), entropy contribution (TS, T = 298.15 K), and total energy (EDFT) of molecules in this work, are taken from the NIST database [9,].

| Species | EDFT (eV) | TS (eV) | T∆S (eV) | EZPE (eV) | ∆EZPE (eV) | (∆EZPE − T∆S) (eV) |
| --- | --- | --- | --- | --- | --- | --- |
| CO2 (g) | −22.98 | 0.66 | / | 0.31 | / | / |
| CO (g) | −14.79 | 0.60 | / | 0.14 | / | / |
| CH4 (g) | −24.04 | 0.46 | / | 1.19 | / | / |
| H2O (l) [] | −14.21 | 0.67 | 0 | 0.59 | 0 | 0 |
| H2 (g) [,] | −6.76 | 0.42 | / | 0.27 | / | / |

Table S9 Zero-pint energy correction (EZPE), entropy contribution (TS, T=298.15 K), total energy (EDFT), and the Gibbs free energy (G) of molecules and adsorbates along the reaction pathway on Sv-In2S3@2H-MoTe2(5), where * represents the adsorption site [9,30,,].

| Species | TS (eV) | EZPE (eV) |
| --- | --- | --- |
| OCH2O* | 0.21 | 0.92 |
| CH2O* | 0.17 | 0.74 |
| CH3O* | 0.25 | 1.04 |
| H* | 0.02 | 0.15 |
| O* | 0.07 | 0.07 |
| OH* | 0.08 | 0.33 |
| CO* | 0.26 | 0.15 |
| OCOH* | 0.24 | 0.62 |
| OCHO* | 0.17 | 0.42 |
| HOCH2O* | 0.24 | 1.24 |
| H2O* | 0.17 | 0.64 |

Table S10 Summary of state-of-the-art photocatalytic CO2RR catalysts.

| Photocatalyst | Light Source | Experimental Condition | Main Product | Yield (µmol·g−1·h−1) | Reference |
| --- | --- | --- | --- | --- | --- |
| Sv-In2S3@2H-MoTe2(5) | 300 W Xe lamp | Pure CO2 gas, gas-solid, water | CH4 | 31.18 | Our work |
|  |  |  | CO | 25.85 |  |
|  |  |  | H2 | 12.50 |  |
| Bi2O2(OH)(NO3) with surface Br ions | 300 W Xe lamp | Pure CO2 gas, gas-solid, water | CO | 8.12 | [] |
| Cs2SnI6 Perovskite Nanocrystal/SnS2 Nanosheet Heterojunction | A 150 mW·cm−2 Xe lamp (λ > 400 nm) | Pure CO2 gas, gas-solid, water, CH3OH | CH4 | 3.03 | [] |
| Single Cu Atom/Crystalline g-C3N4 | 300 W Xe lamp | Pure CO2 gas, gas-solid | CH4 | / | [] |
|  |  |  | CO | 3.09 |  |
| Monolayer N-doped graphene on CdS hollow spheres | A 350 W Xe lamp (λ > 420 nm) | Pure CO2 gas, gas-solid, water | CH4 | 0.33 | [23] |
|  |  |  | CO | 2.59 |  |
| UiO-66/carbon nitride nanosheet heterogeneous photocatalyst | A 300 W Xe lamp (800 nm >λ > 400 nm) | Pure CO2 gas, gas-solid, water | CO | 9.90 | [] |
| Perovskite-like PbBiO2Br | 300 W Xe lamp | Pure CO2 gas, gas-solid | CO | 1.24 | [] |
| ICN-16 | 300 W Xe lamp | Pure CO2 gas | CO | 398.87 | [] |
| GGS/GS | 300 W Xe lamp | Pure CO2 gas, gas-solid, water | C2H4 | 335.67 | [] |
| ZnAl-LDH nanosheets | 300 W Xe lamp | Pure CO2 gas, gas-solid | CO | 7.60 | [] |
| Cs3Bi2I9 perovskite nanocrystals | 32 W UV lamp | Pure CO2 gas, gas-solid, water | CH3OH | 1.49 | [] |
|  |  |  | CO | 7.76 |  |
| Atomically-thin Bi2MoO6 nanosheets with vacancy pairs | 300 W Xe lamp | Pure CO2 gas, gas-solid | CO | 3.62 | [] |
| Ultrathin Pb0.6Bi1.4O2Cl2 | 300 W Xe lamp | Air, gas-solid | CO | 5.16 | [] |
|  |  |  | CH4 | 0.62 |  |
|  |  |  | CH3OH | 1.98 |  |

References

[] J. Nai, S. Wang, Y. Bai, L. Guo, Amorphous Ni(OH)2 Nanoboxes: Fast Fabrication and Enhanced Sensing for Glucose, Small 9, 3147–3152 (2013). https://doi.org/10.1002/smll.201203076

[] Y. Fang, B.Y. Guan, D. Luan, X.W. Lou, Synthesis of CuS@CoS2 double-shelled nanoboxes with enhanced sodium storage properties, Angew. Chem. Int. Ed. 58, 7739–7743 (2019). https://doi.org/10.1002/anie.201902583

[] B. Ravel, M. Newville, ATHENA, ARTEMIS, HEPHAESTUS: data analysis for X-ray absorption spectroscopy using IFEFFIT, J. Synchrotron Rad. 12, 537–541 (2005). https://doi.org/10.1107/S0909049505012719

[] H. Funke, A.C. Scheinost, M. Chukalina, Wavelet analysis of extended x-ray absorption fine structure data, Phys. Rev. B 71, 094110 (2005). https://doi.org/10.1103/PhysRevB.71.094110

[] H. Funke, M. Chukalina, A.C. Scheinost, A new FEFF-based wavelet for EXAFS data analysis, J. Synchrotron Rad. 14, 426–432 (2007). https://doi.org/10.1107/S0909049507031901

[] C. Cheng, B. He, J. Fan, B. Cheng, S. Cao et al., An Inorganic/Organic S-Scheme Heterojunction H2-Production Photocatalyst and its Charge Transfer Mechanism, Adv. Mater. 33, 2100317 (2021). https://doi.org/10.1002/adma.202100317

[] M. Ahmad, X. Quan, S. Chen, H. Yu, Z. Zeng, Operating redox couple transport mechanism for enhancing photocatalytic H2 generation of Pt and CrOx-decorated ZnCdS nanocrystals, Appl. Catal. B Environ. 283, 119601 (2021). https://doi.org/10.1016/j.apcatb.2020.119601

[] A. Zhang, Y. Liang, H. Li, X. Zhao, Y. Chen et al., Harmonizing the Electronic Structures of the Adsorbate and Catalysts for Efficient CO2 Reduction, Nano Lett. 9, 6547–6553 (2019). https://doi.org/10.1021/acs.nanolett.9b02782

[] Z. Wang, J. Zhu, X. Zu, Y. Wu, S. Shang et al., Selective CO2 Photoreduction to CH4 via Pdᵟ+-assisted Hydrodeoxygenation over CeO2 Nanosheets, Angew. Chem. Int. Ed. 61, e202203249 (2022). https://doi.org/10.1002/anie.202203249

[] L. Ju, X. Tan, X. Mao, Y. Gu, S. Smith et al., Controllable CO2 electrocatalytic reduction via ferroelectric switching on single atom anchored In2Se3 monolayer, Nat. Commun. 12, 5128 (2021). https://doi.org/10.1038/s41467-021-25426-5

[] B. Yu, Y. Wu, F. Meng, Q. Wang, X. Jia et al., Formation of hierarchical Bi2MoO6/ln2S3 S-scheme heterojunction with rich oxygen vacancies for boosting photocatalytic CO2 reduction, Chem. Eng. J. 429, 132456 (2022). https://doi.org/10.1016/j.cej.2021.132456

[] W. Dong, J. Jia, Y. Wang, J. An, O.Y. Yang et al., Visible-light-driven solvent-free photocatalytic CO2 reduction to CO by Co-MOF/Cu2O heterojunction with superior selectivity, Chem. Eng. J. 438, 135622 (2022). https://doi.org/10.1016/j.cej.2022.135622

[] J. Jiang, X. Wang, Q. Xu, Z. Mei, L. Duan et al., Understanding dual-vacancy heterojunction for boosting photocatalytic CO2 reduction with highly selective conversion to CH4, Appl. Catal. B Environ. 316, 121679 (2022). https://doi.org/10.1016/j.apcatb.2022.121679

[] Z. Zhang, M. Wang, Z. Chi, W. Li, H. Yu et al., Internal electric field engineering step-scheme-based heterojunction using lead-free Cs3Bi2Br9 perovskite-modified In4SnS8 for selective photocatalytic CO2 reduction to CO, Appl. Catal. B Environ. 313, 121426 (2022). https://doi.org/10.1016/j.apcatb.2022.121426

[] Y. Chai, Y. Chen, J. Shen, M. Ni, B. Wang et al., Distortion of the Coordination Structure and High Symmetry of the Crystal Structure in In4SnS8 Microflowers for Enhancing Visible-Light Photocatalytic CO2 Reduction, ACS Catal. 11, 11029−11039 (2021). https://doi.org/10.1021/acscatal.1c02937

[] W. Gao, S. Li, H. He, X. Li, Z. Cheng et al., Vacancy-defect modulated pathway of photoreduction of CO2 on single atomically thin AgInP2S6 sheets into olefiant gas, Nat. Commun. 12, 4747 (2021). https://doi.org/10.1038/s41467-021-25068-7

[] J. Jiang, X. Zou, Z. Mei, S. Cai, Q. An et al., Understanding rich oxygen vacant hollow CeO2@MoSe2 heterojunction for accelerating photocatalytic CO2 reduction, J. Colloid Interf. Sci. 611, 644–653 (2022). https://doi.org/10.1016/j.jcis.2021.12.108

[] Y. Liu, D. Shen, Q. Zhang, Y. Lin, F. Peng, Enhanced photocatalytic CO2 reduction in H2O vapor by atomically thin Bi2WO6 nanosheets with hydrophobic and nonpolar surface, Appl. Catal. B Environ. 283, 119630 (2021). https://doi.org/10.1016/j.apcatb.2020.119630

[] Y. Huang, K. Wang, T. Guo, J. Li, X. Wu et al., Construction of 2D/2D Bi2Se3/g-C3N4 nanocomposite with High interfacial charge separation and photo-heat conversion efficiency for selective photocatalytic CO2 reduction, Appl. Catal. B Environ. 277, 119232 (2020). https://doi.org/10.1016/j.apcatb.2020.119232

[] X. Wang, Y. Wang, M. Gao, J. Shen, X. Pu et al., BiVO4/Bi4Ti3O12 heterojunction enabling efficient photocatalytic reduction of CO2 with H2O to CH3OH and CO, Appl. Catal. B Environ. 270, 118876 (2020). https://doi.org/10.1016/j.apcatb.2020.118876

[] X. Chen, Q. Li, J. Li, J. Chen, H. Jia, Modulating charge separation via in situ hydrothermal assembly of low content Bi2S3 into UiO-66 for efficient photothermocatalytic CO2 reduction, Appl. Catal. B Environ. 270, 118915 (2020). https://doi.org/10.1016/j.apcatb.2020.118915

[] X. Jin, C. Lv, X. Zhou, H. Xie, S. Sun et al., A bismuth rich hollow Bi4O5Br2 photocatalyst enables dramatic CO2 reduction activity, Nano Energy 64, 103955 (2019). https://doi.org/10.1016/j.nanoen.2019.103955

[] C. Bie, B. Zhu, F. Xu, L. Zhang, J. Yu, In Situ Grown Monolayer N-Doped Graphene on CdS Hollow Spheres with Seamless Contact for Photocatalytic CO2 Reduction, Adv. Mater. 31, 1902868 (2019). https://doi.org/10.1002/adma.201902868

[] X. Li, Y. Sun, J. Xu, Y. Shao, J. Wu et al., Selective visible-light-driven photocatalytic CO2 reduction to CH4 mediated by atomically thin CuIn5S8 layers, Nat. Energy 4, 690–699 (2019). https://doi.org/10.1038/s41560-019-0431-1

[] P. Zhang, D. Luan, X.W. (David) Lou, Fabrication of CdS Frame-in-Cage Particles for Efficient Photocatalytic Hydrogen Generation under Visible-Light Irradiation, Adv. Mater. 32, 2004561 (2020). https://doi.org/10.1002/adma.202004561

[] K. Li, Y. Cai, X. Yang, S. Wang, C. Teng et al., H2S Involved Photocatalytic System: A Novel Syngas Production Strategy by Boosting the Photoreduction of CO2 While Recovering Hydrogen from the Environmental Toxicant, Adv. Funct. Mater. 32, 2113002 (2022). https://doi.org/10.1002/adfm.202113002

[] S. Mukherjee, D. Dutta, M. Uzhansky, E. Koren, Excitons and light-emission in semiconducting MoSi2X4 two-dimensional materials, npj 2D Mater Appl. 6, 37 (2022). https://doi.org/10.1038/s41699-022-00355-z

[] Y. Geng, D. Chen, N. Li, Q. Xu, H. Li et al., Z-Scheme 2D/2D α-Fe2O3/g-C3N4 heterojunction for photocatalytic oxidation of nitric oxide, Appl. Catal. B Environ. 280, 119409 (2021). https://doi.org/10.1016/j.apcatb.2020.119409

[] Z. Zhang, M. Wang, Z. Chi, W. Li, H. Yu et al., Internal electric field engineering step-scheme-based heterojunction using lead-free Cs3Bi2Br9 perovskite-modified In4SnS8 for selective photocatalytic CO2 reduction to CO, Appl. Catal. B Environ. 313, 121426 (2022). https://doi.org/10.1016/j.apcatb.2022.121426

[] WebBook NC. <07838353.pdf>. https://webbooknistgov/chemistry/

[] S. Fang, X. Zhu, X. Liu, J. Gu, W. Liu et al., Uncovering near-free platinum single-atom dynamics during electrochemical hydrogen evolution reaction, Nat. Commun. 11, 1029  (2020). https://doi.org/10.1038/s41467-020-14848-2

[] NIST-JANAF Thermochemical Tables. https://janaf.nist.gov/

[] J. Rossmeisl, A. Logadottir, J. K. Nørskov, Electrolysis of water on (oxidized) metal surfaces, Chem. Phys. 319, 178–184 (2005). https://doi.org/10.1016/j.chemphys.2005.05.038

[] D. Raciti, L. Cao, K.J.T. Livi, P.F. Rottmann, X. Tang et al., Low-overpotential electroreduction of carbon monoxide using copper nanowires, ACS Catal. 7, 4467–4472 (2017). https://doi.org/10.1021/acscatal.7b01124

[] A.A. Peterson, F. Abild-Pedersen, F. Studt, J. Rossmeisl, J.K. Norskov, How copper catalyzes the electroreduction of carbon dioxide into hydrocarbon fuels, Energ. Environ. Sci. 3, 1311–1315 (2010). https://doi.org/10.1039/C0EE00071J

[] L. Hao, L. Kang, H. Huang, L. Ye, K. Han et al., Surface-Halogenation-Induced Atomic-Site Activation and Local Charge Separation for Superb CO2 Photoreduction, Adv. Mater. 31, 1900546 (2019). https://doi.org/10.1002/adma.201900546

[] X. Wang, Y. Huang, J. Liao, Y. Jiang, L. Zhou et al., In Situ Construction of a Cs2SnI6 Perovskite Nanocrystal/SnS2 Nanosheet Heterojunction with Boosted Interfacial Charge Transfer, J. Am. Chem. Soc. 141, 13434–13441 (2019). https://doi.org/10.1021/jacs.9b04482

[] J. Wu, X. Li, W. Shi, P. Ling, Y. Sun et al., Efficient Visible-Light-Driven CO2 Reduction Mediated by Defect-Engineered BiOBr Atomic Layers, Angew. Chem. Int. Ed. 57, 8719–8723 (2018). https://doi.org/10.1002/ange.201803514

[] L. Shi, T. Wang, H. Zhang, K. Chang, J. Ye, Electrostatic Self-Assembly of Nanosized Carbon Nitride Nanosheet onto a Zirconium Metal-Organic Framework for Enhanced Photocatalytic CO2 Reduction, Adv. Funct. Mater. 25, 5360–5367 (2015). https://doi.org/10.1002/adfm.201502253

[] B. Wang, J. Di, L. Lu, S. Yan, G. Liu et al., Sacrificing ionic liquid-assisted anchoring of carbonized polymer dots on perovskite-like PbBiO2Br for robust CO2 photoreduction, Appl. Catal. B Environ. 254, 551–559 (2019). https://doi.org/10.1016/j.apcatb.2019.04.068

[] C. Ding, X. Lu, B. Tao, L. Yang, X. Xu et al., Interlayer Spacing Regulation by Single-Atom Indium𝜹+–N4 on Carbon Nitride for Boosting CO2/CO Photo-Conversion, Adv. Funct. Mater. 2302824 (2023). https://doi.org/10.1002/adfm.202302824

[] J. Wang, C. Yang, L. Mao, X. Cai, Z. Geng et al., Regulating the Metallic Cu-Ga Bond by S Vacancy for Improved Photocatalytic CO2 Reduction to C2H4, Adv. Funct. Mater. 33, 2213901 (2023). https://doi.org/10.1002/adfm.202213901

[] Y. Zhao, G. Chen, T. Bian, C. Zhou, G. I. N. Waterhouse et al., Defect-Rich Ultrathin ZnAl-Layered Double Hydroxide Nanosheets for Efficient Photoreduction of CO2 to CO with Water, Adv. Mater. 27, 7824–7831 (2015). https://doi.org/10.1002/adma.201503730

[] S. S. Bhosale, A. K. Kharade, E. Jokar, A. Fathi, S. Chang et al., Mechanism of Photocatalytic CO2 Reduction by Bismuth-Based Perovskite Nanocrystals at the Gas-Solid Interface, J. Am. Chem. Soc. 141, 20434–20442 (2019). https://doi.org/10.1021/jacs.9b11089

[] J. Di, X. Zhao, C. Lian, M. Ji, J. Xia et al., Atomically-thin Bi2MoO6 nanosheets with vacancy pairs for improved photocatalytic CO2 reduction, Nano Energy 61, 54–59 (2019). https://doi.org/10.1016/j.nanoen.2019.04.029

[] X. Feng, R. Zheng, C. Gao, W. Wei, J. Peng et al., Unlocking bimetallic active sites via a desalination strategy for photocatalytic reduction of atmospheric carbon dioxide, Nat. Commun. 13, 2146 (2022). https://doi.org/10.1038/s41467-022-29671-0