Supplementary Information

Bioinspired multifunctional self-sensing actuated gradient hydrogel for soft-hard robot remote interaction

He Liu1, Haoxiang Chu1, Hailiang Yuan1, Deliang Li1, Weisi Deng1, Zhiwei Fu1, Ruonan Liu1, Yiying Liu1, Yixuan Han1, Yanpeng Wang1, Yue Zhao1, Xiaoyu Cui1, *, Ye Tian1, 2, *

1College of Medicine and Biological Information Engineering, Northeastern University, Shenyang 110169, China

2Foshan Graduate School of Northeastern University, Foshan, 528300, China

Corresponding author:

Dr. Xiaoyu Cui, E-mail: cuixy@bmie.neu.edu.cn

Dr. Ye Tian, E-mail: tianye@bmie.neu.edu.cn

Fig. S1 FTIR spectra of SA, NIPAM, PS hydrogel and PSM hydrogel

Fig. S2 Scheme of measuring the bending angle (θ) of the hydrogel actuator

Fig. S3 Thermo-responsive actuation a angle change curve, b physical diagram of the hydrogel without CaCl2 soaking in water at 50 °C

Fig. S4 The deswelling ratio of PSM hydrogels soaked in CaCl2 for 50 s, 100 s, 150 s and 200 s

Fig. S5 Thermo-responsive actuation of hydrogels after soaking CaCl2 for a 50 s, b 100 s, c 200 s in water at 50 °C

Fig. S6 The Young's modulus of PSM hydrogels soaked in CaCl2 for 50 s, 100 s, 150 s and 200 s

Fig. S7 Thermo-responsive actuation of a PSM0.2, b PSM0.4, c PSM0.8 hydrogels in water at 50 °C

Fig. S8 Deswelling curve of PSM hydrogel in water at 50 °C

Fig. S9 Thermo-responsive actuation of hydrogels with a thickness of a 2 mm and b 3 mm in water at 50 °C

Fig. S10 Temperature response changes of a PSM0.2, b PSM0.4 c PSM0.8 hydrogels under NIR light irradiation (808 nm, 1 W/cm2)

Fig. S11 Temperature response changes of PSM0.6 hydrogel under 808 nm NIR light irradiation with a 0.5 W/cm2, b 1.5 W/cm2 , c 2 W/cm2

Fig. S12 Shape deformation of PSM hydrogel actuators coating Ca2+ in the a bottom and b top directions

Fig. S13 Diagram of encoded information written by coating Ca2+

Fig. S14 Brightness changes of LED in the undeformed, stretched and folded states of PSM hydrogels

Fig. S15 a Photothermal sensing mechanism. b The relative resistance changes of PSM hydrogel under NIR irradiation

Fig. S16 The relative resistance changes of PSM hydrogel under different joints include a wrist, b arm and c leg

Fig. S17 Hardware schematic of a PSM hydrogel and the signal transmission system, b Robotic hand and the signal receiver system

Table S1. Summarization for the bending speed and bending amplitude of hydrogel actuators

| Material | Structure | Bending speed | Bending amplitude | Stimulation conditions | Sample size (mm3) | Ref |
| --- | --- | --- | --- | --- | --- | --- |
| PNIPAM/ XLG/ HEA | Gradient | 9.8°/s | 206° | 50 ℃ water | 25 × 5 × 1 | [S1] |
| PNIPAM /XLG | Gradient | 2.38°/s | 57.2° | 50 ℃ water | 25 × 5 × 1 | [S2] |
| P(NIPAM-co-SPA)/ TCNC | Gradient | 10.2°/s | 225° | 60 ℃ water | 25 × 5 × 0.3 | [S3] |
| PNIPAM/ XLG/NFC | Bilayer | 9°/s | 180° | 50 ℃ water | 65 × 7 × 2 | [S4] |
| PNIPAM/ PAAM- PTCA | Bilayer | 6.1°/s | 305° | 45 ℃ water | —— | [S5] |
| PNIPAM/ XLG/ MoO2 | Bilayer | 3°/s | 90° | NIR 808 nm 0.8 W/cm2 | —— | [S6] |
| PNIPAM/PVA | Bilayer | 2.1°/s | 65° | NIR 808 nm 0.2 W/cm2 | —— | [S7] |
| PNIPAM/ SA/MoO2 | Gradient | 21°/s | 336° | 50 ℃ water | 50 × 10 × 1 | This work |

Notes: The comparison is only rough because these hydrogels have different sample sizes and stimulation conditions

Table S2. Comparison of the main conductive parameters of PSM hydrogel and conductive hydrogel strain sensors in previous mainstream work

| Material | Strain (%) | Gauge Factor | Linear or Nonlinear | Conductive mechanism | Ref |
| --- | --- | --- | --- | --- | --- |
| PAA/NCT | 500 | 2.69 | Linear | Ionic conduction | [S8] |
| TA@HAP NWs/PVA(W/EG) | 350 | 2.84 | Linear | Ionic conduction | [S9] |
| PAAM/SA/LiCl/CaCl2/glycerin | 0-100 | 0.45 | Nonlinear | Ionic conduction | [S10] |
|  | 200-300 | 2.31 |  |  |  |
| [EMIm][DCA]/WPU | 0-30 | 0.53 | Nonlinear | Ionic conduction | [S11] |
|  | 30-100 | 0.83 |  |  |  |
|  | 100-200 | 1.38 |  |  |  |
| HF(PVA-C/P) | 400 | 2.1 | Linear | Electronic conduction | [S12] |
| MWCNTs-PDMS | 160 | 3.77 | Linear | Electronic conduction | [S13] |
| PVA-CBA/PAAm/TA/ Ti3C2Tx | 0-80 | 1.2 | Nonlinear | Electronic conduction | [S14] |
|  | 80-150 | 1.57 |  |  |  |
|  | 150-220 | 2.34 |  |  |  |
|  | 220-280 | 3.51 |  |  |  |
| PVA/G/PDA/AgNPs | 0-70 | 0.94 | Nonlinear | Electronic conduction | [S15] |
|  | 70-315 | 0.13 |  |  |  |
| PNIPAM/SA/ MoO2 | 600 | 3.94 | Linear | Electronic conduction | This work |

Supporting Movie 1 Thermo-responsive actuation behavior of hydrogels

Supporting Movie 2 PSM hydrogel gripper grabs metal sheet from 50 °C water

Supporting Movie 3 Bioinspired jellyfish swimming under NIR switch

Supporting Movie 4 Self-assembly folding cube

Supporting Movie 5 Brightness changes of LED in the undeformed, stretched and folded states of PSM hydrogel

Supporting Movie 6 Remote interaction of soft-hard robot via IoT

Reference

[S1] Y. Tan, D. Wang, H. Xu, Y. Yang, X. L. Wang, F. Tian, P. Xu, W. An, X. Zhao, S. Xu. Rapid recovery hydrogel actuators in air with bionic large-ranged gradient structure. ACS Appl. Mater. Interfaces. 10(46), 40125-40131 (2018). https://doi.org/10.1021/acsami.8b13235

[S2] Y. Tan, D. Wang, H. Xu, Y. Yang, W. An, L. Yu, Z. Xiao, S. Xu. A fast, reversible, and robust gradient nanocomposite hydrogel actuator with water-promoted thermal response. Macromol. Rapid Commun. 39(8), e1700863 (2018). https://doi.org/10.1002/marc.201700863

[S3] J. Lin, Y. Han, Y. Cui, W. Zhao, C. Chang. Ionic coordination strengthening of temperature-driven gradient hydrogel actuators with rapid responsiveness. Compos. B. Eng. 245, (2022). https://doi.org/10.1016/j.compositesb.2022.110210

[S4] Q. Zhao, Y. Liang, L. Ren, Z. Yu, Z. Zhang, F. Qiu, L. Ren. Design and fabrication of nanofibrillated cellulose-containing bilayer hydrogel actuators with temperature and near infrared laser responses. J Mater Chem B. 6(8), 1260-1271 (2018). https://doi.org/10.1039/c7tb02853a

[S5] B. Y. Wu, X. X. Le, Y. K. Jian, W. Lu, Z. Y. Yang, Z. K. Zheng, P. Theato, J. W. Zhang, A. Zhang, T. Chen. Ph and thermo dual-responsive fluorescent hydrogel actuator. Macromol. Rapid Commun. 40(4), e1800648 (2019). https://doi.org/10.1002/marc.201800648

[S6] Z. Sun, C. Wei, W. Liu, H. Liu, J. Liu, R. Hao, M. Huang, S. He. Two-dimensional moo(2) nanosheet composite hydrogels with high transmittance and excellent photothermal property for near-infrared responsive actuators and microvalves. ACS Appl. Mater. Interfaces. 13(28), 33404-33416 (2021). https://doi.org/10.1021/acsami.1c04110

[S7] N. Chen, Y. Zhou, Y. Liu, Y. Mi, S. Zhao, W. Yang, S. Che, H. Liu, F. Chen, C. Xu, G. Ma, X. Peng, Y. Li. Conductive photo-thermal responsive bifunctional hydrogel system with self-actuating and self-monitoring abilities. Nano Res. 15(8), 7703-7712 (2022). https://doi.org/10.1007/s12274-022-4394-3

[S8] X. Jing, P. Feng, Z. Chen, Z. Xie, H. Li, X.-F. Peng, H.-Y. Mi, Y. Liu. Highly stretchable, self-healable, freezing-tolerant, and transparent polyacrylic acid/nanochitin composite hydrogel for self-powered multifunctional sensors. ACS Sustainable Chem. Eng. 9(28), 9209-9220 (2021). https://doi.org/10.1021/acssuschemeng.1c00949

[S9] J. Wen, J. Tang, H. Ning, N. Hu, Y. Zhu, Y. Gong, C. Xu, Q. Zhao, X. Jiang, X. Hu, L. Lei, D. Wu, T. Huang. Multifunctional ionic skin with sensing, uv‐filtering, water‐retaining, and anti‐freezing capabilities. Adv. Funct. Mater. 31(21), 2011176 (2021). https://doi.org/10.1002/adfm.202011176

[S10] X.-y. Wang, H.-J. Kim. Ultra-stretchable dual-network ionic hydrogel strain sensor with moistening and anti-freezing ability. Prog. Org. Coat. 166, 106784 (2022). https://doi.org/10.1016/j.porgcoat.2022.106784

[S11] B. Zhao, J. Yan, F. Long, W. Qiu, G. Meng, Z. Zeng, H. Huang, H. Wang, N. Lin, X. Y. Liu. Bioinspired conductive enhanced polyurethane ionic skin as reliable multifunctional sensors. Adv. Sci. 10(19), e2300857 (2023). https://doi.org/10.1002/advs.202300857

[S12] Q. Zhang, Q. Wang, G. Wang, Z. Zhang, S. Xia, G. Gao. Ultrathin and highly tough hydrogel films for multifunctional strain sensors. ACS Appl. Mater. Interfaces. 13(42), 50411-50421 (2021). https://doi.org/10.1021/acsami.1c15784

[S13] K. Zhang, C. Song, Z. Wang, C. Gao, Y. Wu, Y. Liu. A stretchable and self-healable organosilicon conductive nanocomposite for a reliable and sensitive strain sensor. J. Mater. Chem. C. 8(48), 17277-17288 (2020). https://doi.org/10.1039/d0tc04719h

[S14] T. Gong, Z. N. Li, H. Liang, Y. Li, X. Tang, F. Chen, Q. Hu, H. Wang. High-sensitivity wearable sensor based on a mxene nanochannel self-adhesive hydrogel. ACS Appl. Mater. Interfaces. 15(15), 19349-19361 (2023). https://doi.org/10.1021/acsami.3c01748

[S15] L. Fan, J. Xie, Y. Zheng, D. Wei, D. Yao, J. Zhang, T. Zhang. Antibacterial, self-adhesive, recyclable, and tough conductive composite hydrogels for ultrasensitive strain sensing. ACS Appl. Mater. Interfaces. 12(19), 22225-22236 (2020). https://doi.org/10.1021/acsami.0c06091