Support Information for

The Fundamental Understanding of Hydrogen Evolution Reaction on Zinc Anode Surface: A First-Principles Study

Xiaoyu Liu1, Yiming Guo1, Fanghua Ning1, *, Yuyu Liu1, Siqi Shi2, Qian Li3, Jiujun Zhang1, Shigang Lu1, and Jin Yi1, *

1 Institute for Sustainable Energy & Department of Chemistry, Shanghai University, Shanghai 200444, China.

2 School of Materials Science and Engineering, Shanghai University, Shanghai 200444, China.

3 College of Materials Science and Engineering, National Engineering Research Center for Magnesium Alloys, Chongqing University, Chongqing 400044, China.

*Corresponding author

E-mail: fhning@shu.edu.cn; jin.yi@shu.edu.cn

Supplementary Figures

Fig. S1 The side views of the slab models. a Zn (002) surface, b Zn (100) surface, c Zn (101) surface, d Zn (102) surface, e Zn (103) surface.

Fig. S2 The ∆GH* obtained after considering Van der Waals (VDW) interactions.

Fig. S3 The comparative water adsorption energy on several crystal surface of Zn anode.

Fig. S4 Hydrogen adsorption energy (∆EH*) at several crystal surfaces of the zinc anode as a function of different hydrogen coverage. The H coverage indicates the number of hydrogens absorbed per unit area.

Fig. S5 The electrostatic potential at several crystal surface of Zn anode. a Zn (002) surface, b Zn (100) surface, c Zn (101) surface, d Zn (102) surface, e Zn (103) surface.

Fig. S6 The energy barriers and reaction pathways of Heryrovsky step and Tafel step on a flat crystal surface (002) and b uneven crystal surface (101) of Zn anode.

Fig. S7 The Bader charge of surface Zn, and correlation between the Bader charge and generalized coordination number CN.

Fig. S8 The differential charge density induced by H adsorption for a Zn (002), b Zn (100), c Zn (101), d Zn (102), e Zn (103) surface models. The isosurfaces are all set to 0.001 e/Bohr3. The yellow and blue isosurfaces indicate loss and gain electrons, respectively.

Fig. S9 The schematic diagram of the CN of Zn atom with lowest ∆GH* at a Zn (102), b Zn (101), and c Zn (103) surface. The schematic diagram of the CN'of Zn atom with higher ∆GH* at d Zn (102), e Zn (101), and f Zn (103) surface.

Fig. S10 The schematic diagram of the CN of Zn atom at a Zn (002) and b Zn (100) surface. The schematic diagram of CN' of Zn atom at c uneven Zn (002) and d uneven Zn (100) surface.

Fig. S11 The adsorption energy of H on flat and uneven Zn (002) surface.

Supplementary Tables

Table S1. The computational details about k-points densities applied for Brillouin zone integration and the information of slab models.

| Miller indices | Lattice parameters | Layer number | Atom number | K-Points | k-points densities (/Å-1) |
| --- | --- | --- | --- | --- | --- |
| (0 0 2) | a = b = 10.66 Å c = 39.78 Å α = β = 90.00° γ =120.00° | 4 | 64 | 3 3 1 | 32 32 40 |
| (1 0 0) | a = 8.01 Å b = 9.79 Å c = 48.53 Å α=β=γ= 90.00° | 6 | 72 | 3 3 1 | 24 29 49 |
| (1 0 1) | a = 11.87 Å b = 10.44 Å c = 37.00 Å α = β = 90.00° γ =102.70° | 5 | 80 | 3 3 1 | 36 31 37 |
| (1 0 2) | a = 13.53 Å b = 7.99 Å c = 29.69 Å α = β =γ= 90.00° | 6 | 96 | 3 4 1 | 41 32 30 |
| (1 0 3) | a = 17.11 Å b = 7.98 Å c = 26.71 Å α = β = 90.00° γ =98.94° | 5 | 102 | 1 3 1 | 17 24 27 |

Table S2. The ∆GH* values and the corresponding structures for H adsorbed at different sites of Zn (101) surface.

| Surface structures | Adsorption site | ∆GH* (eV) |
| --- | --- | --- |
|  | Bridge | 0.023 |
|  | Bridge | 0.363 |
|  | Bridge | 0.250 |
|  | Bridge | 0.242 |

Table S3. The ∆GH* values and the corresponding structures for H adsorbed at different sites of Zn (102) surface.

| Surface structures | Adsorption site | ∆GH* (eV) |
| --- | --- | --- |
|  | Bridge | 0.174 |
|  | Bridge | 0.334 |
|  | Bridge | 0.277 |
|  | Bridge | 0.285 |
|  | Bridge | 0.328 |

Table S4. The ∆GH* values and the corresponding structures for H adsorbed at different sites of Zn (103) surface.

| Surface structures | Adsorption site | ∆GH* (eV) |
| --- | --- | --- |
|  | Bridge | -0.054 |
|  | Bridge | 0.058 |
|  | Top | 0.199 |
|  | Bridge | 0.340 |

Table S5. The ∆GH* values and the corresponding structures for H adsorbed at different sites of Zn (002) surface.

| Surface structures | Adsorption site | ∆GH* (eV) |
| --- | --- | --- |
|  | Bridge | 0.589 |
|  | Top | 0.577 |
|  | Hollow-fcc | 0.647 |
|  | Hollow-hcp | 0.630 |

Table S6. The ∆GH* values and the corresponding structures for H adsorbed at different sites of Zn (100) surface.

| Surface structures | Adsorption site | ∆GH* (eV) |
| --- | --- | --- |
|  | Hollow | 0.290 |
|  | Bridge | 0.392 |
|  | Bridge | 0.458 |
|  | Bridge | 0.357 |
|  | Top | 0.652 |

Table S7. Details of Gibbs free energy correction for H adsorbed on (002) and (100) surface with different H coverages. n represent the number of adsorbed H atoms. ZPEH* and TSH* for n > 1 are the average ZPEH* and TSH* of n H* respectively.

| Miller indices | Adsorption site | n | H coverage (Å-2) | ∆EH* (eV) | ZPEH* (eV) | TSH* (eV) | 12ZPEH2 (eV) | 12TSH2 (eV) | ∆GH* (eV) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (0 0 2) | top | 1 | 0.010 | 0.563 | 0.105 | 0.000 | 0.140 | 0.049 | 0.577 |
|  |  | 2 | 0.020 | 0.617 | 0.073 | 0.018 |  |  | 0.581 |
|  |  | 4 | 0.041 | 0.742 | 0.133 | 0.052 |  |  | 0.731 |
|  | bridge | 1 | 0.010 | 0.600 | 0.093 | 0.013 | 0.140 | 0.049 | 0.589 |
|  |  | 2 | 0.020 | 0.619 | 0.071 | 0.008 |  |  | 0.590 |
|  |  | 4 | 0.041 | 0.645 | 0.045 | 0.025 |  |  | 0.574 |
| (1 0 0) | bridge | 1 | 0.009 | 0.379 | 0.082 | 0.012 | 0.140 | 0.049 | 0.357 |
|  |  | 2 | 0.018 | 0.442 | 0.065 | 0.064 |  |  | 0.351 |
|  |  | 4 | 0.037 | 0.464 | 0.150 | 0.068 |  |  | 0.505 |
|  | hollow | 1 | 0.009 | 0.339 | 0.066 | 0.015 | 0.140 | 0.049 | 0.298 |
|  |  | 2 | 0.018 | 0.430 | 0.137 | 0.009 |  |  | 0.467 |
|  |  | 4 | 0.037 | 0.503 | 0.134 | 0.009 |  |  | 0.537 |

Table S8. Details of Gibbs free energy correction for H adsorbed on (101), (102), and (103) surface with different H coverages. n represent the number of adsorbed H atoms. ZPEH* and TSH* for n > 1 are the average ZPEH* and TSH* of n H* respectively.

| Miller indices | Adsorption site | n | H coverage (Å-2) | ∆EH* (eV) | ZPEH* (eV) | TSH* (eV) | 12ZPEH2 (eV) | 12TSH2 (eV) | ∆GH* (eV) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (1 0 1) | bridge | 1 | 0.008 | -0.041 | 0.164 | 0.010 | 0.140 | 0.049 | 0.023 |
|  |  | 2 | 0.017 | -0.034 | 0.165 | 0.014 |  |  | 0.026 |
|  |  | 4 | 0.033 | 0.004 | 0.167 | 0.015 |  |  | 0.065 |
| (1 0 2) | bridge | 1 | 0.009 | 0.107 | 0.168 | 0.011 | 0.140 | 0.049 | 0.174 |
|  |  | 2 | 0.018 | 0.109 | 0.173 | 0.010 |  |  | 0.181 |
|  |  | 6 | 0.055 | 0.142 | 0.261 | 0.013 |  |  | 0.217 |
| (1 0 3) | bridge | 1 | 0.007 | -0.101 | 0.152 | 0.013 | 0.140 | 0.049 | -0.054 |
|  |  | 2 | 0.015 | -0.003 | 0.151 | 0.014 |  |  | 0.043 |
|  |  | 4 | 0.030 | 0.047 | 0.155 | 0.015 |  |  | 0.096 |

Table S9. The Bader charge of surface Zn near the adsorption sites with the lowest Gibbs free energy.

| Miller indices | Bader charge of surface Zn (e) | Net charge of surface Zn (e) |
| --- | --- | --- |
| (0 0 2) | 11.972 | -0.028 |
| (1 0 0) | 11.977 | -0.023 |
| (1 0 1) | 12.000 | 0.000 |
| (1 0 2) | 11.993 | -0.007 |
| (1 0 3) | 12.002 | 0.002 |