Table S1. Performance comparison with Zn-ion hybrid supercapacitors

| Energy storage system (Cathode//Electrolyte//Anode) | Operating voltage | Capacitance | Energy density | Cycling stability | Reference |
| --- | --- | --- | --- | --- | --- |
| AC//2 M ZnSO4 (aq.)//Zn | 0.2~1.8 V | 272.25 F/g (0.1 A/g) | 84.0 Wh/Kg | 91% after 10, 000 cycles | Energy Storage Mater. 2018,13, 96–102 |
| AC//1 M Zn(CF3SO3)2 (DOL-DME)//Zn | 0~1.8 V | 116 F/g (0.5 A/g) | 44.9 Wh/Kg | \ | Energy Storage Mater. 2018,13, 96–102 |
| AC//1M Zn(CF3SO3)2 (AN)//Zn | 0~1.8 V | 130 F/g (2 A/g) | 52.7 Wh/Kg | 92% after 22, 000 cycles | Energy Storage Mater. 2018,13, 96–102 |
| AC//2M ZnSO4 (aq.)//Zn | 0.5~1.5 V | 259 F/g (0.05 A/g) | 36.0 Wh/kg | 100% after 10, 000 cycles | Adv. Mater. 2019, 31, 1806005 |
| CNT// ZnSO4 (aq. or gel.)//Zn | 0.2~1.8 V | 83.2 mF/cm2 (1 mA/cm2) | 29.6 μWh/cm2 | 87% after 6, 000 cycles | Energy Environ. Sci., 2018, 11, 3367--3374 |
| N-PC//1M ZnSO4//Zn | 0-1.8V | 177.8 mAh g-1 (4.2 A g-1) | 107.3 Wh kg-1 | 73.6% after 100,000 cycles | Adv. Mater., 2019, 1904948 |
| L-NS-CNS//2 M ZnSO4//Zn | 0.2-1.8 V | 233.4 F g-1 (0.1 A g-1) | 91 Wh kg-1 | 94.2% after 18, 000 cycles | Adv. Funct. Mater. 2022, 32, 2209914 |
| AC//ZnMg-0.1//Zn | 0.2-1.85 V | 154 mAh g-1 (1 A g-1) | \ | 98.7% after 10, 000 cycles | Adv. Energy Mater., 2021, 2101158 |
| O-PC//3M Zn(ClO4)2//Zn | 0-1.9 V | 340.7 F g-1 (0.1 A g-1) | 104.8 Wh kg-1 | 99.2% after 30, 000 cycles | Adv. Energy Mater.2020, 10, 2001705 |
| aMEGO//0.5m+1m-H2O/AN electrolyte//Zn | 0~2.2 V | 192 F/g (0.5 A/g) | 129 Wh kg-1 | 88% after 120, 000 cycles | This work |

Table S2. . Coulombic efficiency comparison of different electrolyte systems

| Electrolyte system | Test Protocol | CE (%) | Ionic conductivity | Reference |
| --- | --- | --- | --- | --- |
| 4m Zn(OTF)2+0.5m Me3EtNOTF-H2O | 0.5 mA cm-2, 0.5 mAh cm-2 | 99.9% (1000 cycles) | ~25 mS cm-1 | Nat. Nanotech., 2021, 16, 902 |
| 1m Zn(TFSI)2+20m LiTFSI-H2O | CV at 1 mV s-1 -0.6-0.6 V | 99.7% (200 cycles) | \ | Nat. Mater. 2018, 17, 543 |
| 4m Zn(BF4)2-EG | 1 mA cm-2, 0.5 mAh cm-2 | 99.4% (400 cycles) | 4.5 mS cm-1 | Nat. Sustain., 2022, 5, 205 |
| Zn(CF3SO3)2-Methanol | 2.93 mA cm-2 2.93 mAh cm-2 | 99.9% (140 cycles) | 8-15 mS cm-1 | Proc. Natl. Acad. Sci. U. S. A., 2022, 24, e2121138119 |
| Zn(ClO4)2-H2O- Succinonitrile eutectic electrolyte | 0.5 mA cm-2, 0.5 mAh cm-2 | 98.4% (45-90 cycles) | 17.66 mS cm-1 | Joule, 2020, 7, 1557 |
| ZnSO4-H2O-Methanol | 1 mA cm-2, 0.5 mAh cm-2 | 99.7% (900 cycles) | 1.68 mS cm-1 | Angew Chem Int Edit 2021, 60 (13), 7366 |
| ZnSO4-glucose-H2O | 1 mA cm-2, 0.5 mAh cm-2 | 97.2% (200 cycles) | \ | Angew Chem Int Edit 2021, 60 (33), 18247 |
| 0.5m Zn(CF3SO3)2+1m LiTFSI-H2O/AN | 5 mA cm-2, 0.5 mAh cm-2 | 97.3% (3000 cycles) | 23 mS cm-1 | This work |