Supporting Information for

Enhancing the Performance of Perovskite Light-Emitting Diodes via Synergistic Effect of Defect Passivation and Dielectric Screening

Xuanchi Yu1, 2, Jia Guo1, *, Yulin Mao1, Chengwei Shan2, Fengshou Tian2, Bingheng Meng2, Zhaojin Wang2, Tianqi Zhang1, Aung Ko Ko KYAW2, Shuming Chen2, Xiaowei Sun2, Kai Wang2, Rui Chen2, * and Guichuan Xing1, *

1 Institute of Applied Physics and Materials Engineering, University of Macau, Avenida da Universidade, Taipa, Macao 999078, P. R. China

2 Department of Electrical and Electronic Engineering, Southern University of Science and Technology, Shenzhen 518055, P. R. China

* Corresponding authors. E-mail: gcxing@um.edu.mo (Guichuan Xing); chenr@sustech.edu.cn (Rui Chen); jiaguo@um.edu.mo (Jia Guo)

Supplementary Figures and Tables

Fig. S1 PL spectra of control and target perovskite films with different thickness

Fig. S2 TA measurements for control and target perovskite films following excitation at 360 nm. Pseudo color TA spectra of the a control and b target films. TA spectra at selected probe delay times for the c control and d target films

Fig. S3 XRD patterns of quasi-2D perovskite films without and with different KBr concentration

Fig. S4 XPS spectra of a K 2p signals, b Pb 4f signals, c Br 3d signals and d N 1s signals of perovskite films without and with different KBr concentration

Fig. S5 a Average thickness of the control and target perovskite thin films at four different sites. b The distribution of four sites in the actual film

Fig. S6 Cross-sectional SEM images of a control and b target PeLEDs. c Device structure of fabricated PeLEDs

Fig. S7 SEM images of a control and b target perovskite films

Fig. S8 AFM a 2D and b 3D images of control perovskite films. AFM c 2D and d 3D images of target perovskite films

Fig. S9 Capacitance-Voltage (C–V) curve of control and target PeLEDs

Fig. S10 EL spectra of a control and b target PeLEDs at 0 to 8 V bias with 0.1 V interval

Fig. S11 CIE coordinate of control and target PeLEDs

Fig. S12 Operational lifetime tested at a constant current density of 1.6 mA cm–2 for control and 1.3 mA cm–2 for target PeLEDs

Table S1 Lifetimes extracted from the TRPL decays of the control and target films, excited by a 360 nm laser

|  | Control | Target |
| --- | --- | --- |
| A1 | 0.42 ± 0.02 | 0.37 ± 0.02 |
| τ1 (ns) | 9.33 ± 0.69 | 9.19 ± 0.87 |
| A2 | 0.56 ± 0.02 | 0.63 ± 0.02 |
| τ2 (ns) | 58.95 ± 2.18 | 67.45 ± 2.63 |
| τavg (ns) | 53.69 | 63.10 |

Table S2 XPS fitting results of perovskite films without and with different KBr concentration

|  | C | N | Pb | Br | K | Atomic ratio (C:N:Pb:Br:K) |
| --- | --- | --- | --- | --- | --- | --- |
| w/o KBr | 34.71 | 15.65 | 9.4 | 40.24 | 0 | 3.7: 1.7: 1: 4.3: 0 |
| 0.05 M KBr | 32.44 | 14.16 | 8.99 | 40.48 | 3.92 | 3.6: 1.6: 1: 4.5: 0.4 |
| 0.1 M KBr | 38.78 | 12.02 | 7.39 | 35.17 | 6.64 | 5.2: 1.6: 1: 4.8: 0.9 |
| 0.15 M KBr | 34.31 | 11.64 | 7.58 | 39.29 | 7.18 | 4.5: 1.5: 1: 5.18: 0.95 |

Table S3 PLQY, PL average lifetimes (avg), radiative decay rates (kr), and nonradiative recombination rates (knr) of control and target perovskite films

|  | Control | Target |
| --- | --- | --- |
| PLQY (%) | 66.5 | 89.5 |
| avg (ns) | 53.69 | 63.10 |
| kr (107 s-1) | 1.24 | 1.42 |
| knr (107 s-1) | 0.624 | 0.166 |

Table S4 Performance metrics of the state-of-the-art green PeLEDs

| Perovskite | EQE (%) | Luminance (cd/m2) | CE (cd/A) | Von (V) | References |  |
| --- | --- | --- | --- | --- | --- | --- |
| CsPbBr3:PEABr = 1:0.4 | 32.1 | 1.1 × 104 | 111.7 | 2.5 | Adv. Mater. 2024, 2400421 |
| PEA2(FAPbBr3)2PbBr4 | 30.84 | 3.9× 104 | 115.32 | ~3 | Adv. Mater. 2023, 35, 2302283 |
| PEA2(FAPbBr3)2PbBr4 | 20.82 | ~1 × 104 | ~82 | ~2.8 | Nano-Micro Lett. 2023, 15, 119 |  |
| PEA2FAn-1PbnBr3n+1 (n = 5) | 21.2 | > 6.1 × 104 | - | ~3 | Adv. Funct. Mater. 2021, 31, 2103890 |  |
| PEA2FAn-1PbnBr3n+1 (n = 5) | 22.2 | 5.4 × 104 | - | 3 | Light Sci Appl. 2022, 11, 69 |  |
| PEA2Csn-1PbnBr3n+1 | 21.0 | 4.8 × 104 | - | 2.9 | J. Phys. Chem. C. 2023, 127, 19, 9388–9396 |  |
| PEA2(FAPbBr3)2PbBr4 | 25.9 | 2.9 × 104 | 108.1 | 2.9 | Nano Lett. 2023, 23, 23, 11082–11090 |  |
| CsPbBr3:PEABr = 1:0.4 | 19.3 | 1.2 × 104 | 61.7 | 2.6 | Adv. Optical Mater. 2022, 10, 2200276 |  |
| PEA2FAn-1PbnBr3n+1 (n = 5) | 20.83 | 5.9 × 104 | 90.98 | < 3 | Our work |  |