Supporting Information for

Boosted Lithium-Ion Transport Kinetics in n-Type Siloxene Anodes Enabled by Selective Nucleophilic Substitution of Phosphorus

Se In Kim1, Woong-Ju Kim1, Jin Gu Kang2, *, and Dong-Wan Kim1, *

1School of Civil, Environmental and Architectural Engineering, Korea University, Seoul 02841, South Korea

2Nanophotonics Research Center, Korea Institute of Science and Technology, Seoul, 02792, South Korea

*Corresponding authors. E-mail: dwkim1@korea.ac.kr (Dong-Wan Kim); lucid1@kist.re.kr  (Jin Gu Kang)

Supplementary Note S1

Using the elemental analysis results obtained via ICP-OES, we determined the doping concentrations of the doped SX samples. The number density of the SX molecules (NSX) is:

(S1)

where NA is Avogadro’s number (6.02×1023 mol-1), ρSX is the density of SX (1.54 g cm-3) [S1–S3], and MW is the molecular weight of SX (222 g mol-1). Thus, the doping concentration (ND, in atoms cm-3) can be calculated by:

(S2)

where a factor of 6 is the number of Si sites in one formula unit of SX (i.e., Si6O3H6), and xSi and xP are the measured atomic percentages of Si and P, respectively.

Supplementary Figures and Tables

Fig. S1 a Low- and b high-magnification SEM images of SX. b Magnified image of the square region in a

Fig. S2 a Low- and b high-magnification TEM images of SX. b Magnified image of the square region in a

Fig. S3 EDX elemental mapping of Si, O, and P in SX

Fig. S4 Survey XPS spectra of a SX and b n-SX

Fig. S5 Full-range FTIR transmittance spectra of SX, n-SX, and H-SX. Peaks are indexed with their corresponding vibrational modes on the image top

Fig. S6 CV curves of H-SX/A (left panel) and n-SX/V (right) at a scan rate of 0.1 mV s-1 during first, 5th, 15th, and 50th cycles

Fig. S7 Plots of (dE/dQ)-1 vs. E for a SX/A and b n-SX/A in the 0.01- 0.6 V range, acquired from their galvanostatic voltage curves at 200 mA g-1

Fig. S8 C.E. of SX/A, H-SX/A, and n-SX/V at 200 mA g-1

Fig. S9 Nyquist plots of SX/A at its a lithiated and b delithiated state during first, 10th, 20th, 50th, and 100th cycles. Open circles and solid lines denote the measured data and fitted results, respectively

Fig. S10. Plots of Z’ vs. ω−1/2 for a,b n-SX/A and c,d SX/A at their lithiated a,c and delithiated b,d states over a series of cycles (first, 10th, 20th, 50th, and 100th). Measured data were fitted with linear-regression to extract the Li diffusion coefficients

Fig. S11 Post-cycling a low- and b high-magnification SEM images of SX/A and c low- and d high-magnification SEM images of n-SX/A (after 100 cycles)

Fig. S12 High-resolution XPS Si 2p spectra of a SX/A and b n-SX/A after 100 cycles

Table S1 ICP-OES elemental analysis results and doping concentrations

| Electrode | Doping process condition |  | Content (at%) |  | Doping concentration (atoms cm-3) |
| --- | --- | --- | --- | --- | --- |
|  | SX:NaH2PO2 | Ar flow rate (sccm) | Si | P |  |
| SX | N.A. | N.A. | 49.6±0.001 | 0 | 0 |
| n-SX | 1:2 | 100 | 51.7±0.003 | 0.05±0.02 | 2.4×1019 |
| n-SX-101 | 1:10 | 100 | 56.0±0.02 | 0.08±0.04 | 3.6×1019 |
| n-SX-102 | 1:10 | 200 | 55.4±0.005 | 0.15±0.004 | 6.7×1019 |
| n-SX-103 | 1:10 | 300 | 49.4±0.001 | 0.16±0.02 | 8.1×1019 |

Table S2 Key electrochemical properties of the electrodes at 2000 mA g-1

| Electrodes | Activation cycle | Post-activation capacity (mAh g-1) | Capacity retention (%) |
| --- | --- | --- | --- |
| n-SX | 60 | 552 | 44 |
| n-SX-101 | 25 | 621 | 39 |
| n-SX-102 | 25 | 594 | 73 |
| n-SX-103 | 15 | 756 | 56 |
| 1n3S | 60 | 329 | 67 |
| 1n1S | 30 | 315 | 56 |
| 3n1S | 14 | 413 | 45 |
| SX | 230 | 153 | 90 |

Table S3 Performance summary of siloxene-based electrodes for lithium ion batteries

| Material | Engineering |  | CD (mA g-1) | Capacity (mAh g-1) | Cycle number | Retention (%) | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Intrinsic | External |  |  |  |  |  |
| n-SX-102 | Doping | N.A. | 2000 | 594 | 500 | 73 | This work |
| SX/SiOx | Oxidization | N.A. | 750 | ~700 | 300 | 98.6 | [S2] |
| SX/SiOx | Oxidization | N.A. | 1000 | 506 | 800 | ~99 | [S4] |
| SX | Oxidization | N.A. | 1000 | 750 | 200 | 77 | [S3] |
| SX | N.A. | Binder selection | 1000 | 231 | 1400 | 55 | [S5] |
| rGO-SX | N.A. | Aerogel-mediated | 1000 | 243 | 1000 | 99.5 | [S6] |
| COF-SX | N.A. | Surface modification | 2000 | 584 | 1000 | ~99 | [S7] |
| G-SX | N.A. | Surface modification | 4100 | 1040 | 1000 | 70 | [S8] |
| LM-SX | N.A. | Matrix-embedded | 2000 | 847 | 300 | ~99 | [S9] |
| Li-SX | N.A. | Prelithiated | 5000 | ~680 | 724 | 80 | [S10] |
| SX | N.A. | N.A. | 193 | 1845 | 58 | 79 | [S11] |

rGO: reduced graphene oxide; COF: covalent organic framework; G: graphene; LM: liquid metal

Supplementary References

- S. Yamanaka, H. Matsu-ura, M. Ishikawa, New deintercalation reaction of calcium from calcium disilicide. Synthesis of layered polysilane. Mater. Res. Bull. 31, 307-316 (1996). https://doi.org/10.1016/0025-5408(95)00195-6

- R. Fu, Y. Li, Y. Wu, C. Shen, C. Fan et al., Controlling siloxene oxidization to tailor SiOx anodes for high performance lithium ion batteries. J. Power Sources. 432, 65-72 (2019). https://doi.org/10.1016/j.jpowsour.2019.05.071

- D. J. Arnot, W. Li, D. C. Bock, C. A. Stackhouse, X. Tong et al., Low-oxidized siloxene nanosheets with high capacity, capacity retention, and rate capability in lithium-based batteries. Adv. Mater. Interfaces 9, 2102238 (2022). https://doi.org/10.1002/admi.202102238

- Y. Ren, X. Yin, L. Xiang, R. Xiao, H. Huo et al., Layer stacked SiOx microparticle with disconnected interstices enables stable interphase and particle integrity for lithium-ion batteries. J. Energy Chem. 86, 300-307 (2023). https://doi.org/10.1016/j.jechem.2023.07.023

- S. I. Kim, W.-J. Kim, J. G. Kang, D.-W. Kim, Intermolecular interaction engineering to enhance lithium-ion storage in two-dimensional oxidized silicon nanosheet anodes. Chem. Eng. J. 467, 143364 (2023). https://doi.org/10.1016/j.cej.2023.143364

- S. A. Alomari, D. P. Dubal, J. MacLeod, N. Motta, Three-dimensional nitrogen-doped rGO-siloxene nanocomposite anode for Li-ion storage. Appl. Surf. Sci. 624, 157099 (2023). https://doi.org/10.1016/j.apsusc.2023.157099

- Y. Zhang, Y. Wu, Y. An, C. Wei, L. Tan et al., Ultrastable and high-rate 2D siloxene anode enabled by covalent organic framework engineering for advanced lithium-ion batteries. Small Methods. 6, 2200306 (2022). https://doi.org/10.1002/smtd.202200306

- K. T. Kumar, M. J. Kumar Reddy, G. S. Sundari, S. Raghu, R. A. Kalaivani et al., Synthesis of graphene-siloxene nanosheet based layered composite materials by tuning its interface chemistry: an efficient anode with overwhelming electrochemical performances for lithium-ion batteries. J. Power Sources. 450, 227618 (2020). https://doi.org/10.1016/j.jpowsour.2019.227618

- Y. Zhang, L. Tan, Y. Wu, Y. An, Y. Liu et al., Self-healing and ultrastable anode based on room temperature liquid metal reinforced two-dimensional siloxene for high-performance lithium-ion batteries. Appl. Mater. Today 26, 101300 (2022). https://doi.org/10.1016/j.apmt.2021.101300

- H. Shen, Y. An, Q. Man, J. Wang, C. Liu et al., Controlled prelithiation of siloxene nanosheet anodes enables high performance 5 V-class lithium-ion batteries. Chem. Eng. J. 454, 140136 (2023). https://doi.org/10.1016/j.cej.2022.140136

- L. C. Loaiza, L. Monconduit, V. Seznec, Siloxene: a potential layered silicon intercalation anode for Na, Li and K ion batteries. J. Power Sources 417, 99-107 (2019). https://doi.org/10.1016/j.jpowsour.2019.02.030