Supporting Information for

Polymer Fiber Rigid Network with High Glass Transition Temperature Reinforces Stability of Organic Photovoltaics

Qiao Zhou1, Cenqi Yan1, *, Hongxiang Li1, Zhendong Zhu1, Yujie Gao1, Jie Xiong1, Hua Tang2, Can Zhu3, Hailin Yu1, Sandra P Gonzalez Lopez2, Jiayu Wang1, Meng Qin1, Jianshu Li1, Longbo Luo1, *, Xiangyang Liu1, Jiaqiang Qin1, Shirong Lu4, Lei Meng3, Frédéric Laquai2, Yongfang Li3, Pei Cheng1, *

1 College of Polymer Science and Engineering, State Key Laboratory of Polymer Materials Engineering, Sichuan University, Chengdu, 610065, P. R. China

2 KAUST Solar Center, Physical Sciences and Engineering Division, King Abdullah University of Science and Technology (KAUST), Thuwal, Kingdom of Saudi Arabia

3 Beijing National Laboratory for Molecular Sciences, CAS Key Laboratory of Organic Solids, Institute of Chemistry, Chinese Academy of Sciences, Beijing, 100190, P. R. China

4 Department of Material Science and Technology, Taizhou University, Taizhou, 318000, P. R. China

*Corresponding authors. E-mail: yancenqi@scu.edu.cn (Cenqi Yan); luolongbo@scu.edu.cn (Longbo Luo); chengpei@scu.edu.cn (Pei Cheng)

Supplementary Figures and Tables

Fig. S1 SEM images of ANF films with different dispersion concentrations

Fig. S2 Transmittance of ANF film

Fig. S3 AFM images of active layers with and without ANF

Fig. S4 a 2D and b 1D GIWAXS diffraction patterns of neat PM6, BTP-eC9, ANF-fresh and ANF-aged films

Fig. S5 Normalized absorption spectra of PM6:BTP-eC9 blend films without and with ANF before and after heating at 130 °C for 3 h

Table S1 Photovoltaic parameters decay of PM6: BTP-eC9-based OPVs with ANF of different dispersion concentrations heated at 130 °C for 0, 10, 20, 30, 60, 120, and 180 min

| ANF dispersion concentration (mg mL-1) | heating time (min) | remaining VOC ratio a) | remaining JSC ratio a) | remaining FF ratio a) | remaining PCE ratio a) |
| --- | --- | --- | --- | --- | --- |
| 0 | 0 | 1.00 | 1.00 | 1.00 | 1.00 |
| 0 | 10 | 0.957 | 1.01 | 0.945 | 0.907 |
| 0 | 20 | 0.943 | 1.02 | 0.941 | 0.899 |
| 0 | 30 | 0.940 | 1.02 | 0.939 | 0.897 |
| 0 | 60 | 0.921 | 1.02 | 0.923 | 0.865 |
| 0 | 120 | 0.903 | 1.02 | 0.912 | 0.837 |
| 0 | 180 | 0.894 | 1.01 | 0.909 | 0.820 |
| 0.23 | 0 | 1.00 | 1.00 | 1.00 | 1.00 |
| 0.23 | 10 | 0.985 | 1.01 | 0.963 | 0.954 |
| 0.23 | 20 | 0.981 | 1.02 | 0.975 | 0.971 |
| 0.23 | 30 | 0.978 | 1.02 | 0.972 | 0.970 |
| 0.23 | 60 | 0.974 | 1.03 | 0.971 | 0.971 |
| 0.23 | 120 | 0.965 | 1.03 | 0.964 | 0.951 |
| 0.23 | 180 | 0.962 | 1.02 | 0.959 | 0.938 |
| 0.46 | 0 | 1.00 | 1.00 | 1.00 | 1.00 |
| 0.46 | 10 | 0.987 | 1.00 | 0.968 | 0.955 |
| 0.46 | 20 | 0.982 | 1.01 | 0.975 | 0.965 |
| 0.46 | 30 | 0.979 | 1.01 | 0.977 | 0.966 |
| 0.46 | 60 | 0.975 | 1.02 | 0.974 | 0.960 |
| 0.46 | 120 | 0.970 | 1.01 | 0.970 | 0.946 |
| 0.46 | 180 | 0.967 | 1.00 | 0.964 | 0.933 |
| 0.91 | 0 | 1.00 | 1.00 | 1.00 | 1.00 |
| 0.91 | 10 | 0.989 | 1.00 | 0.970 | 0.959 |
| 0.91 | 20 | 0.982 | 1.01 | 0.972 | 0.960 |
| 0.91 | 30 | 0.979 | 1.01 | 0.973 | 0.960 |
| 0.91 | 60 | 0.976 | 1.01 | 0.969 | 0.951 |
| 0.91 | 120 | 0.972 | 1.01 | 0.968 | 0.945 |
| 0.91 | 180 | 0.970 | 1.00 | 0.962 | 0.931 |

a) Average value of eight independent devices

Table S2 Average and best device data based on PM6: L8-BO, PM6: PC71BM, and PTB7-Th: IEICO-4F blend films without and with ANF before and after heating at 130 °C for 180 min

| active layer | ANF | heating time (min) | VOC (V) | JSC (mA cm-2) | FF (%) | PCE (%) |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  |  |  | best | average a) |
| PM6:L8-BO | w/o | 0 | 0.878 | 24.6 | 76.4 | 16.5 | 16.1 |
|  | w/o | 180 | 0.790 | 24.8 | 65.3 | 12.8 | 13.0 |
|  | w | 0 | 0.875 | 24.9 | 74.4 | 16.2 | 16.0 |
|  | w | 180 | 0.843 | 25.2 | 68.9 | 14.6 | 14.5 |
| PM6:PC71BM | w/o | 0 | 0.872 | 12.9 | 61.8 | 6.93 | 6.55 |
|  | w/o | 180 | 0.816 | 11.7 | 57.3 | 5.46 | 5.05 |
|  | w | 0 | 0.861 | 12.8 | 54.6 | 6.01 | 5.55 |
|  | w | 180 | 0.826 | 11.8 | 52.7 | 5.15 | 5.03 |
| PTB7-Th:IEICO-4F | w/o | 0 | 0.725 | 24.3 | 58.8 | 10.3 | 9.87 |
|  | w/o | 180 | 0.588 | 23.6 | 48.4 | 6.71 | 6.87 |
|  | w | 0 | 0.727 | 23.9 | 57.8 | 10.1 | 9.65 |
|  | w | 180 | 0.712 | 24.0 | 52.6 | 9.01 | 8.65 |

a) Average value of eight independent devices