Supporting Information for

Defect Engineering with Rational Dopants Modulation for High-Temperature Energy Harvesting in Lead-Free Piezoceramics

Kaibiao Xi1,†, Jianzhe Guo1,†, Mupeng Zheng1, Mankang Zhu1, Yudong Hou1,

Key Laboratory of Advanced Functional Materials, Ministry of Education, College of Materials Science and Engineering, Beijing University of Technology, Beijing 100124, P. R. China

†Kaibiao Xi and Jianzhe Guo contributed equally to this work.

*Corresponding author. E-mail: ydhou@bjut.edu.cn (Yudong Hou)

Supplementary Figures

Fig. S1 The room-temperature XRD patterns of BF-BT-xMn ceramics in the 2θ range of 10°-90° and 30.5°-32.5°

Fig. S2 (a-c) SEM images of the polished and acid etched cross-section of x = 0.1, 0.3 and 0.4 samples, and the insets show the corresponding grain size distribution; (d) The density of the BF-BT-xMn ceramics

Fig. S3 (a) P-E loops and (b) S-P curves of x = 0.0, 0.2 and 0.5 samples

Fig. S4 The r-T curves of (a) x = 0.0 and (b) x = 0.5 sample ceramics measured at different frequency

Fig. S5 The kp of the BF-BT-xMn ceramics

Fig. S6 (a) The ln -1000/T curves of x = 0.0, x = 0.2 and x = 0.5 ceramics fitted by DC impedance; (b) The conductance activation energy Ea of the three samples

Fig. S7 Rg and Rgb of x = 0.0, 0.2 and 0.5 samples measured at 250 oC

Fig. S8 The TC of the BF-BT-xMn ceramics

Fig. S9 The relationship between the Vopen and frequency of the cantilever PEHs system

Fig. S10 (a-c) The Vopen and ISC of the three PEHs tested at different temperature; (d-f) The output power with load resistance of the three PEHs tested at different temperature.

Fig. S11 The  of the three PEHs tested at different temperature

Table S1 The length of B-O bond of x = 0.0, x = 0.2 and x = 0.5 samples

|  | R3c (lB-O = a/2) | R3c (lB-O = c/2) | Pm-3m (lB-O = c/2) |
| --- | --- | --- | --- |
| x = 0.0 | 2.81940 Å | 6.9436 Å | 2.00545 Å |
| x = 0.2 | 2.83155 Å | 6.9473 Å | 2.00720 Å |
| x = 0.5 | 2.82145 Å | 6.9150 Å | 2.00595 Å |