Supporting Information for

An Artificial Intelligence-Assisted Flexible and Wearable Mechanoluminescent Strain Sensor System

Yan Dong1, *, Wenzheng An1, Zihu Wang1 and Dongzhi Zhang1,*

1College of Control Science and Engineering, China University of Petroleum (East China), Qingdao 266580, P. R. China

*Corresponding authors. E-mail: dzzhang@upc.edu.cn (Dongzhi Zhang); yandong@upc.edu.cn (Yan Dong)

Supplementary Figures

Fig. S1 Schematic illustration of the preparation process of SFLC film

Fig. S2 (a) and (b) SEM image of the ZnS:Cu fluorescent particles for the fabrication of the SFLC film. (c) XRD of the ZnS:Cu fluorescent particles

Fig. S3 (a) Schematic illustration of the ZnS:Cu-SG/PDMS film stripping test. (b) Stripping force vs displacement curve of the ZnS:Cu-SG/PDMS film

Fig. S4 (a) Stripping force vs displacement curves of the SFLC film after different stretching cycles. (b) Stripping force at the beginning of detachment of PDMS layer and the SG layer of the SFLC film

Fig. S5 Photos of SFLC film fabricated by different methods (a) drop-casting method (b) brush-casting method, the CNTs film in the red circles is not uniform

Fig. S6 Effects of number of lift-cast cycles of the top CNTs layers on the strain sensing performance of the SFLC film

Fig. S7 Effects of ZnS:Cu concentration in the SG layer on the performance of the SFLC film. (n = 5, mean ± s.d.)\

Fig. S8 Effects of PDMS layer deformation on the detected fluorescent intensity

Fig. S9 SEM images showing the surface morphology of the top CNTs shielding layer after (a) 0, (b) 100, (c) 300, and (d) 500 stretching cycles. (e) PL spectrum and (f) comparison of the peak intensity of the PL spectrum of the SFLC film under the same strain after different stretching cycles

Table S1 List of features for the color data for neural network training and strain prediction

| No. | Feature | Description | No. | Feature | Description |
| --- | --- | --- | --- | --- | --- |
| 1 | Rm | Mean value of R channel | 13 | Vm | Mean value of V channel |
| 2 | Gm | Mean value of G channel | 14 | Xm | Mean value of X channel |
| 3 | Bm | Mean value of B channel | 15 | Ym | Mean value of Y channel |
| 4 | Rm/RGBn | Ratio of Rm and RGBn | 16 | Zm | Mean value of Z channel |
| 5 | Gm/RGBn | Ratio of Gm and RGBn | 17 | Lm | Mean value of L channel |
| 6 | Bm/RGBn | Ratio of Bm and RGBn | 18 | am | Mean value of a channel |
| 7 | RGBn | Sum of Rm, Gm, Bm | 19 | bm | Mean value of b channel |
| 8 | Intensity (unweighted) | Grey scale formula result 0.299*Rm+0.587* Gm+0.114* Bm | 20 | HSVn | Sum of Hm, Sm, Vm |
| 9 | Cbm | Mean value of Cb channel -0.172*Rm-0.339* Gm+0.511* Bm+128 | 21 | XYZn | Sum of Xm, Ym, Zm |
| 10 | Crm | Mean value of Cr channel 0.511*Rm-0.428* Gm-0.083* Bm+128 | 22 | Lab | Sum of Lm, am, bm |
| 11 | Hm | Mean value of H channel | 23 | Strain | Strain of the sensor |
| 12 | Sm | Mean value of S channel | 24 | CT | Color temperature |

Table S2 Parameters of 1D-CNN-GRU model for strain prediction

| Layer | Name | Input shape | Number of neurons | Convolution kernel | Step size | Return sequences | Activation function | Output shape |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | InputLayer | 24×1 | － | － | － | － | － | 24×1 |
| 2 | Conv1D | 24×1 | 32 | (1,1) | 1 | － | Relu | 24×32 |
| 3 | MaxPooling1D | 24×32 | － | － | 1 | － | － | 24×32 |
| 4 | Conv1D | 24×32 | 64 | (1,1) | 1 | － | Relu | 24×64 |
| 5 | Conv1D | 24×32 | 64 | (1,1) | 1 | － | Relu | 24×64 |
| 6 | MaxPooling1D | 24×64 | － | － | 1 | － | － | 24×64 |
| 7 | Conv1D | 24×64 | 128 | (1,1) | 1 | － | Relu | 24×128 |
| 8 | Conv1D | 24×64 | 128 | (1,1) | 1 | － | Relu | 24×128 |
| 9 | MaxPooling1D | 24×128 | － | － | 1 | － | － | 24×128 |
| 10 | GRU | 24×128 | 64 | (1,1) | － | True | Linear | 24×64 |
| 11 | GRU | 24×64 | 64 | (1,1) | － | False | Linear | 64 |
| 12 | Dense | 64 | 1 | － | － | － | Linear | 1 |

Fig. S10 (a) Comparison of the coefﬁcient of determination (R2) of the output results of the three neural network models. (b) Comparison of the predicted strains (yellow dots) obtained under different color temperature with the true strain values (blue line) without color temperature auto-correction

Fig. S11 (a) RGB values extracted from phots of the same SFLC film taken by smartphones of different brands. (b) RMSE, MAE, and R2 values obtained using photos taken by smartphones of different brands

Table S3 RMSE, MAE, and R2 values obtained using photos taken by smartphones of different brands

Table S4 Effects of repetitive bending on the strain prediction performance of the sensor system

Table S5 Effects of repetitive twisting on the strain prediction performance of the sensor system

Fig. S12 The strain prediction results of repetitive testing of the sensor film after multiple times of (a) bending, (b) twisting, and (c) stretching

Fig. S13 Algorithm flow chart showing the training and optimization process of the 5D-CNN-GRU neural network for hand gesture recognition

Fig. S14 Process of the color data extraction and conversion to RGB distribution from the image of a human hand wearing the smart glove

Table S6 Parameters of 5D-CNN-GRU model for hand gesture recognition

| Layer | Name |  | Input shape | Number of neurons | Return sequences | Activation function | Output shape |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | Input | Chanel 1 | 765×1 | － | － | － | 765×1 |
|  |  | Chanel 2 | 765×1 |  |  |  | 765×1 |
|  |  | Chanel 3 | 765×1 |  |  |  | 765×1 |
|  |  | Chanel 4 | 765×1 |  |  |  | 765×1 |
|  |  | Chanel 5 | 765×1 |  |  |  | 765×1 |
| 2 | Function model |  | 765×1 | － | － | － | 753×64 |
|  |  |  | 765×1 |  |  |  | 753×64 |
|  |  |  | 765×1 |  |  |  | 753×64 |
|  |  |  | 765×1 |  |  |  | 753×64 |
|  |  |  | 765×1 |  |  |  | 753×64 |
| 3 | Concatenate |  | 753×64 | － | － | － | 753×320 |
|  |  |  | 753×64 |  |  |  |  |
|  |  |  | 753×64 |  |  |  |  |
|  |  |  | 753×64 |  |  |  |  |
|  |  |  | 753×64 |  |  |  |  |
| 4 | GRU |  | 753×320 | 64 | True | Linear | 753×64 |
| 5 | GRU |  | 753×64 | 32 | False | Linear | 32 |
| 6 | Dense |  | 32 | 1 | － | Softmax | 11 |

Table S7 The network parameters of 5D-CNN-GRU Functional model

| Layer | Name | Input shape | Number of neurons | Convolution kernel | Step size | Activation function | Output shape |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | InputLayer | 765×1 | － | － | － | － | 765×1 |
| 2 | Conv1D | 765×1 | 16 | (4,1) | 1 | Relu | 762×16 |
| 3 | Conv1D | 762×16 | 16 | (4,1) | 1 | Relu | 759×16 |
| 4 | MaxPooling1D | 759×16 | － | － | 1 | － | 759×16 |
| 5 | Conv1D | 759×16 | 64 | (4,1) | 1 | Relu | 756×64 |
| 6 | Conv1D | 756×64 | 64 | (4,1) | 1 | Relu | 753×64 |
| 7 | MaxPooling1D | 753×64 | － | － | 1 | － | 753×64 |