Supporting Information for

Low-Temperature Fabrication of Stable Black-Phase CsPbI3 Perovskite Flexible Photodetectors towards Wearable Health Monitoring

Yingjie Zhao1,*, Yicheng Sun1, Chaoxin Pei1, Xing Yin1, Xinyi Li3, Yi Hao1, Mengru Zhang1, Meng Yuan3, Jinglin Zhou4, Yu Chen4, and Yanlin Song2,*

1College of Chemistry and Pingyuan Laboratory, Zhengzhou University, Zhengzhou 450001, P. R. China

2Key Laboratory of Green Printing, Institute of Chemistry, Chinese Academy of Sciences, Beijing 100190, P. R. China

3Key Laboratory of Bio-inspired Materials and Interfacial Science, Technical Institute of Physics and Chemistry, Chinese Academy of Sciences, Beijing 100190, P. R. China

4Institute of High Energy Physics, Chinese Academy of Sciences, Beijing 100049, P. R. China

*Corresponding authors. E-mail: zhaoyingjie5@zzu.edu.cn (Yingjie Zhao); ylsong@iccas.ac.cn (Yanlin Song)

Supplementary Figures

Fig. S1 Schematic diagram of the preparation process of black-phase CsPbI3 perovskite films

Fig. S2 Schematic diagram of the crystal of the a δ-phase and the b black-phase perovskite

Fig. S3 Color evolution of perovskite films with DPPOCl additive at different annealing times under 50 ℃

Fig. S4 Schematic diagram of crystal orientation for perovskite films a without the DPPOCl additive and b with the DPPOCl additive

Fig. S5 XRD patterns of the fabricated perovskite films and the standard diffraction peaks of α-CsPbI3 phase and-CsPbI3 phase, confirming the formation of the -CsPbI3 phase

Fig. S6 The absorption spectra of perovskite film without the DPPOCl additive under an annealing temperature of 50 ℃

Fig. S7 XPS spectra of perovskite films with the DPPOCl additive and without the DPPOCl additive

Fig. S8 The FTIR spectra result of H-bond for perovskite film with DPPOCl additive (blue line) and DPPOCl film (black line)

Fig. S9 The morphology of perovskite film without the DPPOCl additive under an annealing temperature of 50 ℃

Fig. S10 The PL stability of perovskite films with the DPPOCl additive at nitrogen atmosphere

Fig. S11 a Logarithmic I-V curve of the photodetector based on perovskite devices without the DPPOCl additive. b Photocurrent and responsivities of perovskite devices without the DPPOCl additive under different irradiation powers ranging from 2.38 × 10-1 to 416 mW cm−2

Fig. S12 On-off stability tests of 176 cycles for perovskite devices with DPPOCl additive under a fixed irradiation power of 416.9 mW cm−2 at 5V bias

Fig. S13 Response speed for perovskite devices without the DPPOCl additive under a fixed irradiation power of 416.9 mW cm−2 at 5V bias

Fig. S14 Statistical responsivities and detectivities from ten different devices under a fixed light intensity of 2.38 × 10-1 mW cm−2. Error bars represent standard deviation

Fig. S15 Normalized responsivities from ten different devices in the air (humidity: 40%; temperature: 25℃) for different times, indicating that devices with the DPPOCl additive possess superior stability

Fig. S16 Photograph of large-size perovskite films with the DPPOCl additive

Fig. S17 Statistical normalized photocurrent imaging map of flexible perovskite film devices without the DPPOCl additive under a fixed light intensity of 416.9 mW cm−2

Fig. S18 Statistical responsivity from thirty different flexible perovskite film devices without the DPPOCl additive

Fig. S19 Logarithmic I-V curve of the photodetector before bending test and after 100 bending cycles test based on perovskite devices. a with DPPOCl additive and b without DPPOCl additive under a fixed irradiation power of 416.9 mW cm−2 and dark conditions

Supplementary Table

Table S1 Device performance parameters comparison between previously reported all-inorganic CsPbI3 perovskite film photodetectors and the present perovskite devices

| Device structure | Substrate | Responsivity (A W-1) | Detectivity (Jones) | Response speed (rise/decay) | Wavelength (nm) | Refs. |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| photoconductor | flexible | 42.1 | 1.3 × 1014 | 290.0/340.0 μs | 680 | This work |
| photodiode | rigid | 0.2 | 2.0 × 1010 | 2.0/2.0 μs | 690 | [S1] |
| photoconductor | rigid | 3.0 × 10-4 | 1.2 × 109 | 2.4/1.1 s | solar light | [S2] |  |
| photodiode | rigid | 0.43 | 2.2 × 1011 | 0.28/1.1 ms | 550 | [S3] |  |
| photodiode | rigid | 0.035 | 1.8 × 1012 | / | 640 | [S4] |  |
| photodiode | rigid | 8.2 | 1.4 × 1012 | 25/30.6 μs | 300-700 | [S5] |  |
| photodiode | rigid | 0.16 | 2.7 × 1012 | 13.9/12.7μs | 690 | [S6] |  |
| photoconductor | flexible | 0.13 | / | 6.0/7.1 ms | 650 | [S7] |  |
| photodiode | rigid | 0.1 | 5.0 × 1013 | / | 450 | [S8] |  |
| photodiode | rigid | 0.4 | 2.4 × 1012 | 7 μs/8 μs | 650-680 | [S9] |  |
| photoconductor | flexible | 0.75 | 3.5 × 1010 | / | 530 | [S10] |  |

Supplementary References

- J. A. Steele, T. Braeckevelt, V. Prakasam, G. Degutis, H. Yuan, et al. An embedded interfacial network stabilizes inorganic CsPbI3 perovskite thin films. Nat. Commun. 13(1), 7513 (2022). https://doi.org/10.1038/s41467-022-35255-9

- K. Maity, U. Pal, H. K. Mishra, P. Maji, P. Sadhukhan, et al. Piezo-phototronic effect in highly stable CsPbI3-pvdf composite for self-powered nanogenerator and photodetector. Nano Energy. 92, 106743 (2022). https://doi.org/10.1016/j.nanoen.2021.106743

- J. Li, G. Zhang, Z. Zhang, J. Li, Z. Uddin, et al. Defect passivation via additive engineering to improve photodetection performance in CsPbI2Br perovskite photodetectors. ACS Appl. Mater. Interfaces 13(47), 56358-56365 (2021). https://doi.org/10.1021/acsami.1c19323

- K. M. Sim, A. Swarnkar, A. Nag, D. S. Chung. Phase stabilized α‐CsPbI3 perovskite nanocrystals for photodiode applications. Laser Photonics Rev. 12(1), 1700209 (2017). https://doi.org/10.1002/lpor.201700209

- S. Pal, A. Ghorai, S. Mahato, S. K. Ray. Piezo‐phototronic effect‐induced self‐powered broadband photodetectors using environmentally stable α‐CsPbI3 perovskite nanocrystals. Adv. Opt. Mater. 11(16), 2300233 (2023). https://doi.org/10.1002/adom.202300233

- C. Zhao, P. Liu, W. Cai, W. Xu, M. U. Ali, et al. Polymer‐assisted phase stable γ‐CsPbI3 perovskite film for self‐powered and ultrafast photodiodes. Adv. Mater. Interfaces. 9(9), 2102212 (2022). https://doi.org/10.1002/admi.202102212

- M. Wang, W. Tian, F. Cao, M. Wang, L. Li. Flexible and self‐powered lateral photodetector based on inorganic perovskite CsPbI3–CsPbBr3 heterojunction nanowire array. Adv. Funct. Mater. 30(16), 1909771 (2020). https://doi.org/10.1002/adfm.201909771

- C. Bi, S. V. Kershaw, A. L. Rogach, J. Tian. Improved stability and photodetector performance of CsPbI3 perovskite quantum dots by ligand exchange with aminoethanethiol. Adv. Funct. Mater. 29(29), 1902446 (2019). https://doi.org/10.1002/adfm.201902446

- M. I. Pintor Monroy, I. Goldberg, K. Elkhouly, E. Georgitzikis, L. Clinckemalie, et al. All-evaporated, all-inorganic CsPbI3 perovskite-based devices for broad-band photodetector and solar cell applications. ACS Appl. Electron. Mater. 3(7), 3023-3033 (2021). https://doi.org/10.1021/acsaelm.1c00252

- Y. Zhou, J. Luo, Y. Zhao, C. Ge, C. Wang, et al. Flexible linearly polarized photodetectors based on all‐inorganic perovskite CsPbI3 nanowires. Adv. Opt. Mater. 6(22), 1800679 (2018). https://doi.org/10.1002/adom.201800679