Supporting Information for

Lattice Anchoring Stabilizes α-FAPbI3 Perovskite for High-Performance X-Ray Detectors

Yu-Hua Huang1, Su-Yan Zou1, Cong-Yi Sheng1, Yu-Chuang Fang1, Xu-Dong Wang1, *, Wei Wei1, Wen-Guang Li1 and Dai-Bin Kuang1, *

1 Key Laboratory of Bioinorganic and Synthetic Chemistry of Ministry of Education, LIFM, GBRCE for Functional Molecular Engineering, School of Chemistry, IGCME, Sun Yat-Sen University, Guangzhou 510275, P. R. China

*Corresponding authors. E-mail: wangxd26@mail.sysu.edu.cn (Xu-Dong Wang); kuangdb@mail.sysu.edu.cn (Dai-Bin Kuang)

Supplementary Figures

Fig. S1 1H NMR spectrum of the (a) (HtrzT)PbI3(0.5)/FAPbI3, (b) (HtrzT)PbI3(1.0)/FAPbI3, (c) (HtrzT)PbI3(1.5)/FAPbI3

Fig. S2 Optical photographs of (HtrzT)PbI3/FAPbI3 perovskite microcrystals (a) before and (b) after annealing at 150 °C

Fig. S3 The XRD patterns of freshly prepared FAPbI3 and (HtrzT)PbI3/FAPbI3 microcrystals

Fig. S4 (a) The XRD patterns of FAPbI3 and (HtrzT)PbI3/FAPbI3 microcrystals after annealing at 150 °C. (b) Magnified (002) diffraction peaks in the region shaded in red in (a)

Fig. S5 The photograph of the (HtrzT)PbI3(1.0)/FAPbI3 films (a) w/o and (d) with hot-pressing. The SEM images of the (HtrzT)PbI3(1.0)/FAPbI3 films (b) w/o and (e) with hot-pressing. Cross-sectional SEM images of the (HtrzT)PbI3(1.0)/FAPbI3 films (c) w/o and (f) with hot-pressing

Fig. S6 The thickness profile curves of the (a) FAPbI3, (b) (HtrzT)PbI3(0.5)/FAPbI3 and (c) (HtrzT)PbI3(1.5)/FAPbI3 films with hot-pressing

Fig. S7 (a) The TEM image of (HtrzT)PbI3(1.0)/FAPbI3, are the same as that in Fig. 1c. Images in (b) and (c) are fast Fourier transform (FFT) of the blue and green dashed square in a, corresponding to the FAPbI3 and (HtrzT)PbI3 perovskites, respectively

Fig. S8 The crystal structure of 1D (HtrzT)PbI3 perovskite

Fig. S9 (a) SEM image and (b) the corresponding EDS line scan spectrum (S element) of (HtrzT)PbI3(1.0)/FAPbI3 perovskite film

Fig. S10 TGA curves of FAPbI3 and (HtrzT)PbI3(1.0)/FAPbI3

Fig. S11 The XRD patterns of FAPbI3 and (HtrzT)PbI3/FAPbI3 perovskite microcrystals after being stored in a nitrogen atmosphere for (a) 0 day and (b) 105 days

Fig. S12 The XRD patterns of FAPbI3 and (HtrzT)PbI3/FAPbI3 perovskite films after being stored in a nitrogen atmosphere for (a) 0 day and (b) 105 days. (c) Diffraction peaks of FAPbI3 film in the region shaded in blue in (a)

Fig. S13 The XRD patterns of FAPbI3 and (HtrzT)PbI3/FAPbI3 perovskite microcrystals (a) before and (b) after light aging (100 mW cm-2) for 60 hours

Fig. S14 Secondary electron cutoff XPS spectra and valence spectra of (a) FAPbI3 and (b) (HtrzT)PbI3. Schematic illustration of the band structure of (c) FAPbI3 and (HtrzT)PbI3, and (d) (HtrzT)PbI3/FAPbI3 perovskite.

Fig. S15 (a) Absorption spectrum of (HtrzT)PbI3. (b) Kubelka-Munk plot for determining the band gap of the (HtrzT)PbI3

Fig. S16 PL mappings of (a) α-FAPbI3 and (b) (HtrzT)PbI3(1.0)/FAPbI3 perovskite

Fig. S17 AFM topography of (a) FAPbI3 and (b) (HtrzT)PbI3(1.0)/FAPbI3 films

Fig. S18 The I-V curve of the (HtrzT)PbI3 device in the dark

Fig. S19 (a) X-ray responses of the FAPbI3 and (HtrzT)PbI3/FAPbI3 films under a series of dose rates from 631.2 to 60.26 µGyair s-1. (b) The X-ray induced current density versus dose rate of the FAPbI3 and (HtrzT)PbI3/FAPbI3 perovskite detectors

Fig. S20 Attenuation efficiencies as a function of material thickness for Si, α-Se, CdTe, and FAPbI3 at 22 keV X-ray photons

Fig. S21 The X-ray responses of the device based on the (a) (HtrzT)PbI3(1.0)/FAPbI3 and (b) FAPbI3 films under on-off X-ray irradiation with various dose rates at -3 V bias

Fig. S22 The noise currents of the FAPbI3 and (HtrzT)PbI3(1.0)/FAPbI3 devices

Fig. S23 The response time of (a) FAPbI3 and (b) (HtrzT)PbI3(1.0)/FAPbI3 devices under X-ray irradiation

Fig. S24 Sampling at nine points on an area of 5 cm × 5 cm for PL mappings of (HtrzT)PbI3(1.0)/FAPbI3 perovskite films (a) without and (b) with hot-pressing. The scale bars are 100 µm

Fig. S25 Backside optical image of “pig” with a copper coin for X-ray imaging

Supplementary Tables

Table S1 The composition of organic precursor solution for the FAPbI3 and (HtrzT)PbI3/FAPbI3 perovskite films

| Sample | Mole fractions of HtrzT:FA | HtrzT/mmol | FAAc/mmol | HI/mL | H3PO2/μL |
| --- | --- | --- | --- | --- | --- |
| FAPbI3 | 0:1 | 0 | 5 | 0.5 | 20 |
| (HtrzT)PbI3(0.5)/FAPbI3 | 0.5:1 | 2.5 | 5 | 1.25 | 50 |
| (HtrzT)PbI3(1.0)/FAPbI3 | 1:1 | 5 | 5 | 2.5 | 100 |
| (HtrzT)PbI3(1.5)/FAPbI3 | 1.5:1 | 7.5 | 5 | 3.75 | 150 |

Table S2 Crystal Data for the (HtrzT)PbI3 single crystal

| Compound | (HtrzT)PbI3 |
| --- | --- |
| Empirical formula | C2H4I3N3PbS |
| Formula weight | 690.03 |
| Crystal system | orthorhombic |
| Space group | Pna21 |
| Unit cell dimensions | a = 13.9364(5) Å, b = 8.9355(3) Å c = 8.7176(3) Å α = 90o, β = 90o, γ = 90o |
| Volume | 1085.59(7) Å3 |
| Z | 4 |
| Density (calculated) | 4.222 g cm-3 |
| F(000) | 1176.0 |
| Index ranges | -19 ≤ h ≤ 19, -12 ≤ k ≤ 12, -11 ≤ l ≤ 11 |
| Independent reflections | 2813 [Rint = 0.0595, Rsigma = 0.0431] |
| Data/restraints/parameters | 2813/1/92 |
| Goodness-of-fit on F2 | 1.031 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0284, wR2 = 0.0537 |
| Largest diff. peak/hole | 1.14/-1.14 e.Å-3 |

Table S3 Lifetime of TRPL for the FAPbI3 and (HtrzT)PbI3/FAPbI3 perovskite films

| Sample | τ1/ns | Rel1% | τ2/ns | Rel2% | τavg/ns |
| --- | --- | --- | --- | --- | --- |
| FAPbI3 | 32.87 | 72.4 | 409.6 | 27.6 | 137 |
| (HtrzT)PbI3(0.5)/FAPbI3 | 100.2 | 56.77 | 617.6 | 43.23 | 324 |
| (HtrzT)PbI3(1.0)/FAPbI3 | 126.2 | 52.22 | 704.6 | 47.78 | 403 |
| (HtrzT)PbI3(1.5)/FAPbI3 | 203.7 | 39.35 | 1197.2 | 60.65 | 806 |

Table S4 Lifetime of TA for the FAPbI3 and (HtrzT)PbI3(1.0)/FAPbI3 films

| Sample | τ1/ps | Rel1% | τ2/ps | Rel2% | τavg/ps |
| --- | --- | --- | --- | --- | --- |
| FAPbI3 | 441.5 | 6.92 | 5189 | 93.08 | 4861 |
| (HtrzT)PbI3(1.0)/FAPbI3 | 696.7 | 4.41 | 10180 | 95.59 | 9762 |