Supporting Information for

Multifunctional MXene for Thermal Management in Perovskite Solar Cells

Zhongquan Wan1,2*, Runmin Wei2, Yuanxi Wang1, Huaibiao Zeng2, Haomiao Yin1, Muhammad Azam1, Junsheng Luo1*, Chunyang Jia1*

1National Key Laboratory of Electronic Films and Integrated Devices, School of Integrated Circuit Science and Engineering, University of Electronic Science and Technology of China, 611731 Chengdu, P. R. China

2Shenzhen Institute for Advanced Study, University of Electronic Science and Technology of China, 518110 Shenzhen, P. R. China

*Corresponding authors. E-mail: zqwan@uestc.edu.cn (Zhongquan Wan); luojs@uestc.edu.cn (Junsheng Luo); cyjia@uestc.edu.cn (Chunyang Jia)

# Supplementary Figures and Tables

Fig. S1 Schematic diagram of the multilayer Ti3C2TX

Fig. S2 TEM image of single layer or few layer Ti3C2TX nanosheets

Fig. S3 XPS survey spectra of the Ti3C2TX

Fig. S4 High-resolution XPS spectra of Ti 2p and C 1s for Ti3C2TX

Fig. S5 Schematic diagram of films cooling test process: Transfer from 85 ℃ hot plate to room temperature cooling platform

Fig. S6 Infrared thermal images of ITO/perovskite and ITO/ Ti3C2TX-modified perovskite films under a cooling test

Fig. S7 Comparison image of perovskite precursor solution without and with Ti3C2TX

Fig. S8 AFM images of perovskite films without and with 0.01 wt%, 0.03 wt%, 0.05 wt%, 0.10 wt% Ti3C2TX

Fig. S9 EDS spectra of 0.03 wt% Ti3C2TX-modified perovskite film

Fig. S10 I–V curves (log–log plots) of the pure perovskite device with the structure of ITO/PVK/Au and ITO/PVK-0.03 wt% Ti3C2TX/Au

Fig. S11 J–V curves (log–log plots) of the pure hole device with the structure of ITO/PEDOT:PSS/PVK-Ti3C2TX/Spiro-OMeTAD/Au

Fig. S12 Nyquist plots of the PSCs with and without Ti3C2TX under dark condition

Equation S1 Carrier mobility calculation formula

J=9ε0εrμVeff28L3

J is the measured current density, Veff is the effective voltage defined as the difference between the applied voltage (Vapp) and the built-in voltage (Vbi), L is the film thickness,ε0 is the vacuum permittivity, εr is the relative dielectric constant, and μ is the carrier mobility.

Table S1 Comparison of thermal conductivities of various thermally conductive materials

| Thermally conductive materials | Thermal conductivity |
| --- | --- |
| h-BN | 51.1 W m-1 K-1 |
| Al2O3 | ~20-30 W m-1 K-1 |
| SiO2 | ~5 W m-1 K-1 |
| Zeolite | 1 W m-1 K-1 |
| Ti3C2TX | 55.8 W m⁻¹ K⁻¹ |

Table S2 Input parameters for the simulation of PSC

| Input parameter | ITO | SnO2 | Perovskite | Spiro-OMeTAD | Au |
| --- | --- | --- | --- | --- | --- |
| Thickness (nm) | 100 | 50 | 500 | 350 | 50 |
| K (W·m-1·k-1) | 10 | 5 | 0.413 | 0.49 | 318 |
| h (W·m-2·k-1) | 3.1×108 | - | - | - | 9.6×109 |
| ρ (kg·m-3) | 7120 | 6950 | 4000 | 4128 | 19300 |
| Cp (J·kg-1·K-1) | 345 | 350 | 258 | 262 | 128 |

Table S3 The fitting parameters of TRPL

| Simple | A1 | τ1 (ns) | A2 | τ2 (ns) | ave (ns) |
| --- | --- | --- | --- | --- | --- |
| PVK | 0.943 | 7.628 | 0.344 | 868.744 | 848.50 |
| 0.03wt% Ti3C2TX-modified PVK | 0.824 | 9.276 | 0.369 | 931.975 | 911.91 |

Table S4 The photovoltaic parameters of the PSCs

| PSC | Voc (V) | Jsc (mA/cm2) | FF (%) | PCE (%) |
| --- | --- | --- | --- | --- |
| PVK | 1.145 | 25.18 | 82.2 | 23.70 |
| 0.01wt% Ti3C2TX-modified PVK | 1.151 | 25.22 | 81.6 | 23.69 |
| 0.03wt% Ti3C2TX-modified PVK | 1.177 | 25.29 | 84.4 | 25.13 |
| 0.05wt% Ti3C2TX-modified PVK | 1.167 | 25.28 | 82.4 | 24.30 |
| 0.10wt% Ti3C2TX-modified PVK | 1.157 | 25.24 | 80.9 | 23.62 |

Table S5 Literature survey of the works on the thermal stability (85 ℃) of unencapsulated PSCs based on other thermal management strategies

| Year | Strategy | Champion PCE (%) | Aging time (h) | PCE/PCE0 (%) | Refs. |
| --- | --- | --- | --- | --- | --- |
| 2020 | Enhancing the thermal conductivity of Spiro with Al2O3 | 21.20 | 720 | 60 | [S1] |
| 2021 | Enhancing the thermal conductivity of Spiro with SiO2 | 22.29 | 1468 | 67 | [S2] |
| 2021 | Enhancing the thermal conductivity of PCBM with PS | 18.34 | 100 | 64 | [S3] |
| 2023 | Enhancing the thermal conductivity of Spiro with zeolite | 23.42 | 720 | 61 | [S4] |
| 2023 | Enhancing the thermal conductivity of PVK with h-BN | 19.8 | 300 | 85 | [S5] |
| 2025 | Enhancing the thermal conductivity of PVK with Ti3C2TX | 25.13 | 1000 | 86 | This work |

Table S6 Literature survey of the works on the thermal stability (85 ℃) of unencapsulated PSCs based on PVK/Spiro-OMeTAD

| Device’s structure | Aging time (h) | PCE/PCE0 (%) | Refs. |
| --- | --- | --- | --- |
| ITO/SnO2/PCBM/PVK/Spiro-OMeTAD/Au | 1000 | 85.0 | [S6] |
| FTO/SnO2/PVK/Spiro-OMeTAD/Au | 27 | 85.0 | [S7] |
| FTO/SnO2/PVK/Spiro-OMeTAD/Au | 100 | 90 | [S8] |
| ITO/SnO2/PVK/Spiro-OMeTAD/Au | 450 | 92.0 | [S9] |
| FTO/bl-TiO2/mp-TO2/PVK/Spiro-OMeTAD/Au | 245 | 0 | [S10] |
| FTO/c-TiO2/mp-TO2/PVK/Spiro-OMeTAD/Au | 100 | 80.0 | [S11] |
| ITO/SnO2/MoO3/PVK/Spiro-OMeTAD/Au | 558 | 90.0 | [S12] |
| ITO/SnO2/TMPU/PVK/TMFS/Spiro-OMeTAD/Au | 500 | 94.2 | [S13] |
| ITO/SnO2/MgAc2/PVK/Spiro-OMeTAD/Au | 1250 | 80.0 | [S14] |
| FTO/TiO2/SnO2/PVK/Spiro-OMeTAD/Au | 200 | 60.0 | [S15] |
| FTO/SnO2/PVK/Spiro-OMeTAD/Au | 310 | 85.0 | [S16] |
| FTO/SnO2/PVK/Spiro-OMeTAD/Au | 500 | 92.4 | [S17] |
| FTO/SnO2/PVK/Spiro-OMeTAD/Au | 140 | 70.0 | [S18] |
| ITO/SnO2/PVK-Ti3C2TX/Spiro-OMeTAD/Au | 1000 | 86.0 | This work |

Supplementary References

- K. Choi, J. Lee, H. Choi, G.-W. Kim, H.I. Kim et al., Heat dissipation effects on the stability of planar perovskite solar cells. Energy Environ. Sci. 13(12), 5059–5067 (2020). https://doi.org/10.1039/D0EE02859B

- F. Pei, N. Li, Y. Chen, X. Niu, Y. Zhang et al., Thermal management enables more efficient and stable perovskite solar cells. ACS Energy Lett. 6(9), 3029–3036 (2021). https://doi.org/10.1021/acsenergylett.1c00999

- Z. Zhang, Y. Tang, Y. Wang, Z. Zeng, R. Shi et al., Heat transfer enhancement of n-type organic semiconductors by an insulator blend approach. ACS Appl. Mater. Interfaces 14(26), 30174–30181 (2022). https://doi.org/10.1021/acsami.2c05503

- W. Wang, J. Zhang, K. Lin, J. Wang, B. Hu et al., Heat diffusion optimization in high performance perovskite solar cells integrated with zeolite. J. Energy Chem. 86, 308–317 (2023). https://doi.org/10.1016/j.jechem.2023.07.001

- Y. Yin, Y. Zhou, S. Fu, X. Zuo, Y.-C. Lin et al., Enhancing crystallization in hybrid perovskite solar cells using thermally conductive 2D boron nitride nanosheet additive. Small 19(15), e2207092 (2023). https://doi.org/10.1002/smll.202207092

- W. Song, L. Rakocevic, R. Thiruvallur Eachambadi, W. Qiu, J.P. Bastos et al., Improving the morphology stability of spiro-OMeTAD films for enhanced thermal stability of perovskite solar cells. ACS Appl. Mater. Interfaces 13(37), 44294–44301 (2021). https://doi.org/10.1021/acsami.1c11227

- W. Zhang, L. He, D. Tang, X. Li, Surfactant sodium dodecyl benzene sulfonate improves the efficiency and stability of air-processed perovskite solar cells with negligible hysteresis. Sol. RRL 4(11), 2000376 (2020). https://doi.org/10.1002/solr.202000376

- M. Chen, P. Li, C. Liang, H. Gu, W. Tong et al., Enhanced efficiency and stability of perovskite solar cells by 2D perovskite vapor-assisted interface optimization. J. Energy Chem. 45, 103–109 (2020). https://doi.org/10.1016/j.jechem.2019.10.006

- S. Tan, I. Yavuz, N. De Marco, T. Huang, S.J. Lee et al., Steric impediment of ion migration contributes to improved operational stability of perovskite solar cells. Adv. Mater. 32(11), e1906995 (2020). https://doi.org/10.1002/adma.201906995

- H. Zheng, G. Liu, C. Zhang, L. Zhu, A. Alsaedi et al., The influence of perovskite layer and hole transport material on the temperature stability about perovskite solar cells. Sol. Energy 159, 914–919 (2018). https://doi.org/10.1016/j.solener.2017.09.039

- K.-M. Lee, S.Y. Abate, J.H. Yang, W.-H. Chiu, S. Ahn et al., Facile synthesis of spiro-core-based hole-transporting material for high-performance and stable perovskite solar cells. Chem. Eng. J. 454, 139926 (2023). https://doi.org/10.1016/j.cej.2022.139926

- C. Liang, H. Gu, Y. Xia, Z. Wang, X. Liu et al., Two-dimensional Ruddlesden–Popper layered perovskite solar cells based on phase-pure thin films. Nat. Energy 6(1), 38–45 (2021). https://doi.org/10.1038/s41560-020-00721-5

- Z. Yi, X. Li, B. Xiao, Q. Jiang, Y. Luo et al., Dual-interface engineering induced by silane coupling agents with different functional groups constructing high-performance flexible perovskite solar cells. Chem. Eng. J. 469, 143790 (2023). https://doi.org/10.1016/j.cej.2023.143790

- M. Guli, Y. Zhang, R. Li, W. He, C. Lan et al., MgAc2-modified SnO2 electron transport layer for highly efficient and thermal stable perovskite solar cells. Nano Lett. 24(45), 14183–14190 (2024). https://doi.org/10.1021/acs.nanolett.4c02824

- Yukta, R.D. Chavan, A. Mahapatra, D. Prochowicz, P. Yadav et al., Improved efficiency and stability in 1, 5-diaminonaphthalene iodide-passivated 2D/3D perovskite solar cells. ACS Appl. Mater. Interfaces 15(46), 53351–53361 (2023). https://doi.org/10.1021/acsami.3c09887

- C. Shi, J. Li, S. Xiao, Z. Wang, W. Xiang et al., Alcohol-dispersed polymer complex as an effective and durable interface modifier for n-i-p perovskite solar cells. J. Energy Chem. 93, 243–252 (2024). https://doi.org/10.1016/j.jechem.2024.01.075

- Y.S. Shin, J. Lee, D.G. Lee, J.W. Song, J. Seo et al., Damp-heat stable and efficient perovskite solar cells and mini-modules with a tBP-free hole-transporting layer. Energy Environ. Sci. 18(7), 3269–3277 (2025). https://doi.org/10.1039/D4EE05699J

- K. Choi, J. Lee, H.I. Kim, C.W. Park, G.-W. Kim et al., Thermally stable, planar hybrid perovskite solar cells with high efficiency. Energy Environ. Sci. 11(11), 3238–3247 (2018). https://doi.org/10.1039/c8ee02242a