Supporting Information for

Achieving Wide Temperature Range Physi- and Chemical Hydrogen Sorption in a Structural Optimized Mg/N-Doped Porous Carbon Nanocomposite

Yinghui Li 1, 2, Li Ren1, 2, Zi Li1, 2, Yingying Yao1, 2, Xi Lin1, Wenjiang Ding1, 2, Andrea C. Ferrari3, *, Jianxin Zou1, 2, 3, *

1Shanghai Key Laboratory of Hydrogen Science & Center of Hydrogen Science, Shanghai Jiao Tong University, Shanghai 200240, P. R. China

2National Engineering Research Center of Light Alloys Net Forming & State Key Laboratory of Metal Matrix Composites, Shanghai Jiao Tong University, Shanghai, 200240, P. R. China

3Cambridge Graphene Centre, University of Cambridge, Cambridge, CB3 0FA, U. K.

*Corresponding authors. E-mail: acf26@eng.cam.ac.uk (Andrea C. Ferrari); zoujx@sjtu.edu.cn (Jianxin Zou)

Supplementary Figures

Fig. S1 Schematic illustration of rN-pC preparation

Fig. S2 a XRD patterns of ZIF-8 (simulated), as-synthesized ZIF-8, N-pC and rN-pC. b Pore-size distribution of ZIF-8, N-pC and rN-pC. c Survey XPS spectra of N-pC and rN-pC and d Raman spectra of N-pC and rN-pC under excitation of 514 nm laser

Fig. S3 Raman spectra of N-pC and rN-pC under excitation of a 325nm, b 532nm, c 633nm lasers, and d I(D)/I(G) (the ratio of peak areas) dispersion with the change of excitation wavelengths with error bars

Fig. S4 SEM images of a ZIF-8, b N-pC and c rN-pC

Fig. S5 Typical TEM images of a rN-pC and b, c N-pC at different scales, and d representative BF image as well as corresponding EDS elemental mapping results of N-pC

Fig. S6 Experimental H2 adsorption and fitting of rN-pC at 196 and -186 oC under ultralow pressure

Fig. S7 Top and side views of optimized geometries of H2 adsorbed on a graphene, b C sites in graphitic N doped graphene, c N sites in graphitic N doped graphene, and d C sites in pyridinic N doped graphene

Fig. S8 Density of States (DOS) for modelled substrates

Fig. S9 Iso-surfaces of charge density difference for H2 adsorbed on a graphene, b N sites in graphitic N doped graphene, c C sites in graphitic N doped graphene, d N sites in pyridinic N doped graphene, and e C sites in pyridinic N doped graphene

Fig. S10 a Typical TEM and b HRTEM images of the as-synthesized pure Mg

Fig. S11 a TEM image of 60MgH2/rN-pC and b corresponding SAED pattern

Fig. S12 a Typical TEM, and b, c, d the corresponding HRTEM images, e TEM image and f corresponding HAADF image and EDS elemental mapping (C, N, Mg) results of the hydrogenated 60MgH2@rN-pC composite after 10 cycles at 275 oC

Fig. S13 FTIR spectra of rN-pC, pure MgH2 and 60MgH2/rN-pC

Fig. S14 a N2 adsorption/desorption isotherms and b pore size distribution of rN-pC and 60MgH2@rN-pC

Fig. S15 a Experimental H2 adsorption of 60MgH2/rN-pC at 196 and -186 oC under ultralow pressure and b equivalent isosteric heat of H2 adsorption fitting of 60MgH2/rN-pC

Fig. S16 DSC curves and corresponding Kissinger’s plots of the pure MgH2

Fig. S17 JMAK plots and the corresponding lnK-1000/T plots of a, b 60MgH2/rN-pC and c, d pure MgH2 for dehydrogenation

Fig. S18 Isothermal a dehydrogenation and b rehydrogenation curves of the pure MgH2 at different temperatures

Fig. S19 Isothermal dehydrogenation curves of 60MgH2/rN-pC at 225 oC and 250 oC for a relatively long time (~8h)

Fig. S20 a PCT curves of 60MgH2/rN-pC at different temperatures and corresponding b fitting plot

Fig. S21 Reversible hydrogen absorption/desorption cycling profiles of 60MgH2@rN-pC at 275 °C

Fig. S22 Reversible hydrogen absorption/desorption cycling profiles of the pure MgH2 at 350 °C

Fig. S23 Hydrogen desorption curves of 60MgH2@rN-pC at 275 oC and the pure MgH2 obtained under 350 °C at different cycles

Fig. S24 Reversible hydrogen absorption/desorption cycling profiles of the pure MgH2 at 350 oC for 25 cycles and 60MgH2@rN-pC at 300 oC for 30 cycles

Fig. S25 High-resolution a C 1s, b N 1s, and c Mg 2p spectra of the hydrogenated 60MgH2@rN-pC composite after 10 cycles at 275 oC

Fig. S26 Continuous desorption curve of the 60MgH2@rN-pC composites

About the waste heat to trigger MgH2 desorption hypothesis, we provide a quantitative energy balance calculation based on the MgH2–solid oxide fuel cells (SOFC) powered prototype car [S1].

Supposing that there is 1 kg of composite material, including 400 g porous carbon and 600 g MgH2. According to the references, the specific heat capacities of porous carbon and MgH2 can be determined as ~0.8 J g-1 K-1 [S2, S3] and ~1.4 J g-1 K-1 [S4], respectively. The working efficiency of SOFC is considered as 60% [S1, S5], and the use of 8 g H2 in SOFC would provide waste heat of: 285.8 kJ mol-1×8 g/2.0 g mol-1×40%=457.3 kJ. If the utilization rate of the waste heat is 60% [S6] and the heat loss rate of the hydrogen storage tank is considered as 20% [S7, S8], it can increase the temperature of the composite from room temperature to: ΔT=457.3 kJ×60%×80%/(0.8 J g-1 K-1×400 g +1.4 J g-1 K-1×600 g) =189.2 K. The result indicates that the 60MgH2@rN-pC composite can be heated to ~214 oC by the waste heat, which is higher than its onset desorption temperature of 175 oC.

Fig. S27 Optical photographs of a 100mg 60MgH2@rN-pC powder and b, c the corresponding pellet compacted under 500 MPa from different views

Fig. S28 The optical photographs of a compression machine and its b compaction pressure indicator.

The compression machine was a PC-12 type tablet press from Tianjin Jingtuo Company and its effective force range is 0-12 Tons. A cylindrical die with the inner diameter of 10 mm was used for pelletizing. Based on the effective force and the size of die, the effective pressure range is 0-1500 MPa. In this work, a compression pressure of 500 MPa (4 Tons) was employed on the composite pellets.

Supplementary Equations

Equation S1 The high-pressure H2 isotherms adsorption at 77K and 87K were modelled using a semi-empirical methodology [S9]. The high-pressure H2 isotherms were measured by HPSA-auto device, and were fitted using the Tóth equation:

m=100ρA-PMZRTθvp

to represent the filling fraction θ:

θ=bp1+bpc1/c

the compressibility factor Z that accounts for the fact that hydrogen is not an ideal gas at 77 K, Z is approximate as:

Z=1-1.378×10-3p+7.02630×10-6p2

where ρA is the density of adsorbate in g cm-3, b is the affinity constant in MPa-1, c is a heterogeneity parameter, and vp is the pore volume in cm3 g-1. p is the pressure in MPa, R = 8.314 J mol-1 K-1 is the molar gas constant, T is the temperature in K and M = 2.01588 g mol-1 is the molar mass of H2.

Equation S2 The density functional theory (DFT) is an advanced method to calculate pore size distribution and pore volume based on adsorption isotherm data, especially for the accurate analysis of micropores (<2 nm) and mesopores (2-50 nm) [S10]. The integral equation of isothermal adsorption for the case of distributed pore sizes can be written as the convolution:

Qp=dHqp,Hf(H)

Where Q(p) is the total quantity of adsorbate at pressure p, q(p,H), the Kernel function, is the density functional description of the adsorption isotherm for an ideally homo-porous material characterized by pore width H, and f(H) is the desired pore surface area distribution function with respect to H.

Equation S3 To assess the interaction between H2 molecules and the rN-pC, the isosteric heat of adsorption (Qst) was calculated using the Clausius-Clapeyron equation [S11], H2 isotherm data at T1 (77 K) and T2 (87 K) were fitted with Langmuir equation.

δlnPδTn=QstRT2

Qst=-RlnPT2-lnPT1T2-1-T1-1

Equation S4 The desorption apparent activation energy (Ea) was obtained by fitting DSC data using Kissinger method [S12].

lnβTP2=-EaRTp+C

where β represents the heating rate, Tp refers to the peak temperature, R is the gas constant (R = 8.314 J mol−1 K−1), and C is a constant.

Equation S5 The enthalpy of the reaction between hydrogen and Mg was calculated by Van’t Hoff equation [S13].

lnpH2eqp0=∆HoRT-∆SoR

Where pH2eq is the equilibrium pressure (plateau pressure) at the temperature T, p0 is the reference state (o, 1 bar), ∆Ho and ∆So represent the enthalpy and entropy change of the reaction, and R is the gas constant (R = 8.314 J mol−1 K−1).

Supplementary Tables

Table S1 the specific surface area, pore size distribution and pore volume of ZIF-8, N-pC and rN-pC

|  | SBET(m2 g-1) | VDFT(mL g-1) | SDFT(MP) (m2 g-1) | VDFT(MP) (mL g-1) |
| --- | --- | --- | --- | --- |
| ZIF-8 | 1877.3 | 0.711 | 1367.9 | 0.666 |
| N-pC | 1146.5 | 0.920 | 921.5 | 0.271 |
| rN-pC | 1525.4 | 1.498 | 1326.3 | 0.447 |

MP: micropore

Table S2 Semiquantitative atomic fraction of XPS of N-pC and rN-pC (at%)

|  | C | N | O |
| --- | --- | --- | --- |
| N-pC | 95.16 | 2.33 | 2.51 |
| rN-pC | 91.48 | 5.97 | 2.55 |

Table S3 Semiquantitative atomic fraction of STEM of N-pC and rN-pC (at%)

|  | C | N | O |
| --- | --- | --- | --- |
| N-pC | 94.7 | 1.36 | 3.98 |
| rN-pC | 94.4 | 2.06 | 3.52 |

Table S4 The high-pressure H2 isotherms adsorption at 77K and 87K were modelled using a semi-empirical methodology for rN-pC and 60MgH2/rN-pC

| Sample | ρA (g cm-3) | b (MPa-1) | c | vp (cm3 g-1) | R2 | Max excess adsorption (wt%) |
| --- | --- | --- | --- | --- | --- | --- |
| rN-pC | 0.02629 | 532.995 | 0.29197 | 1.77791 | 0.9983 | 2.49 |
| 60MgH2/rN-pC | 0.04542 | 3407.31 | 0.20782 | 0.34015 | 0.9995 | 0.66 |

Supplementary References

- X. Wang, L. Shao, S. Hu, Z. Li, H. Guo et al., A techno-economic study of photovoltaic-solid oxide electrolysis cell coupled magnesium hydride-based hydrogen storage and transportation toward large-scale applications of green hydrogen. Energy Environ. Sci. 17(22), 8429–8456 (2024). https://doi.org/10.1039/D4EE04224G

- M. Amirul Islam, K. Thu, B. B. Saha, Specific heat capacity of mangrove and waste palm trunk in raw, carbonized and activated form, IEICES, 4,151-152 (2018).

- M. Kano, M. Momota, T. Okabe, K. Saito, Specific heat capacity of new porous carbon materials: Woodceramics. Thermochim. Acta 292(1–2), 175–177 (1997). https://doi.org/10.1016/S0040-6031(96)03110-3

- P. Larpruenrudee, N.S. Bennett, Y. Gu, R. Fitch, M.S. Islam, Design optimization of a magnesium-based metal hydride hydrogen energy storage system. Sci. Rep. 12(1), 13436 (2022). https://doi.org/10.1038/s41598-022-17120-3

- J. Rechberger, A. Kaupert, J. Hagerskans, L. Blum, Demonstration of the first European SOFC APU on a heavy duty truck. Transp. Res. Procedia 14, 3676–3685 (2016). https://doi.org/10.1016/j.trpro.2016.05.442

- Metropolitan.fi. Data Center Heats Homes: Yandex Sells Server Waste Energy to District Heating.

- X. Lin, C.-L. Yin, L. Ren, Y. Li, Z. Li et al., A one- and three-dimensional coupled model and simulation investigation for the large-scale oil-heating type Mg-based hydrogen storage tank. Chem. Eng. J. 472, 144943 (2023). https://doi.org/10.1016/j.cej.2023.144943

- L. Shao, X. Lin, L. Bian, Y. Wang, S. Hu et al., Engineering control strategy of hydrogen gas direct-heating type Mg-based solid state hydrogen storage tanks: a simulation investigation. Appl. Energy 375, 124134 (2024). https://doi.org/10.1016/j.apenergy.2024.124134

- V.P. Ting, A.J. Ramirez-Cuesta, N. Bimbo, J.E. Sharpe, A. Noguera-Diaz et al., Direct evidence for solid-like hydrogen in a nanoporous carbon hydrogen storage material at supercritical temperatures. ACS Nano 9(8), 8249–8254 (2015). https://doi.org/10.1021/acsnano.5b02623

- M.L. Occelli, J.P. Olivier, J.A. Perdigon-Melon, A. Auroux, Surface area, pore volume distribution, and acidity in mesoporous expanded clay catalysts from hybrid density functional theory (DFT) and adsorption microcalorimetry methods. Langmuir 18(25), 9816–9823 (2002). https://doi.org/10.1021/la020567o

- S. Poyet, S. Charles, Temperature dependence of the sorption isotherms of cement-based materials: Heat of sorption and Clausius–Clapeyron formula. Cem. Concr. Res. 39(11), 1060–1067 (2009). https://doi.org/10.1016/j.cemconres.2009.07.018

- R.L. Blaine, H.E. Kissinger, Homer Kissinger and the Kissinger equation. Thermochim. Acta 540, 1–6 (2012). https://doi.org/10.1016/j.tca.2012.04.008

- J.F. Stampfer Jr, C.E. Holley Jr, J.F. Suttle, The magnesium-hydrogen System1-3. J. Am. Chem. Soc. 82(14), 3504–3508 (1960). https://doi.org/10.1021/ja01499a006