Supporting Information for

Heteroatom-Coordinated Fe-N₄ Catalysts for Enhanced Oxygen Reduction in Alkaline Seawater Zinc-Air Batteries

Wenhan Fang3,4, Kailong Xu1,2, Xinlei Wang1,2, Yuanhang Zhu5, Xiuting Li5, Hui Liu1,2, Danlei Li3, 4*, Jun Wu1, 2*

1Department of School of Metallurgy and Environment, Central South University, Changsha 410083, P. R. China

2State Key Laboratory of Advanced Metallurgy for Non-ferrous Metals, Changsha 410083, P. R. China

3Department of Chemistry and Materials Science, School of Science, Xi’an Jiaotong-Liverpool University, Suzhou 215123, P. R. China

4Department of Chemistry, University of Liverpool L69 7ZD, the United Kingdom

5Institute for Advanced Study, Shenzhen University, Shenzhen 518060, P. R. China

*Corresponding authors. E-mail: danlei.li@xjtlu.edu.cn (Danlei Li); wujun@csu.edu.cn (Jun Wu)

Supplementary Figures

Fig. S1 HRTEM pattern of a) S-Fe-N4, d) Fe-N4. STEM-EDS mapping of b) S-Fe-N4, e) Fe-N4. c) HAADF-STEM image of S-Fe-N4

Fig. S2 XRD pattern of Fe-N4

Fig. S3 Pore volume increment curves of Cl-Fe-N4 and S-Fe-N4

Fig. S4 Deconvoluted high-resolution XPS spectra of a) N 1s, b) S 2p for Fe-N4. c) Fe 2p for Cl-Fe-N4, S-Fe-N4, and Fe-N4. d) XPS survey spectrum of Cl-Fe-N4, S-Fe-N4 and Fe-N4

Fig. S5 k3-weighted Fe k-edge EXAFS fitting curves of a) Fe-N₄ and reference samples in k space. EXAFS fitting curve of b) Fe-N₄, c) Cl-Fe-N₄ and d) S-Fe-N₄ in R space. Wavelet transform EXAFS analysis of the Fe k-edge for e) Fe metallic foil and f) FeᴵᴵPc

Fig. S6 LSV polarization curves of Cl-Fe-N4, S-Fe-N4, Fe-N4 and Pt/C using RDE at 1600 rpm in a) 0.1 M KOH, b) 0.1 M KOH with 0.5 M KCl. Catalyst loading: 0.75 mg cm⁻²

Fig. S7 K-L plots at different rotating speeds in a) 0.1 M KOH, b) 0.1 M KOH with 0.5 M KCl and c) alkaline synthetic seawater (pH = 13) of Cl-Fe-N4; in d) 0.1 M KOH, e) 0.1 M KOH with 0.5 M KCl and f) alkaline synthetic seawater of S-Fe-N4; g) 0.1 M KOH, h) 0.1 M KOH with 0.5 M KCl and i) alkaline synthetic seawater of Fe-N4

Fig. S8 CV curves of a) Cl-Fe-N4, b) S-Fe-N4, c) Fe-N4 in alkaline synthetic seawater. Catalyst loading: 0.1 mg cm⁻²

Fig. S9 LSV polarization curves before and after CA test of a) Cl-Fe-N4, b) S-Fe-N4, c) Fe-N4 using RDE at 1600 rpm in alkaline synthetic seawater (pH=13) with a scan rate of 10 mV s⁻¹. Catalyst loading: 0.75 mg cm⁻².

Fig. S10 The long cycling curves of Cl-Fe-N4 and S-Fe-N4 at 10 mA cm−2 in alkaline synthetic seawater

Fig. S11 a) SEM pattern and b) EDS mapping before the zinc-air battery test, and c) SEM pattern and d) EDS mapping after the test of Cl-Fe-N4

Fig. S12 Deconvoluted high-resolution XPS spectra of a) Cl 2p, b) Fe 2p, c) N 1s and d) O 1s for Cl-Fe-N4 before and after the zinc-air battery test

Fig. S13 Theoretical structures of the surface of a) unoccupied Fe-N4 single atom site, Fe-N4 single atom site adsorbed by b) -O, c) -OOH, d) -OH, e) -O2

Fig. S14 Theoretical structures of the surface of a) unoccupied S-Fe-N4 single atom site, S-Fe-N4 single atom site adsorbed by b) -O, c) -OOH, d) -OH, e) -O2

Fig. S15 Theoretical structures of the surface of a) unoccupied Cl-Fe-N4 single atom site, Cl-Fe-N4 single atom site adsorbed by b) -O, c) -OOH, d) -OH, e) -O2

Fig. S16 The Bader charge of Fe-N4. Purple ball: Fe; Green ball: Cl; Yellow ball: S; Grey ball: C; Blue ball: N; Red ball: O; White ball: H

Fig. S17 Adsorption Energy and Configuration of Cl⁻ on Cl-Fe-NC

Supplementary Tables

Table S1 Atomic ratios in different samples based on XPS analysis

|  | C | N | O | S | Cl | Fe |
| --- | --- | --- | --- | --- | --- | --- |
| Cl-Fe-N4 | 88.62 % | 4.73 % | 6.00 % | 0.36 % | 0.34 % | 0.13 % |
| S-Fe-N4 | 88.21 % | 4.21 % | 6.90 % | 0.81 % | \ | 0.11 % |
| Fe-N4 | 92.15 % | 3.55 % | 4.14 % | 0.08 % | \ | 0.10 % |

Table S2 N species ratios in different samples based on XPS analysis

|  | pyrrolic | pyridinic | Fe-N | N-oxide | graphitic-N |
| --- | --- | --- | --- | --- | --- |
| Cl-Fe-N4 | 51.59 % | 23.49 % | 0.34 % | 7.55 % | 17.03 % |
| S-Fe-N4 | 53.92 % | 15.72 % | 5.88 % | 7.3 % | 17.18 % |
| Fe-N4 | 44.49 % | 16.25 % | 11.54 % | 8.54 % | 19.18 % |

Table S3 Curve fitting parameters of Fe K-edge EXAFS

| Samplea | Path | Nb | R(Å) c | σ2(10-3Å2) d | ΔE0(eV) | R-factor |
| --- | --- | --- | --- | --- | --- | --- |
| S-Fe-N4 | Fe-N | 4.40 | 2.02 | 7.18 | -0.56 | 0.016 |
|  | Fe-S | 0.90 | 2.67 | 30.05 |  |  |
| Cl-Fe-N4 | Fe-N | 4.04 | 1.91 | 6.34 | -9.92 | 0.009 |
|  | Fe-Cl | 0.78 | 2.17 | 0.04 |  |  |
| Fe-N4 | Fe-N | 4.0 | 1.96 | 5.64 | -4.49 | 0.014 |

aS02was fixed as 1.0. Data ranges: 3.0 < k ≤ 8.0 Å-1,1.0 ≤ R < 3.0 Å.

bN is the coordination number.

cR is the distance between absorber and backscatter atoms. dσ2is the Debye-Waller factor. R-factor is residual factor.

Table S4 Atomic ratios of Cl-Fe-N4 before and after zinc-air battery test based on XPS analysis

|  | C | N | O | Fe | Cl |
| --- | --- | --- | --- | --- | --- |
| Before the test | 75.69% | 4.11% | 19.46% | 0.15% | 0.59% |
| After the test | 67.31% | 3.07% | 28.45% | 0.09% | 1.08% |