Supporting Information for

Electrocatalytic Self-Coupling of N-Heterocyclic Amides for Energy-Efficient Bipolar Hydrogen Production

Yuqiang Ma1,  Meng Li1,  Dandan Zhang1,  Cihang Wang1,  Yu Li1,  Zihang Zhao1,  Xiaogang Mu2,  Jun Hu1 , Xiang Hu3*, Jiachen Li1*,  Haixia Ma1, 2*, Zhenhai Wen3

1 Xi'an Key Laboratory of Special Energetic Materials, School of Chemical Engineering, Northwest University, Xi’an 710127, P. R. China

2 Zhijian Laboratory, Xi’an 710025, P. R. China

3 State Key Laboratory of Structural Chemistry, and Fujian Provincial Key Laboratory of Materials and Techniques toward Hydrogen Energy, Fujian Institute of Research on the Structure of Matter, Chinese Academy of Sciences, Fuzhou, Fujian 350002, P. R. China

*Corresponding authors. E-mail: mahx@nwu.edu.cn (Haixia Ma); huxiang@fjirsm.ac.cn (Xiang Hu); lijiachen@nwu.edu.cn (Jiachen Li)

S1 Electrochemically active surface area (ECSA) calculation

The ECSA of the catalysts layer can be calculated as:

ECSA=CdlCs

Where the specific capacitances (Cs) were chosen as Cs = 0.040 mF cm−2 in 1.0 M KOH. Cdl was derived as the average value of linear fitted slope by plotting both the anodic and cathodic current against the scan rate from the corresponding cyclic voltammetry (CV) curves at non-faradic potential.

S2 Pt mass activity calculation method

Because Pt species were supported by NiS2@CC in the measurements, the contributions of the NiS2@CC should be deducted. Therefore, the Pt mass activities of Pts,n@NiS2@CC can be calculated based on Fig. 2g using the following equation:

Pt mass activity of Pts,n@NiS2@CC:

JmassPt=JareaPts,n@NiS2@CC-JareaNiS2@CCmassPt

S3 TOF calculated method

The conversion efficiency of Pts,n@NiS2@CC was evaluated by the TOF values (s–1), which can be obtained according to the Eq:

TOF=Total numberofH2 turnover/geometric area (cm2)Total number of activesites/geometric area(cm2)

The total number of H2 turnovers were calculated by the Eq:

Total H2 turnovers =

[J (mA cm-2)]1C103mA1mol e-96485C1 mol H22 mol e-[6.02×1023molecules H21 mol H2]

The number of active sites was calculated by the total mass of the Pt quantified by the ICP-OES. The current density (J) from LSV can be converted to TOF according to the Eq:

TOF=3.12×1015Number of active sites×|J| (s-1)

S4 Electricity input (W) of the coupling system per m3 of H2 produced (kWh per m3 H2) was calculated method

W=n×F×U×10003600×Vm

Where the n is the number of electrons transferred for H2 production (n = 2), U is the applied cell voltage in the two-electrode cell, Vm is the molar volume of H2 at normal temperature and pressure (22.4 mol L−1 ), F is Faraday constant (96485 C mol−1 ).

S5 Experimental Section

Preparation of Ni(OH)2@CC: The carbon cloth (CC, 1 × 3 cm) substrate underwent sequential purification via ultrasonic cleaning in acetone, ultrapure water, and ethanol (10 min each) to eliminate surface oxides and insoluble contaminants. Subsequently, a precursor solution was formulated by dissolving Ni(NO3)2·6H2O (0.20 g), urea (CH4N2O, 0.23 g), and NH4F (70 mg) in 15 mL deionized water under vigorous stirring. This homogeneous mixture was transferred into a Teflon-lined autoclave containing the pretreated CC, followed by hydrothermal treatment at 120 °C for 6 h to in situ grow Ni(OH)2 nanostructures on the carbon framework. The resulting Ni(OH)2/CC composite was collected, rinsed thoroughly, and dried at 60 °C to serve as the precursor for subsequent sulfidation processes.

Material characterizations: Scanning electron microscopy (SEM) images of the samples were obtained by Hitachi, Su8010. Transmission electron microscopy (TEM), high-resolution TEM (HRTEM) and element mapping was performed using FEI Talos F200X microscopy. XPS was performed on the Thermo Scientific Nexsa spectrum. The microstructure of the samples was analyzed using an FEI Themis Z transmission electron microscope equipped with spherical aberration correction (AC-TEM). The X-ray powder diffraction (XRD) patterns were recorded using a Bruker D8 Advance. X-ray absorption spectroscopy (XAS) measurements were performed at beamline 1W1B of the Beijing Synchrotron Radiation Facility (BSRF), where the storage ring operates at a typical energy of 2.5 GeV. The spectra were acquired in fluorescence mode with energy calibration established using standard Pt foil and PtO2 reference materials. Chemical composition analysis was performed using an Agilent 5110 inductively coupled plasma optical emission spectrometer (ICP-OES). The ¹H and ¹³C nuclear magnetic resonance (NMR) spectra were recorded on a Bruker 400 MHz NMR spectrometer. X-ray photoelectron spectroscopy (XPS) was performed with Thermo Scientific Nexsa. Raman spectra were obtained by Thermo DXR green laser (532 nm). The deuterated DAT substrates and DATOR products were characterized by ¹³C and ¹H nuclear magnetic resonance (NMR) spectroscopy using a Bruker Advance 400 MHz spectrometer, with measurements conducted in deuterium oxide (D2O) at 25 °C.

In situ attenuated total reflection Fourier-transform infrared (ATR-FTIR): The reaction mechanism of DATOR was probed using in situ Fourier transform infrared spectroscopy (FTIR) conducted on a Nicolet IS50 FTIR spectrometer equipped with a mercury cadmium telluride (MCT) cryogenic detector, coupled with a Pike Technologies VeeMAX III attenuated total reflectance (ATR) accessory and Jackfish J1 electrochemical cell. The working electrode was fabricated by depositing a 50 nm gold film via vacuum sputter deposition onto a silicon ATR crystal, serving as an architectural support for CuO/CF catalyst immobilization. The CuO NW catalyst ink was prepared through ultrasonic exfoliation of CuO/CF (1 cm2 geometric area) in a ternary solvent system comprising: Ethanol (0.5 mL, ≥ 99.7%), Deionized water (0.5 mL, 18.2 MΩ·cm) and Nafion ionomer solution (40 μL, 5 wt% in lower aliphatic alcohols, Dupont D520).The homogeneous colloidal suspension was subsequently deposited onto the gold-coated substrate via micro-syringe drop-casting followed by ambient drying at 25 ℃ under relative humidity < 40%.

In situ differential electrochemical mass spectrometry (DEMS): The gaseous products generated during the anodic DATOR process were analyzed using an in situ differential electrochemical mass spectrometry (DEMS) system (Shanghai Linglu Instrument Equipment) under ultrahigh vacuum conditions (< 10−7 Pa). The electrochemical cell and vacuum chamber were physically isolated by a microporous polytetrafluoroethylene (PTFE) membrane, enabling selective gas permeation while effectively preventing electrolyte contamination. Trace-level gaseous species were quantitatively monitored through real-time mass spectrometric detection integrated with the electrochemical setup.

Electrochemical characterizations: All electrochemical measurements were conducted using a CHI760e electrochemical workstation (Chenhua, Shanghai). The hydrogen evolution reaction (HER) performance was evaluated in a three-electrode configuration, where the as-prepared Pts,n@NiS2@CC served as the working electrode, with high-purity graphite and Hg/HgO electrodes functioning as the counter electrode and reference electrode, respectively. The electrolyte consisted of 1.0 M KOH aqueous solution. Linear sweep voltammetry (LSV) was performed within a potential window of -0.6 to -1.5 V (vs. Hg/HgO) at a scan rate of 2 mV s−1. The catalytic stability was further assessed through cyclic voltammetry (CV) and chronopotentiometric (CP) measurements. For the anodic DATOR system characterization, a three-electrode setup was employed using CuO/CF as the working electrode, Pt wire as the counter electrode, and Hg/HgO as the reference electrode. The electrolyte solutions contained 1.0 M KOH with varying DAT concentrations (0.1, 0.2, 0.3, 0.4 M). LSV tests were conducted in the potential range of 0.6-1.8 V (vs. RHE). All measured potentials in three-electrode systems were subjected to IR compensation using the following equation:

E (vs. RHE) = E (vs. Hg/HgO)+ 0.059 × pH + 0.098

The HER||DATOR coupling system was tested in a two-electrode system completed in an H-type electrolyzer. Pts,n@NiS2@CC and CuO/CF were used as the cathode and anode, respectively, with a working area of 0.25 cm−2. The cathode and anode were divided into two chambers in the middle by an anion exchange membrane (FumasepFAA-3-50). The cathode and anode chambers used 1.0 M KOH and 1.0 M KOH + 0.2 M DAT as electrolytes, respectively. The AEMWE device also used the same electrode types as described above, except that the working area of both electrodes was 1.0 cm−2. The AEMWE device was operated with a CHI760e (Brilliance) equipped with a current amplifier, using 1.0 M KOH and 1.0 M KOH + 0.2 M DAT as the cathodic and anodic electrolytes, respectively, at room temperature. MKOH and 1.0 M KOH + 0.2 M DAT, respectively, for cathode electrolyte and anode electrolyte to study the flow cell performance. The separation of DAAT products was based on the difference in solubility. The pH was adjusted to neutral with sulfuric acid, stirred at 100 °C for 30 min, and treated with a thermal filter. The stability tests were conducted via chronopotentiometry at a current density of 500 mA cm−2 for 500 h. Due to the rapid consumption of the DAT substrate and water during the prolonged stability evaluation, the electrolyte was subjected to irregular replenishment to maintain consistent reaction conditions.

Theoretical calculations: Density functional theory (DFT) calculations were performed using the Vienna Ab initio Simulation Package (VASP 6.4.2) with the projector augmented wave (PAW) pseudopotential method. The electron exchange-correlation interactions were treated within the generalized gradient approximation (GGA) using the Perdew-Burke-Ernzerhof (PBE) functional. A plane-wave basis set with an energy cutoff of 500 eV was employed to expand the Kohn-Sham wavefunctions, ensuring convergence of the electronic structure calculations. The Brillouin zone integration was sampled using a Γ-centered 3 × 3 × 1 k-point mesh generated through the Monkhorst-Pack scheme. Electronic self-consistency was achieved through iterative solution of the Kohn-Sham equations using the self-consistent field (SCF) method, with convergence criteria set to 1 × 10−5 eV for total energy differences. Structural optimizations were performed using the conjugate gradient algorithm, requiring atomic forces to converge below 0.05 eV/Å and lattice stresses within 0.1 GPa. Van der Waals interactions between adsorbates and catalyst surfaces were explicitly considered through Grimme DFT-D3 dispersion correction method. Reaction pathways were investigated using the climbing image nudged elastic band (CI-NEB) method to identify transition states and minimum energy paths. Thermodynamic properties were calculated through vibrational frequency analysis, with zero-point energy (ZPE) corrections and entropy contributions evaluated in the harmonic approximation. The Gibbs free energy change (ΔG) was determined using the relation:

ΔG=ΔEads+ΔEZPE-TΔS

where ΔEads is the difference between the energies of the product and reactant molecules adsorbed on the surface of the catalyst, calculated by DFT; ΔEZPE and ΔS are the zero-point energy and entropy changes obtained from the vibrational frequency, respectively.

The adsorption energy (ΔEads) is defined as:

ΔEads=E(total)-E(surface)-E(adsorbate)

E(total) is the total energy of the adsorbate and the catalyst, then E(surface) is the energy of the catalyst and E(adsorbate) is the energy of the adsorbate.

Supplementary Figures and Tables

Fig. S1 a) XRD patterns of Ni(OH)2. b, c) SEM and d, e) TEM images of Ni(OH)2. HAADF-STEM image and elemental mappings of O and Ni, respectively, for Ni(OH)2

Fig. S2 a, b) SEM and c, d) TEM images of NiS2. HAADF-STEM image and elemental mappings of S and Ni, respectively, for NiS2

Fig. S3 Contact angle of water droplets sitting on the surface of the a) CC substrate, b) NiS2@CC, c) Pts,n@NiS2@CC

Fig. S4 Low resolution a) TEM and b) SEM of Pts,n@NiS2@CC

Fig. S5 AC-HAADF STEM images of Pts,n@NiS2@CC

Fig. S6 AC-STEM-HAADF images and Pt mapping of Pts,n@NiS2@CC

Fig. S7 a) XPS survey spectra of NiS2@CC and Pts,n@NiS2@CC. b) Ni 2p and c) S 2p XPS spectra of NiS2@CC and Pts,n@NiS2@CC. d) Pt 4f XPS spectra of Pts,n@NiS2@CC

Fig. S8 HER performance curves at different KOH concentrations (0.5 M and 2.0 M)

Fig. S9 TEM images and particle size distribution of a) Pt-2.0 and b) Pt-3.0. c) Pt 4f XPS spectra of Pt-2.0 and Pt-3.0

Fig. S10 HER with and without 10 mM KSCN and 10 mM EDTA in the alkaline electrolytes

Fig. S11 a) Pt-0.1 and b) Pt-2.0 of HER performance with and without 10 mM EDTA in the alkaline electrolytes

Fig. S12 a) XRD patterns of MoS2@CC and VS2@CC. b) HER performance of difference samples. c) Comparison of the overpotential at −100 mA cm−2 and −10 mA cm−2 for different samples

Fig. S13 EIS Nyquist plots of NiS2@CC, Pts,n@NiS2@CC and CC@Pt/C

Fig. S14 CV curves of a)NiS2@CC and b) Pts,n@NiS2@CC over anon-faradic potential range with various scan rates of 2.5, 5, 10, 25, 50 and 100 mV s-1

Fig. S15 Normalized Fitted HER Performance Curve

Fig. S16 a) LSV curve of initial and after 2000 CVs cycle. b) CP test of Pt/C and Pts,n@NiS2@CC

Fig. S17 Structural and morphological characterizations of Pts,n@NiS2@CC after the CP test. a) XRD patterns of Pts,n@NiS2@CC. b) XPS survey spectrum and High-resolution spectra of (c) Ni 2p, (d) S 2p and (e) Pt 4f signals for Pts,n@NiS2@CC after CP test. f) Raman spectra of Pts,n@NiS2@CC after CP test. g) SEM images of Pts,n@NiS2@CC. h) Low and high-resolution TEM images of Pts,n@NiS2@CC. i) Elemental mappings of Ni, Pt and S respectively, for Pts,n@NiS2@CC

Fig. S18 HER hydrogen production efficiency and Faraday electron efficiency

Fig. S19 Theoretical model diagram for Pts, Ptn and Pts,n load NiS2

Fig. S20 Differential charge density diagram of Pts@NiS2 and Ptn@NiS2

Fig. S21 Pts,n@NiS2@CC total element DOS diagram

Fig. S22 H* (red cycle) adsorption model diagram

Fig. S23 Structural models of initial state, transition state, and final state of Volmer pathway on Ptn@NiS2@CC

Fig. S24 Structural models of initial state, transition state, and final state of Volmer pathway on Pts,n@NiS2@CC Pt SA Site

Fig. S25 Structural models of initial state, transition state, and final state of Volmer pathway on Pts@NiS2@CC

Fig. S26 Structural models of initial state, transition state, and final state of Volmer pathway on NiS2@CC

Fig. S27 schematic diagram of conversion from CF to CuO/CF

Fig. S28 SEM images of Cu(OH)2

Fig. S29 Contact angle of water droplets sitting on the surface of the a) CF, b) Cu(OH)2/CF, c) CuO/CF

Fig. S30 a) XRD patterns of CuO/CF and CuOH)2/CF. b) SEM and c) TEM images CuO of CuO/CF. c) Elemental mappings of Cu and O respectively, for CuO/CF

Fig. S31 DATOR performance curves at different KOH concentrations

Fig. S32 Performance curve of DATOR added with TEMPO and IPA

Fig. S33 Theoretical model diagram for DAT, DAAT and DAAT+OH* load CuO

Fig. S34 Differential charge density diagram of DAT on CuO surface

Fig. S35 Mechanism diagram of With or without OH* induced DATOR (path 2-4)

Fig. S36 Mechanism diagram of without OH* induced DATOR (Path 3,4)

Fig. S37 Illustration of possible synergistically catalytic mechanism of alkaline DATOR on CuO

Fig. S38 Schematic diagram of HER||DATOR coupling device

Fig. S39 Structural and morphological characterizations of CuO/CF after the CP test. a) XRD patterns of CuO/CF. b) XPS survey spectrum and High-resolution spectra of c) Cu 2p signals for CuO/CF after CP test. d) SEM images of Pts,n@NiS2@CC. e) Low and high-resolution TEM images of Pts,n@NiS2@CC. f) Elemental mappings of Ni, Pt and S respectively, for Pts,n@NiS2@CC. g) CP test of CuO/CF

Fig. S40 In-situ infrared spectrum of OH*

Fig. S41 Faradaic efficiency of DATOR at various current densities

Table S1 Comparison of OWS working potentials and HER performance for the Pts,n@NiS2@CC at 10 mA cm–2 with those of recently reported state-of-the-art electrocatalysts

| Catalysts | η10 | Tafel | Refs. |
| --- | --- | --- | --- |
| Pts,n@NiS2@CC | 36.7 | 33 | This work |
| Ru3Ni3NAS | 39 | 26.9 | iscience, 2019, 11, 492 |
| a-RuTe2PNRS | 36 | 36 | Nat. Commun., 2019, 10, 5692 |
| Ni-BDT-A | 80 | 70 | Nat. Commun., 2017, 8, 14580 |
| Er2Si2O7:IrO2 | 170 | 59 | ACS Catal., 2018, 8, 8830 |
| Ir-Ni thin films | 60 | 40 | Catal. Lett., 2019, 150, 1325 |
| IrCo@NC | 45 | 80 | Adv. Mater., 2018, 30, 1705324 |
| Ni/Graphene | 29 | 87 | Mater. Chem. And physics, 2021, 272, 125049 |
| Ni-Mo-Cu | 49 | 62 | Surf. Coat. Tech., 2023, 465, 129596 |
| Ni-Co alloys | 69.8 | 89.7 | Int. J. Hydrog. Energy., 2019, 44, 29946 |
| Ni-Mo-S | 37 | 63.42 | Int. J. Hydrog. Energy., 2021, 46, 3821 |
| Co-MoS2 | 58 | 100 | Appl. surface. Sci., 2020, 516, 146094 |
| Co-Mn@Ni-Se | 22.1 | 45.05 | Appl. Catal. B Environ., 2023, 325, 122355 |
| NiFe-LDH-Vo@NiRu | 24 | 92.4 | Chem. Eng. J., 2022, 137226 |
| Ni3S2@NGCLS/NF | 134 | 99 | Chem. Eng. J., 2022, 401, 126045 |
| NiS2/V-MXene | 179 | 85 | J. Catal., 2019, 375, 8 |
| NiCoP/NF | 60 | 51.4 | J. power sources., 2021, 484, 229269 |
| Ni-NiCoPx/NCF | 23 | 30 | Chem. Eng. J., 2020, 402, 126257 |
| NiCo2O4@Ni2P | 141 | 86 | Mater. Today. Energy., 2020, 17, 100490 |
| P Vo NiCo2O4 | 175 | 55 | J. Power Sourece., 2021, 490, 229541 |
| CoSe2/N-CNT | 84 | 62 | ACS. Appl. Mater. Interface., 2019, 11, 3372 |
| NiCoN | 48 | 78.7 | J. Mater. Chem. A, 2019, 7, 19728 |
| FeOOH@Co4N | 92 | 34 | ACS. Appl. Mater. Interface., 2019, 11, 5152 |
| NiS2/CoS2/C | 165 | 72 | Nano. Energy., 2021, 105940 |
| Ru/Co3O4 | 30.96 | 57.87 | Chem. Commun., 2019, 55, 3781 |
| Cr0.2Ni0.8 | 106 | 71 | Int. J. Hydrog. Energy, 2020, 45, 17533 |
| Cr-doped cop nanorods | 36 | 54 | Cell Rep. Phys. Sci., 2020, 100136 |
| PtSA-NiSe-V | 45 | 52 | Angew. Chem. Int. Ed, 2023. |
| Ni2P/CoP-Pt | 44.5 | 58.4 | Adv. Funct. Mater., 2023. |
| Pt-Ni(OH)X | 58 | 84 | Adv. Energy. Mater., 2023. |
| Ni2P-Ni12P5@Ni3S2/NF | 34 | 146 | Adv. Mater., 2022. |
| PtSA-Ni3Fe LDH | 45 | 37.8 | Energ. Environ. Sci., 2021. |
| PtNi10/C | 66 | 16.73 | J. Colloid Interface Sci. , 2023, 634, 897-905 |
| Mixture phases PtFe | 28 | 42 | Small., 2022, 18, 2106947 |
| PtFeNiCuCo | 27 | 34.7 | J. phys.Conf. Ser., 2022, 2254, 012006 |
| Pt/NiCo@C | 48 | 130 | Electrochimica Acta., 2023, 460, 142634 |
| Ni-MOF@Pt | 102 | 88 | Nano Lett., 2019, 19, 8447 |
| Ni3S2@20 Co-MOF/CP | 140 | 90.3 | Fuel Process. Technol., 2022, 229, 107174 |
| CoO/N-S-UPCNPs-600 | 120 | 94 | Chem. Electro. Chem., 2019, 6, 3940 |

Table S2 Comparison of potential at 10 mA cm–2 for anodic oxidation reaction to upgrade chemicals with recently reported hybrid water electrolysis. (HMF: 5-Hydroxymethylfurfural)

| Catalysts | Substrate | Potential(E10) | Ref. |
| --- | --- | --- | --- |
| CuO/CF | DAT | 0.96 | This work |
| Mo-Co4N | Methanol | 1.427 | J. Mater. Chem. A, 2021, 9, 21094 |
| Co(OH)2@HOS/CP | Methanol | 1.497 | Adv. Funct. Mater., 2020, 30, 1909610 |
| CoCu-bi-MOF | Methanol | 1.365 | Appl. mater. lnterf., 2018, 10, 25422 |
| FeRu-MOF | Methanol | 1.32 | esci., 2023, 100118 |
| NiIr-MOF/NF | Methanol | 1.33 | Appl. Catal. B-environ., 2022, 121667 |
| 4MOFNs | Methanol | 1.365 | J. Colloid. lnterf. Sci, 2022, 616, 279 |
| Ni2P/NiMoP | urea | 1.35 | Esci., 2021, 1, 69 |
| Ni3N/N0.2Mo0.8N | urea | 1.348 | Chem. Eng. J., 2021, 409, 128240 |
| Ni-Mo-O | urea | 1.38 | Energ. Environ. Sci., 2018, 8, 1-7 |
| Ni2Fe(CN)6 | urea | 1.38 | Nat. Energ., 2021, 6, 904 |
| CoS2/MoS2 | urea | 1.29 | Adv. Funct. Mater., 2018, 8, 1801775 |
| NiMoO4@NiFeP | urea | 1.30 | Adv. Energ.Mater., 2019, 9, 1900390 |
| Ni-Mo-N | Glycerol | 1.36 | Nat. Commun, 2019, 10, 5335 |
| HEA-CoNiCuMnMo | Glycerol | 1.34 | J. Am.Chem. Soc., 2022, 144, 7224 |
| MnO2 | Glycerol | 1.38 | Angew. Chem. Int. Ed., 2021, 133, 21634 |
| Rhx[Ni(OH)2]y/C | Glycerol | 1.29 | Int. J. Hydrogen. Energ., 2023, 48, 31091 |
| Ru-NixPy/N-C | Glycerol | 1.36 | Ind. Eng. Chem. Res., 2019, 58, 16077 |
| Ru@Ni-B/NF | Glycerol | 1.24 | Chem. Rev., 2019,120, 526 |
| MoO2-FeP | HMF | 1.486 | Adv. Mater., 2020, 32, 2000455 |
| Co-CoSx@CN | HMF | 1.29 | Chem. sci., 2022, 13, 4647 |
| Ni(OH)2/NF | HMF | 1.39 | Chem. Suschem., 2021, 14, 2935 |
| δ-MnO2/NF | HMF | 1.35 | Chem. Mater., 2022, 34, 3123 |
| CuCoO4/NF | HMF | 1.23 | Angew. Chem. Int. Ed., 2020, 33, 385 |
| W-doped Ni3S2@NF | HMF | 1.34 | Sci. China. Chem., 2023, 66, 3636 |