Supporting Information for

Direct Repair of the Crystal Structure and Coating Surface of Spent LiFePO4 Materials Enables Superfast Li-Ion Migration

Yuanqi Lan1, 2#, Jianfeng Wen1#, Yatian Zhang1, Xuexia Lan3, Tianyi Song1, Jie Zhu1, Jing Peng3, Wenjiao Yao1, 2,3 *, Yongbing Tang1, 2, *, Hui-Ming Cheng2, 3

1 Advanced Energy Storage Technology Research Center, Shenzhen Institutes of Advanced Technology, Chinese Academy of Sciences, Shenzhen 518055, P. R. China

2 University of Chinese Academy of Sciences, Beijing 100049, P. R. China

3 Shenzhen Key Laboratory of Energy Materials for Carbon Neutrality, Shenzhen 518055, P. R. China

#Yuanqi Lan and Jianfeng Wen contributed equally to this work.

*Corresponding authors. E-mail: wj.yao@siat.ac.cn (Wenjiao Yao); tangyb@siat.ac.cn (Yongbing Tang)

Supplementary Figures and Tables

Fig. S1 Optical images of (a) s-LFP and (b) re-LFP

Fig. S2 The XRD refinement pattern of the s-LFP black mass

Fig. S3 The XRD patterns of relithiated LFP sample at different hydrothermal temperature for different time

Fig. S4 FTIR patterns of re-LFP, LFP-Hydro, LFP-Hydro-TA and s-LFP

Fig. S5 XRD refinement results of (a) delithiated LFP, and relithiated LFP with hydrothermal reactions for (b) once, (c) twice (d) three times and (e) four times

Fig. S6 TGA of s-LFP, LFP-hydro, LFP-hydro-TA, and re-LFP

Fig. S7 XRD of LFP residual heated at 800 ℃

Fig. S8 Detailed XRD patterns of s-LFP (a) and re-LFP (b) extracted from Fig. 1e, f

Fig. S9 EDX analyses of (a) s-LFP, (b) re-LFP, and (c) LFP-Hydro-TA. (d) EDX element map of LFP-Hydro-TA

Fig. S10 TEM image of s-LFP, showing the FePO4 and Fe2O3 phases on the surface

Fig. S11 TEM image of LFP-Hydro-TA

Fig. S12 O 1s (a) and P 2p (b) XPS spectra of the different LFP samples

Fig. S13 Full XPS spectra of s-LFP, LFP-Hydro-TA and re-LFP

Fig. S14 Charge-discharge profiles of re-LFP, LFP-Hydro-HT and LFP-Hydro

Fig. S15 (a) Cycling performance of LFP-hydro at 2C rate and (b) its charge-discharge profiles at different cycles. (c) GCD profile of LFP-Hydro-HT at 0.1C, 0.5C, 1C and 2C, with discharge capacities of 165, 155, 150, 132 mAh g−1, respectively

Fig. S16 Cycling performance of LFP-Hydro-HT and LFP-Hydro at 0.5C

Fig. S17 Cycling performance of re-LFP at 1C and 2C

Fig. S18 Cycling performance of s-LFP at 1C

Fig. S19 Cycling performance of re-LFP at 4C, 6C, 8C and 10C

Fig. S20 Cycling performance of s-LFP at 4C

Fig. S21 Cycling performance of re-LFP at 0.5C rate, −20 ℃

Fig. S22 Nyquist plots of pristine re-LFP

Fig. S23 Nyquist plot of the cycled re-LFP at −10 ℃ and its equivalent circuit inserted in the figure

Fig. S24 XRD refinements of a cycled c-LFP and b cycled re-LFP electrodes

Fig. S25 Charge-discharge profile of re-LFP in a solid-state electrolyte battery

Table S1 The chemical input and cost for recycling 1 kg s-LFP black mass used in EverBatt modelling

|  | Input materials | Usage (kg) | Price ($) | Products | Price ($) | Production (kg) |
| --- | --- | --- | --- | --- | --- | --- |
| Hydrometallurgy | H2SO4 | 1.24 | 0.01 | FePO4 Li2CO3 | 0.15 10.29 | 0.91 0.266 |
|  | NaOH | 0.01 | 0.35 |  |  |  |
|  | Ammonia | 2.48 | 0.27 |  |  |  |
|  | Na2CO3 | 0.32 | 0.19 |  |  |  |
| Conventional direct regeneration | LiOH | 0.04 | 15.97 | LiFePO4 | 5.07 | 1 |
|  | NMP | 0.1 | 1.32 |  |  |  |
|  | NaOH | 0.01 | 0.35 |  |  |  |
|  | Li2CO3 | 0.02 | 10.29 |  |  |  |
|  | Sucrose | 0.1 | 1.67 |  |  |  |
| This method | NMP | 0.1 | 1.32 | LiFePO4 | 5.07 | 1 |
|  | NaOH | 0.01 | 0.35 |  |  |  |
|  | Li2C2O4 | 0.01 | 111 |  |  |  |
|  | TA | 0.06 | 6.08 |  |  |  |

Table S2 Refinement of the composition of the LFP phase in the s-LFP black mass

| atom | x | y | z | Frac. | Uiso. |
| --- | --- | --- | --- | --- | --- |
| Li1 | 0 | 0 | 0 | 0.9588 | 0.03926 |
| Li2 | 0.282 | 0.25 | 0.9738 | 0.0412 | 0.01200 |
| Fe1 | 0.282 | 0.25 | 0.9738 | 0.9588 | 0.00080 |
| Fe2 | 0 | 0 | 0 | 0.0412 | 0.01100 |
| P | 0.0946 | 0.25 | 0.4182 | 1 | 0.01372 |
| O1 | 0.0973 | 0.25 | 0.7394 | 1 | 0.00305 |
| O2 | 0.4548 | 0.25 | 0.2086 | 1 | 0.00874 |
| O3 | 0.1643 | 0.0481 | 0.2843 | 1 | 0.00358 |
| a=10.32198 Å, b=6.00421 Å, c=4.69154 Å, space group: Pnma, 99.5 wt.%LFP, Rwp: 7.184% |  |  |  |  |  |

Table S3 Elemental analysis of the s-LFP black mass

| LFP sample | Li | Fe |  | P | Al |
| --- | --- | --- | --- | --- | --- |
| s-LFP | 0.994 | 1 | 0.981 |  | 0.0074 |
| LFP-Hydro-TA-HT | 1.011 | 1 | 0.974 |  | 0.0066 |

Table S4 The Rietveld refinement of XRD patterns of relithiated LFP sample at different hydrothermal temperature for different time

| Samples | Phase composition | FeLi ratio | Rwp |
| --- | --- | --- | --- |
| LFP-Hydro-80-10h | 100% LiFePO4 | 3.65% | 3.681% |
| LFP-Hydro-95-10h | 100% LiFePO4 | 1.16% | 3.426% |
| LFP-Hydro-95-4h | 100% LiFePO4 | 2.97% | 3.696% |
| LFP-Hydro-100-4h | 100% LiFePO4 | 1.35% | 3.548% |
| LFP-Hydro-120-4h | 100% LiFePO4 | 1.14% | 3.534% |
| LFP-Hydro-150-4h | 100% LiFePO4 | 0.96% | 3.682% |
| LFP-Hydro-180-4h | 100% LiFePO4 | 1.58% | 3.786% |

Table S5 Refinement of the composition of the LFP phase in the re-LFP

| atom | x | y | z | Frac. | Uiso. |
| --- | --- | --- | --- | --- | --- |
| Li1 | 0 | 0 | 0 | 0.9882 | 0.03926 |
| Li2 | 0.282 | 0.25 | 0.9738 | 0.0118 | 0.01 |
| Fe1 | 0.282 | 0.25 | 0.9738 | 0.9882 | 0.00738 |
| Fe2 | 0 | 0 | 0 | 0.0118 | 0.01 |
| P | 0.0946 | 0.25 | 0.4182 | 1 | 0.01372 |
| O1 | 0.0973 | 0.25 | 0.7394 | 1 | 0.00305 |
| O2 | 0.4548 | 0.25 | 0.2086 | 1 | 0.00874 |
| O3 | 0.1643 | 0.0481 | 0.2843 | 1 | 0.00358 |
| a=10.32198 Å, b=6.00421 Å, c=4.69154 Å, space group: Pnma, Rwp:3.83% |  |  |  |  |  |

Table S6 Comparison of the electrochemical performance of this work with other LFP direct regeneration studies

| Specific capacity mAh g−1 | Rate performance | Long-term cycling | Low-temperature performance | Voltage gap (mV) | Ref. |
| --- | --- | --- | --- | --- | --- |
| 170 (0.1 C); 139.1 (1C) | 100.1 mAh g−1 at 10 C | 76.6% retention after 1000 cycles at 1C; ≈76.8% capacity retention after 1000 cycles at 10 C | 145.7 mAh g−1 (25 °C), 82.2 mAh g−1 (−20 °C), and 152.8 mAh g−1 (50 °C) 0.3C | 58.9 (1 C) | [S1] |
| 146.2 (0.2 C); 141.9 (1 C) | 128.2 mAh g−1 at 5 C. | 98.6% retention after 200 cycles at 1 C. | \ | >150 (1 C) | [S2] |
| 145 (0.5 C) 140 (1C) | ~110 mAh g-1 at 5C | >95% retention after 100 cycles at 0.5C | \ | >150 | [S3] |
| ~170 (0.1C) 162 (0.2C); 144 (2C); | 102 mAh g-1 at 10C | 94.3% retention after 1000 cycles at 0.5 C; No capacity loss after 300 cycles at 2 C, 5C,10C | \ |  | [S4] |
| ~166 (0.1C); 151.9 (0.5C); 142.07 (1C); 133.11 (2 C) | 114.96 mAh g-1 at 5C | 99.1% retention after 200 cycles at 1C; 96.3% retention after 200 cycles at 2 C; 94.7%retention after 200 cycles at 5 C | \ | >150 | [S5] |
| 138.8 (1C); 124.3 (2C) | 107 mAh g−1 at 10C | 98.7% retention after 100 cycles at 1C; 87.9% retention after 500 cycles at 1C | \ | \ | [S6] |
| 162.8 (0.2C); 157.4 (0.5C), 147.9 (1C), | 138.4 mAh g−1 at 2C; 121.5 mAh g−1 at 5C | 99.63% retention after 100 cycles at 0.2C; | \ | \ | [S7] |
| 147.9 (1C), 136.1 (2C) | 113.6, mAh g−1 at 5C; 87.2 mAh g−1 at 10C | 82% retention after 500 cycles at 1 C rate; 86% after 500 cycles at 5 C. | \ | 83 (0.1 C) | [S8] |
| 167.8 (0.2 C); 141.5 (1 C); 131.6 (2 C) | 109.8 mAh g-1 at 109.85C | 92% retention after 300 cycles at 2C | 102.8 mAh g−1 at 1.0 C (−5°C). | \ | [S9] |
| ~138 (1C) | 117 mAh g-1 at 5C; 97 mAh g-1 at 10C | 88% retention after 400 cycles at 5C | ~61 mAh g-1 (0.5C, −20°C) | \ | [S10] |
| 140 (1C) | 117 mAh g-1 at 5C | 88.5% retention after 400 cycles at 1C | ~61 mAh g-1 (0.5C, −20°C) |  | [S11] |
| 135.1 (1C) | 116 mAh g-1 at 5C; 105.5 mAh g-1 at 10C; | 97.5% retention after 300 cycles at 1C | \ | \ | [S12] |
| 140.1 (1C) | 112.8 mAh g-1 at 5C; 93.0 mAh g-1 at 10C; | 93.1 % retention after 500 cycles at 5C; 93.8 % retention after 500 cycles at 10C | \ | \ | [S13] |
| 141.3 (1C) | 113.1mAh g-1 at 5C; 92.4 mAh g-1 at 10C; | 85% after 500 cycles and 72% after 1000 cycles at 1 C | 101.5 mAh g-1 (0.5C, 0°C) | 83 mV | [S14] |
| 161 (0.1 C); 151 (0.5C); 146 (1C); 138 (2C) | ~106.5 mAh g-1 at 10C 122 mAh g-1 at 5C | 69.8% retention (72.3 mAh g-1) after 1000 cycles at 10 C ; 67.8% retention （76.37 mAh g-1) after 1000 cycles at 8C; 97.5% retention after 100 cycles (5C) | ~62.5 mAh g-1 (0.5C, −20°C) | 66 mV (1C) | This work |

Text S1 Calculation of DLi using the PITT technique.

The PITT calculation is based on equation (S1)

lni=ln2∆QDLi/L2-π2DLi/(4L2)t             (S1)

For example, the ln(i)-t curve charged to 3.5V was plotted and the linear fit is shown in Figure 3(c). L equals to the electrode depth mines collector depth, which is about 183 μm. k was fitted to be −7.13529×10−5

DLi = 7.13529×10−5×4×(183×10−4)2∕π2 (cm2/s) =9.684×10−9 (cm2/s)

Based on Equation S1, we calculated the apparent DLi at different voltages during delithiation, as shown in Fig. 3c.

Supplementary References

- K. Jia, J. Ma, J. Wang, Z. Liang, G. Ji et al., Long-life regenerated LiFePO4 from spent cathode by elevating the d-band center of Fe. Adv. Mater. 35(5), 2208034 (2022). https://doi.org/10.1002/adma.202208034

- Q. Jing, J. Zhang, Y. Liu, W. Zhang, Y. Chen et al., Direct regeneration of spent LiFePO4 cathode material by a green and efficient one-step hydrothermal method. ACS Sustainable Chem. Eng. 8(48), 17622-17628 (2020). https://doi.org/10.1021/acssuschemeng.0c07166

- X. Liu, M. Wang, L. Deng, Y.-J. Cheng, J. Gao et al., Direct regeneration of spent lithium iron phosphate via a low-temperature molten salt process coupled with a reductive environment. Ind. Eng. Chem. Res. 61(11), 3831-3839 (2022). https://doi.org/10.1021/acs.iecr.1c05034

- P. Xu, Q. Dai, H. Gao, H. Liu, M. Zhang et al., Efficient direct recycling of lithium-ion battery cathodes by targeted healing. Joule 4(12), 2609-2626 (2020). https://doi.org/10.1016/j.joule.2020.10.008

- B. Chen, M. Liu, S. Cao, H. Hu, G. Chen et al., Direct regeneration and performance of spent LiFePO4 via a green efficient hydrothermal technique. J. Alloys Compd. 924, 166487 (2022). https://doi.org/10.1016/j.jallcom.2022.166487

- J. Wang, S. Ji, Q. Han, F. Wang, W. Sha et al., High performance of regenerated LiFePO4 from spent cathodes via an in situ coating and heteroatom-doping strategy using amino acids. J. Mater. Chem. A 12(25), 15311-15320 (2024). https://doi.org/10.1039/D4TA01098A

- W. Song, J. Liu, L. You, S. Wang, Q. Zhou et al., Re-synthesis of nano-structured LiFePO4/graphene composite derived from spent lithium-ion battery for booming electric vehicle application. J Power Sources. 419, 192-202 (2019). https://doi.org/10.1016/j.jpowsour.2019.02.065

- D. Tang, G. Ji, J. Wang, Z. Liang, W. Chen et al., A multifunctional amino acid enables direct recycling of spent LiFePO4 cathode material. Adv. Mater. 36(5), 2309722 (2024). https://doi.org/10.1002/adma.202309722

- Z. Zeng, P. Xu, J. Li, C. Yi, W. Zhao et al., Large-scale and homogenized strategies of spent LiFePO4 recycling: Reconstruction of targeted lattice. Adv. Funct. Mater. 34(6), 2308671 (2024). https://doi.org/10.1002/adfm.202308671

- G. Ji, J. Wang, Z. Liang, K. Jia, J. Ma et al., Direct regeneration of degraded lithium-ion battery cathodes with a multifunctional organic lithium salt. Nat. Commun. 14(1), 584 (2023). https://doi.org/10.1038/s41467-023-36197-6

- J. Li, R. Shi, J. Wang, Y. Cao, H. Ji et al., Interfacial metal-solvent chelation for direct regeneration of LiFePO4 cathode black mass. Adv. Mater. 37(5), 2414235 (2024). https://doi.org/10.1002/adma.202414235

- X. Qiu, C. Wang, Y. Liu, Q. Han, L. Xie et al., Ambient-pressure relithiation of spent LiFePO4 using alkaline solutions enables direct regeneration of lithium-ion battery cathodes. J. Energy Storage. 105, 114721 (2025). https://doi.org/10.1016/j.est.2024.114721

- C. Feng, Y. Cao, L. Song, B. Zhao, Q. Yang et al., Direct regeneration of industrial LiFePO4 black mass through a glycerol-enabled granule reconstruction strategy. Angew. Chem. -Int. Ed. 64(6), e202418198 (2025). https://doi.org/10.1002/anie.202418198

- Y. Cao, J. Li, D. Tang, F. Zhou, M. Yuan et al., Targeted defect repair and multi-functional interface construction for the direct regeneration of spent LiFePO4 cathodes. Adv. Mater. 36(48), 2414048 (2024). https://doi.org/10.1002/adma.202414048