Supporting Information for

Highly Elastic and Conductive Lamellar Wood Sponge via Cell Wall Reconfiguration Toward Smart Multifunctional Applications

Xin-jian Dai1, Xin Wang1, Ji-hang Hu1, Pan Jiang1*, Xiao-qing Wang1*

1Research Institute of Wood Industry, Chinese Academy of Forestry, Xiangshan Road, Haidian District, Beijing 100091, P. R. China

*Corresponding authors. E-mail: jiangpan@caf.ac.cn (Pan Jiang); wangxq@caf.ac.cn (Xiao-qing Wang)

Supplementary Figures and Tables

Fig. S1 The multiscale cell wall engineering strategy for CWS fabrication

Fig. S2 FTIR spectra of WS and CWS

Fig. S3 Photograph (a), cross section (b), tangential section (c) of CWS and its distribution of interlayer spacing (d)

Fig. S4 Photograph of CWS after chelating with Fe3+ ion

Fig. S5 The reaction mechanism for the oxidative polymerization of Pyrrole monomers

Fig. S6 Photograph of CWS@PPy after being cut in half

Fig. S7 XPS survey spectra (a) and N 1s spectrum (b) of samples

Fig. S8 Photographs of CWS@PPy prepared via the dip-coating method (a-b) and SEM image of the sample (c)

Fig. S9 FTIR spectra of various samples

Fig. S10 Raman spectra of CWS and CWS@PPy

Fig. S11 The element compositions of CWS, CWS@Fe3+, and CWS@PPy

Fig. S12 The X-ray diffraction patterns of various samples

Fig. S13 TEM image showing the continuous PPy nanocoating on the surface of the microfiber bundle

Fig. S14 The volume resistance and electrical conductivity of CWS@PPy with different PPy loading

Fig. S15 SEM images of radial section of CWS@PPy with different polymerization durations

Fig. S16 Electrical conductivity of CWS@PPy (19.61 wt%) with different strain

Fig. S17 Anisotropic electrical conductivity of CWS@PPy

Fig. S18 Photographs of aqueous solutions containing CWS@PPy subjected to ultrasonication d) SEM image of the sample after ultrasonic treatment for 6h

Fig. S19 The acid/alkali tolerance of CWS@PPy

Fig. S20 Schematic diagram of the dynamic impact testing system for the sample

Fig. S21 Viscoelastic properties (storage modulus, loss modulus, and damping ratio) of CWS as a function of temperature (-70 to 90 °C)

Fig. S22 Comparison of compressive elasticity of CWS@PPy and PU sponge in liquid nitrogen

Fig. S23 Photographs showing the mechanical stability of the water-saturated CWS@PPy

Fig. S24 Anisotropic EMI shielding effectiveness of CWS@PPy

Fig. S25 Photograph of customized plastic mold with different sizes

Fig. S26 Electromagnetic shielding effectiveness of customized plastic mold

Fig. S27 Electrical conductivity of CWS@PPy (17.51 wt%) at different strain

Fig. S28 ΔR/R0 of the sensor as a function of strain

Fig. S29 Current response of the CWS@PPy sensor loaded with an ultralight object (~27 Pa)

Fig. S30 Anisotropic thermal conductivity of CWS@PPy

Fig. S31 A homemade testing system for surface temperature measurement

Fig. S32 Density of CWS@PPy with different compressive strains

Fig. S33 The integrated functions of CWS@PPy for innovative application

Table S1 Comparison of the compressive fatigue resistance of CWS@PPy with those of the reported elastic aerogels and foams

| Types | Materials | Strain |  | Cycles |  | Plastic deformation | Stress retention | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Biomass-based | KGM |  | 50% |  | 1000 | 4.3% | 75% | [S1] |
|  | CNF/PMSQ |  | 60% |  | 10 000 | 5.0% | 80% | [S2] |
|  | CNF/MOF |  | 60% |  | 800 | 8.0% | 70% | [S3] |
|  | CNF/CNT/MMT |  | 50% |  | 10 000 | 2.0% | 86.3% | [S4] |
|  | CNF/MOF |  | 50% |  | 1000 | 3.0% | 80.2% | [S5] |
| Synthetic polymer-based | PI/RGO |  | 50% |  | 2000 | 3.0% | 88% | [S6] |
|  | PI/PVP |  | 50% |  | 100 | 3.2% | 86.14% | [S7] |
| Carbon-based | RGO/PAA |  | 50% |  | 1000 | 3.5% | 82.0% | [S8] |
|  | RGO |  | 70% |  | 1000 | 10% | 80% | [S9] |
| Ceramic-based | SiO2/ |  | 60% |  | 1000 | 14.5% | 75% | [S10] |
|  | ZrO2/Al2O3 |  | 60% |  | 1000 | 12.5% | 70% | [S11] |
|  | CWS@PPy |  | 40% |  | 10 000 | 3.5% | 85% | This work |

Note: Konjac glucomannan (KGM); Cellulose nanofibers (CNF); Polymethylsilsesquioxane (PMSQ); Metal-Organic Frameworks (MOF); Carbon nanotube (CNT); montmorillonite (MMT); Polyimide (PI); Polyvinylpyrrolidone (PVP); poly (amic acid) (PAA); Reduced graphene oxide (RGO).

Table S2 Recovery speed of CWS@PPy and other previously reported materials

| Materials | Recover speed | Refs. |
| --- | --- | --- |
| GO-based monolith | 116.6 | [S12] |
| CS–GO based aerogel | 580.0 | [S13] |
| GO-based hybrid aerogel | 792.0 | [S14] |
| CNT-based aerogel | 847.0 | [S15] |
| Ceramic-based aerogel | 860.0 | [S16] |
| Polymer-based carbon aerogel | 860.0 | [S17] |
| GO-based aerogel | 1084.6 | [S18] |
| Ceramic-based sponge | 1233.0 | [S19] |
| CWS@PPy | 1111.0 | This work |

Note: Graphene oxide (GO); Chitosan (CS); Carbon nanotube (CNT)

Table S3 Comparison of SSE value of CWS@PPy with other materials

| Types | Materials |  | Density [g·cm-3] | Frequency [GHz] | EMI SE [dB] | SSE [dB· cm3 ·g-1] | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Wood-based | Carbonized Wood | 0.072 |  | 8.2-12.4 | 77.0 | 1069.4 | [S20] |
|  | Delignified wood/PPy | 0.11 |  | 8.2-12.4 | 22.99 | 209.0 | [S21] |
|  | Carbonized Wood/CNT | 0.541 |  | 8.2-12.4 | 73.7 | 136.2 | [S22] |
|  | Wood/MXene | 0.108 |  | 8.2-12.4 | 72.0 | 666.7 | [S23] |
|  | Carbonized Wood | 0.13 |  | 8.2-12.4 | 60.463 | 465.1 | [S24] |
|  | Wood/MXene | 0.197 |  | 8.2-12.4 | 71.3 | 361.9 | [S25] |
|  | Carbonized Wood | 0.48 |  | 8.2-12.4 | 54.8 | 114.2 | [S26] |
| Polymer-based | Polyurethane/MXene | 0.063 |  | 8.2-12.4 | 76.2 | 1209.5 | [S27] |
|  | polyimide foams | 0.091 |  | 8.2-12.4 | 54.0 | 593.4 | [S28] |
|  | Polyimide/MXene/CNT | 0.152 |  | 8.2-12.4 | 68.2 | 448.7 | [S29] |
|  | Polyimide/MXene | 0.0487 |  | 8.2-12.4 | 62.5 | 1283.4 | [S30] |
|  | Polypropylene/CB | 0.12 |  | 8.2-12.4 | 41.0 | 341.7 | [S31] |
|  | Polyurethane/CNT | 0.020 |  | 8.2-12.4 | 23.0 | 1148.0 | [S32] |
| Cellulose-based | Cellulose/CNT | 0.095 |  | 8.2-12.4 | 20.8 | 219 | [S33] |
|  | Cellulose/PANI | 0.1079 |  | 8.2-12.4 | 85.4 | 791.2 | [S34] |
|  | Cellulose/GO | 0.0569 |  | 8.2-12.4 | 58.4 | 1026.4 | [S35] |
|  | Nanocellulose/CNT | 0.075 |  | 8.2-12.4 | 39.8 | 530.7 | [S36] |
|  | Nanocellulose/MXene | 0.1393 |  | 8.2-12.4 | 110.0 | 789.7 | [S37] |
|  | Cellulose/CNT | 0.087 |  | 8.2-12.4 | 40.2 | 461.95 | [S38] |
|  | Sugarcane | 0.112 |  | 8.2-12.2 | 51.0 | 455.4 | [S39] |
|  | CWS@PPy | 0.06 |  | 8.2-12.4 | 77.18 | 1286.3 | This work |

Note: Carbon nanotube (CNT), Graphene oxide (GO); carbon black (CB); Polyaniline (PANI);

Table S4 Comparison of the maximum sensitivity of CWS@PPy sensor with various reported aerogel and foam-based sensors

| Types | Materials | Sensitivity [kPa-1] | Refs. |
| --- | --- | --- | --- |
| Polymer-based | PI/MXene | 0.14 | [S40] |
|  | PDMS/Ni/EGaIn composite | 0.313 | [S41] |
|  | PU/RGO aerogel | 0.26 | [S42] |
|  | PU/CB aerogel | 0.068 | [S43] |
|  | Melamine/PANI/RGO composite | 0.152 | [S44] |
|  | PU/ANF/MXene | 0.46 | [S45] |
| Cellulose-based | Bamboo fiber/RGO sponge | 0.59 | [S46] |
|  | CNF/CB aerogel | 0.234 | [S47] |
|  | Bamboo cellulose nanofiber | 0.95 | [S48] |
|  | Cellulose carbon sponge | 1.04 | [S49] |
| Wood-based | Wood sponge/RGO | 0.32 | [S50] |
|  | Wood aerogel/PEDOT:PSS | 0.57 | [S51] |
|  | Wood sponge/CNT/ PEDOT:PSS | 1.05 | [S52] |
|  | Wood sponge/Grephene | 0.34 | [S53] |
|  | CWS@PPy | 0.72 | This work |

Note: Polyimide (PI); Polyurethane (PU); Reduced graphene oxide (RGO); Carbon black (CB); polyaniline (PANI); aramid fiber (ANF); Cellulose nanofiber (CNF); Carbon nanotube (CNT)

Table S5 Comparison of thermal conductivity of CWS@PPy among reported aerogels and foams

| Types | Materials | Temperature | Humidity | Thermal conductivity [W m-1 K-1] | Refs. |
| --- | --- | --- | --- | --- | --- |
|  | PBAT | RT | N/A | 0.0378 | [S54] |
| Polymer-based | PU | RT | N/A | 0.038 | [S55] |
|  | PI | RT | N/A | 0.059 | [S56] |
|  | CNF/GSA | RT | N/A | 0.03018 | [S57] |
|  | MFC/CNF/Al3+ | RT | N/A | 0.0403 | [S58] |
| Cellulose-based | CNF/PLA | RT | N/A | 0.041 | [S59] |
|  | CNF/G/Cu2+ | RT | N/A | 0.05 | [S60] |
|  | CNF/MH | RT | N/A | 0.056 | [S61] |
|  | Cel/BT | RT | 60% | 0.063 | [S62] |
|  | AL/PA | RT | 30% | 0.034 | [S63] |
|  | CNF/LGN | RT | N/A | 0.0383 | [S64] |
|  | LigSi | RT | 33% | 0.04 | [S65] |
| Biomass-based | Wastepaper | RT | N/A | 0.044 | [S66] |
|  | SiO2@CFs/SLS | RT | N/A | 0.046 | [S67] |
|  | SA/LS/PA | RT | N/A | 0.047 | [S68] |
|  | Pulp | RT | N/A | 0.068 | [S69] |
|  | Wood foams | RT | N/A | 0.028 | [S70] |
|  | Wood aerogel | RT | N/A | 0.028 | [S71] |
|  | Nanowood | RT | 20% | 0.03 | [S72] |
| Wood-based | Wood aerogel | RT | 50% | 0.037 | [S73] |
|  | Insulwood | RT | 50% | 0.038 | [S74] |
|  | Wood aerogel | RT | N/A | 0.094 | [S75] |
|  | CWS@PPy | RT | 25% | 0.037 | This work |

Note: Poly (butylene adipate-co-terephthalate) (PBAT); Polyurethane (PU); Cellulose nanofiber (CNF); Glycerol succinic anhydride (GSA); Microfibrillated cellulose (MFC); Polylactic acid (PLA); Graphene (G); Magnesium hydroxide (MH); Cellulose (Cel); Bentonite (BT); Ammonium alginate (AL); Phytic acid (PA); Lignin (LGN); silica-mineralized lignin nanocomposite aerogel (LigSi); Sodium lignin sulfonate (SLS); Cellulose fibers (CFs); Sodium alginate (SA); Sodium lignosulfonate (LS);

Supplementary References

- Y. Si, X. Wang, C. Yan, L. Yang, J. Yu et al., Ultralight biomass-derived carbonaceous nanofibrous aerogels with superelasticity and high pressure-sensitivity. Adv. Mater. 28(43), 9512–9518 (2016). https://doi.org/10.1002/adma.201603143

- J. Zhang, Y. Cheng, C. Xu, M. Gao, M. Zhu et al., Hierarchical interface engineering for advanced nanocellulosic hybrid aerogels with high compressibility and multifunctionality. Adv. Funct. Mater. 31(19), 2009349 (2021). https://doi.org/10.1002/adfm.202009349

- S. Zhou, V. Apostolopoulou-Kalkavoura, M.V. Tavares da Costa, L. Bergström, M. Strømme et al., Elastic aerogels of cellulose Nanofibers@Metal-organic frameworks for thermal insulation and fire retardancy. Nano-Micro Lett. 12(1), 9 (2019). https://doi.org/10.1007/s40820-019-0343-4

- T. Zhu, D. Wang, Y. Wang, F. Xu, J. Huang et al., Gelation-constrained freeze-casting fabrication of ultra-homogeneous nanocomposite aerogels with superelasticity and harsh environment tolerance. Adv. Funct. Mater. 35(32), 2503693 (2025). https://doi.org/10.1002/adfm.202503693

- J. Qiao, Q. Song, X. Zhang, S. Zhao, J. Liu et al., Enhancing interface connectivity for multifunctional magnetic carbon aerogels: an in situ growth strategy of metal-organic frameworks on cellulose nanofibrils. Adv. Sci. 11(19), 2400403 (2024). https://doi.org/10.1002/advs.202400403

- Y. Qin, Q. Peng, Y. Ding, Z. Lin, C. Wang et al., Lightweight, superelastic, and mechanically flexible graphene/polyimide nanocomposite foam for strain sensor application. ACS Nano 9(9), 8933–8941 (2015). https://doi.org/10.1021/acsnano.5b02781

- X. Zhao, K. Ruan, H. Qiu, X. Zhong, J. Gu, Fatigue-resistant polyimide aerogels with hierarchical cellular structure for broadband frequency sound absorption and thermal insulation. Adv. Compos. Hybrid Mater. 6(5), 171 (2023). https://doi.org/10.1007/s42114-023-00747-9

- Y. Zhang, P. Min, G. Yue, B. Niu, L. Li et al., Emulsion-based multiscale structural design realizes lightweight and superelastic graphene aerogels for electromagnetic interference shielding. Small 20(48), 2405950 (2024). https://doi.org/10.1002/smll.202405950

- X. Zhao, W. Yao, W. Gao, H. Chen, C. Gao, Wet-spun superelastic graphene aerogel millispheres with group effect. Adv. Mater. 29(35), 1701482 (2017). https://doi.org/10.1002/adma.201701482

- Y. Si, J. Yu, X. Tang, J. Ge, B. Ding, Ultralight nanofibre-assembled cellular aerogels with superelasticity and multifunctionality. Nat. Commun. 5, 5802 (2014). https://doi.org/10.1038/ncomms6802

- X. Zhang, F. Wang, L. Dou, X. Cheng, Y. Si et al., Ultrastrong, superelastic, and lamellar multiarch structured ZrO2–Al2O3 nanofibrous aerogels with high-temperature resistance over 1300 °C. ACS Nano 14(11), 15616–15625 (2020). https://doi.org/10.1021/acsnano.0c06423

- L. Qiu, J.Z. Liu, S.L.Y. Chang, Y. Wu, D. Li, Biomimetic superelastic graphene-based cellular monoliths. Nat. Commun. 3, 1241 (2012). https://doi.org/10.1038/ncomms2251

- H.-L. Gao, Y.-B. Zhu, L.-B. Mao, F.-C. Wang, X.-S. Luo et al., Super-elastic and fatigue resistant carbon material with lamellar multi-arch microstructure. Nat. Commun. 7, 12920 (2016). https://doi.org/10.1038/ncomms12920

- X. Wu, T. Liu, Y. Qiu, Z. Hou, C. Cai et al., Elastic yet strength triboelectric aerogel enabled by constructing a supramolecular system. Adv. Funct. Mater. 35(11), 2417067 (2025). https://doi.org/10.1002/adfm.202417067

- L. Zhuang, D. Lu, J. Zhang, P. Guo, L. Su et al., Highly cross-linked carbon tube aerogels with enhanced elasticity and fatigue resistance. Nat. Commun. 14(1), 3178 (2023). https://doi.org/10.1038/s41467-023-38664-6

- Y. Si, X. Wang, L. Dou, J. Yu, B. Ding, Ultralight and fire-resistant ceramic nanofibrous aerogels with temperature-invariant superelasticity. Sci. Adv. 4(4), eaas8925 (2018). https://doi.org/10.1126/sciadv.aas8925

- Z.-L. Yu, B. Qin, Z.-Y. Ma, J. Huang, S.-C. Li et al., Superelastic hard carbon nanofiber aerogels. Adv. Mater. 31(23), e1900651 (2019). https://doi.org/10.1002/adma.201900651

- L. Lv, P. Zhang, T. Xu, L. Qu, Ultrasensitive pressure sensor based on an ultralight sparkling graphene block. ACS Appl. Mater. Interfaces 9(27), 22885–22892 (2017). https://doi.org/10.1021/acsami.7b07153

- L. Li, C. Jia, Y. Liu, B. Fang, W. Zhu et al., Nanograin–glass dual-phasic, elasto-flexible, fatigue-tolerant, and heat-insulating ceramic sponges at large scales. Mater. Today 54, 72–82 (2022). https://doi.org/10.1016/j.mattod.2022.02.007

- Z. Dai, C. Hu, Y. Wei, W. Zhang, J. Xu et al., Highly anisotropic carbonized wood as electronic materials for electromagnetic interference shielding and thermal management. Adv. Electron. Mater. 9(7), 2300162 (2023). https://doi.org/10.1002/aelm.202300162

- W. Gan, C. Chen, M. Giroux, G. Zhong, M.M. Goyal et al., Conductive wood for high-performance structural electromagnetic interference shielding. Chem. Mater. 32(12), 5280–5289 (2020). https://doi.org/10.1021/acs.chemmater.0c01507

- M. Cheng, W. Ren, H. Li, X. Liu, S. Bandaru et al., Multiscale collaborative coupling of wood-derived porous carbon modified by three-dimensional conductive magnetic networks for electromagnetic interference shielding. Compos. Part B Eng. 224, 109169 (2021). https://doi.org/10.1016/j.compositesb.2021.109169

- M. Zhu, X. Yan, H. Xu, Y. Xu, L. Kong, Ultralight, compressible, and anisotropic MXene@Wood nanocomposite aerogel with excellent electromagnetic wave shielding and absorbing properties at different directions. Carbon 182, 806–814 (2021). https://doi.org/10.1016/j.carbon.2021.06.054

- Y. Yuan, X. Sun, M. Yang, F. Xu, Z. Lin et al., Stiff, thermally stable and highly anisotropic wood-derived carbon composite monoliths for electromagnetic interference shielding. ACS Appl. Mater. Interfaces 9(25), 21371–21381 (2017). https://doi.org/10.1021/acsami.7b04523

- C. Liang, H. Qiu, P. Song, X. Shi, J. Kong et al., Ultra-light MXene aerogel/wood-derived porous carbon composites with wall-like “mortar/brick” structures for electromagnetic interference shielding. Sci. Bull. 65(8), 616–622 (2020). https://doi.org/10.1016/j.scib.2020.02.009

- X. Liu, H. Liu, H. Xu, W. Xie, M. Li et al., Natural wood templated hierarchically cellular NbC/Pyrolytic carbon foams as Stiff, lightweight and High-Performance electromagnetic shielding materials. J. Colloid Interface Sci. 606, 1543–1553 (2022). https://doi.org/10.1016/j.jcis.2021.08.110

- E. Kim, H. Zhang, J.-H. Lee, H. Chen, H. Zhang et al., MXene/polyurethane auxetic composite foam for electromagnetic interference shielding and impact attenuation. Compos. Part A Appl. Sci. Manuf. 147, 106430 (2021). https://doi.org/10.1016/j.compositesa.2021.106430

- J. Li, Y. Ding, N. Yu, Q. Gao, X. Fan et al., Lightweight and stiff carbon foams derived from rigid thermosetting polyimide foam with superior electromagnetic interference shielding performance. Carbon 158, 45–54 (2020). https://doi.org/10.1016/j.carbon.2019.11.075

- T. Xue, Y. Yang, D. Yu, Q. Wali, Z. Wang et al., 3D printed integrated gradient-conductive MXene/CNT/polyimide aerogel frames for electromagnetic interference shielding with ultra-low reflection. Nano-Micro Lett. 15(1), 45 (2023). https://doi.org/10.1007/s40820-023-01017-5

- Z.-H. Zeng, N. Wu, J.-J. Wei, Y.-F. Yang, T.-T. Wu et al., Porous and ultra-flexible crosslinked MXene/polyimide composites for multifunctional electromagnetic interference shielding. Nano-Micro Lett. 14(1), 59 (2022). https://doi.org/10.1007/s40820-022-00800-0

- Y. Li, X. Lan, F. Wu, J. Liu, P. Huang et al., Steam-chest molding of polypropylene/carbon black composite foams as broadband EMI shields with high absorptivity. Compos. Commun. 22, 100508 (2020). https://doi.org/10.1016/j.coco.2020.100508

- Z. Zeng, H. Jin, M. Chen, W. Li, L. Zhou et al., Lightweight and anisotropic porous MWCNT/WPU composites for ultrahigh performance electromagnetic interference shielding. Adv. Funct. Mater. 26(2), 303–310 (2016). https://doi.org/10.1002/adfm.201503579

- H.-D. Huang, C.-Y. Liu, D. Zhou, X. Jiang, G.-J. Zhong et al., Cellulose composite aerogel for highly efficient electromagnetic interference shielding. J. Mater. Chem. A 3(9), 4983–4991 (2015). http://dx.doi.org/10.1039/C4TA05998K

- M. Chen, J. Zhu, K. Zhang, H. Zhou, Y. Gao et al., Carbon nanofiber/polyaniline composite aerogel with excellent electromagnetic interference shielding, low thermal conductivity, and extremely low heat release. Nano-Micro Lett. 17(1), 80 (2024). https://doi.org/10.1007/s40820-024-01583-2

- C. Wan, J. Li, Graphene oxide/cellulose aerogels nanocomposite: Preparation, pyrolysis, and application for electromagnetic interference shielding. Carbohydr. Polym. 150, 172–179 (2016). https://doi.org/10.1016/j.carbpol.2016.05.051

- G. Zhu, L. Giraldo Isaza, B. Huang, A. Dufresne, Multifunctional nanocellulose/carbon nanotube composite aerogels for high-efficiency electromagnetic interference shielding. ACS Sustainable Chem. Eng. 10(7), 2397–2408 (2022). https://doi.org/10.1021/acssuschemeng.1c07148

- L. Chen, T. Mai, X.-X. Ji, P.-L. Wang, M.-Y. Qi et al., 3D printing of customizable and lightweight multilayer MXene/nanocellulose architectures for tunable electromagnetic interference shielding via direct ink writing. Chem. Eng. J. 476, 146652 (2023). https://doi.org/10.1016/j.cej.2023.146652

- B. Haspulat Taymaz, V. Eskizeybek, Lightweight and sustainable recycled cellulose based hybrid aerogels with enhanced electromagnetic interference shielding. Cellulose 32(5), 3335–3354 (2025). https://doi.org/10.1007/s10570-025-06471-5

- Y.-Q. Li, Y.A. Samad, K. Polychronopoulou, K. Liao, Lightweight and highly conductive aerogel-like carbon from sugarcane with superior mechanical and EMI shielding properties. ACS Sustainable Chem. Eng. 3(7), 1419–1427 (2015). https://doi.org/10.1021/acssuschemeng.5b00340

- H. Liu, X. Chen, Y. Zheng, D. Zhang, Y. Zhao et al., Lightweight, superelastic, and hydrophobic polyimide nanofiber/MXene composite aerogel for wearable piezoresistive sensor and oil/water separation applications. Adv. Funct. Mater. 31(13), 2008006 (2021). https://doi.org/10.1002/adfm.202008006

- M. Stevens, G. Yun, T. Hasan, Porous conductive hybrid composite with superior pressure sensitivity and dynamic range. Adv. Funct. Mater. 34(8), 2309347 (2024). https://doi.org/10.1002/adfm.202309347

- H.-B. Yao, J. Ge, C.-F. Wang, X. Wang, W. Hu et al., A flexible and highly pressure-sensitive graphene–polyurethane sponge based on fractured microstructure design. Adv. Mater. 25(46), 6692–6698 (2013). https://doi.org/10.1002/adma.201303041

- X. Wu, Y. Han, X. Zhang, Z. Zhou, C. Lu, Large-area compliant, low-cost, and versatile pressure-sensing platform based on microcrack-designed carbon Black@Polyurethane sponge for human–machine interfacing. Adv. Funct. Mater. 26(34), 6246–6256 (2016). https://doi.org/10.1002/adfm.201601995

- G. Ge, Y. Cai, Q. Dong, Y. Zhang, J. Shao et al., A flexible pressure sensor based on rGO/polyaniline wrapped sponge with tunable sensitivity for human motion detection. Nanoscale 10(21), 10033–10040 (2018). http://dx.doi.org/10.1039/C8NR02813C

- K. Qian, J. Zhou, M. Miao, H. Wu, S. Thaiboonrod et al., Highly ordered thermoplastic polyurethane/aramid nanofiber conductive foams modulated by kevlar polyanion for piezoresistive sensing and electromagnetic interference shielding. Nanomicro Lett. 15(1), 88 (2023). https://doi.org/10.1007/s40820-023-01062-0

- Y. Lv, J. Wei, Z. Huang, Z. Zhang, S. Ding et al., Superelastic bamboo fiber-based spongy aerogel for flexible piezoresistive sensors with wide response range and high sensitivity. Chem. Eng. J. 488, 151053 (2024). https://doi.org/10.1016/j.cej.2024.151053

- Y. Zhang, P. Zhu, H. Sun, X. Sun, Y. Ye et al., Superelastic cellulose sub-micron fibers/carbon black aerogel for highly sensitive pressure sensing. Small 20(13), 2310038 (2024). https://doi.org/10.1002/smll.202310038

- Y. Lv, J. Wei, W. Wang, H. Deng, Z. Huang et al., Superelastic bamboo cellulose nanofiber based carbon aerogel with layered network microstructure for high sensitivity piezoresistive sensor. Int. J. Biol. Macromol. 295, 139553 (2025). https://doi.org/10.1016/j.ijbiomac.2025.139553

- W. Hu, D. Song, X. Shi, L. Zhou, Z. Zhao et al., Anisotropic electronic skin for neurofeedback. Adv. Funct. Mater. 34(11), 2309359 (2024). https://doi.org/10.1002/adfm.202309359

- H. Guan, X. Dai, L. Ni, J. Hu, X. Wang, Highly elastic and fatigue-resistant graphene-wrapped lamellar wood sponges for high-performance piezoresistive sensors. ACS Sustainable Chem. Eng. 9(45), 15267–15277 (2021). https://doi.org/10.1016/j.ijbiomac.2025.139553

- T. Liu, Z. Zhao, R. Liang, H. He, Y. Liu et al., Tough and elastic anisotropic triboelectric materials enabled by layer-by-layer assembly. Adv. Funct. Mater. 35(26), 2500207 (2025). https://doi.org/10.1002/adfm.202500207

- H. Zhang, Q. Zhang, J. Liang, B. Li, J. Zang et al., Pressure and temperature dual-parameter sensor based on natural wood for portable health-monitoring devices. ACS Sustainable Chem. Eng. 11(45), 16194–16204 (2023). https://doi.org/10.1021/acssuschemeng.3c04237

- G. Zhang, P. Li, X. Wang, Y. Xia, J. Yang, Flexible battery-free wireless sensor array based on functional gradient-structured wood for pressure and temperature monitoring. Adv. Funct. Mater. 33(2), 2208900 (2023). https://doi.org/10.1002/adfm.202208900

- Z. Wang, G. Wang, Z. Xu, C. Ma, G. Zhao, Pore-gradient, flexible, and fully-degradable foam with outstanding noise absorption and thermal insulation. Adv. Funct. Mater. 35(37), 2504560 (2025). https://doi.org/10.1002/adfm.202504560

- T.M. Nguyen-Ha, T.B. Nguyen, T.A. Nguyen, L.H. Pham, D.H. Nguyen et al., Novel high-performance sustainable polyurethane nanocomposite foams: Fire resistance, thermal stability, thermal conductivity, and mechanical properties. Chem. Eng. J. 474, 145585 (2023). https://doi.org/10.1016/j.cej.2023.145585

- X.-A. Li, Y. Zong, W. Li, J. Qian, Z. Qiang et al., Achieving ultrahigh transparency and superior mechanical properties in flexible polyimide nanofoams through CO2 foaming for thermal insulation. Adv. Funct. Mater. 34(49), 2409498 (2024). https://doi.org/10.1002/adfm.202409498

- Dinesh, B. Kumar, D.H. Pham, J. Kim, Strong, highly porous and sustainable nanocellulose foam made using bioderived hyperbranched crosslinker for thermal insulation and sound absorption. Carbohydr. Polym. 334, 122016 (2024). https://doi.org/10.1016/j.carbpol.2024.122016

- H. Sun, D. Zheng, Y. Zhu, P. Zhu, Y. Ye et al., Multiscale design for robust, thermal insulating, and flame self-extinguishing cellulose foam. Small 20(12), 2306942 (2024). https://doi.org/10.1002/smll.202306942

- Q. Ren, W. Li, S. Cui, W. Ma, X. Zhu et al., Improved thermal insulation and compressive property of bimodal poly (lactic acid)/cellulose nanocomposite foams. Carbohydr. Polym. 302, 120419 (2023). https://doi.org/10.1016/j.carbpol.2022.120419

- C. Chen, Y. Zhou, W. Xie, T. Meng, X. Zhao et al., Lightweight, thermally insulating, fire-proof graphite-cellulose foam. Adv. Funct. Mater. 33(6), 2204219 (2023). https://doi.org/10.1002/adfm.202204219

- Y. Han, X. Zhang, X. Wu, C. Lu, Flame retardant, heat insulating cellulose aerogels from waste cotton fabrics by in situ formation of magnesium hydroxide nanoparticles in cellulose gel nanostructures. ACS Sustainable Chem. Eng. 3(8), 1853–1859 (2015). https://doi.org/10.1021/acssuschemeng.5b00438

- L. Chen, S. Wang, S. Wang, C. Chen, L. Qi et al., Scalable production of biodegradable, recyclable, sustainable cellulose–mineral foams via coordination interaction assisted ambient drying. ACS Nano 16(10), 16414–16425 (2022). https://doi.org/10.1021/acsnano.2c05635

- M. Cao, B.-W. Liu, L. Zhang, Z.-C. Peng, Y.-Y. Zhang et al., Fully biomass-based aerogels with ultrahigh mechanical modulus, enhanced flame retardancy, and great thermal insulation applications. Compos. Part B Eng. 225, 109309 (2021). https://doi.org/10.1016/j.compositesb.2021.109309

- H. Wang, J. Kim, Development of lightweight, high-strength, and highly porous ligno-nanocellulosic foam with excellent antioxidant and insulation properties. Carbohydr. Polym. 326, 121616 (2024). https://doi.org/10.1016/j.carbpol.2023.121616

- Q. Fan, R. Ou, X. Hao, Q. Deng, Z. Liu et al., Water-induced self-assembly and in situ mineralization within plant phenolic glycol-gel toward ultrastrong and multifunctional thermal insulating aerogels. ACS Nano 16(6), 9062–9076 (2022). https://doi.org/10.1021/acsnano.2c00755

- B. Zhang, W. Tao, Z. Ren, S. Yue, J. Gou, Biodegradable wastepaper-based foam with ultrahigh energy-absorbing, excellent thermal insulation, and outstanding cushioning properties. ACS Sustainable Chem. Eng. 11(49), 17543–17551 (2023). https://doi.org/10.1021/acssuschemeng.3c06230

- H. Dong, S. Wei, W. Chen, B. Lu, Z. Cai et al., Bioinspired lignocellulose foam: exceptional toughness and thermal insulation. ACS Nano 19(12), 11712–11727 (2025). https://doi.org/10.1021/acsnano.4c11945

- Q. Cen, S. Chen, D. Yang, D. Zheng, X. Qiu, Full bio-based aerogel incorporating lignin for excellent flame retardancy, mechanical resistance, and thermal insulation. ACS Sustainable Chem. Eng. 11(11), 4473–4484 (2023). https://doi.org/10.1021/acssuschemeng.2c07652

- M. Wu, G. Yu, W. Chen, S. Dong, Y. Wang et al., A pulp foam with highly improved physical strength, fire-resistance and antibiosis by incorporation of chitosan and CPAM. Carbohydr. Polym. 278, 118963 (2022). https://doi.org/10.1016/j.carbpol.2021.118963

- X. Shi, R. Bi, Z. Wan, F. Jiang, O.J. Rojas, Solid wood modification toward anisotropic elastic and insulative foam-like materials. ACS Nano 18(11), 7959–7971 (2024). https://doi.org/10.1021/acsnano.3c10650

- J. Song, C. Chen, Z. Yang, Y. Kuang, T. Li et al., Highly compressible, anisotropic aerogel with aligned cellulose nanofibers. ACS Nano 12(1), 140–147 (2018). https://doi.org/10.1021/acsnano.7b04246

- T. Li, J. Song, X. Zhao, Z. Yang, G. Pastel et al., Anisotropic, lightweight, strong, and super thermally insulating nanowood with naturally aligned nanocellulose. Sci. Adv. 4(3), eaar3724 (2018). https://doi.org/10.1126/sciadv.aar3724

- J. Garemark, J.E. Perea-Buceta, D. Rico del Cerro, S. Hall, B. Berke et al., Nanostructurally controllable strong wood aerogel toward efficient thermal insulation. ACS Appl. Mater. Interfaces 14(21), 24697–24707 (2022). https://doi.org/10.1021/acsami.2c04584

- X. Zhao, Y. Liu, L. Zhao, A. Yazdkhasti, Y. Mao et al., A scalable high-porosity wood for sound absorption and thermal insulation. Nat. Sustain. 6(3), 306–315 (2023). https://doi.org/10.1038/s41893-022-01035-y

- Z. Liu, T. Liu, H. Dong, B. Yang, X. Li et al., Diatom-inspired nanoscale heterogeneous assembly strategy for constructing thermal insulating wood-based aerogels with exceptional strength, resilience, degradability, and flame retardancy. ACS Nano 19(7), 6826–6839 (2025). https://doi.org/10.1021/acsnano.4c11549