Supporting Information for

Modulation of Trichromatic Emission Centers in Organic–Inorganic Hybrids for Optoelectronic Applications

Weidong Cai1, Chongyuan Li1, Qiang Guo1, Fuxiang Ji2, Muyi Zhang3, Yiqiang Zhan1*

1College of Future Information Technology, Fudan University, Shanghai 200438, P. R. China

2Institute of Computational Physics, Zurich University of Applied Sciences, Technikumstrasse 71, Winterthur 8400, Switzerland

3Department of Physics, Chemistry, and Biology (IFM), Linköping University, Linköping SE-58183, Sweden

*Corresponding author. E-mail: yqzhan@fudan.edu.cn (Yiqiang Zhan)

Supplementary Figures and Tables

Fig. S1 Experimental and simulated XRD patterns with inserted optical photo of (NEA)2MnBr4 crystal

Fig. S2 PL decay curves of the (NEA)2MnBr4 at the emission wavelengths of 425 nm and 660 nm

Fig. S3 PL spectra of precursor NEABr under excitation wavelength of 340 nm

Fig. S4 Photoluminescence excitation (PLE) pattern of precursor NEABr film at emission peak 435 nm and (NEA)2MnBr4 film at emission peak 425 nm and 660 nm

Fig. S5 CIE coordinates of (NEA)2MnBr4 film under different temperatures

Fig. S6 Solubility bar graph of precursors NEABr and MnBr2

Fig. S7 The spin-coated film of precursors (a) MnBr2 and (b) NEABr (c) MnBr2 particles on the tin foil inside the spin coater

Fig. S8 Energy dispersive X-ray spectroscopy (EDS) results of (a) pristine crystal (NEA)2MnBr4, (b) spin-coated films in region II and (c) spin-coated films in region I

Fig. S9 PL spectra of pristine film, spin coating film and chiral spin coating film

Fig. S10 PL spectrum of (NEA)2MnBr4 film under different temperatures

Fig. S11 Corresponding CIE coordinates of spin coating film and drop casting film under different temperatures

Fig. S12 The (NEA)2MnBr4 film is obtained by (a) the drop casting method and (b) the spin coating method

Fig. S13 Statistical histogram of film component ratio (EDS) and roughness (AFM) in the center and edge areas of the spin-coated film

Fig. S14 The PLQY of (NEA)2MnBr4 film

Fig. S15 XRD and PL Stability measurements of (NEA)2MnBr4 after sample with encapsulation is placed in air after two years

Fig. S16 (a) Templates for spray-painting the university logo. (b) We collect powder after spin coating on substrate, then cover them inside the protective glass of LED chips to light up the LED

Fig. S17 (a) Emission spectrum of white LED. (b) J–V curve of the fabricated photoluminescent excitation device, the inserted image is the CCT (Correlated Color Temperature) coordinates. (c) R1–R8 values of the device’s white-light emission with CRI90 (Color Rendering Index) in the wavelength range of 380–780 nm

Fig. S18 Radioluminescence (RL) spectrum of (NEA)2MnBr4 film

Fig. S19 X-ray image of the standard X-ray resolution pattern plate with scintillator and its bright-field image

Fig. S20 The LFP grayscale distribution map was obtained along the direction indicated by the yellow straight line of the stained LFP

Fig. S21 (a) Humidity-dependent PL spectra. (b) The linear relationship between the P value (P=Pr/Pg) and the humidity level

Table S1 Crystallographic data of (NEA)2MnBr4

| Empirical formula | C24H28Br4MnN2 |
| --- | --- |
| Formula weight | 719.06 |
| Temperature/K | 150.0 |
| Crystal system | triclinic |
| Space group | P1 |
| a/Å | 7.5935(3) |
| b/Å | 11.6164(4) |
| c/Å | 15.4735(6) |
| α/° | 90.849(2) |
| β/° | 90.779(2) |
| γ/° | 96.480(2) |
| Volume/Å3 | 1355.87(9) |
| Z | 2 |
| ρcalc g/cm3 | 1.761 |
| μ/mm-1 | 6.395 |
| F(000) | 702.0 |
| Data collection range/° | 4.368 to 52.862 |
| Index ranges | -9 ≤ h ≤ 9, -14 ≤ k ≤ 14, -19 ≤ l ≤ 19 |
| Goodness-of-fit on F2 | 0.941 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0329, wR2 = 0.0666 |
| Final R indexes [all data] | R1 = 0.0443, wR2 = 0.0714 |
| CCDC no. | 2300440 |