Supporting Information for

Construction of Modifiable Phthalocyanine-Based Covalent Organic Frameworks with Irreversible Linking for Efficient Photocatalytic CO2 Reduction

Xuefei Zhou1#, Shaowei Yang1#, Zhengyang Hu1, Zhanwei Chen1, Ying Guo1, Tianshuai Wang1*, Qiuyu Zhang1*, Hepeng Zhang1*

1 Xi’an Key Laboratory of Functional Organic Porous Materials, School of Chemistry and Chemical Engineering, Northwestern Polytechnical University, 710129 Xi’an, P. R. China

#Xuefei Zhou and Shaowei Yang contributed equally to this work.

*Corresponding authors. E-mail: tianshuai@nwpu.edu.cn (Tianshuai Wang); qyzhang@nwpu.edu.cn (Qiuyu Zhang); zhanghepeng@nwpu.edu.cn (Hepeng Zhang)

S1 Experimental Section

S1.1 Chemicals

4-nitrophthalonitrile (98%) was purchased from Shanghai Maclin Biochemical Technology Co., Ltd. 4-hydroxyphthalonitrile (≥97%), hydroquinone (AR) and 4,4-dihydroxydiphenyl (99%), Cobalt(II) acetate tetrahydrate (≥99.9%) and tris(2,2′-bipyridyl)dichlororuthenium(II) (98%) were purchased from Shanghai Aladdin Biochemical Technology Co., Ltd. 1,8-diazabicyclo[5.4.0]undec-7-ene (DBU) (99%) and n-pentanol (GC, >99%) were purchased from Shanghai Yien Chemical Technology Co., Ltd. N, N-Dimethylformamide (DMF) (AR), Acetonitrile (MeCN) (AR), Triethanolamine (TEOA) (AR), ethanol (AR) and Sodium sulfate anhydrous (AR) were purchased from Guangdong Guanghua Sci-Tech Co., Ltd. Potassium carbonate anhydrous (AR) was purchased from Tianjin Kemiou Chemical Reagent Co., Ltd. The above reagents were of analytical grade and used directly without any further purification before the experiment. Nafion solution (5 wt%) was purchased from Sigma-Aldrich LLC.

S1.2 Characterization

The 1H NMR measurement was performed using Bruker Advance 500MHz Bruke. IR spectra were confirmed through Nicolet™ iS50 FTIR Spectrometer. Powder X-ray diffraction (PXRD) patterns of catalysts were recorded on a Brooke GmbH X-ray diffractometer (Germany). The 2θ angle ranged from 1° to 50° with a scan step of 5°/min. Field emission scanning electron microscopy (FE-SEM, FEI Verious G4) and transmission electron microscopy (TEM, FEI Talos F200X TEM, operating voltage 200 kV) were used to study the morphology and structure of the samples. N2 and CO2 adsorption-desorption was measured with the 3H-2000PS2 type PS2-0790 Surface Area Porosity Analyzer. The element composition of the samples was analyzed by X-ray photoelectron spectroscopy (XPS, Axis Ultra DLD by Kratos Company in the United Kingdom.

S1.3 Photocurrents and Mott-Schottky (MS) curve measurements

5 mg of catalysts were meticulously distributed within a solution comprising Nafion (100 µL) and ethanol (900 µL), followed by ultrasonic treatment. Apply 200 µL of the solution dropwise on the surface of the FTO conductive glass and air dry. The FTO glass, coated with the catalyst, acted as a photoelectrode. A conventional system of a three-electrode cell in a solution of pH = 7 was used.

S1.4 Photocatalytic CO2RR Cyclic experiments

Following 1 hour of illumination, the catalyst is isolated from the reaction solution via filtration. Wash with ethanol and deionized water several times during the filtration process. Subsequently, vacuum drying at 60 °C yields the regenerated solid sample. Upon adding equivalent volumes of fresh acetonitrile, H2O, and [Ru(bpy)3]Cl2·6H2O, CO2 is reintroduced into the photocatalytic system for the next photocatalytic cycle.

S1.5 Determination of quenching rate (kq)

A reported method [S1] was followed to calculate the kq in the steady-state measurements, where the fluorescence intensity of photo-excited Ru-PS in the presence of a quencher was measured and fitted to the Stern-Volmer equation.

IOI=1+KQ=1+kqτ0[Q]                             (S1)

In this equation, I0 and I are the fluorescence intensity values in the absence and presence of the quencher, K is the Stern-Volmer constant for dynamic quenching, kq is the apparent rate of bimolecular quenching, τ0 is the lifetime of the excited state without quencher, and [Q] is the concentration of the quencher.

S1.6 Apparent quantum efficiency

The apparent quantum efficiency (AQE) measurements for CoBOP under monochromatic irradiation. Specifically, AQE was determined at 365, 420, 500, 600, 700, and 800 nm using the following equation:

AQE %=2×nco×NA×h×cS×P×T×λ×100%

Where nco is the molar amount of CO, NA is Avogadro’s constant (6.022 × 1023 mol-1), h is Planck’s constant (6.63 × 10-34 m2 kg s-1), c is the speed of light (3 × 108 m·s-1), S is the irradiation area (cm2), P is the irradiation intensity (W cm-2), T is the irradiation time (s), and λ is the wavelength of the incident light.

S1.7 Computation methods

All quantum chemical calculations were performed with the Gaussian 16 program using the level of B3LYP/6-311+G(d,p) [S2].

S2 Supplementary Figures and Tables

Fig. S1 1H NMR spectra of OP. (500 MHz, DMSO-d6) δ 8.23 (d, J = 8.7 Hz, 2H), 8.05 (d, J = 2.6 Hz, 2H), 7.71 (dd, J = 8.7, 2.5 Hz, 2H)

Fig. S2 1H NMR spectra of POP. (500 MHz, DMSO-d6) δ 8.14 (d, J = 8.8 Hz, 2H), 7.87 (d, J = 2.6 Hz, 2H), 7.52 (dd, J = 8.8, 2.7 Hz, 2H), 7.34 (s, 4H)

Fig. S3 HR-MS spectrum of OP

Fig. S4 HR-MS spectrum of POP

Fig. S5 FT-IR spectra of 4-Nitrophthalonitrile and OP

Fig. S6 FT-IR spectra of hydroquinone and POP

Fig. S7 FT-IR spectra of BOP and CoBOP

Fig. S8 FT-IR spectra of OP and CoOP

Fig. S9 FT-IR spectra of POP and CoPOP

Fig. S10 AB Stacking simulated PXRD crystal structure based on theoretical structural simulation using the Materials Studio package of CoOP a, CoPOP b, and CoBOP c

Fig. S11 XPS spectra of CoBOP

Fig. S12 a C 1s XPS spectra of CoBOP. b O 1s XPS spectra of CoBOP

Fig. S13 XPS spectra of CoOP

Fig. S14 a C 1s XPS spectra of CoOP. b N 1s XPS spectra of CoOP. c O 1s XPS spectra of CoOP. d Co 2p XPS spectra of CoOP

Fig. S15 XPS spectra of CoPOP

Fig. S16 a C 1s XPS spectra of CoPOP. b N 1s XPS spectra of CoPOP. c O 1s XPS spectra of CoPOP. d Co 2p XPS spectra of CoPOP

Fig. S17 a SEM images of CoOP with 2 μm. b SEM images of CoOP with 1 μm. c, d SEM images of CoOP with 500 nm

Fig. S18 a SEM images of CoPOP with 2 μm. b SEM images of CoPOP with 1 μm. c, d SEM images of CoPOP with 500 nm

Fig. S19 a SEM images of CoBOP with 2 μm. b SEM images of CoBOP with 1 μm. c, d SEM images of CoBOP with 500 nm

Fig. S20 a TEM images of CoOP. b EDS mapping pictures of CoOP

Fig. S21 a TEM images of CoPOP. b EDS mapping pictures of CoPOP

Fig. S22 Nitrogen adsorption and desorption isotherms of CoOP a, CoPOP b, CoBOP c. The pore size distribution of CoOP d, CoPOP e, and CoBOP f by BJH (desorption)

Fig. S23 CO2 sorption isotherms in CoOP

Fig. S24 CO2 sorption isotherms in CoPOP

Fig. S25 CO2 sorption isotherms in CoPOP

Fig. S26 Qst curve of CO2 of CoOP

Fig. S27 Qst curve of CO2 of CoPOP

Fig. S28 Qst curve of CO2 of CoBOP

Fig. S29 TGA spectra of CoOP, CoPOP, and CoBOP

Fig. S30 XRD spectra of CoOP after immersion in various solutions

Fig. S31 XRD spectra of CoPOP after immersion in various solutions

Fig. S32 XRD spectra of CoBOP after immersion in various solutions

Fig. S33 Mott-Schottky curves of CoOP at different frequencies

Fig. S34 Mott-Schottky curves of CoPOP at different frequencies

Fig. S35 Mott-Schottky curves of CoBOP at different frequencies

Fig. S36 a Valence band XPS spectra of the CoOP, CoPOP, and CoBOP. b Band-structure (vs. vacuum) diagram based on UV-vis spectra and XPS-VB for CoOP, CoPOP, and CoBOP

Fig. S37 LUMO of CoOP、CoPOP and CoBOP

Fig. S38 1H NMR spectra of the liquid products resulting from the pCO2RR mediated by CoOP, CoPOP, and CoBOP

Fig. S39 Time-dependent photocatalytic activity of CoBOP

Fig. S40 AQE of production catalyzed by CoBOP as a function of the related spectra

Fig. S41 XRD and FT-IR spectra before and after photocatalytic reaction of CoBOP

Fig. S42. Photocatalytic performance with different CoBOP dosages

Fig. S43 Transient photocurrent response of CoOP, CoPOP, and CoBOP at 0.2 M Na2SO4 electrolyte

Fig. S44 EIS plots of the CoOP, CoPOP, and CoBOP at 0.2 M Na2SO4 electrolyte

Fig. S45 a Steady-state PL spectra of CoOP, CoPOP, and CoBOP. b Time-resolved PL decay spectra of CoOP, CoPOP, and CoBOP

Fig. S46 a Steady-state PL spectra of a CH3CN solution containing 0.05 mM Ru-PS in the presence of 0~0.10 mM CoBOP, respectively. b Linear fitting of the ratio of PL intensity versus CoBOP

Fig. S47 a Steady-state PL spectra of a CH3CN solution containing 0.05 mM Ru-PS in the presence of 0~0.10 mM CoPOP, respectively. b Linear fitting of the ratio of PL intensity versus CoPOP

Fig. S48 a Steady-state PL spectra of a CH3CN solution containing 0.05 mM Ru-PS in the presence of 0~0.10 mM CoOP, respectively. b Linear fitting of the ratio of PL intensity versus CoOP

Table S1 The performance comparison of COF photocatalysts using photosensitizer and sacrificial agent for photocatalytic CO2-to-CO conversion

| Photocatalyst | Photosensitizers | Sacrificial Agent | solution components | CO Yield mmol g-1 h-1 | H2 Yield mmol g-1 h-1 | CO Yield μmol h-1 | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- |
| CoBOP 0.2 mg | [Ru(bpy)3]Cl2 1 mg/mL | TEOA | MeCN/H2O 20 mL | 426 | 288 | 85.2 | This work |
| CoBOP 0.5 mg | [Ru(bpy)3]Cl2 1 mg/mL | TEOA | MeCN/H2O 20 mL | 147.2 | 94.4 | 73.6 | This work |
| CoBOP 1 mg | [Ru(bpy)3]Cl2 1 mg/mL | TEOA | MeCN/H2O 20 mL | 83.7 | 54.7 | 83.7 | This work |
| CoPOP 1 mg | [Ru(bpy)3]Cl2 1 mg/mL | TEOA | MeCN/H2O 20 mL | 68.8 | 46.2 | 68.8 | This work |
| CoOP 1 mg | [Ru(bpy)3]Cl2 1 mg/mL | TEOA | MeCN/H2O 20 mL | 53.6 | 32.6 | 53.6 | This work |
| TPy-COF-Co 1 mg | [Ru(bpy)3]Cl2 1.25 mg/mL | TEOA | MeCN/H2O 6 mL | 26.9 | 14.7 | 26.9 | [S3] |
| Co/Cu3-TPA-COF 1 mg | [Ru(bpy)3]Cl2 1 mg/mL | TEOA | MeCN/H2O 5 mL | 25.2 | 6.23 | 25.2 | [S4] |
| USTB-11(Cu,Ni) 2 mg | [Ru(bpy)3]Cl2 6 mg/mL | TEOA | MeCN/H2O 5 mL | 22.13 | 0.45 | 44.26 | [S5] |
| Co-2,3-DHTA-COF 1 mg | [SRu(bpy)3]Cl2 0.22 mg/mL | TEOA | MeCN/H2O 46 mL | 18.00 | 0.81 | 18 | [S6] |
| EPCo-COF-AT 2 mg | [SRu(bpy)3]Cl2 0.5 mg/mL | TEOA | MeCN/H2O 20 mL | 17.70 | 0.40 | 35.4 | [S7] |
| JUC-640-Co 3 mg | [Ru(bpy)3]Cl2 0.25 mg/mL | BIH | MeCN/H2O 20 mL | 15.14 | 0.90 | 45.42 | [S8] |
| TT-Por(Co)-COF 5 mg | [SRu(bpy)3]Cl2 6 mg/mL | TEOA | MeCN/H2O 5 mL | 10.50 | 8.94 | 52.5 | [S9] |
| CoPor-DPP-COF 2 mg | [SRu(bpy)3]Cl2 0.625 mg/mL | TIPA | MeCN/H2O 16 mL | 10.20 | 2.24 | 20.4 | [S10] |
| COF-367-Co NSs 5 mg | [SRu(bpy)3]Cl2 0.95 mg/mL | AA | 0.1 M KHCO3 20 mL | 10.16 | 3.00 | 50.8 | [S11] |
| Co-PyPor-COF 2 mg | [SRu(bpy)3]Cl2 1.25 mg/mL | TEOA | MeCN/H2O 8 mL | 9.60 | 0.33 | 19.2 | [S12] |
| CdS/TpBpy-20% 2 mg | Co(bpy)32+ | TEOA | MeCN/H2O 15 mL | 8.80 | 1.71 | 17.6 | [S13] |
| Co-TAPB-COF-1 10 mg | [SRu(bpy)3]Cl2 0.6 mg/mL | TEOA | MeCN/H2O 100 mL | 8.39 | 11.31 | 83.9 | [S14] |
| Ni-COF 2 mg | [SRu(bpy)3]Cl2 1.25 mg/mL | TEOA | MeCN/H2O 6 mL | 5.31 | 0.29 | 10.62 | [S15] |
| Ni-TP-CON 5 mg | [SRu(bpy)3]Cl2 2 mg/mL | TEOA | MeCN/H2O 10 mL | 4.98 | 0.13 | 24.9 | [S16] |
| NiPc-CoPOP 2 mg | [SRu(bpy)3]Cl2 1 mg/mL | TEOA | MeCN/H2O 10 mL | 4.27 | 3.64 | 8.54 | [S17] |
| Ni@TPHH-COF 5 mg | [SRu(bpy)3]Cl2 1.17 mg/mL | TEOA | MeCN/H2O 6 mL | 3.28 | 0.17 | 16.4 | [S18] |
| HOF-25-Re 2 mg | [SRu(bpy)3]Cl2 | TIPA | MeCN | 3.03 | 0.26 | 6.06 | [S19] |
| CoNi-COF-3 1 mg | [SRu(bpy)3]Cl2 0.86 mg/mL | TEOA | MeCN/H2O 5 mL | 2.57 | 0.25 | 2.57 | [S20] |
| CoP-TPE-COF 15 mg | [SRu(bpy)3]Cl2 5 mg/mL | TEOA | MeCN/H2O 6 mL | 2.41 | 1.54 | 36.15 | [S21] |
| H-COF-Ni 2 mg | [SRu(bpy)3]Cl2 5 mg/mL | TEOA | MeCN/H2O 6 mL | 2.31 | 0.10 | 4.62 | [S22] |
| TFBD-COF-Co-SA 10 mg | [SRu(bpy)3]Cl2 0.6 mg/mL | TEOA | MeCN 50 mL | 1.48 | 0.16 | 14.8 | [S23] |
| Co@COF-TVBT-Bpy 2 mg | [SRu(bpy)3]Cl2 0.3 mg/mL | TEOA | MeCN/H2O 11.6 mL | 1.13 | 1.13 | 2.26 | [S24] |
| CH3-TPPD 5 mg | [SRu(bpy)3]Cl2 1.2 mg/mL | TEOA | MeCN/H2O 6 mL | 1.03 | 0.27 | 5.15 | [S25] |
| DQTP COF-Co 20 mg | [SRu(bpy)3]Cl2 0.45 mg/mL | TEOA | MeCN 50 mL | 1.02 | 0.11 | 20.4 | [S26] |
| CTF-Bpy-Co 10 mg | [SRu(bpy)3]Cl2 0.325 mg/mL | TEOA | MeCN/H2O 20 mL | 1.02 | 0.20 | 10.2 | [S27] |
| Fe-SAS/TrCOF 5 mg | [SRu(bpy)3]Cl2 2 mg/mL | TEOA | MeCN/H2O 5 mL | 0.98 | 0.04 | 4.9 | [S28] |
| Ni-TpBpy 10 mg | [SRu(bpy)3]Cl2 1.3 mg/mL | TEOA | MeCN/H2O 5 mL | 0.81 | 0.03 | 8.1 | [S29] |
| Ni-PCD@TD-COF 5 mg | [SRu(bpy)3]Cl2 2 mg/mL | TEOA | MeCN/H2O 10 mL | 0.48 | 0.01 | 2.4 | [S30] |
| α-Fe2O3@Por-CTF 20 mg | [SRu(bpy)3]Cl2 1 mg/mL | TEOA | MeCN/H2O 5 mL | 0.4 | 0.03 | 8 | [S31] |

Table S2 Atomic coordinates for geometrically optimized CoOP using FORCITE calculation

| CoOP | Space group: P1 a=15.6 Å, b=15.4, Å c=3.5Å α=94.8°, β=94.0°, γ= 89.3° |  |  |  |
| --- | --- | --- | --- | --- |
| C1 | C | 1.23296 | -1.46239 | -0.60229 |
| C2 | C | 1.23226 | -1.54885 | -0.54671 |
| C3 | C | 1.32226 | -1.57577 | -0.51446 |
| N4 | N | 1.37489 | -1.50705 | -0.53806 |
| C5 | C | 1.32249 | -1.43747 | -0.59044 |
| C6 | C | 1.54195 | -1.2431 | -0.37551 |
| C7 | C | 1.45585 | -1.24216 | -0.47684 |
| C8 | C | 1.43058 | -1.32818 | -0.51958 |
| N9 | N | 1.49867 | -1.38201 | -0.45874 |
| C10 | C | 1.56663 | -1.32859 | -0.37082 |
| N11 | N | 1.34845 | -1.3543 | -0.58362 |
| C12 | C | 1.76732 | -1.54896 | -0.47702 |
| C13 | C | 1.76554 | -1.4623 | -0.36555 |
| C14 | C | 1.67576 | -1.43767 | -0.3613 |
| N15 | N | 1.62417 | -1.50733 | -0.45785 |
| C16 | C | 1.67759 | -1.57626 | -0.52508 |
| N17 | N | 1.64891 | -1.35458 | -0.32235 |
| C18 | C | 1.45624 | -1.77239 | -0.54813 |
| C19 | C | 1.5424 | -1.77242 | -0.59707 |
| C20 | C | 1.56761 | -1.68711 | -0.5847 |
| N21 | N | 1.49915 | -1.63324 | -0.53803 |
| C22 | C | 1.43087 | -1.68621 | -0.51975 |
| N23 | N | 1.34851 | -1.6592 | -0.5044 |
| C24 | N | 1.65198 | -1.66149 | -0.58614 |
| C25 | C | 1.84459 | -1.59355 | -0.53217 |
| C26 | C | 1.92207 | -1.54637 | -0.46891 |
| C27 | C | 1.91844 | -1.45672 | -0.3398 |
| C28 | C | 1.83991 | -1.41345 | -0.29125 |
| C29 | C | 1.58978 | -1.16755 | -0.30572 |
| C30 | C | 1.54621 | -1.08879 | -0.34941 |
| C31 | C | 1.45728 | -1.08574 | -0.46916 |
| C32 | C | 1.41085 | -1.16448 | -0.52614 |
| C33 | C | 1.41113 | -1.84951 | -0.52767 |
| C34 | C | 1.45739 | -1.92888 | -0.55796 |
| C35 | C | 1.54625 | -1.92702 | -0.6242 |
| C36 | C | 1.58993 | -1.84883 | -0.63992 |
| C37 | C | 1.15787 | -1.41395 | -0.64622 |
| C38 | C | 1.07995 | -1.45723 | -0.62654 |
| C39 | C | 1.07755 | -1.54648 | -0.55537 |
| C40 | C | 1.15567 | -1.59339 | -0.52146 |
| O41 | O | 1.4125 | -1.00702 | -0.52764 |
| O42 | O | 1.00011 | -1.59164 | -0.52719 |
| Co43 | Co | 1.49926 | -1.50751 | -0.4982 |
| H44 | H | 1.70161 | -1.71513 | -0.64155 |
| H45 | H | 1.84393 | -1.66611 | -0.62579 |
| H46 | H | 1.98043 | -1.41821 | -0.27297 |
| H47 | H | 1.83902 | -1.34108 | -0.19443 |
| H48 | H | 1.66141 | -1.17137 | -0.21697 |
| H49 | H | 1.58208 | -1.0246 | -0.28843 |
| H50 | H | 1.33885 | -1.16338 | -0.60976 |
| H51 | H | 1.33914 | -1.84716 | -0.48764 |
| H52 | H | 1.58399 | -1.99046 | -0.66635 |
| H53 | H | 1.66164 | -1.84971 | -0.68631 |
| H54 | H | 1.16128 | -1.34203 | -0.69595 |
| H55 | H | 1.01634 | -1.4208 | -0.66805 |
| H56 | H | 1.15502 | -1.66562 | -0.47482 |

Table S3 Atomic coordinates for geometrically optimized CoPOP using FORCITE calculation

| CoPOP | Space group: P1 a=19.9 Å, b=20.4, Å c=4.3Å α=66.8°, β=72.0°, γ= 90.0° |  |  |  |
| --- | --- | --- | --- | --- |
| C1 | C | 0.45699 | -0.70028 | -0.5 |
| C2 | C | 0.52173 | -0.70778 | -0.5 |
| C3 | C | 0.54101 | -0.6454 | -0.5 |
| N4 | N | 0.4903 | -0.60115 | -0.5 |
| C5 | C | 0.4388 | -0.63309 | -0.5 |
| C6 | C | 0.29872 | -0.4562 | -0.5 |
| C7 | C | 0.29772 | -0.5197 | -0.5 |
| C8 | C | 0.36011 | -0.54544 | -0.5 |
| N9 | N | 0.39996 | -0.50067 | -0.5 |
| C10 | C | 0.36146 | -0.44605 | -0.5 |
| N11 | N | 0.37839 | -0.60696 | -0.5 |
| C12 | C | 0.52549 | -0.32321 | -0.5 |
| C13 | C | 0.46074 | -0.31572 | -0.5 |
| C14 | C | 0.44146 | -0.3781 | -0.5 |
| N15 | N | 0.49218 | -0.42234 | -0.5 |
| C16 | C | 0.54368 | -0.39039 | -0.5 |
| N17 | N | 0.38088 | -0.38911 | -0.5 |
| C18 | C | 0.68374 | -0.5673 | -0.5 |
| C19 | C | 0.68475 | -0.50379 | -0.5 |
| C20 | C | 0.62237 | -0.47804 | -0.5 |
| N21 | N | 0.58252 | -0.52282 | -0.5 |
| C22 | C | 0.62101 | -0.57745 | -0.5 |
| N23 | N | 0.60158 | -0.6344 | -0.5 |
| N24 | N | 0.60409 | -0.41652 | -0.5 |
| C25 | C | 0.55995 | -0.27354 | -0.5 |
| C26 | C | 0.52533 | -0.21452 | -0.5 |
| C27 | C | 0.45826 | -0.20555 | -0.5 |
| C28 | C | 0.42521 | -0.25778 | -0.5 |
| C29 | C | 0.24374 | -0.41431 | -0.5 |
| C30 | C | 0.18598 | -0.44023 | -0.5 |
| C31 | C | 0.18411 | -0.50722 | -0.5 |
| C32 | C | 0.24149 | -0.54682 | -0.5 |
| C33 | C | 0.7387 | -0.60921 | -0.5 |
| C34 | C | 0.79646 | -0.5833 | -0.5 |
| C35 | C | 0.79834 | -0.51629 | -0.5 |
| C36 | C | 0.74098 | -0.47668 | -0.5 |
| C37 | C | 0.42253 | -0.74995 | -0.5 |
| C38 | C | 0.45715 | -0.80898 | -0.5 |
| C39 | C | 0.52421 | -0.81796 | -0.5 |
| C40 | C | 0.55725 | -0.76573 | -0.5 |
| O41 | O | 0.42001 | -0.14974 | -0.5 |
| C42 | C | 0.45795 | -0.08219 | -0.5 |
| O43 | O | 0.12939 | -0.53301 | -0.5 |
| O44 | O | 0.85307 | -0.4905 | -0.5 |
| C45 | C | 0.92125 | -0.50229 | -0.5 |
| O46 | O | 0.56245 | -0.87376 | -0.5 |
| Co47 | Co | 0.49123 | -0.51175 | -0.5 |
| C48 | C | 0.52203 | 0.94651 | 0.5 |
| C49 | C | 0.55533 | 1.01602 | 0.5 |
| C50 | C | 0.52451 | 1.05869 | 0.5 |
| C51 | C | 0.46044 | 1.02999 | 0.5 |
| C52 | C | 0.42714 | 0.96047 | 0.5 |
| C53 | C | 0.95928 | 1.54312 | 0.5 |
| C54 | C | 1.02908 | 1.53348 | 0.5 |
| C55 | C | 1.06119 | 1.47878 | 0.5 |
| C56 | C | 1.02317 | 1.43336 | 0.5 |
| C57 | C | 0.95337 | 1.443 | 0.5 |
| H58 | H | 0.6106 | -0.28137 | -0.5 |
| H59 | H | 0.54945 | -0.17717 | -0.5 |
| H60 | H | 0.37344 | -0.25285 | -0.5 |
| H61 | H | 0.24562 | -0.36354 | -0.5 |
| H62 | H | 0.1436 | -0.40783 | -0.5 |
| H63 | H | 0.24173 | -0.59669 | -0.5 |
| H64 | H | 0.73681 | -0.65999 | -0.5 |
| H65 | H | 0.83883 | -0.6157 | -0.5 |
| H66 | H | 0.74074 | -0.4268 | -0.5 |
| H67 | H | 0.37189 | -0.74211 | -0.5 |
| H68 | H | 0.43304 | -0.84632 | -0.5 |
| H69 | H | 0.60902 | -0.77066 | -0.5 |
| H70 | H | 0.5452 | 0.91608 | 0.5 |
| H71 | H | 0.60464 | 1.03803 | 0.5 |
| H72 | H | 0.43726 | 1.06042 | 0.5 |
| H73 | H | 0.37782 | 0.93847 | 0.5 |
| H74 | H | 0.93409 | 1.58525 | 0.5 |
| H75 | H | 1.05816 | 1.56793 | 0.5 |
| H76 | H | 1.04835 | 1.39122 | 0.5 |
| H77 | H | 0.92429 | 1.40855 | 0.5 |

Table S4 Atomic coordinates for geometrically optimized CoPOP using FORCITE calculation

| CoBOP | Space group: P1 a=24.7 Å, b=24.0 Å, c=4.0 Å α=72.1°, β=95.6°, γ= 93.6° |  |  |  |
| --- | --- | --- | --- | --- |
| C1 | C | 0.33296 | -0.48337 | -0.5 |
| C2 | C | 0.3297 | -0.53511 | -0.5 |
| C3 | C | 0.38502 | -0.54695 | -0.5 |
| N4 | N | 0.42079 | -0.50469 | -0.5 |
| C5 | C | 0.39024 | -0.46554 | -0.5 |
| C6 | C | 0.53654 | -0.34702 | -0.5 |
| C7 | C | 0.48181 | -0.35047 | -0.5 |
| C8 | C | 0.4628 | -0.40116 | -0.5 |
| N9 | N | 0.50405 | -0.42989 | -0.5 |
| C10 | C | 0.54922 | -0.39606 | -0.5 |
| N11 | N | 0.40987 | -0.41776 | -0.5 |
| C12 | C | 0.66581 | -0.5208 | -0.5 |
| C13 | C | 0.66889 | -0.46886 | -0.5 |
| C14 | C | 0.61342 | -0.4562 | -0.5 |
| N15 | N | 0.57777 | -0.49899 | -0.5 |
| C16 | C | 0.60852 | -0.53886 | -0.5 |
| N17 | N | 0.60002 | -0.40823 | -0.5 |
| C18 | C | 0.46192 | -0.65497 | -0.5 |
| C19 | C | 0.51729 | -0.65482 | -0.5 |
| C20 | C | 0.53619 | -0.60463 | -0.5 |
| N21 | N | 0.49451 | -0.57386 | -0.5 |
| C22 | C | 0.44898 | -0.60561 | -0.5 |
| N23 | N | 0.39811 | -0.59341 | -0.5 |
| N24 | N | 0.58915 | -0.5882 | -0.5 |
| C25 | C | 0.7113 | -0.54453 | -0.5 |
| C26 | C | 0.76155 | -0.51372 | -0.5 |
| C27 | C | 0.76589 | -0.4613 | -0.5 |
| C28 | C | 0.71812 | -0.43797 | -0.5 |
| C29 | C | 0.56888 | -0.29992 | -0.5 |
| C30 | C | 0.54339 | -0.25538 | -0.5 |
| C31 | C | 0.48625 | -0.25896 | -0.5 |
| C32 | C | 0.45519 | -0.30756 | -0.5 |
| C33 | C | 0.42959 | -0.69905 | -0.5 |
| C34 | C | 0.45619 | -0.74447 | -0.5 |
| C35 | C | 0.51395 | -0.74727 | -0.5 |
| C36 | C | 0.54482 | -0.70026 | -0.5 |
| C37 | C | 0.28768 | -0.45961 | -0.5 |
| C38 | C | 0.23771 | -0.49114 | -0.5 |
| C39 | C | 0.23377 | -0.54568 | -0.5 |
| C40 | C | 0.28099 | -0.56786 | -0.5 |
| O41 | O | 0.45958 | -0.2187 | -0.5 |
| O42 | O | 0.81477 | -0.42799 | -0.5 |
| O43 | O | 0.54265 | -0.79158 | -0.5 |
| O44 | O | 0.18618 | -0.58203 | -0.5 |
| C45 | C | 0.47426 | -0.15915 | -0.5 |
| C46 | C | 0.86617 | -0.45243 | -0.5 |
| C47 | C | 0.5295 | -0.85167 | -0.5 |
| C48 | C | 0.13532 | -0.55795 | -0.5 |
| C49 | C | 0.52117 | -0.13452 | -0.5 |
| C50 | C | 0.53343 | -0.07442 | -0.5 |
| C51 | C | 0.49697 | -0.03753 | -0.5 |
| C52 | C | 0.44864 | -0.06169 | -0.5 |
| C53 | C | 0.4376 | -0.12219 | -0.5 |
| C54 | C | 0.87742 | -0.51112 | -0.5 |
| C55 | C | 0.92942 | -0.53235 | -0.5 |
| C56 | C | 0.97281 | -0.49455 | -0.5 |
| C57 | C | 0.96188 | -0.43467 | -0.5 |
| C58 | C | 0.90926 | -0.41436 | -0.5 |
| C59 | C | 0.48524 | -0.87387 | -0.5 |
| C60 | C | 0.4741 | -0.93436 | -0.5 |
| C61 | C | 0.50884 | -0.97383 | -0.5 |
| C62 | C | 0.55502 | -0.95215 | -0.5 |
| C63 | C | 0.56452 | -0.8917 | -0.5 |
| C64 | C | 0.11935 | -0.50512 | -0.5 |
| C65 | C | 0.06694 | -0.48501 | -0.5 |
| C66 | C | 0.02886 | -0.51692 | -0.5 |
| C67 | C | 0.04526 | -0.57048 | -0.5 |
| C68 | C | 0.09739 | -0.59102 | -0.5 |
| Co69 | Co | 0.49927 | -0.50185 | -0.5 |
| H70 | H | 0.70783 | -0.58439 | -0.5 |
| H71 | H | 0.79616 | -0.53024 | -0.5 |
| H72 | H | 0.71959 | -0.39697 | -0.5 |
| H73 | H | 0.61231 | -0.29759 | -0.5 |
| H74 | H | 0.56889 | -0.21957 | -0.5 |
| H75 | H | 0.41183 | -0.31171 | -0.5 |
| H76 | H | 0.3856 | -0.69762 | -0.5 |
| H77 | H | 0.43202 | -0.77708 | -0.5 |
| H78 | H | 0.58891 | -0.69974 | -0.5 |
| H79 | H | 0.29115 | -0.41914 | -0.5 |
| H80 | H | 0.20309 | -0.47379 | -0.5 |
| H81 | H | 0.27974 | -0.60989 | -0.5 |
| H82 | H | 0.54801 | -0.16159 | -0.5 |
| H83 | H | 0.57053 | -0.05648 | -0.5 |
| H84 | H | 0.4199 | -0.0338 | -0.5 |
| H85 | H | 0.40028 | -0.14044 | -0.5 |
| H86 | H | 0.84622 | -0.54105 | -0.5 |
| H87 | H | 0.93472 | -0.57865 | -0.5 |
| H88 | H | 0.99369 | -0.40265 | -0.5 |
| H89 | H | 0.90195 | -0.36833 | -0.5 |
| H90 | H | 0.45948 | -0.84589 | -0.5 |
| H91 | H | 0.43927 | -0.95052 | -0.5 |
| H92 | H | 0.5829 | -0.98191 | -0.5 |
| H93 | H | 0.59945 | -0.87571 | -0.5 |
| H94 | H | 0.14691 | -0.48003 | -0.5 |
| H95 | H | 0.05632 | -0.4453 | -0.5 |
| H96 | H | 0.01885 | -0.59642 | -0.5 |
| H97 | H | 0.1088 | -0.63243 | -0.5 |

Supplementary References

- V.S. Thoi, N. Kornienko, C.G. Margarit, P. Yang, C.J. Chang, Visible-light photoredox catalysis: selective reduction of carbon dioxide to carbon monoxide by a nickel N-heterocyclic carbene–isoquinoline complex. J. Am. Chem. Soc. 135(38), 14413–14424 (2013). https://doi.org/10.1021/ja4074003

- M. J. Frisch and g. W. Trucks and h. B. Schlegel, gaussian 16, revision a.03, gaussian inc. Wallingford ct. (2016).

- P. Fu, C. Chen, C. Wu, B. Meng, Q. Yue et al., Covalent organic framework stabilized single CoN(4)Cl(2) site boosts photocatalytic CO2 reduction into tunable syngas. Angew. Chem. Int. Ed. 64(3), e202415202 (2025). https://doi.org/10.1002/anie.202415202

- X. Lan, H. Li, Y. Liu, Y. Zhang, T. Zhang et al., Covalent organic framework with Donor1-acceptor-Donor2 motifs regulating local charge of intercalated single cobalt sites for photocatalytic CO2 reduction to syngas. Angew. Chem. Int. Ed. 63(31), e202407092 (2024). https://doi.org/10.1002/anie.202407092

- X. Wang, X. Ding, Y. Jin, D. Qi, H. Wang et al., Post-nickelation of a crystalline trinuclear copper organic framework for synergistic photocatalytic carbon dioxide conversion. Angew. Chem. Int. Ed. 62(18), e202302808 (2023). https://doi.org/10.1002/anie.202302808

- Q. Zhang, S. Gao, Y. Guo, H. Wang, J. Wei et al., Designing covalent organic frameworks with Co-O(4) atomic sites for efficient CO2 photoreduction. Nat. Commun. 14(1), 1147 (2023). https://doi.org/10.1038/s41467-023-36779-4

- W. Lin, F. Lin, J. Lin, Z. Xiao, D. Yuan et al., Efficient photocatalytic CO2 reduction in ellagic acid–based covalent organic frameworks. J. Am. Chem. Soc. 146(23), 16229–16236 (2024). https://doi.org/10.1021/jacs.4c04185

- J. Ding, X. Guan, J. Lv, X. Chen, Y. Zhang et al., Three-dimensional covalent organic frameworks with ultra-large pores for highly efficient photocatalysis. J. Am. Chem. Soc. 145(5), 3248–3254 (2023). https://doi.org/10.1021/jacs.2c13817

- S. Zhao, J. Liang, D.-H. Si, M.-J. Mao, Y. Huang et al., Superheterojunction covalent organic frameworks: Supramolecular synergetic charge transfer for highly efficient photocatalytic CO2 reduction. Appl. Catal. B Environ. Energy 333, 122782 (2023). https://doi.org/10.1016/j.apcatb.2023.122782

- X. Wang, X. Ding, T. Wang, K. Wang, Y. Jin et al., Two-dimensional porphyrin-based covalent organic framework with enlarged inter-layer spacing for tunable photocatalytic CO2 reduction. ACS Appl. Mater. Interfaces 14(36), 41122–41130 (2022). https://doi.org/10.1021/acsami.2c12542

- W. Liu, X. Li, C. Wang, H. Pan, W. Liu et al., A scalable general synthetic approach toward ultrathin imine-linked two-dimensional covalent organic framework nanosheets for photocatalytic CO2 reduction. J. Am. Chem. Soc. 141(43), 17431–17440 (2019). https://doi.org/10.1021/jacs.9b09502

- T.-X. Luan, J.-R. Wang, K. Li, H. Li, F. Nan et al., Highly enhancing CO2 photoreduction by metallization of an imidazole-linked robust covalent organic framework. Small 19(44), 2303324 (2023). https://doi.org/10.1002/smll.202303324

- K.H. Do, D.P. Kumar, A.P. Rangappa, J. Lee, S. Yun et al., Design and synthesis of a covalent organic framework bridging CdS nanoparticles and a homogeneous cobalt–bipyridine cocatalyst for a highly efficient photocatalytic CO2 reduction. J. Mater. Chem. A 11(15), 8392–8403 (2023). https://doi.org/10.1039/D3TA00079F

- W. Zhou, X. Wang, W. Zhao, N. Lu, D. Cong et al., Photocatalytic CO2 reduction to syngas using metallosalen covalent organic frameworks. Nat. Commun. 14(1), 6971 (2023). https://doi.org/10.1038/s41467-023-42757-7

- B. Han, X. Ou, Z. Zhong, S. Liang, H. Deng et al., Rational design of FeNi bimetal modified covalent organic frameworks for photoconversion of anthropogenic CO2 into widely tunable syngas. Small 16(38), 2002985 (2020). https://doi.org/10.1002/smll.202002985

- H. Lv, P. Li, X. Li, A. Chen, R. Sa et al., Boosting photocatalytic reduction of the diluted CO2 over covalent organic framework. Chem. Eng. J. 451, 138745 (2023). https://doi.org/10.1016/j.cej.2022.138745

- X.-Y. Dong, Y.-N. Si, Q.-Y. Wang, S. Wang, S.-Q. Zang, Integrating single atoms with different microenvironments into one porous organic polymer for efficient photocatalytic CO2 reduction. Adv. Mater. 33(33), 2101568 (2021). https://doi.org/10.1002/adma.202101568

- M. Dong, J. Zhou, J. Zhong, H.-T. Li, C.-Y. Sun et al., CO2 dominated bifunctional catalytic sites for efficient industrial exhaust conversion. Adv. Funct. Mater. 32(8), 2110136 (2022). https://doi.org/10.1002/adfm.202110136

- B. Yu, L. Li, S. Liu, H. Wang, H. Liu et al., Robust biological hydrogen-bonded organic framework with post-functionalized rhenium(I) sites for efficient heterogeneous visible-light-driven CO2 reduction. Angew. Chem. Int. Ed. 60(16), 8983–8989 (2021). https://doi.org/10.1002/anie.202016710

- J. Wang, W. Zhu, F. Meng, G. Bai, Q. Zhang et al., Integrating dual-metal sites into covalent organic frameworks for enhanced photocatalytic CO2 reduction. ACS Catal. 13(7), 4316–4329 (2023). https://doi.org/10.1021/acscatal.3c00126

- H. Lv, R. Sa, P. Li, D. Yuan, X. Wang et al., Metalloporphyrin-based covalent organic frameworks composed of the electron donor-acceptor dyads for visible-light-driven selective CO2 reduction. Sci. China Chem. 63(9), 1289–1294 (2020). https://doi.org/10.1007/s11426-020-9801-3

- S. Yang, R. Sa, H. Zhong, H. Lv, D. Yuan et al., Microenvironments enabled by covalent organic framework linkages for modulating active metal species in photocatalytic CO2 reduction. Adv. Funct. Mater. 32(17), 2110694 (2022). https://doi.org/10.1002/adfm.202110694

- Y. Yang, Y. Lu, H.-Y. Zhang, Y. Wang, H.-L. Tang et al., Decoration of active sites in covalent–organic framework: an effective strategy of building efficient photocatalysis for CO2 reduction. ACS Sustainable Chem. Eng. 9(39), 13376–13384 (2021). https://doi.org/10.1021/acssuschemeng.1c04994

- J.-X. Cui, Y.-M. Fu, B. Meng, J. Zhou, Z.-Y. Zhou et al., A novel cobalt-anchored covalent organic framework for photocatalytic conversion of CO2 into widely adjustable syngas. J. Mater. Chem. A 10(25), 13418–13427 (2022). https://doi.org/10.1039/D2TA02648A

- M. Dong, W. Li, J. Zhou, S.-Q. You, C.-Y. Sun et al., Microenvironment modulation of imine-based covalent organic frameworks for CO2 photoreduction. Chin. J. Chem. 40(22), 2678–2684 (2022). https://doi.org/10.1002/cjoc.202200046

- M. Lu, Q. Li, J. Liu, F.-M. Zhang, L. Zhang et al., Installing earth-abundant metal active centers to covalent organic frameworks for efficient heterogeneous photocatalytic CO2 reduction. Appl. Catal. B Environ. 254, 624–633 (2019). https://doi.org/10.1016/j.apcatb.2019.05.033

- X. Hu, L. Zheng, S. Wang, X. Wang, B. Tan, Integrating single Co sites into crystalline covalent triazine frameworks for photoreduction of CO2. Chem. Commun. 58(58), 8121–8124 (2022). https://doi.org/10.1039/D2CC02481K

- L. Ran, Z. Li, B. Ran, J. Cao, Y. Zhao et al., Engineering single-atom active sites on covalent organic frameworks for boosting CO2 photoreduction. J. Am. Chem. Soc. 144(37), 17097–17109 (2022). https://doi.org/10.1021/jacs.2c06920

- W. Zhong, R. Sa, L. Li, Y. He, L. Li et al., A covalent organic framework bearing single Ni sites as a synergistic photocatalyst for selective photoreduction of CO2 to CO. J. Am. Chem. Soc. 141(18), 7615–7621 (2019). https://doi.org/10.1021/jacs.9b02997

- H. Zhong, R. Sa, H. Lv, S. Yang, D. Yuan et al., Covalent organic framework hosting metalloporphyrin-based carbon dots for visible-light-driven selective CO2 reduction. Adv. Funct. Mater. 30(35), 2002654 (2020). https://doi.org/10.1002/adfm.202002654

- S. Zhang, S. Wang, L. Guo, H. Chen, B. Tan et al., An artificial photosynthesis system comprising a covalent triazine framework as an electron relay facilitator for photochemical carbon dioxide reduction. J. Mater. Chem. C 8(1), 192–200 (2020). https://doi.org/10.1039/C9TC05297F