Supporting Information for

Activating Progressive Sn2+ Nucleation by Micellar Structure Electrolyte for Dead-Sn-Free Aqueous Batteries

Xiaojia Lan1,2, Zhaoyu Zhang1,2, Yuekai Lin1,2, Wencheng Du1,2, Yufei Zhang1,2, Minghui Ye1,2, Zhipeng Wen1,2, Yongchao Tang1,2, Xiaoqing Liu1,2,*,  and Cheng Chao Li1,2,*

1 School of Chemical Engineering and Light Industry, Guangdong University of Technology, Guangzhou 510006, People’s Republic of China

2 Guangdong Provincial Laboratory of Chemistry and Fine Chemical Engineering Jieyang Center, Jieyang 515200, P. R. China

*Corresponding authors. E-mail: licc@gdut.edu.cn (Cheng Chao Li); liu@gdut.edu.cn (Xiaoqing Liu)

S1 Experimental Section

S1.1 Material Characterizations

Dynamic light scattering was measured by utilizing a zeta potential analyzer (Zetasizer NANO ZS, Malvern, UK). FT-IR spectra were obtained by an FT-IR spectrometer (Nicolet iS5, Thermo Scientific). Raman spectra were collected by using a Raman spectrometer (LabRAM HR Evolution). NMR spectra were provided by NMR spectrometer (JNM-ECZ500R/S1, Japan). SEM images were taken by field emission scanning electron microscope (SU8220, Hitach, Japan). XRD patterns obtained by X-ray diffractometer (D8 VENTURE, Bruker, Germany). In-situ optical microscopy images were gained by a DMM-900C metallographic microscope (Caikon Optical Instrument Co., Ltd, Shanghai). CLSM images were acquired by confocal laser scanning microscope (OLS4100, Olympus, Japan).

S1.2 Simulation methods

The density functional theory calculations for water, salt, and corresponding Sn2+ complexes were performed in the Gaussian. The pictorial representations of the molecular structures were prepared using the Visual Molecular Dynamics and Multiwfn software. An implicit solvation model based on density was used to consider solvent effects. The binding energy (EBinding) of Sn2+ complexes were calculated using the following equation:

𝐸Binding = 𝐸Sn2+-complexe ‒ 𝐸complexe ‒ 𝐸Sn2+

where ESn2+-complex represents the total energy of the complex interacting with Sn2+, Ecomplex is the energy of the complex, and ESn2+ is the energy of a single Sn2+.

Atomistic molecular dynamics simulations have been performed in the GROMACS [S1] (version 2022.6) simulation package using the CHARMM 36 force field [S2] and the TIP3P water model. The parameters for Sn2+ ion used the parameters of the UFF force field. Two systems were simulated, one containing 260 H2SO4, and 26 SnSO4 and 6669 water molecules; the other containing additional 136 sulfolane molecules and water were reduced to 5878 molecules. The molecules were first randomly placed in cubic boxes of around 6 nm and water was used to solvate the whole system. Then, the ions were inserted through random replacement of water molecules. After thousands of steps of energy minimization, the systems were equilibrated for 5 ns under the NPT ensemble and followed the production runs of 10 ns under the canonic ensemble. An integration time-step of 1 fs was used and the temperature was coupled to 298 K using the Nose-Hoover method and a cutoff scheme of 1.2 nm was used for the non-bonded interactions, and the Particle Mesh Ewald method [S3] with a fourierspacing of 0.1 nm was applied for the long range electrostatic interactions. All covalent bonds with hydrogen atoms were constraint using the LINCS algorithm [S4]. The presence of hydrogen bonds was calculated using the common criteria so that the maximum angle of the hydrogen-donor-acceptor was 30 degrees, and the distance between the acceptor and donor atoms was less than 0.35 nm.

Supplementary Figures and Tables

Fig. S1 Optical photographs of various electrolytes containing different contents of sulfone

Fig. S2 The electrostatic potential of sulfone and water

Fig. S3 Binding energy of H2O-H2O and Sulfone-H2O

Fig. S4 DLS analysis of the micelle particle size in MCE-1, MCE-2 and MCE-3

Fig. S5 (a) The Raman spectra of different electrolytes (BE, MCE-1, MCE-2, MCE-3) and (b) The local enlargement signal attributed to SO42-

Fig. S6 (a) The fitted O-H stretching vibration represents water molecules with strong (pale Chestnut), mid (pink) and weak (blue) H-bond and (b) The proportion of strong H-bond water varied by the SL concentration

Fig. S7 3D snapshots of MD simulations for BE with corresponding schematic diagrams of Sn2+ solvation structures

Fig. S8 RDF of Sn-O (H2O), Sn-O (SO42-) and the corresponding coordination numbers in BE

Fig. S9 Mean square displacement (MSD) curves for BE and MCE

Fig. S10 The cycling performance of Sn||Sn at 1 mA cm-2 and 1 mAh cm-2 in different electrolytes

Fig. S11 DLS analysis of the micelle particle size in MCE and BE after 100 cycles

Fig. S12 Variable temperature electrochemical impedance spectroscopy (EIS) results of (a) BE and (b) MCE

Fig. S13 SEM images of Sn anodes after immersion in (a) BE and (b) MCE for 15 days

Fig. S14 (a) complete and (b-c) partial enlarged XRD patterns after immersion in BE and MCE for 15 days

Fig. S15 Optical photos of Sn deposited on Cu substrate in (a) BE and (b) MCE in after LSV test

Fig. S16 The LSV curves of 2 M H2SO4 and 2 M H2SO4 + SL

Fig. S17 The voltage–time curves during Sn nucleation at 1 mA cm‒2

Fig. S18 CV curves of Sn2+ deposition/dissolution curves on the Cu substrates in (a) BE and (b) MCE, insect: the enlargement of the nucleation loop

Fig. S19 CA curves of (a) BE and (b) MCE with an applied potential of −0.33 V, −0.38 V, and −0.43 V

Here, glassy carbon electrodes (GCE) were selected as the working electrodes for nucleation studies due to their inherent advantages aligning closely with the core requirements for characterizing nucleation behavior. First, the GCE exhibits excellent chemical inertness in electrolytes, preventing unexpected side reactions that could interfere with signals from tin nucleation and growth. Second, its smooth, uniform surface provides evenly distributed nucleation sites, minimizing the impact of surface defects or impurities on nucleation kinetics. This is crucial for accurately distinguishing transient nucleation from progressive nucleation patterns through CA curve fitting. Additionally, the GCE's high conductivity and low background current characteristics enable sensitive detection of minute current changes generated during initial nucleation.

Fig. S20 CA curves in BE and MCE under −100 mV

Fig. S21 Magnified view at (a) 1 mA cm-2 and (b) 20 mA cm-2 during magnification testing

Fig. S22 The rate performance of Sn||Cu half cells in (a) BE and (b) MCE

Fig. S23 Coulombic efficiency corresponding to the rate performance of the Sn||Cu half-cell

It is evident that MCE maintains stable operation across all current levels, with CE exhibiting a positive correlation as current gradually increases (~99.5%). In contrast, BE shows severe fluctuations in CE after only a few cycles, likely due to significant dead Sn shedding causing battery failure.

Fig. S24 (a) CE of the Sn stripping/plating in BE and MCE at 5 mA cm‒2, 1 mAh cm‒2 and (b) corresponding capacity-voltage curves from the 1st to 5000th cycle for MCE

Fig. S25 SEM images of Sn anodes cycled in BE at 4 mAh cm-2

Fig. S26 XRD patterns of tin foil after different numbers of cycles in two electrolytes

Fig. S27 Tyndall effect of BE supplemented with 10% v/v DMSO

Fig. S28 SEM images of Sn anodes cycled in BE supplemented with 10% v/v DMSO at 4 mAh cm-2

Fig. S29 CV curves of Sn|BE|Mn and Sn|MCE|Mn at a scan rate of 1 mV s-1 with CF

Fig. S30 XRD pattern of the cathode electrode after 50 cycles

Fig. S31 Binding energy of H2O-Mn3+ and SL-Mn3+

Fig. S32 CV curves of Sn|BE|Mn and Sn|MCE|Mn at a scan rate of 1 mV s-1 with DEF

Fig. S33 Under DEF, the capacity-voltage curves of BE and MCE at different cycle numbers

Fig. S34 Energy efficiency comparison in long-tern cycles

Fig. S35 The capacity-voltage curves of BE+0.05 M CuSO4

Fig. S36 Optical photos of BE battery after failure under DEF

Fig. S37 Under DEF, SEM and elemental mapping of Cu current collector surface after cyclic charging

Supplementary References

- B. Hess, C. Kutzner, D. van der Spoel, E. Lindahl, GROMACS 4:   algorithms for highly efficient, load-balanced, and scalable molecular simulation. J. Chem. Theory Comput. 4(3), 435–447 (2008). https://doi.org/10.1021/ct700301q

- R.B. Best, X. Zhu, J. Shim, P.E.M. Lopes, J. Mittal et al., Optimization of the additive CHARMM all-atom protein force field targeting improved sampling of the backbone ϕ, ψ and side-chain χ1 and χ2 dihedral angles. J. Chem. Theory Comput. 8(9), 3257–3273 (2012). https://doi.org/10.1021/ct300400x

- U. Essmann, L. Perera, M.L. Berkowitz, T. Darden, H. Lee et al., A smooth particle mesh Ewald method. J. Chem. Phys. 103(19), 8577–8593 (1995). https://doi.org/10.1063/1.470117

- B. Hess, H. Bekker, H.J.C. Berendsen, J.G.E.M. Fraaije, LINCS: a linear constraint solver for molecular simulations. J. Comput. Chem. 18(12), 1463–1472 (1997). https://doi.org/10.1002/(sici)1096-987x(199709)18:121463::aid-jcc4>3.3.co;2-l