Supporting Information for

Optical Switching of Robust Ferroelectric Polarization on Epitaxial Hf0.5Zr0.5O2 Integrated with BaTiO3

Wenjing Dong1, Huan Tan2, Jingye Zou1, Alberto Quintana1, Tingfeng Song1, César Magén3,4, Claudio Cazorla5,6,7, Florencio Sánchez1,* , Ignasi Fina1,*

1Institut de Ciència de Materials de Barcelona (ICMAB-CSIC), Campus UAB, Bellaterra 08193, Barcelona, Spain

2Departament de Física, Universitat Autònoma de Barcelona, 08193 Cerdanyola del Vallès, Spain

3Instituto de Nanociencia y Materiales de Aragón (INMA), CSIC-Universidad de Zaragoza, 50009 Zaragoza, Spain

4Departamento de Física de la Materia Condensada, Universidad de Zaragoza, 50018 Zaragoza, Spain

5Group of Characterization of Materials, Departament de Física, Universitat Politècnica de Catalunya, Campus Diagonal Besòs, Av. Eduard Maristany 10–14, 08019 Barcelona, Spain

6Research Center in Multiscale Science and Engineering, Universitat Politècnica de Catalunya, Campus Diagonal-Besòs, Av. Eduard Maristany 10–14, 08019 Barcelona, Spain

7Institució Catalana de Recerca i Estudis Avançats (ICREA), Passeig Lluís Companys 23, 08010 Barcelona, Spain

*Corresponding authors. E-mail: ifina@icmab.es (Ignasi Fina); fsanchez@icmab.es (Florencio Sánchez)

Supplementary Figures and Tables

Fig. S1 (a-e) Optical image (top view) of the deposited Pt electrodes of the samples with BTO thickness of 0, 1.5, 5, 10, 30 and 100 nm, respectively

Fig. S2 (a-e) XRD θ –2 θ scans (measured with a point detector ) of the samples with BTO thickness of 0, 1.5, 5, 10, 30 and 100 nm, respectively

Fig. S3 (a-l) XRD 2 θ –χ images and integrated, in the χ = ±10° range around χ = 0°, θ–2θ scans of samples with BTO thickness of 0, 1.5, 5, 10, 30 and 100 nm as indicated. The † and * symbols mark the positions of the STO(002) reflections due to spurious Cu-K and W-L lines, respectively

Fig. S4 Atomic resolution HAADF images of a representative region where the good crystalline quality of the BTO layer can be observed

Fig. S5 (a) P-V loops for 100 nm BTO sample without HZO at increasing voltage. (b) Leakage current for 100 nm BTO sample. (c) Endurance plots at 1 MHz and 10 V cycling voltage for 100 nm BTO sample

Fig. S6 (a-d) Corresponding to Fig. 3(a-d), I-V loops of HZO/BTO samples with BTO thickness of 0, 1.5, 10 and 100 nm, respectively with and without illumination and in the pristine state and after 106 cycles

Fig. S7 (a-e) Endurance plots at 1 MHz and indicated voltage of samples with BTO thickness of 0, 1.5, 5, 10, 30 and 100 nm. (f-k) P-V and (l-q) I-V loops corresponding to data of a-e

Fig. S8 (a-d) Polarization in dark and (e-h) under illumination loops for reading in the switching spectroscopy experiments. Asymmetric loops account for the presence of imprint electric fields

Fig. S9 (a) PFM amplitude and (b) phase images collected just after poling, respectively, for a HZO single film without BTO. (c, d) Idem collected after waiting 10 min (600 s) under illumination

Fig. S10 PFM amplitude images after (a-c) electrical poling and waiting for 60 s in dark and (d-f) after illuminating the sample for 60 s for 1.5, 10 and 100 nm samples, respectively

Fig. S11 (a) PFM phase images collected after indicated illumination time. Arrows indicate the preset polarization state direction. (b) Phase profiles after indicated illumination time obtained from averaging images of panel (a) along vertical axis. (c) DPhase as a function of illumination time evaluated as the phase contrast of phase profiles in panel (b)

Fig. S12 PFM amplitude and phase images collected just after poling and after 60 s under illumination for (a) 2 nm and (b) 4 nm HZO samples capped with 10 nm BTO