Supporting Information for

Uniform Fast-Kinetic Anode/Cathode Electrolyte Interphases Enable High Performance 3C Li-Metal Batteries with >99.9% Coulombic Efficiencies

Qingyang Cao1, Danchen Fu1, Xuedong He1, Yaohua Huang1, Ningning Yao1, Chunyu Song1, Huawei Song1* and Chengxin Wang1*

1State Key Laboratory of Optoelectronic Materials and Technologies, School of Materials Science and Engineering, Sun Yat-Sen (Zhongshan) University, Guangzhou 510275, People’s Republic of China

*Corresponding authors. E-mail: songhw5@mail.sysu.edu.cn (Huawei Song); wchengx@mail.sysu.edu.cn (Chengxin Wang)

Supplementary Figures and Tables

Fig. S1 EIS plots of pristine Li-metal symmetric cells with electrolytes containing different amounts of FNPB

Fig. S2 Local anion signals in Raman spectra of electrolyte with/without FNPB

Fig. S3 Local cation signals in Raman spectra of electrolyte with/without FNPB

Fig. S4 The Binding Energies of Li metal with FNPB, EC and DEC

Fig. S5  Electrostatic potential surface, with yellow and blue areas representing negative and positive charges, respectively

Fig. S6  One possible reaction pathway between FNPB and Li metal and LiFePO4

Fig. S7 Current-time plots of Li-metal symmetric cells with BE after polarization at a constant potential of 10 mV for 1600 s. The inset plots are the impedance spectra before and after the polarization

Fig. S8 Current-time plots of Li-metal symmetric cells with electrolyte containing FNPB additive after polarization at a constant potential of 10 mV for 1600 s. The inset plots are the impedance spectra before and after the polarization

Fig. S9 Contact angle measurement of BE

Fig. S10 Contact angle measurement of electrolyte after adding FNPB

Fig. S11 Chronoamperoetry test of Li||Li cells in BE and FNPB electrolyte

Fig. S12 SEM image of the pristine Li-metal electrode

Fig. S13 SEM images of Li-metal electrodes plating/stripping in BE at 1 mA cm-2 for 50 cycles

Fig. S14 SEM images of Li-metal electrodes plating/stripping in FNPB at 1 mA cm-2 for 50 cycles

Fig. S15 N 1s XPS depth profiles of the Li-metal electrode cycled in BE after 50 cycles

Fig. S16 Li 1s XPS depth profiles of the Li-metal electrode cycled in BE after 50 cycles

Fig. S17 Li 1s XPS depth profiles of the Li-metal electrode cycled in FNPB after 50 cycles

Fig. S18 B 1s XPS spectrum of the Li-metal electrode cycled in FNPB after 50 cycles

Fig. S19 TOF-SIMS 3D render overlay images of LiNO2- signals for the Li metal electrode cycled in FNPB after 50 cycles

Table S1 Performance comparison of Li-metal batteries with different electrolyte additives

| Electrolyte composition | Positive electrode | Voltages (V) | Performance | CE | References |
| --- | --- | --- | --- | --- | --- |
| 1 M LiPF6 in EC/DEC (TDFA),100 μL | LFP (3 mg cm-) | 2.5-4.2 | 300 cycle (89.4%), 1C | / | [S1] |
| 2M LiFSI in DOL with 3vol% TEB | LFP (2.64 mg cm-2) | 2.5-3.8 | 500 cycle (80.0%), C/2 | 0.5mA 98.49% | [S2] |
| 1 M LiTFSI+0.04 M CH3OK +2%LiNO3 in DME/DOL | LFP (10.5 mg cm-2) | 2.5-3.8 | 350 cycle (91.5%), C/2 | / | [S3] |
| 1 M LiTFSI/DOL-DME (1:1 vol%) with 1 wt% LiNO3(4% 2,2,2-TFTF) | LFP (1.8 mg cm-2) | 2.4-4.2 | 500 cycle (86.0%), | / | [S4] |
| 1 M LiPF6 in EC/DMC (1:1 vol%) with 1% LiNO3 +0.5% HFT | LFP (3 mg cm-2) | 2.5-4.2 | 500cycle (<80.0%),2C | 1mA 97.1% | [S5] |
| 0.6M LiFSI+0.4M LiBOB in EC/EMC(3:7)(B-FC) | NMC622(1.4 mAh cm-2) | 3.0-4.5 | 300 cycle (73.1%), C/2 | / | [S6] |
| 1 M LiPF6 in DEC : EC : EMC (2:3:5 vol%) with 1wt% LiDFP +0.3wt% LiNO3 | LFP (1.25 mAh cm-2) | 2.2-4.1 | 350 cycle (88.0%),1C | 1mA 98.2% | [S7] |
| 1 M LiPF6 in EC/DEC (FNPB),30 μL | LFP (4 mg cm-2) | 2.5-4.0 | 500 cycle (99.9%), 3C | 1mA 98.2% | This work |

Supplementary References

- E. Park, Y.-H. Lee, S.-H. Huh, J. Huh, Y.-E. Sung et al., Bifunctional trimethylsilyl-modified fluorinated ester additive for LiF-rich solid electrolyte interphase in lithium metal batteries. Energy Storage Mater. 78, 104271 (2025). https://doi.org/10.1016/j.ensm.2025.104271

- Y. Guo, Y. Huang, H. Hu, Y. Chen, X. Cai et al., Anion-anchoring enabling fast Li+ transport within wide temperature. Nano Energy 147, 111568 (2026). https://doi.org/10.1016/j.nanoen.2025.111568

- J. Yang, M. Li, Z. Sun, X. Lian, Y. Wang et al., Prolonging the cycling lifetime of lithium metal batteries with a monolithic and inorganic-rich solid electrolyte interphase. Energy Environ. Sci. 16(9), 3837–3846 (2023). https://doi.org/10.1039/d3ee00161j

- S. Yang, M. Hao, Z. Wang, Z. Xie, Z. Cai et al., 2, 2, 2-Trifluoroethyl trifluoroacetate as effective electrolyte additive for uniform Li deposition in lithium metal batteries. Chem. Eng. J. 435, 134897 (2022). https://doi.org/10.1016/j.cej.2022.134897

- J. Jiang, M. Li, X. Liu, J. Yi, Y. Jiang et al., Multifunctional additives to realize dendrite-free lithium deposition in carbonate electrolytes toward low-temperature Li metal batteries. Adv. Energy Mater. 14(27), 2400365 (2024). https://doi.org/10.1002/aenm.202400365

- J. Han, C. Park, D. Jin, S. Kim, C.B. Dzakpasu et al., A bis(2-fluoroethyl) carbonate as a new electrolyte additive for enhancing the long-term cycle performance of Li-metal batteries. J. Electrochem. Soc. 170(2), 020529 (2023). https://doi.org/10.1149/1945-7111/acbca1

- M. Li, C. Chen, H. Luo, Q. Xu, K. Yan et al., Constructing an inorganic-rich solid electrolyte interphase by adjusting electrolyte additives for stable Li metal anodes. J. Mater. Chem. A 12(17), 10072–10080 (2024). https://doi.org/10.1039/d3ta07655e