Supporting Information for

Graphene-Skinned Fiber with Fine Tunable Electrical Resistance via Radical and Substrate Engineering for Electromagnetic-Thermal Fabric

Jie Liang1, Zhaochen Li1, Fang Ye1*, Yuchen Cao1, Yi An1, Xiaomeng Fan1*, Qiang Song1*

1 Science and Technology on Thermostructural Composite Materials Laboratory, Northwestern Polytechnical University, Xi’an 710072, People’s Republic of China

*Corresponding authors. E-mail: yefang511@nwpu.edu.cn (Fang Ye); fanxiaomeng@nwpu.edu.cn (Xiaomeng Fan); songqiang511@nwpu.edu.cn (Qiang Song)

Supplementary Figures

Fig. S1 Sensitivity analysis of (a) C2H2, (b) C6H6, the top 10 elementary reactions affecting the sensitivity of the (c) C2H2, (d) C6H6

Fig. S2 Residence time at different temperatures

Fig. S3 Variation of molar fraction of different gases with deposition temperature: (a) CH4, (b) C2H2

Fig. S4 Carbon content in Graphene based SiO2 fiber cloth at different deposition temperatures

Fig. S5 C 1s peak results of graphene at different deposition temperature: (a) spectrum, (b) bonding proportion

Fig. S6 Raman spectra from different regions of the samples: (a) 1000-1, (b) 1050-1, (c) 1100-1, (d) 1150-1, (e) 1200-1

Fig. S7 Raman spectra fitting results of graphene at different deposition times: (a1) 1000-1, (a2) 1000-2, (a3) T1000-3, (b1) 1050-1, (b2) 1050-2, (b3) 1050-3, (c1) 1100-1, (c2) 1100-2, (c3) 1100-3, (d1) 1150-1, (d2) 1150-2, (d3) 1150-3, (e1) 1200-1, (e2) 1200-2, (e3) 1200-3

Fig. S8 Cross-sectional microstructure of Gr-skinned SiO2 fiber

- Fig. S9 (a) Micro-morphology and (b) coverage and sheet resistance at different deposition temperatures at 1000 ℃

Fig. S10 Electromagnetic wave response characteristics of graphene based SiO2 fiber cloth at different deposition temperatures: (a) total shielding effectiveness, (b) reflection shielding effectiveness, (c) absorption shielding effectiveness

Fig. S11 Transmittance under different structural parameters: (a) Band-stop type, (b) Band-pass type, (c) High-pass type, (d) Low-pass type

Fig. S12 Etching phenomena under different laser parameters: (a) fiber damage, (b) fiber melting, (c) fiber remains intact

Fig. S13 Dielectric constant of acrylic at different temperatures, (a) ε׳, (b) ε״

Fig. S14 Simulated (a) Reflectance, (b) Transmittance, (c) Absorptance at 20 ℃ and 80 ℃