Supporting Information for

Manipulating Interphase Chemistry by Endogenous Doping towards High-Performance Hard Carbon Anodes for Sodium-Ion Batteries

Hang Li1, Yuan Zhou4, Yutian Yang1, Yining Chen1, Yuying Zhang1, 3, Zhe Wang1, Quan Zong5, Guozhao Fang1, Shuang Zhou1, *, and Anqiang Pan1, 2, *

1 School of Materials Science and Engineering, Key Laboratory of Electronic Packaging and Advanced Functional Materials of Hunan Province, Central South University, Changsha 410083, Hunan, P. R. China

2 Xinjiang Key Laboratory of Advanced Metallic Materials Design and Application, Xinjiang Engineering Research Center of Environmental and Functional Materials, School of Materials Science and Engineering, Xinjiang University, Urumqi 830046, Xinjiang, P. R. China

3 Hunan Cngr New Energy Science & Technology Co., Ltd. Changsha 410083, Hunan, P. R. China

4 Science and Technology Project Service Center of Xinjiang Uygur Autonomous Region, Urumqi 830011, Xinjiang, P. R. China

5 College of Materials and Chemistry, China Jiliang University, Hangzhou 310018, Zhejiang, P. R. China

*Corresponding authors. E-mail: zhoushuang2017@csu.edu.cn (Shuang Zhou); pananqiang@csu.edu.cn (Anqiang Pan)

Supplementary Figures and Tables

Fig. S1 Photographs of HC after carbonization at the temperature of 1300 °C

Fig. S2 TG-DSC and DTG curves of 1300-F, 1100-FCA, 1300-FCA, 1500-FCA

Fig. S3 The SEM images of carbon spheres prepared by hydrothermal reaction of fructose with cysteine

Fig. S4 The SEM images of (a-d) 1300-F, (e-h)1100-FCA, (i-l) 1300-FCA, (m-p)1500-FCA

Fig. S5 HRTEM images of 1300-F, 1100-FCA, 1300-FCA, 1500-FCA

Fig. S6 XPS full spectra and elemental content ratio of 1300-F, 1100-FCA, 1300-FCA, 1500-FCA

Fig. S7 High-resolution XPS spectra of 1300-F, 1100-FCA, 1300-FCA, 1500-FCA

Fig. S8 The peak fitting of the d002 peak of the XRD pattern of 1300-F, 1100-FCA, 1300-FCA, 1500-FCA

Fig. S9 The fitted Raman spectra of 1300-F, 1100-FCA, 1300-FCA, 1500-FCA

Fig. S10 Pore diameter distribution of 1300-F, 1100-FCA, 1300-FCA, 1500-FCA

Fig. S11 Small-angle X-ray scattering (SAXS) fitted pattern of 1300-F, 1100-FCA, 1300-FCA and 1500-FCA

Fig. S12 Schematic diagram of closed pores for hard carbon

Fig. S13 CV curves of 1300-F, 1100-FCA, 1300-FCA, 1500-FCA for the first 3 cycles

Fig. S14 GCD curves of 1300-F, 1100-FCA, 1300-FCA, 1500-FCA for the first 3 cycles at 0.05 A g-1, 0.1A g-1, 0.2A g-1

Fig. S15 The rate performance of 0.05 A g-1 to 1.0 A g-1 and the charge/discharge profiles of 1300-FCA at different current densities

Fig. S16 The rate performance of 0.05 A g-1 to 5.0 A g-1 and the charge/discharge profiles of 1300-F, 1100-FCA and 1500-FCA at different current densities

Fig. S17 Cycling performance of 1300-FCA at 0.5 A g-1

Fig. S18 Cycling performance of 1300-FCA at 1.0 A g-1

Fig. S19 XRD patterns of hard carbon prepared from different kinds of amino acids

Fig. S20 The rate performance properties and GCD curves of the first three cycles for hard carbon prepared from different amino acids

Fig. S21 The CV curves and the diffusion- and surface-controlled contributions at various scan rates of 1300-F and 1300-FCA

Fig. S22 The corresponding correlations between peak current (i) and scan rate (v), normalized contribution ratio of capacitive capacities of 1300-F and 1300-FCA

Fig. S23 Na+ ions diffusion coefficients of 1300-F and 1300-FCA

Fig. S24 Gitt curves and Na+ diffusion coefficients of 1300-F and 1300-FCA

Fig. S25 EIS spectra of 1300-F, 1100-FCA, 1300-FCA, 1500-FCA

Fig. S26 DRT analysis obtained from EIS spectra of 1300-F and 1300-FCA

Fig. S27 XPS etching spectra of 1300-F and 1300-FCA for Na 1s

Fig. S28 SEI composition distribution of 1300-F and 1300-FCA calculated from the depth-profiling XPS spectra

Fig. S29 HRTEM analysis obtained from inorganic composition of 1300-F and 1300-FCA

Fig. S30 2D Mapping of 1300-F and 1300-FCA for 3D TOF-SIMS

Fig. S31 DFT analysis model for the top and side view of 1300-F and1300-FCA

Fig. S32 Optimized structures and corresponding adsorption energies of Na adsorbed on 1300-F and 1300-FCA

Fig. S33 Optimized structures of Na salt adsorbed on 1300-F and 1300-FCA

Fig. S34 Rate performance of and cycling performance of NVP//Na half cell

Fig. S35 The digital images of LED light by the full cell

Fig. S36 Cycling performance of NVP//1300-FCA full cell at 0.5 C

Table S1 Analysis parameters of the HC from XRD and Raman spectroscopy

| Sample | d (002) (nm) | La | Lc | ID/IG | BET surface area (m2 g-1) |
| --- | --- | --- | --- | --- | --- |
| 1300-F | 0.370 | 2.24 | 1.08 | 1.36 | 0.6526 |
| 1100-FCA | 0.443 | 1.96 | 0.95 | 1.82 | 2.7574 |
| 1300-FCA | 0.388 | 2.65 | 1.28 | 1.40 | 0.3213 |
| 1500-FCA | 0.368 | 3.18 | 1.54 | 1.35 | 0.1595 |

Table S2 The first cycles charge/discharge capacity and ICE in different current densities

| Current Density (mA g-1) | Sample | Discharge (mAh g-1) | Charge (mAh g-1) | ICE (%) |
| --- | --- | --- | --- | --- |
| 50 mA g-1 | 1300-F | 264.9 | 209 | 79 |
|  | 1100-FCA | 352.0 | 294.5 | 84 |
|  | 1300-FCA | 407.93 | 363.1 | 89 |
|  | 1500-FCA | 355.0 | 311.5 | 88 |
| 100 mA g-1 | 1300-F | 324.9 | 239.9 | 74 |
|  | 1100-FCA | 370.0 | 264.7 | 72 |
|  | 1300-FCA | 402.2 | 343.8 | 86 |
|  | 1500-FCA | 328.9 | 279.3 | 85 |
| 200 mA g-1 | 1300-F | 291.9 | 208.8 | 72 |
|  | 1100-FCA | 362.0 | 254.5 | 70 |
|  | 1300-FCA | 375.7 | 319.6 | 86 |
|  | 1500-FCA | 319.8 | 265.0 | 83 |

Table S3 Summary of representative publication with HC

| Carbon source (temperature of carbonization /℃) | Capacity (half cell) | ICE (%) | Cycling performance (full cell) | Ref |
| --- | --- | --- | --- | --- |
| Fructose (1300 ℃) | 363.0 mAh g−1 at 0.05 A g-1, 100 % retention after 150 cycles at0.1 A g-1, 96 % retention after 300 cycles at 0.3 A g-1, 95 % retention after 300 cycles at 0.5 A g-1, 94 % retention after 700 cycles at 1.0 A g-1, 79 % retention after 2500 cycles at 5.0 A g-1, | 89.0% | 94.2% retention after 300 cycles at 0.5 C, 89.2% retention after 700 cycles at 1.0 C and 98.1% retention for pouch cell after 715 cycles at 1.0 C | This work |
| Pitch (1400 ℃) | 313.83 mAh g−1 at 0.1 C and 91.6 % retention after 200 cycles at 0.1 C | 86.4% | 41.6% retention after 100 cycles at 0.2 C | [S1] |
| Phenolic resin (1400 ℃) | 340.3 mAh g−1 at 0.1 C, 94.9% retention after 250 cycles at 0.5 C and 86.4% retention after 1000 cycles at 2 C | 88.5% | 86.1% retention after 300 cycles at 1.0 C | [S2] |
| Sucrose (1200 ℃) | 352.9 mAh g−1 at 0.02 A g-1 and 95% retention after 200 cycles at 0.05 A g-1. | 88.0% | 82.5% retention after 100 cycles at 1.0 C | [S3] |
| bamboo nodes (1300 ℃) | 346.9 mAh g−1 at 0.05 A g-1 and 90% retention after 1000 cycles at 1.0 A g-1. | 74.0% | 90% retention after 300 cycles at 1.0 A g-1 | [S4] |
| Natural bamboo (1300 ℃) | 350 mAh g−1 at 0.02 A g-1 and 96% retention after 100 cycles at 0.1 A g-1. | 86.8% | Not reported | [S5] |
| D-(+)-glucose (1300 ℃) | 347 mAh g−1 at 0.1 C and 73.1% retention after 300 cycles at 0.5 C. | 85.0% | 75.6% retention after 200 cycles at 0.15 A g-1 | [S6] |
| Coal (1300 ℃) | 356 mAh g−1 at 0.02 A g-1 and 91% retention after 3000 cycles at 1.0 A g-1. | 88.1% | 46.1% retention after 80 cycles at 0.05 A g-1 | [S7] |
| Isotropic coal tar pitch (1300 ℃) | 304 mAh g−1 at 0.1 C and 83.3% retention after 400 cycles at 0.25 C. | 88.4% | Not reported | [S8] |

Supplementary References

[S1] L. Wang, Z. Xu, P. Lin, Y. Zhong, X. Wang, Y. Yuan, J. Tu. Oxygen-crosslinker effect on the electrochemical characteristics of asphalt-based hard carbon anodes for sodium-ion batteries. Adv. Energy Mater. 15(7), 2403084 (2025). https://doi.org/10.1002/aenm.202403084

[S2] J. Lin, Q. Zhou, Z. Liao, Y. Chen, Y. Liu, Q. Liu, X. Xiong. Steric hindrance engineering to modulate the closed pores formation of polymer-derived hard carbon for high-performance sodium-ion batteries. Angew. Chem. Int. Ed. 63(39), e202409906 (2024). https://doi.org/10.1002/anie.202409906

[S3] Y. Liu, J. Yin, R. Wu, H. Zhang, R. Zhang, R. Huo, J. Zhao, K.-Y. Zhang, J. Yin, X.-L. Wu, H. Zhu. Molecular engineering of pore structure/interfacial functional groups toward hard carbon anode in sodium-ion batteries. Energy Storage Mater. 75, 104008 (2025). https://doi.org/10.1016/j.ensm.2025.104008

[S4] L. Zhou, G. Zhang, C. Xu, J. Li, Y. Liu, B. Li, A. Wang, K. Sun. Tailored regulation of graphite microcrystals via tandem catalytic carbonization for enhanced electrochemical performance of hard carbon in the low-voltage plateau. Adv. Funct. Mater. 35(9), 2416061 (2025). https://doi.org/10.1002/adfm.202416061

[S5] Y. Wang, Z. Yi, L. Xie, Y. Mao, W. Ji, Z. Liu, X. Wei, F. Su, C.-M. Chen. Releasing free radicals in precursor triggers the formation of closed pores in hard carbon for sodium-ion batteries. Adv. Mater. 36(26), 2401249 (2024). https://doi.org/10.1002/adma.202401249

[S6] Z. Xu, J. Wang, Z. Guo, F. Xie, H. Liu, H. Yadegari, M. Tebyetekerwa, M. P. Ryan, Y.-S. Hu, M.-M. Titirici. The role of hydrothermal carbonization in sustainable sodium-ion battery anodes. Adv. Energy Mater. 12(18), 2200208 (2022). https://doi.org/10.1002/aenm.202200208

[S7] Y. Huang, Z. Hou, J. Wang, Y. Li, T. Ma, D. Nan, C. Wei, J.-G. Wang. Reconfiguring terminal species of bituminous coal to steer hard carbon toward high-capacity and fast sodium storage. Angew. Chem. Int. Ed. 64(15), e202423864 (2025). https://doi.org/10.1002/anie.202423864

[S8] L. Ji, Y. Zhao, X. Qi, Y. Li, Z. Wei, G. Han, Z. Shao. Metal chloride-induced hydrogen transfer enables efficient conversion of aromatic hydrocarbons for sodium storage. Adv. Funct. Mater. 34(48), 2408242 (2024). https://doi.org/10.1002/adfm.202408242