# Supporting Information for

Low-Temperature CH4 Reforming and Water Splitting with Activated NiO/CeO2 as Oxygen Carrier

Chunli Han1*, Akira Yoko1,2*, Yi-Ping Chang3, Manuel Harder3, Kakeru Ninomiya2, Maiko Nishibori2, Zhong Yin2, Ardiansyah Taufik1, Satoshi Ohara4, and Tadafumi Adschiri1,4*

1 World Premier International Research Center Initiative-Advanced Institute for Materials Research (WPI-AIMR), Tohoku University, Sendai, 980-8577, Japan

2 International Center for Synchrotron Radiation Innovation Smart, Tohoku University, Sendai, 980-8572, Japan

3 European XFEL GmbH, Holzkoppel 4, 22869 Schenefeld, Germany

4 New Industry Creation Hatchery Center, Tohoku University, Sendai, 980-8579, Japan

* Corresponding authors. E-mail: han_chunli@126.com (Chunli Han); akira.yoko.c7@tohoku.ac.jp (Akira Yoko); tadafumi.ajiri.b1@tohoku.ac.jp (Tadafumi Adschiri)

Supplementary Figures and Tables

Fig. S1 TEM images of (a) cubic CeO2, (b) commercial CeO2, and (c) ZrO2 nanoparticles

Fig. S2 Schematic diagram of the continuous-flow fixed-bed catalyst analyzer

Fig. S3 Saturated vapor pressure curve of H2O [S1]

Fig. S4 Calibration curves of mass spectra for CH4 (m/z=15), H2 (m/z=2), CO (m/z=28), and CO2 (m/z=44)

Fig. S5 Mass spectrometry background curves obtained under the same temperature program as the CL POM-WS cycles, without loading oxygen carriers

During the WS step (Ar+H2O), the introduction of steam caused some impurity peaks (purple sharp peaks, m/z = 28), which were attributed to N2 introduced from the steam bubbler. The areas of these impurity peak in the background curves closely matched those observed in the actual CL POM-WS measurements. Therefore, we assigned these intermittent sharp peaks to N2 contamination originating from the steam bubbler.

Fig. S6 (a) TEM images, and (b) Raman spectrum of the 6.5NiO/cCeO2 OC after reaction with CH4 at 600 °C

Fig. S7 Reaction performance of the activated 2.1NiO/cCeO2 OC. (a) 620 °C, (b) 650 °C, (c) 800 °C

Fig. S8 Investigation of the activation inducing factors: (a) Reaction performance of a control sample (2.5NiO/cCeO2-700) at 600 °C, prepared by calcination at 700 °C for 4h, (b) CH4 substituted by H2 during the reduction step, (c) steam substituted by O2 during the reoxidation step, (d) OC reaction performance at 700 °C during POM-WS cycles, (e) Comparison of H2 generation amounts in the POM step using steam and O2 for reoxidation

Fig. S9 Five-cycle CL POM-WS activation processes of NiO/cCeO2 OCs with varying Ni loading amounts

Fig. S10 (a) Raman spectra of 2.5NiO/cCeO2 OC before and after activation. The F2g mode could be attributed to the fluorite cubic structure of CeO2.[2] During activation, there was no carbon deposition. (b, c) CH4/H2O(g)-TPR curves of the activated 2.5NiO/cCeO2 OC with and without atmospheric exposure

Fig. S11 Reaction performance of the activated 2.5NiO/cCeO2 OC at 500 °C

Table S1 Reaction stability of the activated 2.5NiO/cCeO2 OC at 500 °C

|  | POM |  |  |  | WS |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | H2-POM umol/gOC | CO selectivity/% | H2:CO | H2-WS umol/gOC |  | H2 purity/% |
| cycle-1 | 292.2 | 94.8 | 2.8 | 97.1 |  | 98.9 |
| cycle-2 | 274.4 | 95.0 | 2.9 | 96.4 |  | 99.3 |
| cycle-3 | 274.8 | 94.7 | 2.9 | 97.1 |  | 99.4 |
| cycle-4 | 274.0 | 95.3 | 2.8 | 104.2 |  | 99.5 |
| cycle-5 | 273.7 | 95.5 | 2.8 | 111.2 |  | 99.7 |

Fig. S12 Coke deposition amounts during the POM step with varying Ni loading amounts

Fig. S13 Long-term stability evaluation of 2.5NiO/cCeO2 OC at 550 °C. (a) H2 generation amounts in the POM and WS steps over 33 cycles (POM: 10 min, WS: 5 min). (b) CO selectivity, H2:CO molar ratio in the POM step, and H2 purity in the WS step over 33 cycles

Fig. S14 Raman spectra of 2.5NiO/cCeO2 OC after long-term test at 600 °C and 550 °C

Fig. S15 Effects of the support nanoparticles on the OC performance. (a, b) Reaction performances of 2.5NiO/cCeO2 OC and 2.5NiO/ZrO2 OC at 700 °C, (c, d) H2 generation amount and H2:CO molar ratio in the POM step, and (e, f) H2 generation amount and H2 purity in the WS step with NiO/cCeO2 and NiO/ZrO2 as OC at 700 °C

Table S2 Comparison of the reaction performance of 2.5NiO/cCeO2 OC with several representative OCs for the CL methane reforming

| Oxygen carrier | T /°C | POM |  |  | WS |  | Refs. |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Syngas mmol/gOC | H2:CO | CO selectivity/% | H2 mmol/gOC | H2 purity/% |  |
| 2.5NiO/cCeO2 (POM: 20 min, WS: 10 min) a | 600 | 3.6 | 1.9 | 98.7 | 1.0 | 99.1 | This work |
|  | 700 | 6.0 | 1.9 | 98.8 | 1.4 | 99.9 |  |
|  | 800 | 7.8 | 1.9 | 99.4 | 1.9 | 97.0 |  |
| Ni-MoCxOy | 500 | — | 2.0 | 99 | — | — | Chem, 2023 [S3] |
|  | 800 | — | 4.9 | 44 | — | — |  |
| Ni/rABO3 | 570 | — | 2.0 | 80 | — | — | Angew. Chem. Int. Ed., 2020 [S4] |
| 0.5 wt% Rh-LaCeO4−x | 650 | 0.5 | — | 90 | — | — | Adv. Energy. Mater., 2019 [S5] |
| Ni1.5Mg1.5Al-MMO | 700 | 5.8 | 2.3-2.4 | 90-96 | — | — | J. Catalysis, 2026 [S6] |
| LaFe0.5Ni0.5O3 | 700 | 6.7 | ~3.6 | 50.0 | — | — | ACS Catalysis, 2024 [S7] |
| LaCo0.6Fe0.4O3 | 700 | 3.3 | 1.8 | 92.0 | 2.2 | 99.3 | Energ. Conv. Manage., 2020 [S8] |
| 10%CeO2/3DOM LaFeO3 | 800 | 9.9 | 2.0 | 90.0 | 3.4 | ~100 | Appl. Catal. B-Environ. Energy, 2017 [S9] |
| 0.5LaMn0.8Al0.2O3+δ/ LaMn0.7Co0.3O3+δ | 850 | 2.4 | 2.0 | 83.6 | 1.1 | ~100 | Fuel, 2025 [S10] |
| Ca2Fe1.4Al0.6O5 | 850 | 6.9 | 2.0 | 95.5 | 3.16 | 95.4 | Appl. Surf. Sci., 2025 [S11] |
| La0.6Ce0.4Mn0.7Ni0.3O3 | 850 | 4.5 | 2.0 | 60.0 | 2.9 | ~100 | Fuel, 2024 [S12] |
| LaFeO3 | 900 | 4.6 | 2.0 | 97.0 | — | — | Nature Communications, 2024 [S13] |

a. The values were summarized based on Fig. 4a-d.

Fig. S16 Gas generation rate curves using 1 wt%Pt/cCeO2 as OC

Fig. S17 C 1s XPS spectra of the fresh, activated, and long-term used 2.5NiO/cCeO2 OCs

Fig. S18 (a) O 1s XPS spectra of the activated OCs with varying Ni loading amounts. (b) Fitting of O 1s XPS spectrum. Oα and Oβ at 529.1 eV and 531.2 eV represent the CeO2 lattice oxygen and non-lattice oxygen (defective oxygen species, surface hydroxyls, adsorbed oxygen), respectively [S14-S16]. (c) Fitting of Ce 3d XPS spectrum. v0, u0, v′, and u′ represent Ce3+, and other peaks represent Ce4+ [S17]

Fig. S19 H2-TPR profiles of the activated 2.5NiO/cCeO2 and 2.5NiO/sCeO2 OCs

Supplementary References

- N. I. o. S. a. Technology, NIST Chemistry WebBook. 69 (2023).

- C. Andriopoulou, A. Trimpalis, K.C. Petallidou, A. Sgoura, A.M. Efstathiou et al., Structural and redox properties of Ce1–xZrxO2–δ and Ce0.8Zr0.15RE0.05O2–δ(RE: La, Nd, Pr, Y) solids studied by high temperaturein SituRaman spectroscopy. J. Phys. Chem. C 121(14), 7931–7943 (2017). https://doi.org/10.1021/acs.jpcc.7b00515

- X. Zhang, Y. Xu, Y. Liu, L. Niu, Y. Diao et al., A novel Ni–MoCxOy interfacial catalyst for syngas production via the chemical looping dry reforming of methane. Chem 9(1), 102–116 (2023). https://doi.org/10.1016/j.chempr.2022.09.007

- K. Kousi, D. Neagu, L. Bekris, E.I. Papaioannou, I.S. Metcalfe, Endogenous nanoparticles strain perovskite host lattice providing oxygen capacity and driving oxygen exchange and CH4 conversion to syngas. Angew. Chem. Int. Ed. 59(6), 2510–2519 (2020). https://doi.org/10.1002/anie.201915140

- V.P. Haribal, X. Wang, R. Dudek, C. Paulus, B. Turk et al., Modified ceria for “low-temperature” CO2 utilization: a chemical looping route to exploit industrial waste heat. Adv. Energy Mater. 9(41), 1901963 (2019). https://doi.org/10.1002/aenm.201901963

- J. Yuan, J. Cai, H. Zhao, H. Wang, K. Li, Selectivity control of NiO-based oxygen carriers for chemical looping methane anaerobic oxidation to syngas. J. Catal. 453, 116527 (2026). https://doi.org/10.1016/j.jcat.2025.116527

- R. Zhang, G. Liu, C. Huo, J. Liu, B. Zhang et al., Tailoring catalytic and oxygen release capability in LaFe1–xNixO3 to intensify chemical looping reactions at medium temperatures. ACS Catal. 14(10), 7771–7787 (2024). https://doi.org/10.1021/acscatal.4c01386

- M. Lee, H.S. Lim, Y. Kim, J.W. Lee, Enhancement of highly-concentrated hydrogen productivity in chemical looping steam methane reforming using Fe-substituted LaCoO3. Energy Convers. Manag. 207, 112507 (2020). https://doi.org/10.1016/j.enconman.2020.112507

- Y. Zheng, K. Li, H. Wang, D. Tian, Y. Wang et al., Designed oxygen carriers from macroporous LaFeO3 supported CeO2 for chemical-looping reforming of methane. Appl. Catal. B Environ. 202, 51–63 (2017). https://doi.org/10.1016/j.apcatb.2016.08.024

- X. Yin, Y. Sang, S. Wang, L. Shen, Regulation of oxidation state of LaMn0.8Al0.2O3+δ/LaMn0.7Co0.3O3+δ oxygen carriers for chemical looping steam methane reforming. Fuel 397, 135479 (2025). https://doi.org/10.1016/j.fuel.2025.135479

- Y. Zou, H. Liu, J. Liu, C. Wu, R. Li et al., Heterocoordination-driven regulation of Ca2Fe2O5 lattice oxygen for high selectivity syngas and hydrogen production via chemical looping. Appl. Surf. Sci. 703, 163411 (2025). https://doi.org/10.1016/j.apsusc.2025.163411

- J. Ji, L. Shen, Enhanced co-production of high-quality syngas and highly-concentrated hydrogen via chemical looping steam methane reforming over Ni-substituted La0.6Ce0.4MnO3 oxygen carriers. Fuel 368, 131588 (2024). https://doi.org/10.1016/j.fuel.2024.131588

- J. He, T. Wang, X. Bi, Y. Tian, C. Huang et al., Subsurface A-site vacancy activates lattice oxygen in perovskite ferrites for methane anaerobic oxidation to syngas. Nat. Commun. 15(1), 5422 (2024). https://doi.org/10.1038/s41467-024-49776-y

- J. Li, Z. Liu, D.A. Cullen, W. Hu, J. Huang et al., Distribution and valence state of Ru species on CeO2 supports: support shape effect and its influence on CO oxidation. ACS Catal. 9(12), 11088–11103 (2019). https://doi.org/10.1021/acscatal.9b03113

- H. Idriss, On the wrong assignment of the XPS O1s signal at 531–532 eV attributed to oxygen vacancies in photo- and electro-catalysts for water splitting and other materials applications. Surf. Sci. 712, 121894 (2021). https://doi.org/10.1016/j.susc.2021.121894

- D.J. Morgan, Photoelectron spectroscopy of ceria: Reduction, quantification and the myth of the vacancy peak in XPS analysis. Surf. Interface Anal. 55(11), 845–850 (2023). https://doi.org/10.1002/sia.7254

- Y. Zhu, G. Seong, T. Noguchi, A. Yoko, T. Tomai et al., Highly Cr-substituted CeO2 nanoparticles synthesized using a non-equilibrium supercritical hydrothermal process: high oxygen storage capacity materials designed for a low-temperature bitumen upgrading process. ACS Appl. Energy Mater. 3(5), 4305–4319 (2020). https://doi.org/10.1021/acsaem.0c00026