Nano-Micro Letters

Supporting Information for

Carbon Dots Intercalated MXene for Flexible Organic Hydrogel Absorbers with Synergistically Enhanced Dielectric Loss 

Bokai Lu1, Guangkai Jin1, Yuhong Cui1, Tianyi Zhang1, Shujuan Liu1, Qian Ye1, *, Xuqing Liu1, *, Feng Zhou1, 2 

1 State Key Laboratory of Solidification Processing, Center of Advanced Lubrication and Seal Materials, School of Materials Science and Engineering, Northwestern Polytechnical University, Xi'an 710072, P. R. China

2 State Key Laboratory of Solid Lubrication, Lanzhou Institute of Chemical Physics, Chinese Academy of Sciences, Lanzhou 730000, P. R. China
*Corresponding authors. E-mail: yeqian213@nwpu.edu.cn (Qian Ye); xqliu@nwpu.edu.cn (Xuqing Liu)
S1 Experimental section
S1.1 Characterization
The 2D layered structure and surface morphology of MXene, MXene/CDs, and the hydrogels were examined using scanning electron microscopy (SEM, ZEISS Sigma 300 and TESCAN MIRA). The morphology and microstructure of these samples were characterized by double spherical aberration-corrected transmission electron microscopy (Themis Z) and field-emission transmission electron microscopy (TEM, Talos F200X). The thickness of MXene nanosheets was measured using atomic force microscopy (AFM, Dimension Icon). Crystal structure information was obtained by X-ray diffraction (XRD, Rigaku SmartLab SE). Surface chemical compositions of these samples were analyzed by X-ray photoelectron spectroscopy (XPS, PHI 5000 VersaProbe III). The UV-Vis absorbance spectra of TA and CDs were measured using a UV-Vis spectrophotometer (LAMBDA 365). The internal interactions within the organic hydrogels were analyzed by Fourier transform infrared spectroscopy (FT-IR, Thermo Fisher Scientific Nicolet iS20). Changes in the surface charge of these samples were evaluated using a Malvern Zetasizer Nano ZS. The composition and degree of carbonization of MXene and MXene/CDs were investigated by Raman spectroscopy (WITec Alpha300R). The mechanical properties of the hydrogels were assessed at room temperature using a computer-controlled electronic universal testing machine (CMT2502). Electromagnetic parameters of the obtained composites were measured by the waveguide method using a vector network analyzer (Anritsu MS4644A). The electrical conductivity of the samples was measured at room temperature using an ST2643 ultra‑high‑resistance micro‑current tester equipped with an ST2643‑F01 standard annular three‑electrode probe.
S1.2 Microwave absorption test
According to the transmission line theory, attenuation constant can be expressed as [S1]: 
[image: image2.png]a = \Fﬂf \/(uﬂ " ursr) +\/(u” " ursr)z + (ursﬂ + urler)z



            (S1)
Where f represents the frequency of electromagnetic wave, c is the speed of light.
RL and impedance matching (Z) can be calculated through the following formulas [S2, S3]: 
[image: image4.png]7 = Zm

= VI / & tanh[j(2nfd / o)V g



                          (S2)
[image: image6.png]Zin=Zo
Zin+Zy

RL(dB) = 20 log,q




                                          (S3)
Where Zin is the input impedance of absorber, Z0 is the impedance of free space,d is the thickness of absorber.
S2 Supplementary Figures and Tables
  [image: image7.jpg]a 01s blc*s R TA
C1s
= )
s a
z z
'g £ cc CDs
2 2 C-oH \
£ 2l ic-0
TA = | =
800 600 400 200 0 294 202 200 288 286 284 282 280

Binding Energy (eV)

Blinding Energy (eV)




Fig. S1 a XPS full spectra of TA and CDs. b High-resolution XPS spectra of O 1s of TA and CDs
[image: image8.jpg]Absorbance

—TA
CDs

400

500 600
Wavelength (nm)

700




Fig. S2 UV-Vis spectra of TA and CDs solution
  [image: image9.jpg]



Fig. S3 SEM images of a MAX phase, b MXene and c MXene/CDs
 [image: image10.jpg]MXene/CDs
TiO,

[ iTi-0

[ -oH

O1s

MXene

Intensity (a.u)

538 536 534 532 530
Binding Energy (eV)

528

526




Fig. S4 High-resolution XPS spectra of O 1s of MXene and MXene/CDs
 [image: image11.jpg]Transmittance

MXene

4000 3500 3000

2500 2000 1500

Wavenumber (cm™)

1000

500




Fig. S5 FTIR spectra of MXene and MXene/CDs
 [image: image12.jpg]



Fig. S6 SEM images of a blank gel, b MXene gel and c MXene/CDs gel

 
[image: image13.jpg]Attenuation constant

150

Blank gel
MXene gel
MXene/CDs gel

90

9 10 1
Frequency (GHz)

12





Fig. S7 The attenuation constant of blank gel, MXene gel and MXene/CDs gel
[image: image14.jpg]20

=1.0

0.5

0.0

Frequency (GHz)

Frequency (GHz)

1.0 1.0
= Blank gel b = Blank gel c = Blank gel
© MXene gel + MXene gel © MXene gel
MXene/CDs gel MXene/CDs gel MXene/CDs gel
05 05
—— - - D it B D st
- — L 00 = 0.0 —— =
-0.5 -05
-1.0 -1.0
10 1 12 10 1 12 10 1 12

Frequency (GHz)




Fig. S8 The a μ ', b μ'' and c tanδμ of blank gel, MXene gel and MXene/CDs gel
[image: image15.jpg][ | MXene gel
.8|  MXene/CDs gel

[ | Blank gel

0 - < ~ e
(22} N N - o o
(wys .01 %) AyAONpUOD [eOL3O3]T




Fig. S9 The electrical conductivity of blank gel, MXene gel and MXene/CDs gel
[image: image16.jpg][ Blank gel
[ MXene gel

" MXenel/CDs gel




Fig. S10 RL comparison of blank gel, MXene gel and MXene/CDs gel at the same thickness
Table S1 Typical absorbing material and their microwave absorbing properties
	Materials
	Thickness
(mm)
	EAB
(GHz)
	RLmin (dB)
	References

	A6G20T20-2 hydrogel
	2.7
	4.2
	-33.8
	[S4]

	Magnetic cationic hydrogel
	2.5
	5.2
	-45.9
	[S5]

	PI/MXene-S aerogel
	2.5
	5.4
	-33.5
	[S6]

	ZIF hydrogel
	2.19
	6.59
	-23.1
	[S7]

	rGO-MCNTs-Fe3O4 hydrogel
	2.0
	11.4
	-36
	[S8]

	Acid-doped PCPU
	2.5
	5.3
	-27.9
	[S9]

	MXene/CDs hydrogel
	3.1
	3.5
	-47.9
	This work


Supplementary References 
[S1] Y. Ma, Y. Jiang, C. Wang, B. Bao, G. Chen et al., Prune-like MoS2/CoS/GNs composites: a potential ultra-thin wave absorber. J. Alloys Compd. 971, 172679 (2024). https://doi.org/10.1016/j.jallcom.2023.172679 
[S2] M. Qin, L. Zhang, H. Wu, Dual-template hydrothermal synthesis of multi-channel porous NiCo2O4 hollow spheres as high-performance electromagnetic wave absorber. Appl. Surf. Sci. 515, 146132 (2020). https://doi.org/10.1016/j.apsusc.2020.146132 
[S3] X. Zhang, Z. Jia, F. Zhang, Z. Xia, J. Zou et al., MOF-derived NiFe2S4/Porous carbon composites as electromagnetic wave absorber. J. Colloid Interface Sci. 610, 610–620 (2022). https://doi.org/10.1016/j.jcis.2021.11.110 
[S4] Y. Zhang, L. Zhang, B. Zhou, Y. Gao, B. Zhang, Polarization-driven multifunctional organohydrogels with strain sensitivity toward electromagnetic wave absorption. Nano Res. 17(6), 5688–5697 (2024). https://doi.org/10.1007/s12274-024-6403-0 
[S5] H. Yuan, Y. Zhang, G. Lu, F. Chen, T. Xue et al., Transparent organogel based on photopolymerizable magnetic cationic monomer for electromagnetic wave absorbing. J. Ind. Eng. Chem. 109, 538–546 (2022). https://doi.org/10.1016/j.jiec.2022.02.039 
[S6] W. Zhang, E. Ding, W. Zhang, J. Li, C. Luo et al., Microstructure controllable polyimide/MXene composite aerogels for high-temperature thermal insulation and microwave absorption. J. Mater. Chem. C 11(28), 9438–9448 (2023). https://doi.org/10.1039/D3TC01210G
[S7] H. Huang, G. Chen, Z. Li, S. Hui, L. Zhang et al., Constructing multi-polarization in metal–organic framework gels for electromagnetic wave absorption via ethanolamine hetero-coordination. Appl. Surf. Sci. 677, 161052 (2024). https://doi.org/10.1016/j.apsusc.2024.161052 
[S8] H. Zhang, M. Hong, P. Chen, A. Xie, Y. Shen, 3D and ternary rGO/MCNTs/Fe3O4 composite hydrogels: Synthesis, characterization and their electromagnetic wave absorption properties. J. Alloys Compd. 665, 381–387 (2016). https://doi.org/10.1016/j.jallcom.2016.01.091 
[S9] S. Yuan, J. Yang, Study on the mechanism, properties, and application asEMW-absorbing matrix materials of protonic acid-doped heat-resistant conductive polyurethanes. J. Appl. Polym. Sci. 143, e57959 (2026). https://doi.org/10.1002/app.57959  
S11/S6

