Supporting Information for

Directional Reconstruction of Spent Lithium Cobalt Oxide by Microwave Plasma: Efficient Oxygen Evolution Catalyst from Closed-Loop Recovered Resources

Chao Chen1,2, Qixuan Zhu2, Minghui Shan2, Lei Cheng2, Weiwei Wang2, Zhiqiang Lu2, Yi Wang2, Hengda Sun1,2, Yusuke Yamauchi4, 5, 6, Jing Tang3*, Guiyin Xu1,2*

1 Henan Academy of Sciences, School of Materials Science and Engineering, Zhengzhou University, Henan 450052, P. R. China

2 State Key Laboratory of Advanced Fiber Materials, College of Materials Science and Engineering, Donghua University, Shanghai 201620, P. R. China

3 State Key Laboratory of Petroleum Molecular and Process Engineering, Shanghai Key Laboratory of Green Chemistry and Chemical Processes, School of Chemistry and Molecular Engineering, East China Normal University, Shanghai 200062, P. R. China

4 Australian Institute for Bioengineering and Nanotechnology (AIBN) and School of Chemical Engineering, The University of Queensland, Brisbane, Queensland 4000, Australia

5 Department of Materials Process Engineering, Graduate School of Engineering, Nagoya University, Nagoya, Japan

6 Department of Chemical and Biomolecular Engineering, Yonsei University, 50 Yonsei-ro, Seodaemun-gu, Seoul 03722, South Korea

*Corresponding authors. E-mail: jingtang@chem.ecnu.edu.cn (Jing Tang); xuguiyin@dhu.edu.cn (Guiyin Xu)

Supplementary Figures and Tables

Fig. S1 a SEM images of Co3O4. b SEM images of NiFe-LDH

Fig. S2 a HRTEM images of NiFe-LDH. b HRTEM images of Co3O4/NiFe-LDH

Fig. S3 a HRTEM images of (110) crystal planes. b Corresponding IFFT patterns and lattice distance of a. c Corresponding FFT patterns of the selected regions marked of a. d The corresponding lattice spacing distances transferred by fast Fourier transform

Fig. S4 a HRTEM images of (311) crystal planes. b Corresponding IFFT patterns and lattice distance of a. c Corresponding FFT patterns of the selected regions marked of a. d The corresponding lattice spacing distances transferred by fast Fourier transform

Fig. S5 XPS spectra of Co 2p in Co3O4/NiFe-LDH (Co2+ 785.3 eV, Co3+ 780.6 eV)

Fig. S6 Digital photos of bare NF, treated NF, NiFe-LDH and Co3O4/NiFe-LDH

Fig. S7 Cyclic voltammogram (CV) curves of Co3O4/NiFe-LDH

Fig. S8 Linear sweep voltammetry (LSV) curves of Co3O4/NiFe-LDH and Co3O4+NiFe-LDH-mix

Fig. S9 Cyclic voltammogram (CV) curves of a Co3O4/NiFe-LDH. b NiFe-LDH. c Co3O4 at different scan rates (10 ~ 50 mV s-1) in alkaline media

Fig. S10 ECSA-normalized polarization curves of Co3O4/NiFe-LDH and NiFe-LDH

Fig. S11 SEM image of Co3O4/NiFe-LDH after the test

Fig. S12 Elemental mappings of Co3O4/NiFe-LDH catalysts after the test

Fig. S13 FTIR spectra of Co3O4/NiFe-LDH before and after catalytic reaction

Fig. S14 Stability test of the IrO2 for OER at 10 mA cm−2 in 1.0 M KOH

Fig. S15 Digital photos of electrolytic cell

Fig. S16 XRD spectra of Co3O4/NiFe-LDH before and after catalytic reaction

Fig. S17 High-resolution a Co 2p. b Ni 2p and c Fe 2p XPS spectra of Co3O4/NiFe-LDH before and after the stability test

Fig. S18 The stability test of Co3O4/NiFe-LDH in 30 wt% KOH at 500 mA cm−2

Fig. S19 Optimal crystal structural models of a Co3O4. b NiFe-LDH. c Co3O4/NiFe-LDH. The blue, gray and yellow spheres represent Co, Ni and Fe atoms, respectively

a

b

b

c

Fig. S20 Optimized optimal crystal structural models of a Co3O4. b NiFe-LDH. c Co3O4/NiFe-LDH

Fig. S21 Charge density difference analysis. Yellow isosurfaces represent regions of electron accumulation. (Isosurface value: 0.1-1)

Table S1 The element content of Co3O4/NiFe-LDH catalysts determined from ICP-OES results

| Element | ppm | molar ratios |
| --- | --- | --- |
| Co | 3.03 | 1 |
| Ni | 31.9 | 10.58 |
| Fe | 9.67 | 3.37 |

Table S2 The element content of Co3O4/NiFe-LDH catalysts determined from EDS mapping

| Sample | Co/wt% | Ni/ wt% | Fe/ wt% | O/ wt% |
| --- | --- | --- | --- | --- |
| Co3O4/NiFe-LDH | 5.11 | 49.23 | 9.68 | 35.99 |
| After test | 5.01 | 49.03 | 9.60 | 36.37 |

Table S3 Comparisons of OER performance of various electrocatalysts in 1.0 M KOH

| Sample | E η10 (mV) | E η10-noble metal (mV) | References |
| --- | --- | --- | --- |
| Co3O4/NiFe-LDH | 235 | 306 (IrO2) | This work |
| Co3O4/NiFe-LDH-2 | 238 | 306 (IrO2) | This work |
| WQ-Co3O4-400 | 306 | 309 (RuO2) | [S1] |
| Fe-Co3O4 NBs | 254 | 292 (IrO2) | [S2] |
| CoFeV | 266 | ~280 (IrO2) | [S3] |
| NdNi-Co3O4 | 269 | 292 (RuO2) | [S4] |
| Co3O4@Fe1-NC | 318 | -- | [S5] |
| W-Co3O4 | 390 | -- | [S6] |
| Co/Co3O4/CoF2@NSC-CC | 310 | 340 (RuO2) | [S7] |
| Co3O4-VCo | 262 | -- | [S8] |
| Co3C | 330 | -- | [S9] |
| RCO-VO@CC | 253 | -- | [S10] |
| CoFe-FeNC | 296 | 330 (IrO2) | [S11] |
| NiCoS | 248 | 321 (RuO2) | [S12] |
| ELFP-Ni | 250 | 290 (RuO2) | [S13] |
| Fe-LCO/Co3O4 | 312 | 325 (IrO2) | [S14] |
| NCO@7CQDs | 330 | 517 (RuO2) | [S15] |
| FCN-TM/NC | 270 | 314 (RuO2) | [S16] |

Table S4 Comparison of our work with recently reported OER catalysts for AWE electrolyzers in 30 wt% KOH

| Cathode//Anode Catalysts | Temperature (C) | Area (cm2) | Voltage (V) | References |
| --- | --- | --- | --- | --- |
| NF//Co3O4/NiFe-LDH | 80 | 1 | 1.74 @ 0.2 A cm-2 | This work |
| NF//Ni(OH)2 | N/A | N/A | 2.05 @ 1 A cm-2 | [S17] |
| Ni(OH)2TPE //Ni(OH)2TPE | 80 | N/A | 1.8 @ 0.91 A cm-2 | [S18] |
| Ni3S2 /NM-I//Ni3S2/NM-I | 80 | 4 | 1.8 @ 1 A cm-2 | [S19] |
| Co,P-MoS2@NiO// Co,P-MoS2@NiO | 60 | N/A | 1.82 @ 1 A cm-2 | [S20] |
| R-Ni//FeNiHOF | 60 | N/A | 1.81 @1 A cm-2 | [S21] |
| WMo-CoP@NM//NM | 85 | N/A | 2 @1.25 A cm-2 | [S22] |

Supplementary References

- Z. Wang, Z. Li, J. Zhong, B. Zhou, J. Liu et al., A low-temperature solid-to-solid reaction for lithium-ion battery recycling and the utilization of defect-enriched Co3O4 from spent LiCoO2 batteries for efficient oxygen evolution reaction. Appl. Catal. B Environ. Energy 349, 123873 (2024). https://doi.org/10.1016/j.apcatb.2024.123873

- D. Zhao, G.-Q. Yu, J. Xu, Q. Wu, W. Zhou et al., Preparing iron oxide clusters surface modified Co3O4 nanoboxes by chemical vapor deposition as an efficient electrocatalyst for oxygen evolution reaction. Energy Storage Mater. 66, 103236 (2024). https://doi.org/10.1016/j.ensm.2024.103236

- K. Yeom, J. Jo, H. Shin, H. Ji, S. Moon et al., Unraveling surface reconstruction during oxygen evolution reaction on the defined spinel oxide surface. Adv. Funct. Mater. 34(36), 2401095 (2024). https://doi.org/10.1002/adfm.202401095

- T. Li, Z. Wang, L. Wang, M. Wang, Y.-Q. Liu, Nd and Ni Co-doped spinel Co3O4 nanosheet as an effective electrocatalyst for oxygen evolution reaction. Appl. Catal. B Environ. Energy 352, 123990 (2024). https://doi.org/10.1016/j.apcatb.2024.123990

- Y. Xie, Y. Feng, S. Zhu, Y. Yu, H. Bao et al., Modulation in spin state of Co3O4 decorated Fe single atom enables a superior rechargeable zinc-air battery performance. Adv. Mater. 37(5), 2414801 (2025). https://doi.org/10.1002/adma.202414801

- T. Tran-Phu, M. Chatti, J. Leverett, T.K.A. Nguyen, D. Simondson et al., Understanding the role of (W, Mo, Sb) dopants in the catalyst evolution and activity enhancement of Co3O4 during water electrolysis via in situ spectroelectrochemical techniques. Small 19(25), e2208074 (2023). https://doi.org/10.1002/smll.202208074

- H. Li, G. Yan, H. Zhao, P.C. Howlett, X. Wang et al., Earthworm-inspired Co/Co3O4/CoF2@NSC nanofibrous electrocatalyst with confined channels for enhanced ORR/OER performance. Adv. Mater. 36(26), 2311272 (2024). https://doi.org/10.1002/adma.202311272

- R. Zhang, L. Pan, B. Guo, Z.-F. Huang, Z. Chen et al., Tracking the role of defect types in Co3O4 structural evolution and active motifs during oxygen evolution reaction. J. Am. Chem. Soc. 145(4), 2271–2281 (2023). https://doi.org/10.1021/jacs.2c10515

- Y. Oh, J. Theerthagiri, A. Min, C.J. Moon, Y. Yu et al., Pulsed laser interference patterning of transition-metal carbides for stable alkaline water electrolysis kinetics. Carbon Energy 6(5), e448 (2024). https://doi.org/10.1002/cey2.448

- W. Tian, X. Xie, X. Zhang, J. Li, G.I.N. Waterhouse et al., Synergistic interfacial effect of Ru/Co3O4 heterojunctions for boosting overall water splitting. Small 20(27), 2309633 (2024). https://doi.org/10.1002/smll.202309633

- S. Zhang, J. Yang, L. Yang, T. Yang, Y. Liu et al., Boosting ORR/OER bifunctional electrocatalysis by promoting electronic redistribution of Fe-N-C on CoFe-FeNC for ultra-long rechargeable Zn-air batteries. Appl. Catal. B Environ. Energy 359, 124485 (2024). https://doi.org/10.1016/j.apcatb.2024.124485

- M. Chen, Y. Wang, Y. Zhou, B. Guo, L. Wang et al., Efficient metal recovery and electrocatalyst fabrication from spent lithium-ion batteries via green solvent extraction. Green Chem. 27(18), 5126–5135 (2025). https://doi.org/10.1039/d5gc00073d

- J. Liu, Z. Liu, Z. Xiao, Y. Zhu, J. Wang et al., Iodine-mediated redox strategy for sustainable lithium extraction from spent LiFePO4 cathodes. Adv. Mater. 37(26), 2503450 (2025). https://doi.org/10.1002/adma.202503450

- G. Zhang, C. Ye, T. Li, S. Liu, W.-H. Huang et al., Quenching-induced Fe doping on spent cathode materials enhances the oxygen evolution reaction performance. Energy Storage Mater. 80, 104430 (2025). https://doi.org/10.1016/j.ensm.2025.104430

- Q. Liang, Y. Liu, H. Kang, L. Zhou, C. Wang et al., Waste to wealth: Spent LIB anode graphite saved to carbon quantum dots strongly coupled NiCo2O4 catalysts for efficient water oxidation. Chem. Eng. J. 525, 170376 (2025). https://doi.org/10.1016/j.cej.2025.170376

- W. Liu, Z. Liang, S. Jing, J. Zhong, N. Liu et al., Asymmetrical triatomic sites with long-range electron coupling for ultra-durable and extreme-low-temperature zinc-air batteries. Angew. Chem. Int. Ed. 64(21), e202503493 (2025). https://doi.org/10.1002/anie.202503493

- J. Kang, G. Liu, Q. Hu, Y. Huang, L.-M. Liu et al., Parallel nanosheet arrays for industrial oxygen production. J. Am. Chem. Soc. 145(46), 25143–25149 (2023). https://doi.org/10.1021/jacs.3c05688

- W. Kuang, Z. Cui, C. Wang, T. Chen, Q. Wang et al., Self-supported Ni/Ni(OH)2 electrodes for high-performance alkaline and AEM water electrolysis. Adv. Energy Mater. 15(14), 2406080 (2025). https://doi.org/10.1002/aenm.202406080

- W. He, Y. Wang, Y. Zhao, C. Tang, L. Cong et al., Heterointerface-enabled anti-reverse-current electrodes for alkaline water electrolyzers at 1000 mA cm-2. J. Am. Chem. Soc. 148(5), 5232–5242 (2026). https://doi.org/10.1021/jacs.5c17603

- H. Li, J. Xia, J. Zheng, X. Bai, Q. Ren et al., Synergistic co and P co-doping in MoS2/NiO heterostructures for electronic modulation toward high-performance alkaline water electrolysis. Adv. Funct. Mater. e25383 (2025). https://doi.org/10.1002/adfm.202525383

- Y. Chen, Q. Li, Y. Lin, J. Liu, J. Pan et al., Boosting oxygen evolution reaction by FeNi hydroxide-organic framework electrocatalyst toward alkaline water electrolyzer. Nat. Commun. 15(1), 7278 (2024). https://doi.org/10.1038/s41467-024-51521-4

- G. Xu, M. Xing, Z. Qiao, M. Han, Y. Wu et al., Constructing ultra-stable electrocatalysts to achieve adaptability of industrial-level alkaline water electrolyzers for fluctuating renewable energies. Adv. Energy Mater. 15(31), 2500926 (2025). https://doi.org/10.1002/aenm.202500926