Supporting Information for

Adjacent-Site Proximity as a Dominant Activity Descriptor in Single-Atom Pt Catalysts for Hydrogen Evolution Reaction

Xue-Lu Chen1†, Yu-Yang Liu2†, Sudip Biswas1, Yi Yang1, Yi Shi3*, Chun-Gen Liu2*, Xing-Hua Xia1*

1State Key Laboratory of Analytical Chemistry for Life Science, School of Chemistry and Chemical Engineering, Nanjing University, Nanjing 210023, P. R. China

2Institute of Theoretical and Computational Chemistry, School of Chemistry and Chemical Engineering, Nanjing University, Nanjing 210023, P. R. China

3School of Chemistry and Molecular Engineering, East China Normal University, Dongchuan Road 500, Shanghai 200241, P. R. China

†Xue-Lu Chen and Yu-Yang Liu contributed equally to this work.

*Corresponding authors. Email: yshi@chem.ecnu.edu.cn (Yi Shi); cgliu@nju.edu.cn (Chun-Gen Liu); xhxia@nju.edu.cn (Xing-Hua Xia)

S1 Supplementary Calculation Notes

Note S1.1 Calculation of Mass Activity for HER (𝜂@100 mV)

PtSA-0.1/MoS2:

MA=67.45×0.07065×10-36.25×10-4×5.4 %=141.20 A mg-1  #

PtSA-0.14/MoS2:

MA=29.90×0.07065×10-36.25×10-4×4.0 %=84.50 A mg-1  #

PtSA-0.18/MoS2:

MA=6.06×0.07065×10-36.25×10-4×2.3 %=29.77 A mg-1  #

PtSA-0.24/MoS2:

MA=0.43×0.07065×10-36.25×10-4×1.2 %=4.05 A mg-1  #

PtSA-0.3/MoS2:

MA=0.3×0.07065×10-36.25×10-4×0.96 %=3.53 A mg-1  #

20% Pt/C:

MA=48.03×0.07065×10-32×8×10-3×20 %=1.06 A mg-1

Note S1.2 Calculation of TOFs for HER

PtSA-0.1/MoS2:

TOF(@0.05 V)=I2F×n=19.59×0.07065×10-32×96500×6.25×10-4×5.4 %×10-3195=41.45  S-1

TOF(@0.10 V)=67.45×0.07065×10-32×96500×6.25×10-4×5.4 %×10-3195=140.62  S-1

TOF(@0.15 V)=109.88×0.07065×10-32×96500×6.25×10-4×5.4 %×10-3195=232.50  S-1

PtSA-0.14/MoS2:

TOF(@0.05 V)=7.69×0.07065×10-32×96500×6.25×10-4×4.0 %×10-3195=22.00  S-1

TOF(@0.10 V)=29.90×0.07065×10-32×96500×6.25×10-4×4.0 %×10-3195=85.49  S-1

TOF(@0.15 V)=62.65×0.07065×10-32×96500×6.25×10-4×4.0 %×10-3195=179.16  S-1

PtSA-0.18/MoS2:

TOF(@0.05 V)=1.17×0.07065×10-32×96500×6.25×10-4×2.3 %×10-3195=5.79  S-1

TOF(@0.10 V)=6.06×0.07065×10-32×96500×6.25×10-4×2.3 %×10-3195=30.10  S-1

TOF(@0.15 V)=27.32×0.07065×10-32×96500×6.25×10-4×2.3 %×10-3195=135.69  S-1

PtSA-0.24/MoS2:

TOF(@0.05 V)=0.21×0.07065×10-32×96500×6.25×10-4×1.2 %×10-3195=2.02  S-1

TOF(@0.10 V)=0.43×0.07065×10-32×96500×6.25×10-4×1.2 %×10-3195=4.02  S-1

TOF(@0.15 V)=1.32×0.07065×10-32×96500×6.25×10-4×1.2 %×10-3195=12.57  S-1

PtSA-0.3/MoS2:

TOF(@0.05 V)=0.25×0.07065×10-32×96500×6.25×10-4×0.96 %×10-3195=3.07  S-1

TOF(@0.10 V)=0.3×0.07065×10-32×96500×6.25×10-4×0.96 %×10-3195=3.61  S-1

TOF(@0.15 V)=0.46×0.07065×10-32×96500×6.25×10-4×0.96 %×10-3195=5.55  S-1

S2 Supplementary DFT Notes

All density functional theory (DFT) calculations were performed using the VASP 5.4.4 package (1-3). The core-valence interaction was described by the projector augmented wave (PAW) (4) method with an energy cutoff of 500 eV. The exchange and correlation energies were calculated using the RPBE functional (5) with the generalized gradient approximation (GGA) (6). The k-point mesh was sampled using a 3×3×1 Monkhorst-Pack grid, while a (3×4) MoS2 monolayer structure was adopted for the surface simulation, with a slab length of 20 Å. This MoS2 (3×4) slab consisted of 12 Mo atoms and 24 S atoms, with the Mo atoms and bottom S atoms frozen during geometry optimization. The criteria for geometry optimization and self-consistent field convergence were set to 0.05 eV/Å and 10-6 eV, respectively. Zero-point energies and entropy contributions at room temperature (298.15 K) were calculated from vibrational degrees of freedom with the substrate fixed. All structure optimizations and energy calculations were carried out under vacuum conditions. The potential of zero charge (PZC) was the only property calculated in a solvation environment using the implicit solvation model VASPsol (7, 8). These calculations employed a symmetric slab model applied and a slab length of 50 Å. Atomic charges were computed using the atom-in-molecule (AIM) scheme proposed by Bader (9, 10). VASPkit (11) was used for pre-processing and post-processing of data. The Crystal orbital Hamilton population (COHP) (12, 13) and Crystal orbital Bond Index (COBI) (14) analysis were performed using the LOBSTER 3.1.0 package (15).

The ΔGH was adopted to theoretically evaluate the catalytic performance for HER, which was calculated by the following equation:

ΔGH=ΔE+ΔEZPE-TΔS				    (S-1)

where, ΔE is the hydrogen adsorption energy computed by the equation ΔE=E*H-E*-0.5E(H2), where E(*H) and E(*) are the total energies of the model with and without hydrogen adsorbed on the binding site *, respectively; and E(H2) is the total energy of the single hydrogen molecule. ΔEZPE is the correction of the zero-point energy, ΔS represents the difference between in entropies between the adsorbed state and the corresponding freestanding state and T is the absolute temperature (298.15 K in this study).

Note S2.1 Additional Information on Adsorption of Hydrogen Atom

Figure S31 illustrates the specific adsorption sites of H atoms on isolated Pt. Table S7 lists the detailed adsorption energy data for H atoms at different adsorption sites. Figure S32 provides a further insight in the cases where more than three H atoms adsorbed on Ptiso. When one Pt atom adsorbed with four H atoms, two of them were positioned at the distance of just 0.84 Å, indicating the presence of the physically adsorbed H2 molecule. It is worth noting that the adsorption energy of the structure with four adsorbed H atoms was reduced lower (0.0185 eV) when compared to the structure with two adsorbed H atoms. This suggests that the energy barrier for H2 desorption is extremely low. Consequently, we disregarded the adsorption of four or more H atoms on Ptiso in this context. Figure S33 and Table S8 reveal the adsorption behavior of H on Ptiso, considering the presence or absence of surrounding Pt atoms in Structure IV or Structure I. The results indicate that the adsorption of H on Ptiso still largely unaffected by the immediate environment. Table S9 presents data on the vibrational energy and entropy of the H adsorbed on Ptiso in both Structure I and IV, revealing that the environment surrounding the Pt atom has minimal influence.

Figure S34 depicts the adsorption sites of H on Ptadj, while Tables S10-S11 provide calculation results for adsorption energy, along with corresponding vibrational energy and entropy. As shown in Figure S35, there exist two distinct configurations when three H atoms are adsorbed on Ptadj. One of these configurations can trigger the Tafel reaction, while the other cannot. The energy difference between these configurations is small, allowing for the mutual conversion. Figure S36 shows the influence of varying environments on H adsorption energy on Ptadj. Specifically in Structure IV, there is a Ptiso site situated near the Ptadj. The Structure 3H@IV is referred to the case where three H atoms already adsorb on the Ptiso within Structure IV. Data presented in Table S12 highlights certain difference in H adsorption energy between Structure II and IV, while the results for Structure II and 3H@IV are remarkable resemblance. Given that Ptiso exhibits affinity for H adsorption compared to the top H on Ptadj, we believe that whenever top-H adsorption occurs on Ptadj, the Ptiso is already in a state of saturated H adsorption. Therefore, the Structure 3H@IV is more aligned with physical pictures. The resemblance in H adsorption energy findings on Ptadj between Structure II and 3H@IV further suggests that the adsorption environment exerts a limited influence on H adsorption energy on Ptadj.

Figures S37-S39 and Table S13 display the adsorption patterns of H on Ptiso and Ptadj based on a series of substrate materials. The representation of adsorption sites in these systems follows the method which is employed for MoS2. Our calculations reveal that the adsorption energy of top-H on Ptadj keep low data on various substrate materials, indicating excellent HER reaction activity, which agrees well with the experimental results.

Note S2.2 Additional Description of the Pt-H-Pt Three-Center Bonding.

Figure 4c displays the projected wave function derived from the PROCAR file computed by using VASP and visualized with VASPMO. This image depicts the orbitals of Pt and H atoms at an energy level of -7.35 eV relative to the Fermi energy. All pertinent calculations were anchored to the coordinate system displayed in Figure 4c, where the y-axis was aligned with Pt–H–Pt direction. Notably, the image incorporates the non-bonding 5dx2-y2 component, thereby influencing the shape of the visualized projected wave function. The “Pt–H–Pt” three-center bond had a ICOBI of 0.1053, which was comparable to that in Te–Ge–Te three-center bond (1). Figure S40 illustrates the main orbital components of the Pt-H-Pt three-center bond. Detailed analysis demonstrates that 6py-1s-6s (ICOBI=0.0721) constitutes the primary component of the three-center bond, while 6s-1s-6s (ICOBI=0.0266) also contributes to its formation. It is worth noting that although 5dyz-1s-6s (ICOBI=0.0251) of Pt 5dyz orbital makes a positive contribution to the three-center bond, 5dyz-1s-5dyz (ICOBI=-0.0388) offsets this contribution, indicating that the 5dyz orbital is unfavorable for the formation of the three-center bond. Then, we can get the conclusion that the three-center bond is formed by the H 1s orbital and two hybrid orbitals consist of Pt 6s and 6py orbitals.

Supplementary Figures

Fig. S1 (a) Low-magnified TEM image and (b) HR-TEM image of chemically exfoliated MoS2 (ce-MoS2). (c) Low-magnified TEM image of bulk MoS2. (d) AFM image of ultrathin MoS2 nanosheets and corresponding (e) height profiles of the regions of interest indicated in the AFM image. (f) Raman spectrum of the MoS2 sample

Fig. S2 (a) A 3D scheme of the electrochemical apparatus (the synthetic procedure was described in the method section). (b) CVs of the chemical exfoliated MoS2 in an Ar-saturated 0.1 M H2SO4 solution containing 2 mM CuSO4 (black line) or 0.1 M H2SO4 solution (red line) at a scan rate of 20 mV s−1. Peak a is attributed to Cu UPD, whereas peak b corresponds to the bulk deposition of Cu. (c) Corresponding chronoamperometry curves of CuSA-X/MoS2. (d) Potential-response curve of Cu adatoms within Pt precursor at the open-circuit potential

Fig. S3 (a) HAADF-STEM image of CuSA-0.1/MoS2, with red circles highlighting the single atoms of Cu distributed in the MoS2. (b) EDS mapping images, (c) EDS spectrum and (d) Cu 2p XPS spectrum of CuSA-0.1/MoS2 catalyst

Fig. S4 (a) Low-magnified TEM and (b) HR-TEM images of PtSA-MoS2. (c) HAADF-STEM image of PtSA-MoS2. (d) Amplified image of the region enclosed by the green circle of (c) and schematic structure of the unit cells of the 1T-phase MoS2. (e) Amplified image of the region enclosed by the yellow rectangle in (c) and schematic structure of the unit cells of the 2H-phase MoS2. (f) Raman spectrum of the ce-MoS2 sample and PtSA-MoS2 sample

Fig. S5 (a) HAADF-STEM image and (b) corresponding linear intensity distributions along lines of PtSA-0.1/MoS2

Fig. S6 (a) HAADF-STEM image and (b) corresponding linear intensity distributions along lines of PtSA-0.14/MoS2

Fig. S7 (a) HAADF-STEM image and (b) corresponding linear intensity distributions along lines of PtSA-0.18/MoS2

Fig. S8 (a) HAADF-STEM image and (b) corresponding linear intensity distributions along lines of PtSA-0.24/MoS2

Fig. S9 (a) HAADF-STEM image and (b) corresponding linear intensity distributions along lines of PtSA-0.3/MoS2

Fig. S10 HAADF-STEM images of (a) PtSA-0.1/MoS2, (b) PtSA-0.18/MoS2 and (c) PtSA-0.3/MoS2. Inset, Ptiso sites and Ptadj sites are respectively represented in green circle and yellow rectangle

Fig. S11 (a) Mo 3d and (b) S 2p XPS spectra of PtSA-0.1/MoS2 and ce-MoS2. (c) Pt 4f XPS spectra of PtSA-0.1/MoS2 and commercial Pt/C

Fig. S12 (a) Cu 2p, (b) Mo 3d and (c) S 2p XPS spectra of PtSA-X/MoS2

Fig. S13 (a) Fitting of the magnitude of the Fourier transform of the k3-weighted EXAFS (data-blue and fit-red) for PtSA-0.1/MoS2 and (b) corresponding EXAFS fitting curve at k space

Fig. S14 (a) Fitting of the magnitude of the Fourier transform of the k3-weighted EXAFS (data-blue and fit-red) for PtSA-0.14/MoS2 and (b) corresponding EXAFS fitting curve at k space

Fig. S15 (a) Fitting of the magnitude of the Fourier transform of the k3-weighted EXAFS (data-blue and fit-red) for PtSA-0.18/MoS2 and (b) corresponding EXAFS fitting curve at k space

Fig. S16 (a) Fitting of the magnitude of the Fourier transform of the k3-weighted EXAFS (data-blue and fit-red) for PtSA-0.24/MoS2 and (b) corresponding EXAFS fitting curve at k space

Fig. S17 (a) Fitting of the magnitude of the Fourier transform of the k3-weighted EXAFS (data-blue and fit-red) for PtSA-0.30/MoS2 and (b) corresponding EXAFS fitting curve at k space

Fig. S18 (a) Fitting of the magnitude of the Fourier transform of the k3-weighted EXAFS (data-blue and fit-red) for PtSA-X/MoS2 and Pt foil and (b) corresponding EXAFS fitting curves of samples and standard at k space

Fig. S19 Current-time curve of (a) PtSA-0.1/MoS2, (b) PtSA-0.14/MoS2, (c) PtSA-0.18/MoS2, (d) PtSA-0.24/MoS2, (e) PtSA-0.3/MoS2, and (f) ce-MoS2 before and after the injection of SCN- ions in Ar-saturated 0.5 M H2SO4 solution

Fig. S20 Chronoamperometry test of PtSA-0.1/MoS2 at -0.03 V for 20000 s in an Ar-saturated solution of 0.5 M H2SO4

Fig. S21 Comparison of HER activity for PtSA-0.1/MoS2 in 0.5 M H2SO4 solution with the state-of-the-art single-atom catalysts reported previously

Fig. S22 Pt 4f HR-XPS spectra of PtSA-X/MoS2 samples

Fig. S23 CVs of the ce-TMDs modified GCE in an Ar-saturated solution of 0.1 M H2SO4 + 2 mM CuSO4. Inset shows the photographs of good-dispersible ce-TMDs nanosheets suspension in water

Fig. S24 Conventional TEM images of the freshly prepared (a) PtSA-WS2, (b) PtSA-MoSe2 and (c) PtSA-WSe2 samples

Fig. S25 (a) HAADF-STEM images of PtSA-MoS2, PtSA-WS2, PtSA-MoSe2, and PtSA-WSe2 samples. (b) HER polarization curves of PtSA-MoS2, PtSA-WS2, PtSA-MoSe2, and PtSA-WSe2 samples in an Ar-saturated solution of 0.5 M H2SO4 at a scan rate of 50 mV s-1

Fig. S26 (a-b) Pt 4f XPS spectra of PtSA-WS2 and PtSA-WSe2

Fig. S27 HAADF-STEM images of (a) PtSA-0.1/WS2, (b) PtSA-0.3/WS2, (c) PtSA-0/WSe2 and (d) PtSA-0.2/WSe2 samples

Fig. S28 HER polarization curves and mass activity for (a, c) PtSA-X/WS2 and (b, d) PtSA-X/WSe2 samples in an Ar-saturated solution of 0.5 M H2SO4 at a scan rate of 20 mV s-1

Fig. S29 Four DFT slab models (a) Ptiso (Structure I), (b) Ptadj (Structure II), (c) two Ptiso (Structure III), and (d) one Ptiso plus one Ptadj (Structure IV) of various Pt loadings on MoS2

Fig. S30 DFT models of different numbers of (a) 3 Pt atoms, and (b) 4 Pt atoms in adjacent Pt atoms. It suggests that the adjacent effect of single atom Pt is universal

Fig. S31 Hydrogen adsorption sites (a, b and c sites in Table S7) on isolated Pt

Fig. S32 Four hydrogen atoms adsorption (the “a, 2b, c” structure in Table S7) on isolated Pt

Fig. S33 Adsorption energy of different H on isolated Pt at different structures

Fig. S34 Hydrogen adsorption sites (a-e sites in Table S10) on adjacent Pt

Fig. S35 Two different adsorption modes of 3H adsorption on adjacent Pt. (a) Two top-H adsorbed on two Pt atoms, (b) Two top-H adsorbed on one Pt atom

Fig. S36 (a) Adsorption energy of different H on adjacent Pt at different structures, and (b) DFT slab model of 3H@IV

Fig. S37 Hydrogen adsorption energies of the most stable structures on PtSA-MoSe2

Fig. S38 Hydrogen adsorption energies of the most stable structures on PtSA-WS2

Fig. S39 Hydrogen adsorption energies of the most stable structures on PtSA-WSe2

Fig. S40 Orbital-wise and total three-center COBI plots for Pt–H–Pt, corresponding to the structure of Ptadj with a bridge-H adsorption. The corresponding integrated ICOBI (ICOBI) values are given. The plot of 6py-1s-6s contains both 6py-1s-6s and 6s-1s-6py components. 5dyz-1s-6s is the same

Supplementary Tables

| Table S1 EXAFS fitting parameters of PtSA-X/MoS2 and Pt foil |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Sample | Path | CNa | R(Å)b | σ2 (Å2)c | ΔE0(eV)d | R factor |
| Pt L3-edge (Ѕ02=0.899) |  |  |  |  |  |  |
| Pt foil | Pt-Pt | 12* | 2.764±0.002 | 0.0050 | 8.2 | 0.0031 |
| PtSA-0.10/MoS2 | Pt-S | 4.3±0.2 | 2.245±0.011 | 0.0081 | 2.5 | 0.0120 |
| PtSA-0.14/MoS2 | Pt-S | 3.9±0.2 | 2.241±0.007 | 0.0063 | 0.9 | 0.0065 |
| PtSA-0.18/MoS2 | Pt-S | 4.2±0.2 | 2.234±0.010 | 0.0063 | 0.7 | 0.0091 |
| PtSA-0.24/MoS2 | Pt-S | 3.9±0.1 | 2.228±0.006 | 0.0060 | 2.6 | 0.0041 |
| PtSA-0.30/MoS2 | Pt-S | 4.4±0.2 | 2.230±0.009 | 0.0062 | 1.8 | 0.0046 |

Note: aCN, coordination number; bR, the distance between absorber and backscatter atoms; cσ2, the Debye Waller factor value; dΔE0, inner potential correction to account for the difference in the inner potential between the sample and the reference compound; R factor indicates the goodness of the fit. S02 was fixed to 0.899, according to the experimental EXAFS fit of Pt foil by fixing CN as the known crystallographic value. * This value was fixed during EXAFS fitting, based on the known structure of Pt. Fitting conditions: k range：2.0 - 10.5; R range: 1.1-2.5; fitting space: R space; k-weight = 3. A reasonable range of EXAFS fitting parameters: 0.800 < Ѕ02 < 1.000; CN > 0; σ2 > 0 Å2; |ΔE0| < 10 eV; R factor < 0.02.

Table S2 Comparison of HER activity for PtSA-0.1/MoS2 in 0.5 M H2SO4 solution with the state-of-the-art single-atom catalysts reported previously

| Catalyst | Tafel slope (mV dec-1) | Mass activity@ overpotential (A mgpt-1) | TOF@ overpotential (s-1) | Reference |
| --- | --- | --- | --- | --- |
| PtSA-0.1/MoS2 | 32 | 144@0.1 V | 43.1@0.05 V | This work |
| Pt@DG | 53 | 26.05@0.1 V | 26.41@0.1 V | [S2] |
| Pt1/OLC | 36 | 7.40@0.038 V | 90@0.2 V | [S3] |
| Pt@PCM | 63.7 | NA | 12@0.2 V | [S4] |
| Pt1/hNCNC | 24 | 7.60@0.02 V | 7.67@0.02 V | [S5] |
| Pt1/NPC | 28 | 2.86@0.025 V | 100@0.1 V | [S6] |
| Pt-AC/DG-150 | 37.8 | 11.78@0.05 V | 15.7@0.05 V | [S7] |
| Pt-AC/DG-300 | 34.8 | 17.93@0.05 V | 13.4@0.05 V | [S7] |
| PtNx/TiO2 | 34 | 136@0.1 V | 37.97@0.05 V | [S8] |
| Pt-GDY2 | 46.6 | 23.64@0.1 V | 23.9@0.05 V | [S9] |
| Os/CNS | 41 | NA | 10.55@0.05 V | [S10] |
| ALD100Pt/NGNs | 29 | NA | 2.12@0.05 V | [S11] |
| Pt1/NMHCS | 56 | 2.07@0.05 V | 2.09@0.05 V | [S12] |
| Ptdoped@WCx | 20 | 14.28@0.1 V | 1.04@0.05 V | [S13] |
| Pt SASs/AG | 29.33 | 22.4@0.05 V | 1.63@0.04 V | [S14] |
| ALD50Pt/NGNs | 29 | NA | 10.2@0.05 V | [S11] |
| Pt1/NMC | 29 | ~8@0.05 V | 8.08@0.05 V | [S15] |
| Pt1/NCP | 28.5 | 6.6@0.05 V | 6.72@0.05 V | [S16] |
| NGA-COF@Pt | 21.8 | 18.2@44 mV | 18.4@44 mV | [S17] |
| Pt1/N-C | 14.2 | NA | 22.07@50 mV | [S18] |
| Pt/TiBxOy | NA | 37.8@50mV | 33.2@50 mV | [S19] |
| Pt1/NNGF | 29.1 | 14.6@50mV | 14.1@50 mV | [S20] |
| Pt- PVP/TNR@GC | 27 | 16.5@50mV | 16.67@50 mV | [S21] |
| PtOx/TiO2 | 52 | NA | 6.95@50 mV | [S8] |
| Pt1/PI@CP | 27.5 | 106.9@0.1 V | 35@0.05 V | [S22] |
| PtNx/TiO2 | 34 | 136@0.1 V | 37.9@0.05 V | [S23] |
| Pt/MoS2-NTA/Ti3C2 | 35 | 46.5@0.1 V | 47.0@0.1 V | [S24] |
| PtSA@Mo2C@NC | 26 | 75.21@0.1 V | 14.4@0.1 V | [S25] |
| Pt/np-Co0.85Se | 35 | 1.32@0.1 V | 3.93@0.1 V | [S25] |
| Ti3C2Tx-PtSA | 45 | 23.21@0.1 V | 23.45@0.1 V | [S27] |
| PtCu/WO3@CF | 45.9 | 7.3@0.1 V | 10.9@0.1 V | [S28] |
| Pt-SAs/MoSe2 | 28 | 34.4@0.1 V | 151@0.2 V | [S29] |
| MAC@Pt 1000 | 24.9 | 1.5@0.1 V | 0.52@40 mV | [S30] |
| Pt-SA0.056/Mo-L | 31.1 | 2.06@0.1 V | 1.2@140 mV | [S31] |
| Pt-MoAl1-xB | 78.8 | 4@0.1 V | 0.63@0.1 V | [S32] |
| 0.22Pt-HMoS2 | 34.83 | ~2@0.1 V | NA | [S33] |

Table S3 Average oxidation state of Pt calculated from the XPS spectra of the PtSA-X/TMDs catalysts

| Sample | Content (%) | Average oxidation state of Pt |
| --- | --- | --- |
| PtSA-0.10/MoS2 | 1.3 (Pt4+) | 1.97 |
|  | 95.7 (Pt2+) |  |
|  | 3.0 (Pt0) |  |
| PtSA-0.14/MoS2 | 13.0 (Pt4+) | 2.10 |
|  | 78.9 (Pt2+) |  |
|  | 8.1 (Pt0) |  |
| PtSA-0.18/MoS2 | 25.5 (Pt4+) | 2.22 |
|  | 67.8 (Pt2+) |  |
|  | 6.7 (Pt0) |  |
| PtSA-0.24/MoS2 | 25.5 (Pt4+) | 2.37 |
|  | 67.8 (Pt2+) |  |
|  | 6.7 (Pt0) |  |
| PtSA-0.3/MoS2 | 20 (Pt4+) | 2.40 |
|  | 80 (Pt2+) |  |
| PtSA-0.1/WS2 | 11.5 (Pt4+) | 1.21 |
|  | 37.5 (Pt2+) |  |
|  | 51 (Pt0) |  |
| PtSA-0/WSe2 | 31.4 (Pt4+) | 2.63 |
|  | 68.6 (Pt2+) |  |

For XPS analysis, the average oxidation state of Pt is calculated according to the below equation：

Ptδ+= Content%Pt4+× 4 + Content%Pt2+× 2 + Content%Pt0× 0

Table S4 Potential of zero charge (PZC) calculated for different model systems

| Ads. form | NPtiso | NPtadj | Epzc(V) |
| --- | --- | --- | --- |
| MoS2 | 0 | 0 | 1.0638 |
| I | 1 | 0 | 0.8224 |
| II | 0 | 2 | 0.7597 |
| III | 2 | 0 | 0.5649 |
| IV | 1 | 2 | 0.5025 |

Note: The PZCs are presented as the potential vs SHE.

Table S5 Extra charge injected into the electrode surface from external circuit at an electrode potential of 0 V vs SHE for different electrode materials

| Ads. form | qex(e) |
| --- | --- |
| I | -1.1358 |
| II | -1.0909 |
| III | -0.8405 |
| IV | -0.7779 |

Table S6 Hydrogen adsorption free energies of the most stable structures on Pt

| Adsorption site | ΔGad(eV) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | 1st H | 2nd H | 3rd H | 4th H | 5th H |
| Ptiso | -0.1426 | -0.1193 | -0.4594 | - | - |
| Ptadj | -0.5616 | -0.0997 | -0.0722 or -0.0550 | 0.1811 | 0.1087 |

Table S7 The adsorption energies of different H adsorption on Ptiso

| H number | Adsorption site | Energy | Total Ead (eV) | Ead per atom (eV) |
| --- | --- | --- | --- | --- |
| 0 | - | -244.6285 | - | - |
| 1 | a | -248.4863 | -0.3707 | -0.3707 |
| 1 | b | -248.2980 | -0.1825 | -0.1825 |
| 1 | c | -248.2982 | -0.1826 | -0.1826 |
| 2 | b, c | -252.3179 | -0.7153 | -0.3576 |
| 2 | a, c | -252.3230 | -0.7203 | -0.3602 |
| 2 | a, b | -252.3238 | -0.7211 | -0.3606 |
| 3 | a, b, c | -256.5369 | -1.4471 | -0.4824 |
| 4 | 2a, b, c | -259.2187 | -0.6418 | -0.1604 |
| 4 | a, 2b, c | -259.3157 | -0.7389 | -0.1847 |

Table S8 Adsorption energies of different H adsorption on Ptiso at different structures

| H number | Adsorption site | I | IV |
| --- | --- | --- | --- |
| 1 | a | -0.3707 | -0.3931 |
| 2 | a, b | -0.3504 | -0.3714 |
| 3 | a, b, c | -0.7260 | -0.7144 |

Table S9 Vibrational energies and entropies for the most stable structure on Ptiso. T=298.15 K

| Ads. form | NH@Ptiso | Ezpe(eV) | EV(eV) | S(J/mol K) | TS(eV) | Gcorr(eV) |
| --- | --- | --- | --- | --- | --- | --- |
| I | 0 | 0.1729 | 0.3464 | 110.4140 | 0.3412 | 0.0052 |
|  | 1 | 0.3751 | 0.5575 | 112.1344 | 0.3465 | 0.2110 |
|  | 2 | 0.5924 | 0.7842 | 117.9665 | 0.3645 | 0.4197 |
|  | 3 | 0.8394 | 1.0357 | 120.2911 | 0.3717 | 0.6640 |
| IV | 0 | 0.1736 | 0.3467 | 109.9675 | 0.3398 | 0.0068 |
|  | 1 | 0.3762 | 0.5575 | 111.8872 | 0.3457 | 0.2118 |
|  | 2 | 0.5891 | 0.7827 | 119.6924 | 0.3699 | 0.4128 |
|  | 3 | 0.8413 | 1.0355 | 118.5289 | 0.3663 | 0.6693 |

Table S10 Adsorption energies of different H adsorption sites on Ptadj

| H number | Adsorption site | Energy | Total Ead (eV) | Ead per atom (eV) |
| --- | --- | --- | --- | --- |
| 0 | - | -248.5108 | - | - |
| 1 | a | -252.5213 | -0.5234 | -0.5234 |
| 1 | c | -252.7895 | -0.7915 | -0.7915 |
| 2 | c, e | -256.5853 | -1.1002 | -0.5501 |
| 2 | c, d | -252.5213 | -1.0195 | -0.5098 |
| 3 | c, d, e | -260.3675 | -1.3954 | -0.4651 |
| 3 | c, a, e | -260.3027 | -1.3305 | -0.4435 |
| 3 | c, b, e | -260.3689 | -1.3968 | -0.4656 |
| 4 | c, b, d, e | -264.2730 | -1.8138 | -0.4534 |
| 5 | c, a, b, d, e | -268.0981 | -2.1518 | -0.4304 |

Table S11 Vibrational energies and entropies for some structures on Ptadj. T=298.15 K

| Number of H@Ptadj | Adsorption site | Ezpe(eV) | EV(eV) | S(J /mol K) | TS(eV) | Gcorr(eV) |
| --- | --- | --- | --- | --- | --- | --- |
| 0 | - | 0.3000 | 0.6059 | 198.2921 | 0.6127 | -0.0069 |
| 1 | c | 0.4919 | 0.7983 | 193.3963 | 0.5976 | 0.2007 |
| 2 | c, e | 0.6886 | 1.0084 | 200.9849 | 0.6211 | 0.3874 |
| 3 | c, d, e | 0.9104 | 1.2390 | 205.1213 | 0.6338 | 0.6052 |
| 3 | c, a, e | 0.8902 | 1.2209 | 205.2180 | 0.6341 | 0.5868 |
| 3 | c, b, e | 0.8923 | 1.2218 | 204.6922 | 0.6325 | 0.5893 |
| 4 | c, b, d, e | 1.1097 | 1.4482 | 208.8082 | 0.6452 | 0.8030 |
| 5 | c, a, b, d, e | 1.3257 | 1.6747 | 215.1256 | 0.6648 | 1.0100 |

Table S12 Adsorption energies of different H adsorption on aggregated Pt at different structures.

| H number | Adsorption site | II | IV | 3H@IV |
| --- | --- | --- | --- | --- |
| 1 | c | -0.7915 | -0.7233 | -0.7692 |
| 2 | c, e | -0.3087 | -0.3886 | -0.3311 |
| 3 | c, d, e | -0.2951 | -0.2548 | -0.2893 |
| 3 | c, a, e | -0.2303 | -0.2181 | -0.2259 |
| 3 | c, b, e | -0.2965 | -0.3142 | -0.2983 |
| 4 | c, b, d, e | -0.4170 | -0.4007 | -0.4100 |
| 5 | c, a, b, d, e | -0.3380 | -0.2837 | -0.3341 |

Table S13 Adsorption energies of different H adsorption on Pt at different systems.

| Pt atom type | H number | Adsorption site | MoSe2 | WS2 | WSe2 |
| --- | --- | --- | --- | --- | --- |
|  | 1 | a | -0.3941 | -0.3945 | -0.4109 |
| Ptiso | 2 | a, b | -0.3976 | -0.4624 | -0.4882 |
|  | 3 | a, b, c | -0.6046 | -0.7696 | -0.6212 |
|  | 1 | c | -0.7186 | -0.7985 | -0.7226 |
|  | 2 | c, e | -0.3221 | -0.3729 | -0.4038 |
| Ptadj | 3 | c, d, e | -0.2392 | -0.2751 | -0.2326 |
|  | 3 | c, b, e | -0.3549 | -0.3949 | -0.4254 |
|  | 4 | c, b, d, e | -0.3025 | -0.3813 | -0.3018 |
|  | 5 | c, a, b, d, e | -0.3643 | -0.4033 | -0.4401 |

Supplementary References

- J. Hempelmann, P.C. Müller, C. Ertural, R. Dronskowski, The orbital origins of chemical bonding in Ge−Sb−Te phase-change materials. Angew. Chem. Int. Ed. 61(17), e202115778 (2022). https://doi.org/10.1002/anie.202115778

- Q. Yang, H. Liu, P. Yuan, Y. Jia, L. Zhuang et al., Single carbon vacancy traps atomic platinum for hydrogen evolution catalysis. J. Am. Chem. Soc. 144(5), 2171–2178 (2022). https://doi.org/10.1021/jacs.1c10814

- D. Liu, X. Li, S. Chen, H. Yan, C. Wang et al., Atomically dispersed platinum supported on curved carbon supports for efficient electrocatalytic hydrogen evolution. Nat. Energy 4(6), 512–518 (2019). https://doi.org/10.1038/s41560-019-0402-6

- H. Zhang, P. An, W. Zhou, B.Y. Guan, P. Zhang et al., Dynamic traction of lattice-confined platinum atoms into mesoporous carbon matrix for hydrogen evolution reaction. Sci. Adv. 4(1), eaao6657 (2018). https://doi.org/10.1126/sciadv.aao6657

- Z. Zhang, Y. Chen, L. Zhou, C. Chen, Z. Han et al., The simplest construction of single-site catalysts by the synergism of micropore trapping and nitrogen anchoring. Nat. Commun. 10, 1657 (2019). https://doi.org/10.1038/s41467-019-09596-x

- T. Li, J. Liu, Y. Song, F. Wang, Photochemical solid-phase synthesis of platinum single atoms on nitrogen-doped carbon with high loading as bifunctional catalysts for hydrogen evolution and oxygen reduction reactions. ACS Catal. 8(9), 8450–8458 (2018). https://doi.org/10.1021/acscatal.8b02288

- Q. Cheng, C. Hu, G. Wang, Z. Zou, H. Yang et al., Carbon-defect-driven electroless deposition of Pt atomic clusters for highly efficient hydrogen evolution. J. Am. Chem. Soc. 142(12), 5594–5601 (2020). https://doi.org/10.1021/jacs.9b11524

- X. Cheng, Y. Lu, L. Zheng, Y. Cui, M. Niibe et al., Charge redistribution within platinum–nitrogen coordination structure to boost hydrogen evolution. Nano Energy 73, 104739 (2020). https://doi.org/10.1016/j.nanoen.2020.104739

- X.-P. Yin, H.-J. Wang, S.-F. Tang, X.-L. Lu, M. Shu et al., Engineering the coordination environment of single-atom platinum anchored on graphdiyne for optimizing electrocatalytic hydrogen evolution. Angew. Chem. Int. Ed. 57(30), 9382–9386 (2018). https://doi.org/10.1002/anie.201804817

- D. Cao, H. Xu, H. Li, C. Feng, J. Zeng et al., Volcano-type relationship between oxidation states and catalytic activity of single-atom catalysts towards hydrogen evolution. Nat. Commun. 13, 5843 (2022). https://doi.org/10.1038/s41467-022-33589-y

- N. Cheng, S. Stambula, D. Wang, M.N. Banis, J. Liu et al., Platinum single-atom and cluster catalysis of the hydrogen evolution reaction. Nat. Commun. 7, 13638 (2016). https://doi.org/10.1038/ncomms13638

- P. Kuang, Y. Wang, B. Zhu, F. Xia, C.-W. Tung et al., Pt single atoms supported on N-doped mesoporous hollow carbon spheres with enhanced electrocatalytic H2-evolution activity. Adv. Mater. 33(18), 2008599 (2021). https://doi.org/10.1002/adma.202008599

- T. Ma, H. Cao, S. Li, S. Cao, Z. Zhao et al., Crystalline lattice-confined atomic Pt in metal carbides to match electronic structures and hydrogen evolution behaviors of platinum (adv. mater. 41/2022). Adv. Mater. 34(41), 2270284 (2022). https://doi.org/10.1002/adma.202270284

- S. Ye, F. Luo, Q. Zhang, P. Zhang, T. Xu et al., Highly stable single Pt atomic sites anchored on aniline-stacked graphene for hydrogen evolution reaction. Energy Environ. Sci. 12(3), 1000–1007 (2019). https://doi.org/10.1039/c8ee02888e

- H. Wei, H. Wu, K. Huang, B. Ge, J. Ma et al., Ultralow-temperature photochemical synthesis of atomically dispersed Pt catalysts for the hydrogen evolution reaction. Chem. Sci. 10(9), 2830–2836 (2019). https://doi.org/10.1039/c8sc04986f

- R. Li, J. Xu, Q. Zhao, W. Ren, R. Zeng et al., Cathodic corrosion as a facile and universal method for the preparation of supported metal single atoms. Nano Res. 15(3), 1838–1844 (2022). https://doi.org/10.1007/s12274-021-3767-3

- Z. Zhang, Z. Zhang, C. Chen, R. Wang, M. Xie et al., Single-atom platinum with asymmetric coordination environment on fully conjugated covalent organic framework for efficient electrocatalysis. Nat. Commun. 15, 2556 (2024). https://doi.org/10.1038/s41467-024-46872-x

- S. Fang, X. Zhu, X. Liu, J. Gu, W. Liu et al., Uncovering near-free platinum single-atom dynamics during electrochemical hydrogen evolution reaction. Nat. Commun. 11, 1029 (2020). https://doi.org/10.1038/s41467-020-14848-2

- X. Cheng, B. Xiao, Y. Chen, Y. Wang, L. Zheng et al., Ligand charge donation–acquisition balance: a unique strategy to boost single Pt atom catalyst mass activity toward the hydrogen evolution reaction. ACS Catal. 12(10), 5970–5978 (2022). https://doi.org/10.1021/acscatal.2c00891

- J. Xu, R. Li, R. Zeng, X. Yan, Q. Zhao et al., Platinum single atoms supported on nanoarray-structured nitrogen-doped graphite foil with enhanced catalytic performance for hydrogen evolution reaction. ACS Appl. Mater. Interfaces 12(34), 38106–38112 (2020). https://doi.org/10.1021/acsami.0c09615

- C. Li, Z. Chen, H. Yi, Y. Cao, L. Du et al., Polyvinylpyrrolidone-coordinated single-site platinum catalyst exhibits high activity for hydrogen evolution reaction. Angew. Chem. Int. Ed. 59(37), 15902–15907 (2020). https://doi.org/10.1002/anie.202005282

- S. Zhang, Z. Wu, Y. Liu, J. Bai, Y. Ding et al., Single-atom platinum immobilized on polyimide for highly efficient and durable hydrogen evolution electrocatalysis. Adv. Energy Mater. 15(17), 2403945 (2025). https://doi.org/10.1002/aenm.202403945

- X. Cheng, Y. Lu, L. Zheng, Y. Cui, M. Niibe et al., Charge redistribution within platinum–nitrogen coordination structure to boost hydrogen evolution. Nano Energy 73, 104739 (2020). https://doi.org/10.1016/j.nanoen.2020.104739

- S. Jiao, M. Kong, Z. Hu, S. Zhou, X. Xu et al., Pt atom on the wall of atomic layer deposition (ALD)-made MoS2 nanotubes for efficient hydrogen evolution. Small 18(16), 2105129 (2022). https://doi.org/10.1002/smll.202105129

- C. Yue, C. Feng, G. Sun, N. Liu, H. Hao et al., Hierarchically stabilized Pt single-atom catalysts induced by an atomic substitution strategy for an efficient hydrogen evolution reaction. Energy Environ. Sci. 17(14), 5227–5240 (2024). https://doi.org/10.1039/D3EE04457B

- K. Jiang, B. Liu, M. Luo, S. Ning, M. Peng et al., Single platinum atoms embedded in nanoporous cobalt selenide as electrocatalyst for accelerating hydrogen evolution reaction. Nat. Commun. 10, 1743 (2019). https://doi.org/10.1038/s41467-019-09765-y

- J. Zhang, E. Wang, S. Cui, S. Yang, X. Zou et al., Single-atom Pt anchored on oxygen vacancy of monolayer Ti3C2Tx for superior hydrogen evolution. Nano Lett. 22(3), 1398–1405 (2022). https://doi.org/10.1021/acs.nanolett.1c04809

- L. Liu, Y. Wang, Y. Zhao, Y. Wang, Z. Zhang et al., Ultrahigh Pt-mass-activity hydrogen evolution catalyst electrodeposited from bulk Pt. Adv. Funct. Mater. 32(20), 2112207 (2022). https://doi.org/10.1002/adfm.202112207

- Y. Shi, Z.-R. Ma, Y.-Y. Xiao, Y.-C. Yin, W.-M. Huang et al., Electronic metal–support interaction modulates single-atom platinum catalysis for hydrogen evolution reaction. Nat. Commun. 12, 3021 (2021). https://doi.org/10.1038/s41467-021-23306-6

- M. Sheng, X. Bin, Y. Yang, Y. Tang, W. Que, In situ electrosynthesis of MAX-derived electrocatalysts for superior hydrogen evolution reaction. Small 18(32), 2203471 (2022). https://doi.org/10.1002/smll.202203471

- H. Yuan, D. Jiang, Z. Li, X. Liu, Z. Tang et al., Laser synthesis of PtMo single-atom alloy electrode for ultralow voltage hydrogen generation. Adv. Mater. 36(5), 2305375 (2024). https://doi.org/10.1002/adma.202305375

- S.J. Park, T.H. Nguyen, D.T. Tran, V.A. Dinh, J.H. Lee et al., Delaminated MBene sheets beyond usual 2D transition metal materials for securing Pt single atoms to boost hydrogen evolution. Energy Environ. Sci. 16(9), 4093–4104 (2023). https://doi.org/10.1039/D3EE01314F

- J. Zhu, Y. Tu, L. Cai, H. Ma, Y. Chai et al., Defect-assisted anchoring of Pt single atoms on MoS2 nanosheets produces high-performance catalyst for industrial hydrogen evolution reaction. Small 18(4), 2104824 (2022). https://doi.org/10.1002/smll.202104824