Supporting Information for

Ion-Sieving Dual-Network Hydrogel Electrolytes Couple Accelerated Ion Transport with Iodide-Shuttle Suppression in Aqueous Zn-I2 Batteries

Ming Chen1, Jia Cheng1, Yixin Zhao1, Wei Fu1, Wen Li1, 2*, Yunhai Zhu3, 4*, and Fanlu Meng1, 2, 3*

1 School of Materials Science and Engineering, Ocean University of China, Qingdao 266404, P. R. China

2 Key Laboratory of Marine Equipment Materials and Protection of Shandong Province, Qingdao 266404, P. R. China

3 Aerospace Special Power Source Technology Innovation Center, Tianfu Jiangxi Laboratory, Chengdu 641419, P. R. China

4 State Key Laboratory of New Textile Materials and Advanced Processing Technologies, Wuhan Textile University, Wuhan 430200, China

*Corresponding authors. E-mail: liwen3710@ouc.edu.cn (Wen Li); yhzhu@wtu.edu.cn (Yunhai Zhu); mengfanlu@ouc.edu.cn (Fanlu Meng)

Supplementary Note

In ZnSO4 aqueous solution (pH≈5-6), the amino groups (pKa≈6.5) on CMCS are readily protonated to -NH3+, while the carboxyl groups (pKa≈4.5-5.0) are partially dissociated into -COO-. Upon the addition of tert-butylamine (pKa≈10.7), its stronger basicity compared to the amino groups of CMCS enables it to preferentially capture free H+ in the solution, leading to an increase in the local pH. According to acid-base equilibrium principles, the presence of tB shifts the equilibrium toward the deprotonated state, thereby reducing the proportion of protonated -NH3+ groups.

-NH3+↔-NH2+H+

In addition, the increase in local pH shifts the equilibrium toward dissociation, thereby promoting the formation of -COO- groups.

-COOH↔-COO-+H+

Meanwhile, the reduction of -NH3+ groups weaken the electrostatic attraction between -NH3+ and -COO-, thereby releasing previously associated -COO- groups.

In summary, tB establishes a locally weakly alkaline microenvironment within the gel network, thereby suppressing the protonation of -NH2 groups, eliminating positive charge centers, promoting the dissociation of -COOH groups, and increasing the density of negatively charged sites. The elimination of electrostatic attraction between -NH3+ and -COO- promotes the extension of CMCS chains and exposes additional -COO- groups. These synergistic effects collectively enable precise regulation of charge polarity and provide a molecular basis for subsequent rapid Zn2+ transport and electrostatic repulsion of polyiodide species.

Supplementary Figures

Fig. S1 Cyclic performance of Zn//Zn symmetric cells assembled with different hydrogel electrolytes at current density of 1 mA cm-2 and area capacity matching of 1 mAh cm-2

To clarify the effect of alkyl groups on the hydrogel performance, ammonia and isobutylamine are used to replace tert-butylamine, and corresponding symmetric cells are assembled to evaluate cycling performance. In the PAM-CMCS-NH3·H2O hydrogel, the effect of alkyl groups is eliminated, whereas in the PAM-CMCS-iB hydrogel, an alternative alkyl structure is introduced. The results show that the cycling performance of the assembled symmetric cells is comparable to that of PAM-CMCS-tB, suggesting that the enhanced performance primarily originates from the weakly alkaline environment established by tert-butylamine, which promotes further deprotonation of amino groups and dissociation of carboxyl groups.

Fig. S2 1H NMR spectra of PAM-CMCS-tB hydrogel

For the quantitative analysis of carboxyl content in PAM-CMCS-tB hydrogel, sodium formate is used as the internal standard, with its characteristic -CHO peak serving as the reference, and the carboxyl content is calculated using the following formula:

Content-COOH=ICMCSNCMCSIHCOONaNHCOONa×nHCOONa/mgel

Here, I is the integrated area of the target peak, N is the number of protons in the target group, n denotes the amount (in moles) of the internal standard in the sample, and m is the mass of the hydrogel sample.

Fig. S3 XPS spectra of all elements

Fig. S4 a Stress-strain curves of the PAM-CMCS-tB hydrogel after immersion in 2 M ZnSO4 for different times. b The stress-strain behavior of the PAM-CMCS-tB hydrogel electrolyte evolves with increasing cycle number

Fig. S5 Composition changes of different gel electrolytes in deionized water

Fig. S6 Comparison of water retention capabilities of various hydrogels in different media at 25 °C. a 2 M ZnSO4, b deionized water

Fig. S7 SEM images of different hydrogels. a PAM, b PAM-CMCS, c PAM-CMCS-tB

Fig. S8 Pore volume of different hydrogels

Fig. S9 XRD patterns of different hydrogels

Fig. S10 The radius of gyration (Rg) of the hydrogel electrolyte, as determined by SAXS

Fig. S11 Molecular dynamics simulations showing the structural configuration of the a PAM-CMCS-tB and b PAM-CMCS hydrogel network. (PAM in the system has been hidden.)

Fig. S12 Molecular dynamics simulation calculates the radius of rotation of CMCS chains in polymers

Fig. S13 LSV curves for a HER and b OER

Fig. S14 Tafel plots of Zn anodes in different hydrogel electrolytes

Fig. S15 The zeta potential in different hydrogel systems

Fig. S16 Stainless steel foil was used as working electrode and counter electrode, and symmetrical cells were assembled with different gel electrolytes to measure ionic conductivity. a Nyquist plots, b Ionic conductivity

The ionic conductivity (σ) of the hydrogel electrolyte was calculated using the equation:

σ=lRA

where l is the thickness of the hydrogel electrolyte, R is the resistance obtained from the impedance spectrum of the symmetric cell, and A is the contact area of the electrode.

Fig. S17 a-c Electrochemical impedance spectroscopy (EIS) spectra of Zn//Zn symmetric cells employing PAM, PAM-CMCS, and PAM-CMCS-tB hydrogel electrolytes at various temperatures, respectively. d-f Corresponding Arrhenius plots used to calculate the activation energies (Ea) for ion transport in each system

The activation energy was determined by fitting the impedance data to the Arrhenius equation:

1Rct=Aexp-EaRT

where A denotes the pre-exponential factor, R is the universal gas constant, T is the absolute temperature, and Rct represents the charge-transfer resistance obtained from EIS measurements at various temperatures.

Fig. S18 Zn deposition/stripping rate performance of Zn//Zn symmetric cells at different current densities

Fig. S19 Zn deposition/stripping voltage profiles in half-cell tests. a PAM and b PAM-CMCS hydrogel electrolytes

Fig. S20 Coulombic efficiency cycling performance under half cell testing

Fig. S21 Chronoamperometric curves recorded at a constant potential of 20 mV, with the inset showing Nyquist plots obtained before and after polarization. a PAM and b PAM-CMCS hydrogel electrolytes

The Zn2+ transference number was calculated using the following equation:

tZn2+=IS∆V-I0R0Io∆V-IsRs

where ΔV denotes the applied potential difference; I0 and R0 are the initial current and interfacial resistance before polarization, and Is and Rs represent the steady-state current and resistance after polarization.

Fig. S22 SEM images of Zn anode surfaces after 100 cycles of plating/stripping at 1 mAh cm-2 for a PAM, b PAM-CMCS, and c PAM-CMCS-tB hydrogel electrolytes

Fig. S23 The average roughness (Ra) and maximum height (Rz) of the zinc electrode after cycling

Fig. S24 Images of the electrode surface under a laser confocal microscope after 100 cycles at 1 mA cm-2 and 1 mAh cm-2 for a, b PAM, c, d PAM-CMCS, and e, f) PAM-CMCS-tB hydrogel electrolytes

Fig. S25 The adsorption configurations of different molecules on the Zn (002) surface are shown as follows: a H2O, b AM, c vertically oriented CMCS, and d horizontally oriented CMCS

Fig. S26 Optical images of the polyiodide ion diffusion in H-type cells separated by PAM-CMCS hydrogel

Fig. S27 UV-vis absorption spectra of the solution in the right chamber at different time intervals using PAM-CMCS hydrogel

Fig. S28 UV-vis absorption spectra of the solution in the right chamber of the H-type cell were collected at various time intervals for a the glass fiber membrane, b the PAM-CMCS hydrogel and c the PAM-CMCS-tB hydrogel

Fig. S29 Calculated binding energies between polyiodide ions and functional groups on PAM-CMCS-tB polymer chains: a I3- and b I5-

Fig. S30 In situ Raman spectra of Zn-I2 cells were recorded at various voltages during a single charge-discharge cycle using a the liquid electrolyte and b the PAM-CMCS-tB hydrogel electrolyte

Fig. S31 a, b Voltage-time profiles and corresponding in situ Raman spectra of Zn-I2 batteries during one charge-discharge cycle using the PAM-CMCS hydrogel electrolyte

Fig. S32 EDS image of NC@I2

Fig. S33 CV curves of Zn/PAM-CMCS-tB/I2 cells at different scan rates

Fig. S34 Charge-discharge profiles at various current densities

Fig. S35 Nyquist plots of Zn-I2 full cells

Fig. S36 Static evaluation of the initial state of charge (SoC)

Fig. S37 Cycling performance at 1 C rate

Fig. S38 GCD curves of Zn/PAM-CMCS-tB/I2 cells at 1 C rate for different number of cycles

Fig. S39 GCD curves of a PAM-CMCS-tB and b LE electrolytes at representative cycles.

Fig. S40 Optical photos of NC@I2 cathode (cropped to 3.5 × 4.5 cm)

Fig. S41 Optical photos of gel electrolyte before and after immersion in 2 M ZnSO4 (cropped to 4.0 × 5.0 cm)

Fig. S42 Optical image of the monitoring device powered by a PAM-CMCS-tB hydrogel-based pouch cell

Supplementary Tables

Table S1 Mechanical properties and ionic conductivity of the dual-network hydrogel

| Electrolyte | Tensile strength (kPa) | Fracture strain (%) | Ionic conductivity (mS cm-1) | Ref |
| --- | --- | --- | --- | --- |
| HACC-co-PAM | ≈150 | 590 | 16.8 | [S1] |
| PNMA/SA | 838 | - | 33.1 | [S2] |
| PAPTMA | 96 | 680 | 28.7 | [S3] |
| G/PAAm/AG | 72.4 | 489.2 | 26.4 | [S4] |
| This work | 30.7 | 518 | 18.1 |  |

Table S2 A summary of the advanced performance of the recently reported Zn-I2 battery

|  | Symmetrical cell | Full cell |  | Refs. |
| --- | --- | --- | --- | --- |
| Electrolyte | Lifespan (mA cm-2; mAh cm-2; h) | Cycle performance (A g-1; mAh g-1; cycles; retention rate) | Reaction type (electron transfer) |  |
| Hydrogel Electrolyte (ZnSO4) | 1; 1; 2100 | 2; 94.1; 1000; 96.4% | 2 | [S5] |
| Hydrogel Electrolyte (ZnSO4) | 0.5; 0.5; 3500 | 20; ≈100; 85000; 90.1% | 2 | [S6] |
| Hydrogel Electrolyte (ZnSO4) | 1; 1; 3000 | 2 C; 200; 2000; 82% | 2 | [S7] |
| Hydrogel Electrolyte (ZnSO4) | 1; 1; 5000 | 2 C; 205; 2000; 82.9% | 2 | [S8] |
| Hydrogel Electrolyte (ZnSO4) | 1; 0.25; 6300 | 2; 185.6; 8000; - | 2 | [S9] |
| Hydrogel Electrolyte (ZnSO4) | 5; 5; 1385 | 5 C; 287.8; 3700; - | 4 | [S10] |
| Hydrogel Electrolyte (Zn(ClO4)2) | 1; 1; 2000 | 2 C; 200; 2000; 100% | 2 | [S11] |
| Hydrogel Electrolyte (Zn(ClO4)2) | -; -; - | 1; ≈610; 4000; 91% | 4 | [S12] |
| Hydrogel Electrolyte (ZnCl2) | 5; 2; 1200 | 1 C; 215.1; 1000; 96.5% | 2 | [S13] |
| Hydrogel Electrolyte (ZnCl2) | 0.2; -; 2400 | 0.2; ≈150; 4500; - | 4 | [S14] |
| Liquid Electrolyte (ZnSO4) | 2; 2; 1800 | 0.2; 219.3; 1000; 88.7% | 2 | [S15] |
| Liquid Electrolyte (ZnSO4) | -; -; - | 20; 138; 63000; 95% | 2 | [S16] |
| Liquid Electrolyte (ZnSO4) | 1; 1; 7000 | 1; 158.6; 13000; 75.2% | 2 | [S17] |
| Liquid Electrolyte (ZnSO4) | 0.5; 0.5; 2250 | 4; 303.4; 6000; 96% | 4 | [S18] |
| Liquid Electrolyte (ZnSO4) | 1; 1; 2100 | 1 C; ≈410; 600; 93.4% | 4 | [S19] |
| Hydrated Eutectic Electrolyte (ZnSO4) | 5; 5; ≈600 | 2 C; 404.6; 3000; 76.2% | 4 | [S20] |

Supplementary References

- L. Yang, C. Xu, L. Liu, Y. Li, Z. Chen et al., Network-reinforcing HACC-co-PAM hydrogel electrolytes for suppressed zinc dendrite growth and high-performance zinc-ion batteries. EES Batteries 1(3), 633-639 (2025). https://doi.org/10.1039/D5EB00055F

- W. Zeng, S. Zhang, J. Lan, Y. Lv, G. Zhu et al., Double network gel electrolyte with high ionic conductivity and mechanical strength for zinc-ion batteries. ACS Nano 18(38), 26391-26400 (2024). https://doi.org/10.1021/acsnano.4c09879

- D. Lin, Y. Lin, R. Pan, J. Li, A. Zhu et al., Water-restrained hydrogel electrolytes with repulsion-driven cationic express pathways for durable zinc-ion batteries. Nano-Micro Lett. 17(1), 193 (2025). https://doi.org/10.1007/s40820-025-01704-5

- C. Ji, X. Lin, Y. Hong, J. Liu, A. Liu et al., A robust dual-network hydrogel electrolyte coupled with a porous carbon material for flexible quasi-solid-state zinc ion hybrid supercapacitors. New J. Chem. 48(19), 8753-8762 (2024). https://doi.org/10.1039/d4nj00310a

- X. Zhang, J. Li, F. Xie, X. Xu, X. Sun et al., Polyzwitterionic gel electrolyte: Dual optimization of polyiodide shuttle suppression and anode stabilization in aqueous Zn‐I2 batteries. Adv. Funct. Mater. 35(39), 2505132 (2025). https://doi.org/10.1002/adfm.202505132

- L. Tang, J. Gao, J. Xu, C. Shao, T. Mu et al., Liquid metal synergistic polyanion self-adaptable gel electrolyte for stabilizing dual electrode/electrolyte interfaces in ultra-durable Zn‐I2 batteries. Energy Storage Mater. 84, 104786 (2026). https://doi.org/10.1016/j.ensm.2025.104786

- J. L. Yang, Z. Yu, J. Wu, J. Li, L. Chen et al., Hetero‐polyionic hydrogels enable dendrites‐free aqueous Zn‐I2 batteries with fast kinetics. Adv. Mater. 35(44), 2306531 (2023). https://doi.org/10.1002/adma.202306531

- J. L. Yang, T. Xiao, T. Xiao, J. Li, Z. Yu et al., Cation‐conduction dominated hydrogels for durable zinc-iodine batteries. Adv. Mater. 36(21), 2313610 (2024). https://doi.org/10.1002/adma.202313610

- Y. Wang, K. Zhong, J. Zhang, Q. Li, Z. Zhan et al., Concomitant zinc dendrite mitigation and iodide shuttle confinement: A bifunctional zwitterionic hydrogel electrolyte unlocking ultralong‐cycling aqueous zinc‐iodine batteries. Adv. Funct. Mater. e26937 (2025). https://doi.org/10.1002/adfm.202526937

- R. Liu, D. Wang, Z. Gao, D. Yang, Y. Li et al., Low-self-discharge nanoconfined hydrogel electrolyte for stable high-energy-density aqueous zinc-iodine batteries. ACS Nano 20(6), 5217-5227 (2026). https://doi.org/10.1021/acsnano.5c20669

- Y. Liu, F. Li, J. Hao, H. Li, S. Zhang et al., A polyanionic hydrogel electrolyte with ion selective permeability for building ultra‐stable Zn‐I2 batteries with 100 °C wide temperature range. Adv. Funct. Mater. 34(29), 2400517 (2024). https://doi.org/10.1002/adfm.202400517

- Y. Liu, L. Zhang, L. Liu, Q. Ma, R. Wang et al., All‐climate energy‐dense cascade aqueous Zn‐I2 batteries enabled by a polycationic hydrogel electrolyte. Adv. Mater. 37(46), 2415979 (2025). https://doi.org/10.1002/adma.202415979

- S. J. Zhang, J. Hao, H. Wu, Q. Chen, C. Ye et al., Protein interfacial gelation toward shuttle‐free and dendrite‐free Zn-iodine batteries. Adv. Mater. 36(35), 2404011 (2024). https://doi.org/10.1002/adma.202404011

- Z. Hu, Z. Han, H. Liu, X. Jiang, K. Bai et al., Mechanically strong and tough ionic liquid gel electrolyte for four-electron zinc-iodine batteries. J. Am. Chem. Soc. 147(50), 46632-46641 (2025). https://doi.org/10.1021/jacs.5c18431

- W. Liu, H. Ma, L. Zhao, W. Qian, B. Liu et al., Anionically-reinforced nanocellulose separator enables dual suppression of zinc dendrites and polyiodide shuttle for long-cycle Zn‐I2 batteries. Nano-Micro Lett. 18(1), 59 (2025). https://doi.org/10.1007/s40820-025-01921-y

- F. Wang, R. Ma, Z. Chen, T. Yin, Z. Yan et al., Click chemistry‐inspired fixation catalysis for long‐life zinc-iodine batteries. Adv. Mater. 38(2), e11980 (2025). https://doi.org/10.1002/adma.202511980

- Y. Tan, W. Xu, F. Yang, J. Tao, D. Li et al., Dynamic polyiodide‐trapping and proton‐capturing dual‐network engineering for high‐areal‐capacity, long‐cycling and high‐temperature Zn‐I2 batteries. Adv. Mater. 38(12), e22609 (2026). https://doi.org/10.1002/adma.202522609

- K. Du, H. Qi, C. Zhang, W. Xu, D. Chen et al., Halogenated organic acid additive rendered highly reversible four‐electron transfer zinc‐iodine batteries by strengthened interhalogen interaction and protons supply. Adv. Funct. Mater. e27634 (2025). https://doi.org/10.1002/adfm.202527634

- H. Wu, S. J. Zhang, J. Vongsvivut, Y. Jiang, J. Hao et al., Quasi‐solid cathode additive enables highly reversible four‐electron I-/I0/I+ conversion in aqueous Zn‐I2 batteries. Adv. Mater. 38(3), e11680 (2025). https://doi.org/10.1002/adma.202511680

- L. Liu, L. Zhang, Y. Liu, S. Zhang, R. Wang et al., Enhanced redox kinetics of aqueous I-/I2/I+ conversion chemistry in hydrated eutectic electrolyte over a wide temperature range. Adv. Energy Mater. 15(38), 2501460 (2025). https://doi.org/10.1002/aenm.202501460