Supporting Information for

Amine-Salt-Assisted Solution Crystallization of Inorganic Perovskite Single Crystals for High-Performance X-ray Detection

Yujia Jiang1#, Depeng Chu1#, Jiacheng Pi1, Naiming Liu1, Xueni Sun1, Yunxia Zhang2, Ziyang Feng1, Yuquan Wang3, Wenjie Chen3, Xinxin Wang3, Jingyun Tian1, Lei Zhao1, Binxia Jia1, Ruixin Shi1, Yihui He3*, Yucheng Liu1*, Shengzhong (Frank) Liu1,4,5,*

1Key Laboratory of Applied Surface and Colloid Chemistry Ministry of Education, Shaanxi Provincial Basic Discipline (Surface and Interface Chemistry) Research Center, Shaanxi Key Laboratory for Advanced Energy Devices, Shaanxi Engineering Lab for Advanced Energy Technology, School of Materials Science and Engineering, Shaanxi Normal University, Xi’an 710119, P. R. China

2School of Science, Xi’an University of Posts & Telecommunications, Xi’an 710121, P. R. China

3State Key Laboratory of Radiation Medicine and Protection, School of Radiation Medicine and Protection and Collaborative Innovation Center of Radiation Medicine of Jiangsu Higher Education Institutions, Soochow University, Suzhou 215123, P. R. China

4State Key Laboratory of Catalysis, Dalian National Laboratory for Clean Energy, Dalian Institute of Chemical Physics, Chinese Academy of Sciences, Dalian 116023, P. R. China

5Center of Materials Science and Optoelectronics Engineering, University of Chinese Academy of Sciences, Beijing 100049, P. R. China

#Yujia Jiang and Depeng Chu contributed equally to this work.

*Corresponding authors. E-mail: liuyc@snnu.edu.cn (Yucheng Liu); yhhe@suda.edu.cn (Yihui He); szliu@dicp.ac.cn (Shengzhong (Frank) Liu)

S1	Characterizations and Methods

Theoretical calculation

All quantum chemical calculations were conducted using Gaussian 16 A.03 software [S1]. The PBE0 functional was applied in combination with the Grimme D3(BJ) dispersion correction for all computations [S2-S4]. Geometry optimizations and frequency analyses were performed employing the def2-SVPbasis set for all atoms [S5, S6], while single-point energy calculations were carried out using the larger def2-TZVPP basis set [S5, S6]. To account for solvation effects in DMSO, the Solvation Model based on Solute Electron Density (SMD) implicit solvation model was incorporated during the single-point energy evaluations [S7]. The Gibbs free energy (G) and enthalpy (H) at 298.15 K were subsequently obtained using the Shermo software [S8].

Theoretical models were constructed according to the experimental feed ratio of CsCl:PbCl2: amine salt (MAI/MABr/MACl) = 2:3:2. Solvation was represented by three DMSO molecules per solute unit to approximate the primary solvent shell. The systems investigated together with their corresponding molecular ratios include: CsCl-PbCl2 (2:3), CsCl-PbCl2-DMSO (2:3:3), and CsCl-PbCl2-MAI/MABr/MACl-DMSO (2:3:3:3). The binding energy of each system was defined as the Gibbs free energy difference between the complex and its isolated components. For instance, the binding energy of the CsCl-PbCl2-MAI-DMSO system is calculated as:

∆G(CsCl-PbCl2-MAI-DMSO)=G(CsCl-PbCl2-MAI-DMSO)-2G(CsCl)-3G(PbCl2)-2G(MAI)-3G(DMSO)

Material characterizations

X-ray diffraction (XRD) patterns of the SCs were measured on a Rigaku MiniFlex 600 X-ray diffractometer with a Cu tube, the tube was operated at an acceleration voltage of 40 kV and a beam current of 20 mA. High-resolution XRD rocking curves were measured using an X’Pert pro MRD X-ray diffractometer (Cu-target) which was operated at 40 kV and 20 mA. X-ray photoelectron spectroscopy (XPS) measurements were carried out using an Escalab 250Xi spectrometer (Thermo Fisher Scientific). 1H nuclear magnetic resonance (NMR) measurements were employed to analyze the C-H bonding environments by using a Bruker Avance HD X500 spectrometer operating at 500 MHz. Absorbance spectra of the SCs were measured by using a Shimadzu UV-Vis-NIR spectrometer (Shimadzu, UV-3600). The steady-state and time-resolved photoluminescence characteristics of CsPbCl3 SC were investigated using a Pico-Quant FT-100. Thermogravimetric (TG) and differential scanning calorimetry (DSC) were performed using a TA SDT-Q600 V20.9 (Build 20) instrument. The SEM images were measured using a field emission SEM (Hitachi, SU-8020) and the compositions of the SCs were measured employing the energy-dispersive X-ray spectroscopy (EDX) of the SU-8020 (Shimadzu, EDX-7000).

Relative dielectric constant (ε) measurements

The capacitance-frequency curves of the SCs were measured using an impedance analyzer (Agilent 4980A Precision LCR Meter) over a wide frequency range from 0.03 MHz to 10 MHz to determine the capacitance of the SCs. The relative permittivity (ε) was calculated by the following equation:

ε=cdε0A

where d and A are the thickness and the electrode area respectively, and ε0 is the vacuum permittivity.

Space-charge-limited current (SCLC) measurements

The dark current-voltage characteristics of the SC detetors were measured using a precision source meter (Keysight Technologies, B2902A). The experimental I-V datas were analyzed within the framework of the widely used space-charge-limited current (SCLC) model. By fitting the measured curves to the SCLC equation, the trap density of states (ntrap) of the SCs was quantitatively extracted. Specifically, in the linear ohmic region of the dark current-voltage curve, the average trap density was calculated according to the following formula:

ntrap=2εε0VTELqL2

where ε is the dielectric constant and ε0 the vacuum permittivity. q is the elementary charge, L the thickness of the SC, and VTFL the trap-filled limit voltage. The VTFL can be read directly from the dark current-voltage curve, therefore the trap density can be calculated.

Mobility of hole carriers measurements

Mobility of hole carriers were assessed using ~1 μCi 241Am (5.5 MeV) α particle and ~10 μCi 57Co (122 keV) γ-ray sources. Bismuth (Bi) and gold (Au) electrodes were prepared via thermal evaporation with the thickness of 70 nm. Both electrodes were connected to Cu wires using Ag paint and then to outer readout circuits. The as-fabricated devices placed in a shielding box were connected to an eV-550 preamplifier. The negative bias voltage was applied on the Au electrode via the eV-550 preamplifier using ORTEC 710 Bias Supply and the alpha particles and γ-rays were irradiated from Bi electrode. The induced signals from the device were further amplified using an ORTEC model 572A amplifier with a shaping time constant of 10 μs. The shaped signals were then digitized by a dual 16 K input multichannel analyzer (ORTEC-927), finally generating a response spectrum displayed on MAESTRO-32 software.

Photoconductivity measurements

For photoconductivity measurements, X-rays were used for illumination light. The I-V curves of the SC detectors under X-ray irradiation were measured and the X-ray response current was fitted using the modified Hecht equation to derive the μτ product with the following formula:

I=IoμτVL21-exp⁡(-L2μτV)1+LVsμ

where I0 is the saturated photocurrent, L is the thickness of the SC detector, V is the applied bias and τ is the carrier lifetime.

Detection limit evaluation by the signal-to-noise ratio (SNR) of the SC X-ray detectors According to measuring the response current of the SC detector under on-off X-rays, the average dark current and the average X-ray response current are obtained. Then we confirm the dose rate corresponding to an output with a signal-to-noise ratio (SNR) of 3 as the limit of detection at a fixed bias and the SNR is calculated as follows:

SNR= IsignalInoise

where the signal current (Isignal) is calculated by subtracting the average dark current (Idark) from the average X-ray response current (Iphoto) detected by the detector. The noise current (Inoise) was obtained by calculating the standard deviation of the x-ray response current:

Inoise= 1N iN(Ii-Iphoto)2

Finally, we measured the X-ray response current over time at different dose rates to determine the detection limit.

X-ray detector performance measurements

All X-ray response measurements of the CsPbCl3 SC detectors were conducted at room temperature under ambient atmospheric conditions. The detector was enclosed within a custom-fabricated lead-shielding chamber to suppress electromagnetic interference, eliminate stray optical illumination, and reduce radiation exposure to operators. X-ray irradiation was provided by a tungsten-anode source (Spellman, XRB150PN600) operated at an accelerating voltage of 70 kV. The tube current was systematically varied in the range of 1-3.5 mA to control the incident dose rate. Additional dose-rate modulation was achieved by introducing five aluminum attenuators with a thickness of 3 mm between the source and the detector. The absolute dose rate was calibrated using a high-precision silicon diode dosimeter (RaySafe-X2, Fluke). The photocurrent response time of the SC detector was measured by a precision source meter (FS-Pro). To evaluate the temporal response characteristics, pulsed X-rays of variable frequency were generated using a lead chopper.

X-ray imaging

X-ray imaging experiments were conducted using a dedicated system composed of a lead-shielded enclosure, a tungsten-anode X-ray source, a motorized X-Y translation stage (Thorlabs, MLS203-1) and a precision source meter (Keysight B2911B). The specimen was mounted on the translation stage which provided controlled bidirectional displacement under continuous X-ray irradiation. The photocurrent of the SC detector was simultaneously acquired by the precision source meter in correspondence with the stage coordinates, enabling precise two-dimensional scanning. The resulting spatially correlated data were used to reconstruct high-resolution X-ray transmission images of the specimen.

S2	Supplementary Figures and Tables

Fig. S1 Solubility of CsCl and PbCl2 in DMSO solvent at room temperature.

Fig. S2 The structural formulas of monomers and coordinated systems used for energy calculation. a-f Monomer structures of CsCl, PbCl2, DMSO, MAI, MABr and MACl. g-j The coordinated structures of CsCl-PbCl2-DMSO, CsCl-PbCl2-DMSO-MAI, CsCl-PbCl2-DMSO-MABr and CsCl-PbCl2-DMSO-MACl systems.

Fig. S3 Photographs of single crystals grown in the solution with different additives. a With MACl. b With FACl.

Fig. S4 Photographs of CsPbCl3 SCs grown in the pristine solution (without additives). Many obvious cracks can be recognized inside in the SCs.

Fig. S5 High-resolution XPS spectra of I 3d for the CsPbCl3 SCs grown from the solution with MAI.

Fig. S6 Elemental composition and distribution in the SCs grown from the solution with MAI. a-c XPS spectra of Cs 3d, Pb 4f, and Cl 2p of the SC. d SEM images of the SC. e-g SEM-EDS mapping of Cs, Pb, Cl for the SC. h Energy-dispersive X-ray spectra of the SC.

Fig. S7 Elemental composition and distribution in the SCs grown from the solution with FAI. a-e XPS spectra of Cs 3d, Pb 4f, Cl 2p and I 3d of the SC. f SEM images of the SC. g-i SEM-EDS mapping of Cs, Pb, Cl for the SC. j Energy-dispersive X-ray spectra of the SC. k Comparison of calculated Cs:Pb:Cl ratio in the SC with experimental results measured by XPS and EDS, respectively.

Fig. S8 Elemental composition and distribution in the SCs grown from the solution with MABr. a-e XPS spectra of Cs 3d, Pb 4f, Cl 2p and Br 3d of the SC. f SEM images of the SC. g-j SEM-EDS mapping of Cs, Pb, Cl and Br for the SC. k Energy-dispersive X-ray spectra of the SC. l Comparison of calculated Cs:Pb:Cl ratio in the SC with experimental results measured by XPS and EDS, respectively.

Fig. S9 Elemental composition and distribution in the SCs grown from the solution with FABr. a-e XPS spectra of Cs 3d, Pb 4f, Cl 2p and Br 3d of the SC. f SEM images of the SC. g-j SEM-EDS mapping of Cs, Pb, Cl and Br for the SC. k Energy-dispersive X-ray spectra of the SC. l Comparison of calculated Cs:Pb:Cl ratio in the SC with experimental results measured by XPS and EDS, respectively.

Fig. S10 Photoluminescence spectrum of the CsPbCl3 SC.

Fig. S11 Absorption spectrum and corresponding band gap calculation of the CsPbCl3 SC grown from the solution with MAI.

Fig. S12 Dark current-voltage (I-V) curves of the CsPbCl3 SCs.

Fig. S13 X-ray response current of the CsPbCl3 SC detector. a Response current of the SC detector under on−off X-rays with different dose rates. b Dose rate dependence response of the SC detector under X-ray irradiation at different electric fields.

Fig. S14 Normalized X-ray response of the CsPbCl3 SC detector after storage for 35 days in air environment.

Table S1 Theoretical calculations of optimized total electronic and Gibbs free energies of individual molecular species

| Molecular species | Gibbs free energy (G) (kcal mol-1) |
| --- | --- |
| DMSO | -346973.34 |
| CsCl | -301436.3 |
| PbCl2 | -698513.59 |
| MAI | -246908.9 |
| MABr | -1675200.83 |
| MACl | -348766.57 |

Table S2 Theoretical optimized total electronic and Gibbs free energies of multi-component molecular complexes

| Molecular complex | Optimized total electronic energy (E) (kcal·mol-1) | Gibbs free energy (G) (kcal mol-1) |
| --- | --- | --- |
| CsCl-PbCl2 | -2698334.28 | -2698413.37 |
| CsCl-PbCl2-DMSO | -3742470.53 | -3739399.36 |
| CsCl-PbCl2-MACl-DMSO | -4432179.17 | -4436938.49 |
| CsCl-PbCl2-MABr-DMSO | -7099577.83 | -7089809.64 |
| CsCl-PbCl2-MAI-DMSO | -4236590.38 | -4233228.83 |

Table S3 The Gibbs free energy change of the calculated multi-component molecular complexes

| Molecular complex | ΔG (kcal mol-1) |
| --- | --- |
| CsCl-PbCl2-DMSO | -65.97 |
| CsCl-PbCl2-MACl-DMSO | -71.96 |
| CsCl-PbCl2-MABr-DMSO | -74.59 |
| CsCl-PbCl2-MAI-DMSO | -77.64 |

Table S4 Comparison of the key parameters of the SC X-ray detector in this study and other detectors

| Materials | Sensitivity (μC Gy-1 cm2) | Electric field or voltage | μτ product (cm2 V-1 s-1) | Detection limit (nGy s-1) | Electric field or voltage | Ref. |
| --- | --- | --- | --- | --- | --- | --- |
| CsPbCl3 SC | 76,624 | 20 V mm-1 | 6.3 × 10-3 | 47.9 | 1 V mm-1 | This work |
| Cs3Bi2I9 SC | 1,652.3 | 50 V mm-1 | 7.97 × 10-4 | 130 | 50 V mm-1 | [S9] |
| Cs3Bi2I9 SC | 59 464.4 | 150 V | 5.53 × 10-4 | 1.27 | 5 V | [S10] |
| Cs2AgBiBr6 SC | 105.0 | 50 V | 6.3 × 10-3 | 59.7 | 5 V | [S11] |
| Cs4PbI6 SC | 451.5 | 30 V | 9.7 × 10-4 | - | - | [S12] |
| CsPbBr3 Film | 1,450 | 300 V | - | 500 | 100 V | [S13] |
| CsPbBr3 SC | 4086 | 5 V mm-1 | - | - | - | [S14] |
| CsPbBr3 SC | 6021.99 | 50 V | 5.14 × 10-3 | 1890 | 5 V | [S15] |
| CsPbBr3 SC | 10,833 | 435 V mm-1 | 9.4 × 10-4 | 32 | 435 V mm-1 | [S16] |
| CsPbBr3 film | 55,684 | 5 V mm-1 | 1.32 × 10-2 | 215 | ~4.2 V mm-1 | [S17] |
| CsPbBr3 SC | 46180 | 500 V mm-1 | 8.11 × 10-4 | 10.81 | - | [S18] |
| CsPbBr3 SC | 55722 | 300 V mm-1 | 2.4 × 10-4 | - | - | [S19] |
| CsPbCl2.995I0.005 SC | 2.19 × 105 | 100 V mm-1 | 1.02 × 10-3 | - | - | [S20] |
| α-Se | ~20 | 10000 V mm-1 | - | - | - | [S21] |
| CZT | 20 | 250 V mm-1 | - | 145 | - | [S22] |

Supplementary References

- M. Frisch, G. Trucks, H. Schlegel, G. Scuseria, M. Robb et al., Gaussian 09, Revision C.01. Gaussian, Inc., Wallingford, CT (2016).

- C. Adamo, V. Barone, Toward reliable density functional methods without adjustable parameters: The PBE0 model. J. Chem. Phys. 110(13), 6158–6170 (1999). https://doi.org/10.1063/1.478522

- S. Grimme, Density functional theory with London dispersion corrections. Wires Comput. Mol. Sci. 1(2), 211–228 (2011). https://doi.org/10.1002/wcms.30

- S. Grimme, S. Ehrlich, L. Goerigk, Effect of the damping function in dispersion corrected density functional theory. J. Comput. Chem. 32(7), 1456–1465 (2011). https://doi.org/10.1002/jcc.21759

- F. Weigend, R. Ahlrichs, Balanced basis sets of split valence, triple Zeta valence and quadruple Zeta valence quality for H to Rn: Design and assessment of accuracy. Phys. Chem. Chem. Phys. 7(18), 3297–3305 (2005). https://doi.org/10.1039/b508541a

- F. Weigend, Accurate coulomb-fitting basis sets for H to Rn. Phys. Chem. Chem. Phys. 8(9), 1057–1065 (2006). https://doi.org/10.1039/b515623h

- A.V. Marenich, C.J. Cramer, D.G. Truhlar, Universal solvation model based on solute electron density and on a continuum model of the solvent defined by the bulk dielectric constant and atomic surface tensions. J. Phys. Chem. B 113(18), 6378–6396 (2009). https://doi.org/10.1021/jp810292n

- T. Lu and Q. Chen, Interaction region indicator: A simple real space function for identifying interaction regions from molecular wavefunctions and electron density. Comput. Theor. Chem. 1200, 113249 (2021). https://doi.org/10.1016/j.comptc.2021.113249

- Y. Zhang, Y. Liu, Z. Xu, H. Ye, Z. Yang et al., Nucleation-controlled growth of superior lead-free perovskite Cs3Bi2I9 single-crystals for high-performance X-ray detection. Nat. Commun. 11, 2304 (2020). https://doi.org/10.1038/s41467-020-16034-w

- M. Yang, A. Li, X. Hao, L. Wu, W. Tian et al., Highly sensitive X-ray detector made of large lead-free perovskite Cs3Bi2I9 single crystals with anisotropic response. Adv. Opt. Mater. 11(15), 2203066 (2023). https://doi.org/10.1002/adom.202203066

- W. Pan, H. Wu, J. Luo, Z. Deng, C. Ge et al., Cs2AgBiBr6 single-crystal X-ray detectors with a low detection limit. Nat. Photonics 11(11), 726–732 (2017). https://doi.org/10.1038/s41566-017-0012-4

- Q. Xu, C. Li, J. Nie, Y. Guo, X. Wang et al., Highly sensitive and stable X-ray detector based on a 0D structural Cs4PbI6 single crystal. J. Phys. Chem. Lett. 12(1), 287–293 (2021). https://doi.org/10.1021/acs.jpclett.0c03411

- G.J. Matt, I. Levchuk, J. Knüttel, J. Dallmann, A. Osvet et al., Sensitive direct converting X-ray detectors utilizing crystalline CsPbBr3 perovskite films fabricated via scalable melt processing. Adv. Mater. Interfaces 7(4), 1901575 (2020). https://doi.org/10.1002/admi.201901575

- J. Peng, C.Q. Xia, Y. Xu, R. Li, L. Cui et al., Crystallization of CsPbBr3 single crystals in water for X-ray detection. Nat. Commun. 12(1), 1531 (2021). https://doi.org/10.1038/s41467-021-21805-0

- J. Di, H. Li, J. Su, H. Yuan, Z. Lin et al., Reveal the humidity effect on the phase pure CsPbBr3 single crystals formation at room temperature and its application for ultrahigh sensitive X-Ray detector. Adv. Sci. 9(2), 2103482 (2022). https://doi.org/10.1002/advs.202103482

- L. Pan, Z. Liu, C. Welton, V.V. Klepov, J.A. Peters et al., Ultrahigh-flux X-ray detection by a solution-grown perovskite CsPbBr3 single-crystal semiconductor detector. Adv. Mater. 35(25), 2211840 (2023). https://doi.org/10.1002/adma.202211840

- W. Pan, B. Yang, G. Niu, K.-H. Xue, X. Du et al., Hot-pressed CsPbBr3 quasi-monocrystalline film for sensitive direct X-ray detection. Adv. Mater. 31(44), 1904405 (2019). https://doi.org/10.1002/adma.201904405

- Y. Hua, G. Zhang, X. Sun, P. Zhang, Y. Hao et al., Suppressed ion migration for high-performance X-ray detectors based on atmosphere-controlled EFG-grown perovskite CsPbBr3 single crystals. Nat. Photonics 18(8), 870–877 (2024). https://doi.org/10.1038/s41566-024-01480-5

- X. Sun, G. Zhang, W. Ma, Y. Hua, H. Liu et al., Growth of two-inch perovskite CsPbBr3 single-crystal with high irradiation resistance for X-ray detection. Adv. Mater. 38(1), e12788 (2026). https://doi.org/10.1002/adma.202512788

- J. Tian, R. Shi, D. Chu, N. Liu, J. Pi et al., Portable dosimeter with ultralow detection limit enabled by large size solution grown inorganic perovskite single crystal. Adv. Mater. 38(18), e22163 (2026). https://doi.org/10.1002/adma.202522163

- S. Kasap, J.B. Frey, G. Belev, O. Tousignant, H. Mani et al., Amorphous selenium and its alloys from early xeroradiography to high resolution X-ray image detectors and ultrasensitive imaging tubes. Phys. Status Solidi B: . 246(8), 1794–1805 (2009). https://doi.org/10.1002/pssb.200982007

- S. Tokuda, H. Kishihara, S. Adachi, T. Sato, Preparation and characterization of polycrystalline CdZnTe films for large-area, high-sensitivity X-ray detectors. J. Mater. Sci. Mater. Electron. 15(1), 1–8 (2004). https://doi.org/10.1023/A:1026297416093