Supporting Information for

High-Strength, Self-Sensing Multiphase Hydrogels for Load-Bearing Actuation and Logical Human–Machine Interaction

Zhilin Zhang1, Jiayi Gu1, Lina Wang2, Xingchen Cui1, Xu Zhai4, Yue Xu1, He Liu2, Deliang Li2, Bingle Li2, Ye Tian2, *, Baoyang Lu3, *, Yu Fu1, 4, * and Tieqiang Wang1, *

1 Department of Chemistry, College of Sciences, Northeastern University, Shenyang 110819, P. R. China

2 College of Medicine and Biological Information Engineering, Northeastern University, Shenyang 110169, P. R. China

3 Jiangxi Province Key Laboratory of Flexible Electronics, Jiangxi Science and Technology Normal University, Jiangxi Science & Technology Normal University, Nanchang, 330013, P. R. China

4 School of Chemical and Environmental Engineering, Sichuan University of Science and Engineering, Zigong 643000, P. R. China

*Corresponding authors. E-mail: wangtieqiang@mail.neu.edu.cn (Tieqiang Wang); tianye@bmie.neu.edu.cn (Ye Tian); luby@jxstnu.edu.cn (Baoyang Lu); fuyu@mail.neu.edu.cn (Yu Fu)

### Supplementary Figures and Tables

Fig. S1 Properties of pure PNIPAM hydrogels with different crosslinker contents. a The ratio of mass of the hydrogel to that of the initial hydrogel when the water is dehydrated to equilibrium at 50 ℃. b Stress-strain curves. Therefore, without specific notes, PPS hydrogels with 2 mg/mL BIS content are employed in light of its optimal deswelling and swelling kinetics and mechanical performances for the following characterizations and applications.

Fig. S2 The performance was optimized by immersion in sodium alginate solutions of different concentrations and cross-linking in calcium chloride for 60 s (i.e., 0, 0.2, 0.4, 0.6 and 0.8 wt.%). a The ratio of mass of the hydrogel to that of the initial hydrogel when the water is dehydrated to equilibrium at 50 ℃. b Stress-strain curves. Therefore, without specific notes, PPS hydrogels with 0.6 wt.% content are employed in light of its optimal deswelling and swelling kinetics and mechanical performances for the following characterizations and applications.

Fig. S3 FT-IR spectra of PNIPAM, PANI, SA and PANI/PNIPAM-SA samples. PANI/PNIPAM-SA combines the characteristic peaks of PANI, PNIPAM and SA.

Fig. S4 a XPS Spectra of PPS Hydrogel. b High resolution XPS spectra of PPS hydrogel Ca2+.

Fig. S5 SEM image and EDS mapping image of PPS hydrogel. a SEM image of PPS hydrogel. Distribution map of b Cl and c Ca elements of PPS hydrogel.

Fig. S6 Photographs and cross-sectional SEM images of hydrogels at different temperatures. a PNIPAM swelling at 20 °C. b PNIPAM deswelling at 50 °C. c PANI/PNIPAM swelling at 20 °C. d PANI/PNIPAM deswelling at 50 °C. e PANI/PNIPAM-SA swelling at 20 °C. f PANI/PNIPAM-SA deswelling at 50 °C.

Fig. S7 N2 adsorption-desorption isotherms of a PNIPAM hydrogel, b PP and c PPS hydrogel.

Fig. S8 Equilibrium swelling rate of PNIPAM, PP, PPS hydrogels.

Fig. S9 Rapid photothermal response mechanism. a SEM images (left) and optical images (right) of normal PNIPAM (N-PNIPAM) hydrogels, sponge-like PNIPAM (S-PNIPAM) hydrogels and PPS hydrogel. b Deswelling kinetics of N-PNIPAM, S-PNIPAM and PPS hydrogel. F Swelling kinetics of N-PNIPAM, S-PNIPAM and PPS hydrogel.

Fig. S10 Mechanical properties of hydrogels at different stages of material preparation. i.e., PNIPAM, PANI-PNIPAM (PP) and PANI-PNIPAM/SA (PPS). Tensile strength and Young’s modulus.

Fig. S11 Rheological test of a PNIPAM, b PP, c PPS hydrogels.

Fig. S12 Flexible and high-strength optical images of PPS hydrogel. Image of a folding, b rolling, c stretching the PPS hydrogels, displaying its soft and flexible essence. Such PPS hydrogel also exhibits remarkably d high strength, by sustaining a weight (50 g) with over 2500 of its own weight.

Fig. S13 Mechanical properties of PPS hydrogels cross-linked for different times in calcium chloride solution.

Fig. S14 Temperature changes of hydrogel under near-infrared light under infrared thermal imaging camera. a PNIPAM, b) PP, c PPS. During the on and off process of NIR light, the intensity of NIR light is 1.6 w cm-2.

Fig. S15 Photothermal performance of PNIPAM, PANI-PNIPAM and PANI-PNIPAM/SA. a Temperature change of hydrogel through the on process of NIR light with 1.6 w cm-2. b Dynamic surface temperature of hydrogel cooling in air.

Fig. S16 The volume change of water gel under near infrared light. a The original state of the hydrogel. b NIR on. c NIR off.

Fig. S17 Photothermal performance of PPS hydrogel. a Dynamic surface temperature of PPS exposed to NIR light with different intensity; b Dynamic surface temperature of PPS cooling in air.

Fig. S18 Irradiation intensity dependent folding angle (left Y-axis) and gravitational potential energy increment (right Y-axis) of PPS hydrogel soft actuator.

Fig. S19 Bending angle and stability of PPS hydrogel after 50 switching cycles under near-infrared light of different powers. a 1.6 W cm-2, b 1.45 W cm-2, c 1.19 W cm-2, d 0.68 W cm-2.

Fig. S20 Sensing performance of PPS hydrogel. a Schematic illustration of hydrogel stretching. b The relative resistance change of PPS hydrogel versus strain.

Fig. S21 The relative resistance change of PPS hydrogels under 100% strain for 200 cycles.

Fig. S22 Electrical monitoring signal by PPS hydrogel actuator under the NIR light with 1.60 w cm-2 for 200 cycles.

Fig. S23 3D printing load schematic diagram. a mb, b mc, c md.

Fig. S24 The bending angle of PPS-900 hydrogel under different loads and different torques.

Fig. S25 Hydrogel array for manufacturing logic gate information encryption system. The hydrogel is PPS-0, PPS-60, PPS-900, PPS-0, PPS-900, PPS-60 from left to right. The diversity of passwords can be reflected by changing the arrangement order of materials.

Fig. S26 Electrical signals of PPS-0 hydrogel under loading conditions.

Table S1 Comparison of the PANI/PNIPAM-SA hydrogel actuator in this work with previously reported PNIPAM hydrogels-based actuator

| Materials | Response time (s) | Recover time (s) | Tensile strength (kPa) | Ref. |
| --- | --- | --- | --- | --- |
| K-MXene/PEDOT:PSS-PNIPAM | 11 | 19 | 12 | Adv. Funct. Mater. 2023, 33, 2214867. |
| CNTs-Ecoflex/PNIPAm | 25 | 105 | 12 | Chem. Eng. J. 2021, 415, 128988. |
| MoO2/ PNIPAM | 30 | 70 | 25 | ACS Appl. Mater. Interfaces 2021, 13, 28, 33404–33416. |
| PDA@MXene/PNIPAM | 15 | - | 27 | Sensor Actuat B-chem. 2023, 390,133899. |
| PNIPAM/TOCN/PAM | 60 | 600 | 24 | Carbohyd. Polym. 2024, 335, 122067. |
| MXene/PNIPAM | 10 | - | 81.88 | Adv. Funct. Mater. 2023, 33, 2301982. |
| PNIPAM-nSiO2 | 60 | 120 | 23 | Macromol. Res. 2023, 31, 625–633. |
| PNIPM/PANI | 15 | 600 | 20.7 | J. Mater. Chem. C, 2023, 11, 6741–6749. |
| PNIPM/PANI | 2.5 | 20 | 18 | Sci. Robot. 2021, 6, eabd5483. |
| PANI/PNIPAM -SA | 7.57 | 5.04 | 86.83 | Our work |

Table S2 Input table showing binary signals denoted by the presence (Yes = 1) or absence (No = 0) of load actuation

| Logic Gate | Input |  |  | Output |
| --- | --- | --- | --- | --- |
|  | PPS-0 | PPS-60 | PPS-900 |  |
| Yes/No | 1 | 1 | 1 | 0 |
|  | 0 | 1 | 1 | 0 |
|  | 0 | 0 | 1 | 1 |
|  | 0 | 0 | 0 | 0 |
|  | 1 | 1 | 0 | 0 |
|  | 1 | 0 | 0 | 0 |
|  | 0 | 1 | 0 | 0 |
|  | 1 | 0 | 1 | 0 |

// --- 1. Initialization and Parameter Setup ---

DEFINE CONSTANT THRESHOLD = 0.04  // Set the relative current change threshold

// Define sensor interfaces for the three hydrogel channels

DEFINE INTERFACE Sensor_Ch1  // Corresponds to PPS-0

DEFINE INTERFACE Sensor_Ch2  // Corresponds to PPS-90

DEFINE INTERFACE Sensor_Ch3  // Corresponds to PPS-900

// Define the robotic hand controller interface

DEFINE INTERFACE Robotic_Hand

// Initialize the robotic hand to its default straight position

Robotic_Hand.execute_action("Keep_Straight")

// --- 2. Main Control Loop (Continuous Monitoring & Response) ---

START LOOP (Infinite Loop):

// Step A: Signal Acquisition (Read relative current change ΔI/I₀)

VARIABLE current_1 = Sensor_Ch1.read_relative_current()

VARIABLE current_2 = Sensor_Ch2.read_relative_current()

VARIABLE current_3 = Sensor_Ch3.read_relative_current()

// Step B: Comparator Logic (Convert analog signals to binary 0 or 1)

// Default assignment is 0

VARIABLE digital_1 = 0

VARIABLE digital_2 = 0

VARIABLE digital_3 = 0

IF current_1 > THRESHOLD THEN digital_1 = 1

IF current_2 > THRESHOLD THEN digital_2 = 1

IF current_3 > THRESHOLD THEN digital_3 = 1

// Step C: Logic Gate Operation (Corresponds to: Y = NOT A AND NOT B AND C)

// The trigger condition is met ONLY when the binary code is strictly 001

VARIABLE trigger_OK = FALSE

IF (digital_1 == 0) AND (digital_2 == 0) AND (digital_3 == 1) THEN:

trigger_OK = TRUE

END IF

// Step D: Robotic Hand Execution

IF trigger_OK == TRUE THEN:

Robotic_Hand.execute_action("OK_Gesture")

ELSE:

// Covers all other cases like 000, 111, 010, 100, etc.

Robotic_Hand.execute_action("Keep_Straight")

END IF

// Add a short delay to prevent system jitter from high-frequency reading (Optional)

DELAY(50 milliseconds)

END LOOP