Supporing Information for

Enhanced Antibiotics Sieving by Exfoliated TiS2 Membranes via Surface Functionalization and Passivation

Ruixin Yan1†, Mingzi Sun2†, Honglu Hu1, Ruijie Yang1, Zhen Zhang1, Weikang Zheng1, Liang Mei1, Ting Ying1, Yue Zhang1, Alicia Kyoungjin An3, Chuyang Y. Tang4, Jingyun Fang5*, Bolong Huang2*, Zhiyuan Zeng1,6*

1Department of Materials Science and Engineering, and State Key Laboratory of Marine Environmental Health, City University of Hong Kong, 83 Tat Chee Avenue, Kowloon, Hong Kong S.A.R. 999077, P. R. China

2Department of Chemistry, City University of Hong Kong, Hong Kong S.A.R. 999077, P. R. China.

3Department of Chemical and Biological Engineering, The Hong Kong University of Science and Technology, Clear Water Bay, Kowloon, Hong Kong S.A.R. 999077, P. R. China

4Department of Civil Engineering, The University of Hong Kong, Hong Kong S.A.R. 999077, P. R. China

5Guangdong Provincial Key Laboratory of Environmental Pollution Control and Remediation Technology, School of Environmental Science and Engineering, Sun Yat-Sen University, Guangzhou 510275, P. R. China

6Shenzhen Research Institute, City University of Hong Kong, Shenzhen 518057, P. R. China

†Ruixin Yan and Mingzi Sun contributed equally to this work.

*Corresponding authors. E-mail: zhiyzeng@cityu.edu.hk (Zhiyuan Zeng); b.h@cityu.edu.hk (Bolong Huang); fangjy3@mail.sysu.edu.cn (Jingyun Fang)

Supplementary Figures

Fig. S1 SEM images of commercial TiS2 powder and their elemental mapping distribution.

Fig. S2 Chemical structure of three quaternary ammonium molecules: DTAB, DDAB, TDAB.

Fig. S3 a) TEM images and elemental mapping of pristine TiS2 nanosheets. b) Raman spectra of bulk and exfoliated TiS2 nanosheets.

Fig. S4 XPS image of bulk TiS2 powders and exfoliated TiS2 nanosheets.

Fig. S5 SEM EDS mapping images of pristine TiS2 membrane. (The porous region corresponds to the PVDF substrate, while the tightly packed layered structure directly above it represents the restacked film.)

Fig. S6 XPS spectra of a) N1s of membranes of TiS2/DT-TiS2/DD-TiS2/TD-TiS2 and DTAB/DDAB/TDAB powders. b, c) Ti2p and S2p of membranes of TiS2/DT-TiS2/DD-TiS2/TD-TiS2. From the XPS spectra before and after the reaction, changes in the binding energies of surface elements can be observed. The N 1s peaks show the presence of ammonium peaks on the surface of TiS2 modified with quaternary ammonium salts, corresponding to the N positions in the three modifiers' powders. This indicates that the positively charged ammonium ends have successfully attached to the TiS2 surface [S1, S2]. The N peak on the unmodified TiS2 surface may originate from nitrogen in the air, with adsorption sites competing with quaternary ammonium ions. After modification, its relative content decreases. From the Ti 2p spectrum, the peaks for TiS2 (456 eV) and TiO2 (459 eV) can be directly identified [S3, S4]. It can be observed that pure TiS2 shows a significant number of oxides during the exfoliation and drying process. In contrast, the samples protected by a quaternary ammonium salt hydrophobic layer maintain a TiS2 content similar to the original powder. Correspondingly, the S 2p spectrum shows only one pair of peaks, indicating that no phase transformation occurred during the exfoliation and modification process. d) EDS mapping of DD-TiS2 nanosheets.

Fig. S7 Optical images of four kinds of modified membranes.

Fig. S8 Raman shift of DTAB/DDAB/TDAB modified TiS2 membrane. The Raman shift of bulk TiS2, identified as the 1T polytype, exhibits two distinct active modes: A1g and Eg, positioned at approximately 332 cm-1 and 230 cm-1, respectively [S5]. The A1g mode is characterized by the out-of-plane vibrations of sulfur atoms, while the Eg mode encompasses both in-plane and out-of-plane vibrations of sulfur atoms. The A1g mode remains largely unchanged, indicating that the modified TiS2 membrane has retained its 1T phase without significant phase transformation. The Eg mode in the modified membrane exhibits a degree of broadening, which could likely be attributed to the surface modification by quaternary ammonium molecules.

Fig. S9 FTIR images of a) commercial DTAB/DDAB/TDAB/bulk TiS2 powders. b) pristine and modified TiS2 membranes. A strong absorption of the -CH2- peak was found in the 2800-3000 cm-1 range and 720 cm-1 for all three modifiers [S6]. After reaction with TiS2 nanosheets, excepts the pristine TiS2, all TiS2 membranes modified with the three quaternary ammonium salts show enhanced absorption of methylene groups, this indicates the successful grafting of alkyl chains on the surface of the membranes.

Fig. S10 SEM images of membrane thickness changes before and after DDAB modification. (The porous region corresponds to the PVDF substrate, while the tightly packed layered structure directly above it represents the restacked film.)

Fig. S11 Structural and morphological comparison between pristine and oxidized TiS2. a) AFM image of a pristine TiS2 nanosheet, showing a smooth and intact surface morphology. b) TEM image of pristine TiS2, revealing a continuous lattice without observable oxidation-induced defects. c) Cross-sectional SEM image of a pristine TiS2 membrane, displaying well-defined and orderly lamellar stacking. d) XRD pattern of the pristine TiS2 membrane, characterized by a sharp (001) reflection, indicative of preserved layered crystallinity. e) AFM image of an oxidized TiS2 nanosheet, where multiple oxidation-induced voids are observed (highlighted by white dashed circles). f) TEM image of oxidized TiS2, showing pronounced voids and contrast variations associated with oxidation (marked by red dashed circles). g) Cross-sectional SEM image of the oxidized TiS2 membrane, exhibiting disrupted lamellar stacking and partial structural collapse after oxidation. h) XRD patterns of TiS2 membranes after 12 h and 24 h RO operation, showing weakened and broadened diffraction features, suggesting a gradual loss of layered order upon oxidation.

Fig. S12 Morphology and thickness characterization of functionalized TiS2 nanosheets. a–c) TEM images of DT-TiS2 (a), DD-TiS2 (b), and TD-TiS2 (c) nanosheets. d–f) AFM topographic images of DT-TiS2 (d), DD-TiS2 (e), and TD-TiS2 (f). g–i) Corresponding AFM height profiles extracted along the indicated lines, showing average thicknesses of ~3 nm for DT-TiS2 (g), ~4 nm for DD-TiS2 (h), and ~6 nm for TD-TiS2 (i).

Fig. S13 a) UV-vis spectra absorbance of TiS2 ink solution. b) linear relationship between TiS2 concentration and absorbance.

Fig. S14 This presented a significant color change from the metallic luster of TiS2 before reverse osmosis, directly illustrating the water sensitivity of the TiS2 membrane. Notably, the surfaces of membranes modified with three types of DTA ions maintained their original metallic luster even after the reverse osmosis test, directly confirming the significant anti-oxidative effect of DTA ions on TiS2 films. The immersion experiments were also conducted in water sink that further validate the protective effect of DTA ions on TiS2. As shown, the unmodified TiS2 membrane exhibits significant cracking and discoloration after 48 hours of immersion, and these damaged areas pose a potential risk of secondary contamination during practical applications. In contrast, the modified TiS2 membrane, which remains stable after modification, not only demonstrates excellent antioxidation properties but also exhibits some degree of swelling inhibition. This remarkable effect is largely due to the rapid electrostatic forces at play during the post-treatment process, which enable the DTA ions to swiftly self-assemble. This results in the N-terminal end aligning closely with the TiS2 side, while the hydrophobic long chains orient towards the water molecules.

Fig. S15 Quantitative oxidation kinetics of pristine TiS2 under three representative conditions: water immersion (blue, derived from time-resolved UV-vis absorbance decay), ambient air drying at 25 °C (green, derived from time-resolved Ti 2p XPS deconvolution), and forced air drying at 60 °C (orange, derived from time-resolved Ti 2p XPS deconvolution). The comparison demonstrates that hydrolysis by H2O, rather than oxidation by molecular O2, is the dominant degradation pathway of TiS2.

Fig. S16 Zeta potential evolution of pristine and ammonium-modified TiS2 nanosheets. a–c) Zeta potential distributions of TiS2 modified with increasing amounts of DTAB (a), DDAB (b), and TDAB (c). Pristine TiS2 exhibits a strongly negative surface potential (≈ –50 to –60 mV). Progressive addition of the quaternary ammonium salts leads to a systematic shift toward positive values, indicating successful adsorption of the cationic headgroups and formation of a surface-stabilizing layer. Complete charge reversal to +70~100 mV is observed at sufficiently high modifier concentrations. d) pH-dependent zeta potentials of pristine TiS2 and the three modified TiS2 samples. While pristine TiS2 becomes unstable and approaches neutral/negative charge across the pH range, all modified samples maintain strongly positive and relatively stable surface potentials from pH 3 to 10, demonstrating the robustness of the interfacial ammonium layers and improved aqueous stability.

Fig. S17 Time‐dependent static contact angles of pristine TiS2, DT‐TiS2, DD‐TiS2, and TD‐TiS2 membranes, showing distinct wetting evolution from 0 ~ 5 min. Pristine TiS2 rapidly loses hydrophobicity, whereas modified membranes retain high contact angles (>85°) over time.

Fig. S18 Contact angle of membranes decorated by different concentrations (40 μL, 80 μL, 160 μL) of DTAB/DDAB/TDAB.

Fig. S19 Advancing and receding contact angle measurements on a DT‐TiS2 membrane under tilting angles of 10° and 50°. The calculated hysteresis (Δθ = θadv − θrec = 17°) indicates a homogeneous and low‐adhesion surface favorable for dynamic water repellence.

Fig. S20 TGA of bulk TiS2 powders and DT/DD/TD-TiS2.

Fig. S21 MD simulations of water droplet before and after interactions with pristine and modified TiS2 surfaces. (a, b) TiS2, (c, d) DT-TiS2, (e, f) DD-TiS2, and (g, h) TD-TiS2. Color bars: Silver balls = Ti, Yellow balls = S, Red balls = O, Grey balls = C, white balls = H. The top blue balls are inert atoms as the block for water molecules during the MD simulations1-5.

Fig. S22 Ratio of water molecules from the droplets located near the surface of pristine and modified TiS2 surfaces.

Fig. S23 The MD simulation models of (a) DD-TiS2 and (b) TiS2 interact with water molecules in the solutions at different angles.

Fig. S24 Adsorption energies of O2 on TiS2, DT-TiS2, DD-TiS2, and  TD-TiS2.

Fig. S25 The image of RO test system. A homemade dead-end filtration cell was used to evaluate membrane permeance under nitrogen pressure. The feed solution was loaded into the stainless-steel filtration cell and pressurized by nitrogen gas applied from the top. The membrane was placed at the bottom of the cell, and the permeate solution was collected through the outlet tubing into a graduated cylinder for volume measurement. The entire setup was placed on a magnetic stirring plate to minimize concentration polarization during filtration.

Fig. S26 Chemical structure of four kinds of antibiotics and their molecular weight.

Fig. S27 Cross-sectional SEM images of pristine and functionalized TiS2 membranes with tunable thicknesses. All membranes were prepared under identical conditions: TiS2 nanosheet dispersions (0.5 mg mL−1 in DI water) were vacuum-filtered onto PVDF substrates (220 nm pore size, 25 mm in diameter) at a constant vacuum of −0.1 MPa and room temperature. Membrane thickness was tuned solely by adjusting the filtered volume (2, 5, 10, 20, or 40 mL), yielding ~200, ~600, ~1000, ~2000, and ~3000 nm stacks, respectively. For the functionalized membranes, 2 mL of 0.1 mM DTAB/DDAB/TDAB (ethanol/water = 1:1 v/v) was subsequently filtered through the freshly wet TiS2 layer under the same vacuum, followed by rinsing with 20 mL DI water. All samples were then vacuum-dried at 100 °C for 12 h. (scale bar: 2 μm)

Fig. S28 Mechanical flexibility and tensile performance of TiS2-based membranes. a) Optical photograph showing the free-standing DT-TiS2 membrane bent into a semicircular shape without visible cracks or delamination, demonstrating excellent flexibility. b–d) SEM images of the membrane surface after bending, confirming continuous and compact morphology for DT-TiS2, DD-TiS2, and TD-TiS2 samples without structural failure. e-j) Cross-sectional SEM images of e) DT-TiS2, f) DD-TiS2, and j) TD-TiS2 membranes before (top row) and after (bottom row) bending. The tightly packed, layered internal structures remain fully intact, further verifying their excellent structural integrity under mechanical deformation.

Fig. S29 Stress–strain curves of PVDF, pristine TiS2, and modified TiS2 membranes (DT-TiS2, DD-TiS2, TD-TiS2), showing improved tensile strength (2.8–3.1 MPa) and good elongation (30–45%) for all modified membranes.

Fig. S30 XPS N 1s spectra of functionalized TiS2 membranes before and after RO tests. a) Fresh DT-TiS2 membrane. b) DT-TiS2 membrane after RO test. c) Fresh DD-TiS2 membrane. d) DD-TiS2 membrane after RO test. e) Fresh TD-TiS2 membrane. f) TD-TiS2 membrane after RO test.

Fig. S31 Ti 2p XPS spectra of pristine and modified TiS2 membranes before and after RO operation. a–d) High-resolution Ti 2p spectra of fresh TiS2, DT-TiS2, DD-TiS2, and TD-TiS2 membranes. e–h) Corresponding Ti 2p spectra after RO tests. The blue peaks correspond to Ti4⁺ (TiS2) and the yellow peaks to Ti4⁺ (TiO2) species. The integrated areas of these deconvoluted peaks were used to evaluate the TiS2/TiO2 ratio, reflecting the degree of surface oxidation before and after RO operation.

Fig. S32 XRD patterns of a) DT-TiS2, b) DD-TiS2, and c) TD-TiS2 membranes before and after RO operation.

Fig. S33 Total organic carbon (TOC) concentrations of permeate water after filtration through different membranes.

Fig. S34 Cyclic stability of DD-TiS2 membranes in antibiotic rejection tests. Permeance (orange, left axis) and rejection rate (green, right axis) of DD-TiS2 membranes tested over 30 consecutive filtration cycles for a) CIP, b) TC (25 mg/L, 25°C).

Fig. S35 Long-term operation stability of DD-TiS2 membranes. (RIF, TC, CIP, and SMX, 25 mg/L, 25 °C)

Fig. S36 UV-vis absorbance before and after adsorption of four kinds of antibiotics.

Fig. S37 SEM images of RO-tested DD-TiS2 membrane.

Fig. S38 SEM EDS mapping of a) fresh DD-TiS2 membrane and b) RO-tested DD-TiS2 membrane.

Fig. S39 AFM images of DD-TiS2 membranes after RO test of SMX/CIP/TC/RIF.

Fig. S40 Techno-economic assessment of TiS2 nanosheet production via the soft-pack battery exfoliation route. a) Cost distribution of producing 1 kg TiS2 nanosheets, showing total cost ≈ $700 kg⁻1, dominated by TiS2 and LiFePO4 raw materials. b) Sankey diagram detailing the cost flow from raw materials, capital, and utilities to individual components. Operational and capital expenses contribute < 0.05%, confirming that the exfoliation and filtration processes are economically scalable. Abbreviations: FCI, fixed capital investment; FCOP, fixed costs of production; UTS, total utilities; CONS, total consumables. c) optical image of pouch-cell using TiS2 as electrode for scalable production.

Fig. S41 Comparison of fabrication energy consumption for different membrane and 2D-material production routes. Energy consumption (kWh·kg⁻1 of material) for several representative fabrication processes, including liquid-phase exfoliation of graphene, chemical exfoliation of MoS2, mechanical shear exfoliation of graphene, rapid Joule-heating (RJH) graphene, graphene obtained from waste precursors, and polymeric blend RO membrane fabrication (literature values).

Fig. S42 Cross-flow filtration performance of the DD-TiS2 membrane. a) Photograph of the laboratory-scale cross-flow filtration setup used in this study. b) Optical images of the DD-TiS2 membranes (effective area ≈ 2 cm2) installed in the stainless-steel cross-flow module. c) Permeance and rejection of four representative antibiotics (SMX, CIP, TC, and RIF at a concentration of 25 ppm, 25°C) under cross-flow operation.

Fig. S43 Antibiotic rejection performance of the three functionalized TiS2 membranes in mixed-antibiotic feeds (RIF + TC + CIP + SMX, each at 25 mg/L) under varying ionic-strength backgrounds. a–c) Rejection rates in NaCl backgrounds of 1, 2, 5, and 10 mM for a) DT-TiS2, b) DD-TiS2, and c) TD-TiS2 membranes. d–f) Corresponding rejection rates under CaCl2 backgrounds of 1, 2, 5, and 10 mM for d) DT-TiS2, e) DD-TiS2, and f) TD-TiS2 membranes. All measurements were performed under dead-end RO operation at 6 bar transmembrane pressure with a 1 cm effective membrane diameter. DD-TiS2 retains the highest rejection (>88% for all four antibiotics) across the entire ionic-strength range in both monovalent and divalent backgrounds, demonstrating robust performance in mixed-solute feeds.

Table S1 Summary of the membrane materials, filtration modes, and operating conditions of the reference works compared in Fig. 5i

| Membrane | Filtration Mode | Operating Pressure | Target Solute & Concentration | Ref. |
| --- | --- | --- | --- | --- |
| PES-GO | Dead-end | 3 bar | Reactive Red 195, 100 mg/L; BSA, 250 mg/L | [S7] |
| NF (PEI/PI) | Dead-end | 13.8 bar | Sulfamerazine, 1 mg/L | [S8] |
| PA-MoS2 | Cross-flow | 8 bar | Four parabens (methyl-, ethyl-, propyl-, benzyl-paraben), 200 μg/L each | [S9] |
| MOF/PI | Cross-flow | 5–11 bar | 21 PhACs, 20 μg/L each; NaCl and MgSO4, 2000 mg/L each | [S10] |
| SW30-GO | Cross-flow | 400 psi | NDMA, 890 μg/L | [S11] |
| PEI | Dead-end | 13.8 bar | Cefadroxil, 1 mg/L; Enrofloxacin, 1 mg/L | [S12] |
| COF | Cross-flow | 5 bar | Five dyes (chrome black T, methyl blue, Congo red, acid fuchsin, rose bengal), 100 mg/L | [S13] |
| TFC | Dead-end | 5 bar | MR, MnB, RosB, BB, 10 mg/L each | [S14] |
| PEI/PAI | Cross-flow | 10 bar | Ciprofloxacin, 1 ppm | [S15] |
| All-carbon | Vacuum filtration | 0.9 bar | Tetracycline hydrochloride (TCH), 500 μM, 20 mL | [S16] |

Table S2 Energy flow data

| Parameter | Value | Unit | Ref |
| --- | --- | --- | --- |
| Battery | -2800 | kW | = – (industrial-scale output / laboratory-scale output) × (battery power × discharge time) |
| Ultrasonic bath | 418 | kW | = Ultrasonic bath scale* unit volumetric energy consumption of the ultrasonic bath |
| Centrifuge | 256 | kW | a |
| Mixer | 47 | kW | =15*Mixer scale^1[S17] |

a：The power consumption of the centrifuge is calculated according to Ref [S18]. As:

Centrifuge Power W= ω2（msrDS2+mLrDL2）

rDS=0.21 m，rDL=0.285 m

mS(solid feed rate) =0.87 kg/s，mL (liquid feed rate)=3.47 kg/s (obtained from the material flow data)

Two operating speeds were evaluated: 3000 rpm (314 rad/s) and 8000 rpm (838 rad/s)

Note: The negative battery energy term is treated as a recoverable energy credit under an idealized industrial energy-recovery assumption.

Table S3 Results of production cost calculation

| Basic Data |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Capacity |  | 1000 | kg/h | Shift position |  | 3 |  | d/y |  |
| Plant life |  | 20 | y | Numbers of operators per shift |  | 5 |  | h/y |  |
| Annual operating days |  | 333 | d/y | Operating labor cost |  | 30000 |  | $/y |  |
| Annual operating hours |  | 8000 | h/y | Nominal Interest Rate |  | 0.1 |  |  |  |
| YIELD ESTIMATE |  |  |  | CAPITAL COSTS |  |  |  |  |  |
| Scale of production set to 1000 kg/h product unit: kg |  |  |  |  |  |  |  | $ |  |
|  |  |  |  | ISBL |  |  |  | 5211333 |  |
|  |  |  |  | OSBL |  |  |  | 2084533 |  |
|  |  |  |  | Engineering and construction costs |  |  |  | 729587 |  |
|  |  |  |  | Contingency charges |  |  |  | 729587 |  |
|  |  |  |  | Fixed Capital Investment (FCI) |  |  |  | 8755039 |  |
| ANNUALIZED CAPITAL CHARGES |  |  |  |  |  |  |  |  |  |
|  |  | $ | Annual capital charge ratio(ACCR) |  |  | $/y |  | $/unit product |  |
| Fixed capital investment |  | 8755039 | 0.117 |  |  | 1028364 |  | 0.129 |  |
| Total Annual Capital Charge(ACC) |  |  |  |  |  | 1028364 |  | 0.129 |  |
| FIXED OPERATING COSTS |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  | $/y |  | $/unit product |  |
| Operating labor |  | 15 | Operators: 30000 $/y each |  |  | 450000 |  | 0.056 |  |
| Supervision |  | 25% | of Operating Labor |  |  | 112500 |  | 0.014 |  |
| Direct salary overhead |  | 40% | of Labor & Superv |  |  | 225000 |  | 0.028 |  |
| Maintenance |  | 3% | of ISBL |  |  | 156340 |  | 0.020 |  |
| Property taxes and insurance |  | 1% | of ISBL |  |  | 52113 |  | 0.007 |  |
| General plant overhead |  | 65% | of Labor + Superv+Direct salary overhead +Maint. |  |  | 613496 |  | 0.077 |  |
| Fixed costs of production (FCOP) |  |  |  |  |  | 1609449 |  | 0.20 |  |
| UTILITIES |  |  |  |  |  |  |  |  |  |
|  | Units | Units/Unit product |  | Units/y | Price $/units |  | $/y |  | $/unit product |
| Battery | kwh | -2.80 |  | -22400000 | 0.05 |  | -1120000 |  | -0.14 |
| Ultrasonic bath | kwh | 0.418 |  | 3343434 | 0.05 |  | 167172 |  | 0.0209 |
| Centrifuge | kwh | 0.256 |  | 2051370 | 0.05 |  | 102568 |  | 0.0128 |
| mixer | kwh | 0.0469 |  | 375000 | 0.05 |  | 18750 |  | 0.00234 |
| Total Utilities (UTS) |  |  |  |  |  |  | -831510 |  | -0.10 |
| CONSUMABLES |  |  |  |  |  |  |  |  |  |
|  | Units |  |  | life time(y) | Price $/units |  | $/y |  | $/unit product |
| PP separator | 5y |  |  | 5 | 561000 |  | 112200 |  | 0.0140 |
| Aluminum coater | 5y |  |  | 5 | 91155 |  | 18231 |  | 0.0023 |
| Total Consumables (CONS) |  |  |  |  |  |  | 130431 |  | 0.016 |
| RAW MATERIAL COSTS |  |  |  |  |  |  |  |  |  |
|  | Units | Units/Unit product |  | Units/y | Price $/units |  | $/y |  | $/unit product |
| TiS2 | kg | 2.5 |  | 20000000 | 226 |  | 4520000000 |  | 565 |
| SupperP carbon | kg | 0.3 |  | 2500000 | 60 |  | 150000000 |  | 19 |
| PVDF | kg | 0.3 |  | 2500000 | 65 |  | 162500000 |  | 20 |
| water | kg | 762.5 |  | 6100000000 | 0.00054 |  | 3294000 |  | 0.41 |
| LiFePO4 | kg | 5.5 |  | 44000000 | 14 |  | 616000000 |  | 77 |
| Cu | kg | 1.2 |  | 9800000 | 10.5 |  | 102900000 |  | 13 |
| Al | kg | 0.5 |  | 4200000 | 2.1 |  | 8820000 |  | 1.1 |
| electrolyte | kg | 0.1 |  | 1000000 | 305 |  | 305000000 |  | 38 |
| Total Raw Materials (RM) |  |  |  |  |  |  | 5868514000 |  | 734 |
| REVENUES |  |  |  |  |  |  |  |  |  |
| Key Products | Units | Units/Unit product |  | Units/y | Price $/units |  | $/y |  | $/unit product |
| TiS2 nanosheets | kg | 1 |  | 8000000 | 4300 |  | 34400000000 |  | 4300 |
| Total Key Product Revenues (REV) |  |  |  |  |  |  | 34400000000 |  | 4300 |
| SUMMARY |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  | $/y |  | $/unit product |
| Variable Cost of Production (VCOP = RM + CONS + UTS) |  |  |  |  |  |  | 5867812921 |  | 733.5 |
| Fixed Cost of Production (FCOP) |  |  |  |  |  |  | 1609449 |  | 0.20 |
| Cash Cost of Production (CCOP) |  |  |  |  |  |  | 5869422371 |  | 733.7 |
| Total Annual Capital Charge (ACC) |  |  |  |  |  |  | 1028364 |  | 0.13 |
| Gross Profit (GP=REV-CCOP) |  |  |  |  |  |  | 28530577629 |  | 3566 |
| Total Cost of Production |  |  |  |  |  |  | 5870450734 |  | 733.8 |

Supplementary References

- N. Saito, A. Urayama, M. Ikezawa, Y. Kondo, Water-durable cesium lead halide perovskite nanocrystals passivated with a cationic gemini surfactant. Adv. Mater. Interfaces 9(5), 2101836 (2022). https://doi.org/10.1002/admi.202101836

- Y. Deng, Y. Xie, K. Zou, X. Ji, Review on recent advances in nitrogen-doped carbons: preparations and applications in supercapacitors. J. Mater. Chem. A 4(4), 1144–1173 (2016). https://doi.org/10.1039/c5ta08620e

- P. Lu, Y. Xia, G. Sun, D. Wu, S. Wu et al., Realizing long-cycling all-solid-state Li-In||TiS(2) batteries using Li(6+x)M(x)As(1-x)S(5)I (M=Si, Sn) sulfide solid electrolytes. Nat. Commun. 14(1), 4077 (2023). https://doi.org/10.1038/s41467-023-39686-w

- C. Wan, X. Gu, F. Dang, T. Itoh, Y. Wang et al., Flexible n-type thermoelectric materials by organic intercalation of layered transition metal dichalcogenide TiS2. Nat. Mater. 14(6), 622–627 (2015). https://doi.org/10.1038/nmat4251

- R. Yang, L. Mei, Q. Zhang, Y. Fan, H.S. Shin et al., High-yield production of mono- or few-layer transition metal dichalcogenide nanosheets by an electrochemical lithium ion intercalation-based exfoliation method. Nat. Protoc. 17(2), 358–377 (2022). https://doi.org/10.1038/s41596-021-00643-w

- M. Ly, T.H. Mekonnen, Cationic surfactant modified cellulose nanocrystals for corrosion protective nanocomposite surface coatings. J. Ind. Eng. Chem. 83, 409–420 (2020). https://doi.org/10.1016/j.jiec.2019.12.014

- V. Vatanpour, S.S. Mousavi Khadem, A. Dehqan, M.A. Al-Naqshabandi, M.R. Ganjali et al., Efficient removal of dyes and proteins by nitrogen-doped porous graphene blended polyethersulfone nanocomposite membranes. Chemosphere 263, 127892 (2021). https://doi.org/10.1016/j.chemosphere.2020.127892

- S. Zhao, Y. Yao, C. Ba, W. Zheng, J. Economy et al., Enhancing the performance of polyethylenimine modified nanofiltration membrane by coating a layer of sulfonated poly(ether ether ketone) for removing sulfamerazine. J. Membr. Sci. 492, 620–629 (2015). https://doi.org/10.1016/j.memsci.2015.03.017

- R. Dai, H. Han, T. Wang, X. Li, Z. Wang, Enhanced removal of hydrophobic endocrine disrupting compounds from wastewater by nanofiltration membranes intercalated with hydrophilic MoS2 nanosheets: Role of surface properties and internal nanochannels. J. Membr. Sci. 628, 119267 (2021). https://doi.org/10.1016/j.memsci.2021.119267

- L.-X. Dong, X.-C. Huang, Z. Wang, Z. Yang, X.-M. Wang et al., A thin-film nanocomposite nanofiltration membrane prepared on a support with in situ embedded zeolite nanoparticles. Sep. Purif. Technol. 166, 230–239 (2016). https://doi.org/10.1016/j.seppur.2016.04.043

- H. Croll, A. Soroush, M.E. Pillsbury, S. Romero-Vargas Castrillón, Graphene oxide surface modification of polyamide reverse osmosis membranes for improved N-nitrosodimethylamine (NDMA) removal. Sep. Purif. Technol. 210, 973–980 (2019). https://doi.org/10.1016/j.seppur.2018.08.070

- S. Zhao, C. Ba, Y. Yao, W. Zheng, J. Economy et al., Removal of antibiotics using polyethylenimine cross-linked nanofiltration membranes: Relating membrane performance to surface charge characteristics. Chem. Eng. J. 335, 101–109 (2018). https://doi.org/10.1016/j.cej.2017.10.140

- H. Fan, J. Gu, H. Meng, A. Knebel, J. Caro, High-flux membranes based on the covalent organic framework COF-LZU1 for selective dye separation by nanofiltration. Angew. Chem. Int. Ed. 57(15), 4083–4087 (2018). https://doi.org/10.1002/anie.201712816

- Y.T. Nam, J. Choi, K.M. Kang, D.W. Kim, H.-T. Jung, Enhanced stability of laminated graphene oxide membranes for nanofiltration via interstitial amide bonding. ACS Appl. Mater. Interfaces 8(40), 27376–27382 (2016). https://doi.org/10.1021/acsami.6b09912

- S.P. Sun, T.A. Hatton, T.-S. Chung, Hyperbranched polyethyleneimine induced cross-linking of polyamide-imide nanofiltration hollow fiber membranes for effective removal of ciprofloxacin. Environ. Sci. Technol. 45(9), 4003–4009 (2011). https://doi.org/10.1021/es200345q

- G.-H. Yang, D.-D. Bao, D.-Q. Zhang, C. Wang, L.-L. Qu et al., Removal of antibiotics from water with an all-carbon 3D nanofiltration membrane. Nanoscale Res. Lett. 13(1), 146 (2018). https://doi.org/10.1186/s11671-018-2555-9

- Q. Dai et al., EverBatt: A closed-loop battery recycling cost and environmental impacts model. Argonne National Laboratory, ANL-19/16 (2019). https://doi.org/10.2172/1530874

- G.R.A. Bell, D.D. Symons, J.R. Pearse, Mathematical model for solids transport power in a decanter centrifuge. Chem. Eng. Sci. 107, 114–122 (2014). https://doi.org/10.1016/j.ces.2013.12.007