Supporting Information for

# Breaking the Specific Capacity Limit: 409% Boost in Manganese-Based Redox Flow Batteries at High Current Densities with a MnO2 Semi-Solid Slurry Electrolyte

Xin Liu 1, 2#, Zhang Chen 1, 2#, Daiqi Zhou 1, 2, Qi Zhao 1, 2, Haitao Feng 3, Yuanyuan Cui 1, 2, *, Changsheng Ding 1, 2, * and Yanfeng Gao 1,2,*

1 School of Materials Science and Engineering, Shanghai University, Shanghai 200444, P. R. China

2 State Key Laboratory of Advanced Refractories, Shanghai University, Shanghai 200444, P. R. China

3 Key Laboratory of Comprehensive and Highly Efficient Utilization of Salt Lake Resources, Qinghai Institute of Salt Lakes, Chinese Academy of Sciences, Xining 810008, P. R. China

#Xin Liu and Zhang Chen have contributed equally to this work.

*Corresponding authors. E-mail: cui-yy@shu.edu.cn (Yuanyuan Cui); dingcs@shu.edu.cn (Changsheng Ding); yfgao@shu.edu.cn (Yanfeng Gao)

Supplementary Figures

Fig. S1 Optical photographs of 0.5 M, 1.5 M, 2.5 M and 3.5 M MnO2 semi-solid slurry electrolytes.

Fig. S2 Optical photographs of the MnO2 semi-solid electrolyte at different standing times.

Fig. S3 The conductivity of slurry electrolytes with different concentrations of MnO2.

Fig. S4 The charge–discharge curves of the batteries with 3.0 M MnO2 at the electrode area of 4 cm2.

Fig. S5 Rate performance of the 1.0 M MnO2 semi-solid slurry electrolyte at the electrode area of 4 and 25 cm2.

Fig. S6 Charge-discharge curves at 30 mA cm-2 under different MnO2 concentrations for a) 4 cm2 (areal capacity: 143.4 mAh cm-2) and b) 25 cm2 (areal capacity: 125 mAh cm-2) electrodes.

Fig. S7 The 1st and 2nd charge–discharge curves of the semi-solid slurry electrolyte with 4 M MnO2 at the current density of 1 mA cm-2.

Fig. S8 The charge-discharge curves at a current density of 50 mA cm-2.

Fig. S9 Energy cost calculation of 4 M MnO2 semi-solid slurry electrolyte compared to other type RFBs.

Fig. S10 Comparison of the current density and specific capacity for semi-solid RFBs.

Fig. S11 Optical photographs of the semi-solid slurry electrolytes with different concentrations of MnO2 after 2nd cycle.

Fig. S12 The utilization rate of converting MnO2 to Mn2+ in semi-solid slurry electrolyte.

Fig. S13 The viscosity measurements of the electrolyte after MnO2 dissolution into soluble Mn2+.

Fig. S14 The concentrations of H⁺ consumed in the anolyte electrolyte after the 2nd cycle at different MnO2 concentrations.

Fig. S15 CV results of the semi-solid slurry electrolytes with a) 0.5 M, b) 1.0 M, c) 1.5 M, d) 2.0 M, e) 2.5 M, f) 3.0 M, g) 3.5 M and h) 4.0 M MnO2 after 2nd cycle at various scan rates.

Fig. S16 SEM images of commercial MnO2 deposited on graphite felt electrodes.

Fig. S17 TEM images of MnO2 corresponding to Pot I and the corresponding magnified view (areas A and B).

Fig. S18 The particle size distribution plots of a) commercial and b) electrolytic MnO2.

Fig. S19 TEM image of electrolytic MnO2 corresponding to Pot Ⅴ.

Fig. S20 Circuit fitting and charge transfer resistances of the commercial MnO2 and electrolytic MnO2.

Fig. S21 a) CV result of the electrolytic MnO2 (Pot Ⅴ) at various scan rates and b) the relationship between oxidation and reduction peak current and scanning rate.

Fig. S22 Optical photographs of 1 M commercial MnO2 and electrolytic MnO2 (Pot Ⅴ) semi-solid slurry electrolytes.

Fig. S23 The charge-discharge curves for the electrolyte without Na4P2O7.

Fig. S24 The specific capacity-voltage profiles of the 1.5 M MnO2 electrolyte at the electrode area of 4 cm2.

Fig. S25 The specific capacity-voltage profiles of the a) 2.0 M MnO2, b) 3.0 M MnO2 and c) 4.0 M MnO2 electrolyte at the electrode area of 25 cm2.

Fig. S26 Evolution of Mn and Fe concentrations in the catholyte and anolyte over 40 cycles using a 1.5 M MnO2 electrolyte with 4 cm2 electrode area.

Fig. S27 The electrodes after long-term cycling at a) 1.0 M, b) 3.0 M and c) 4.0 M MnO2 with 25 cm2 area.

Fig. S28 a) The capacity–voltage profiles and b) long-term cycling performance of Fe/Mn and V/Mn SSFBs.

Table S1 The specific capacity, areal capacity and Mn species concentration in solution of semi-solid slurry electrolyte in this study.

| MnO2 concentration (4 cm2) | Specific Capacity (Ah L-1 Catholyte) | Areal Capacity (mAh cm-2) | Mn species concentration |
| --- | --- | --- | --- |
| 0.5 M |  | 51.2 | 143.3 | 1.38 M |
| 1.0 M | 75.8 | 192.0 | 1.83 M |
| 1.5 M | 98.4 | 284.3 | 2.22 M |
| 2.0 M |  | 109.7 | 369.0 | 2.58 M |
| 2.5 M | 121.8 | 411.4 | 2.99 M |
| MnO2 concentration (25 cm2) |  |  |  |
| 2.0 M | 111.6 | 89.3 | 2.62 M |
| 2.5 M | 120.2 | 96.2 | 2.97 M |
| 3.0 M | 134.9 | 107.9 | 3.25 M |
| 3.5 M | 147.7 | 118.1 | 3.49 M |
| 4.0 M | 156.2 | 125.0 | 3.76 M |

Energy cost calculation (Cenergy):

The chemical cost of storage can be calculated from equation (1): [31,32]

Cenergy= Cchemical + Ctankεsys,d × εq.rt × εv,d     (1)

The definitions of terms were list below:

| Term | Definition |
| --- | --- |
| Cchemical | Combined cost of chemicals used in the negolyte and posolyte |
| Ctank | Bulk tank price (0.15 US$ L-1) normalized by the energy density (kWh L-1) |
| εsys,d | System round trip efficiency taken as a constant of 0.94 |
| εq.rt | Coulombic efficiency of system |
| εv.d | The discharge voltage divided by cell open circuit voltage |

All the references in supplementary information are also cited in main-text

Assuming a 1 Ah system, the chemical cost can be calculated based on equation. 2-4:[31,32]

Cchemical= Cost of negolyte + Cost of posolyteOCV × 1 × 0.001     (2)

Cost of negolyte (US$) =[Pa×Ca+Pa,s×Ca,s]× 1 AhCaPa     (3)

Cost of posolyte (US$) =[Pc×Cc+Pc,s ×Cc,s]× 1 AhCaPc     (4)

The definitions of terms were list below:

| Term | Definition |
| --- | --- |
| Pa and Pc | Price (𝑉𝑆$ mol−1) of active materials |
| Ca and Cc | Concentration (𝑛𝑜𝑚 𝐿−1) of the active materials |
| Pa,s and Pa,s | Price (𝑉𝑆$ mol−1) of supporting materials |
| Cc,s and Cc,s | Concentration (𝑛𝑜𝑚 𝐿−1) of the supporting materials |
| Capa and Capc | Capacity (Ah L-1) at the given concentration |

All the references in supplementary information are also cited in main-text.

The bulk prices for chemicals are listed, and the chemical cost calculation details by using the above equations are presented in Table S3-S6.

Table S2 Calculation of chemical cost of negolyte in this work

|  | Bulk price (US$ kg-1) | Concentration (mol L-1) | MW (kg mol-1) | Capacity (Ah L-1) | Cost (US$ Ah-1) |
| --- | --- | --- | --- | --- | --- |
| Fe2(SO4)3 | 0.3 | 0.5 | 399.878 | 38 | 0.001578 |
| FeSO4·7H2O | 0.878 | 1 | 278.01 |  | 0.006423 |
| MnSO4·H2O | 0.35 | 1 | 169.01 |  | 0.001557 |
| H2SO4 | 0.075 | 3 | 98 |  | 0.00058 |
| Chemical Cost of Negolyte (US$ Ah-1) |  |  |  |  | 0.010139 |

All the price from https://www.alibaba.com.

Table S3 Calculation of chemical cost of posolyte in this work

|  | Bulk price (US$ kg-1) | Concentration (mol L-1) | MW (kg mol-1) | Capacity (Ah L-1) | Cost (US$ Ah-1) |
| --- | --- | --- | --- | --- | --- |
| MnSO4·H2O | 0.35 | 1 | 169.01 | 156.2 | 0.000379 |
| Fe2(SO4)3 | 0.3 | 0.5 | 399.878 |  | 0.000384 |
| Na4P2O7·10H2O | 7.027 | 0.1 | 446.05 |  | 0.002007 |
| MnO2 | 1.5 | 4 | 86.937 |  | 0.003339 |
| H2SO4 | 0.075 | 3 | 98 |  | 0.000141 |
| Chemical Cost of Posolyte (US$ Ah-1) |  |  |  |  | 0.00625 |

All the price from https://www.alibaba.com.

Table S4 Calculation of chemical cost of negolyte and posolyte in Ref. 21

|  | Bulk price (US$ kg-1) | Concentration (mol L-1) | MW (kg mol-1) | Capacity (Ah L-1) | Cost (US$ Ah-1) |
| --- | --- | --- | --- | --- | --- |
| MnBr2 | 10.5 | 2 | 214.746 | 200 | 0.022548 |
| MnSO4·H2O | 0.35 | 1 | 169.01 |  | 0.000296 |
| HClO4 | 98.385 | 2 | 100.46 |  | 0.098838 |
| Chemical Cost (US$ Ah-1) |  |  |  |  | 0.121682 |

All the price from https://www.alibaba.com.

Table S5 Calculation of energy cost

|  | This work | Ref.21 |
| --- | --- | --- |
| Cost of negolyte (US$ Ah-1) | 0.00625 | 0.121682 |
| Cost of posolyte (US$ Ah-1) | 0.010139 | 0.121682 |
| OCV (V) | 0.79 | 2 |
| Cchemical (US$ kWh-1) | 20.74557 | 121.682 |
| Ctank (US$ kWh-1) | 6.212217 | 0.83333 |
| εsys,d | 0.94 | 0.94 |
| εq.rt | 0.99 | 0.99 |
| εv.d | 0.81 | 0.76 |
| Cenergy (US$ kWh-1) | 35.76318 | 173.2263 |

Table S6 The comparison of specific capacity, areal capacity, current density and energy cost for reported Mn-based RFBs

| Battery Type | Specific Capacity (Ah L-1 Catholyte) | Areal Capacity (mAh cm-2) | Current Density (mA cm-2) | Energy cost (US$ kWh-1) | Ref |
| --- | --- | --- | --- | --- | --- |
| Zn-Mn |  | 18 | 40 | 20 | / | 13 |
| Fe-Mn | 36 | 142 | 50 | 53 | 15 |
| Cd-Mn | 200 | 61 | 10 | 173 | 21 |
| Zn-Mn |  | 105 | / | 30 | / | 22 |
| Zn-Mn semi-solid slurry | 92 | / | 1 | 48 | 29 |
| Zn-Mn semi-solid slurry | 25 | / | 0.2 | / | 30 |
| Zn-Mn | 30 | 20 | 40 | / | 34 |
| S-Mn | 40 | 100 | 10 | / | 35 |
| Zn-Mn | 25 | 50 | 20 | / | 36 |
| Zn-Mn | 40 | 80 | 20 | / | 37 |
| Fe-Mn semi-solid slurry | 156 | 125 | 30 | 36 | This work |
|  | 125 | 100 | 40 |  |  |
|  | 183 | 146 | 1 |  |  |

All the references in supplementary information are also cited in main-text.

Table S7 The comparison of specific capacity and current density for reported semi-solid RFBs

| Semi-solid electrolyte | Specific Capacity (Ah L-1) | Current Density (mA cm-2) | Ref |
| --- | --- | --- | --- |
| 11 vol% MnO2 + 4.2 vol% CB | 92 | 1 | 29 |
| Mn3O4@C-MWCNTs | 25 | 0.2 | 30 |
| 10 wt% SiOx |  | 98 | 0.2 | 38 |
| 10 wt% SiOx@LiPN/S | 207 | 0.2 | 39 |
| 5 vol% S-HCS | 82.6 | 1 | 40 |
| 24 vol% CSP@C-LiPAA |  | 280 | 0.3 | 41 |
| 40 vol% LPF-CF | 68 | 0.1 | 42 |
| 20 vol% LFP-PVP | 29 | 1.67 | 43 |
| 138 g L-1 S-KB@rGO | 139 | 0.5 | 44 |
| 150 g L-1 FeSe2 | 36.4 | 24 | 45 |
| Fe3O4 | 99.2 | 20 | 46 |
| Polyoxometalate colloid | 6.3 | 20 | 47 |
| 4 M MnO2 | 156 | 30 | This work |
|  | 125 | 40 |  |
|  | 183 | 1 |  |

All the references in supplementary information are also cited in main-text.

Supplementary Note S1

In this work, MnSO4 and Fe2(SO4)3 were selected as the cathode and anode soluble active species of the battery, respectively, and their respective redox reactions during 1st charging are as follows:

Cathode: Mn3+ + e- ↔ Mn2+ (1.56 V vs SHE)

Anode: Fe2+ ↔ Fe3+ + e- (0.77 V vs SHE)

Adding MnO2 solid particles to the pristine electrolyte requires extra FeSO4 in the anolyte to match the MnO2 electrochemical reaction. The electrochemical reactions occurring during the 1st discharge are presented below.

Cathode: MnO2 + 4H+ + 2e- → Mn2+ + 2H2O (1.22 V vs SHE)

Anode: Fe2+ - e- ↔ Fe3+ (0.77 V vs SHE)

According to the electrochemical equations, 2 M of Fe2+ are required for the complete reaction of 1 M MnO2. Given the low solubility of FeSO4 (≤ 1 M), a larger anolyte volume is necessary primarily to supply sufficient Fe2+ for the reaction, with proton provision serving as an ancillary function. A reduction in anolyte volume lowers the total Fe2+ content, thereby reducing the amount of MnO2 that can react and the corresponding proton demand for charge balance.