Supporting Information for

Aligning Out-of-Plane Polarization in 2D Ferroelectric Perovskite Wafer Boosts Interlayer Carrier Transport for Efficient X-Ray Detection

Chenhao Deng1, Shihai You1, *, Haiqing Zhong2, Xiankan Zeng1, Xiaolong Hao1, Jiasheng Xie1, Zheng Zhou1, Zhangjian Jin1, Huang Ye2, Lijun Xu2, Jianbo Wu3, Panpan Dong1, Wen Li1, Xingxing Jiao1, Weiqing Yang1, *

1 Key Laboratory of Advanced Technologies of Materials (Ministry of Education), School of Materials Science and Engineering, Research Institute of Frontier Science, Southwest Jiaotong University, Chengdu 610031, P. R. China

2 State Key Laboratory of Functional Crystals and Devices, Fujian Institute of Research on the Structure of Matter, Chinese Academy of Sciences, Fuzhou 350002, P. R. China

3 Department of Materials Science and Engineering, City University of Hong Kong, Hong Kong SAR 999077, P. R. China

* Corresponding authors. E-mail: shihai.you@swjtu.edu.cn (Shihai You); wqyang@swjtu.edu.cn (Weiqing Yang)

S1 Supporting Figures

Fig. S1 a) Inorganic layer of (Mpda)PbBr4 constructed by distorted [PbBr6] octahedra through corner-sharing. b) Pb-Br bond lengths in two distinct [PbBr6] octahedra (labeled with 1 and 2).

According to the formula [S1],

∆d=1616di-d0d02#(S1)

in which Δd denotes the degree of distortion, and di and d0 are individual and average Pb-Br bond lengths. The distortion degrees of the two [PbBr6] octahedra are calculated to be 30×10-5 (1) and 25×10-5 (2), respectively, showing they are highly distorted.

Fig. S2 Comparison of simulated and experimental powder XRD patterns of (Mpda)PbBr4.

Fig. S3 TG curve of (Mpda)PbBr4 powders under N2 atmosphere.

Fig. S4 XRD patterns of (Mpda)PbBr4 wafers under different hot-pressing parameters: a) holding time, b) temperature, c) pressure, and d) different pressure with temperature of 170 °C. This systematically study gives the optimal fabrication parameters: 170 °C, 300 MPa, and 60 min.

Fig. S5 XPS spectrum of (Mpda)PbBr4 scanning from 0 to 1200 eV.

Fig. S6 Frequency-dependent relative dielectric constant of (Mpda)PbBr4 wafer.

Fig. S7 The PFM topography of (Mpda)PbBr4 film.

Fig. S8 Schematic configuration of the (a) out-of-plane (vertical) and (b) in-plane (lateral) directions in (Mpda)PbBr4 wafer.

Fig. S9 Attenuation efficiency of (Mpda)PbBr4, Si, α-Se, and (PEA)2PbBr4 for 20 keV X-rays versus thickness.

Fig. S10 Photograph of Ag/(Mpda)PbBr4 wafer/Ag vertical device.

Fig. S11 Comparison of photocurrent response of (Mpda)PbBr4 wafer as fabricated and after poling under X-ray irradiation (external bias of 1 V), showing a significant enhancement.

Fig. S12 J-t curves of (Mpda)PbBr4 wafer detector under X-ray irradiation operated under different external bias voltages (e.g., 1, 2, 4, and 8 V).

Fig. S13 J-t curves of (Mpda)PbBr4 wafer detector under low dose rate X-ray irradiation.

Fig. S14 Detection limits of (Mpda)PbBr4 wafer detector operated at different bias voltages.

S2 Supporting Tables

Table S1 The atomic coordinates of Pb and N in crystal structure of (Mpda)PbBr4 collected at 293 K [S2]

| Atom | Atomic coordinate |  | Coordinate of charge center |
| --- | --- | --- | --- |
| Pb | Pb1i (0.74103, 0.60812, 0.04472) | Pb1ii (0.24103, 0.39188, 0.54472) | (0.49103, 0.5, 0.29472) |
|  | Pb2i (0.23971, 0.09787, 0.04251) | Pb2ii (0.73971, 0.90213, 0.54251) | (0.48971, 0.5, 0.29251) |
| N | N1i (0.75060, 0.17830, 0.93020) | N1ii (0.25060, 0.82170, 0.43020) | (0.50060, 0.5, 0.68020) |
|  | N2i (0.42340, 0.99500, 0.71321) | N2ii (0.92340, 0.00500, 0.21321) | (0.67340, 0.5, 0.46321) |
|  | N3i (0.24680, 0.52590, 0.92020) | N3ii (0.74680, 0.47410, 0.42020) | (0.49680, 0.5, 0.67020) |
|  | N4i (0.93550, 0.50800, 0.71320) | N4ii (0.43550, 0.49200, 0.21320) | (0.68550, 0.5, 0.46320) |

According to the point charge model, we assume that the centers of the positive charges of Mpda cation and the centers of negative charges of [PbBr6] octahedra are locating at N and Pb atoms, respectively.

Thus, spontaneous polarization intensity (Ps) along the c-axis,

Ps = (qNrN + qPbrPb) × Z × c / V

= [(e × 0.68020) × 2 + (e × 0.46321) × 2 + (e × 0.67020) × 2 + (e × 0.46320) × 2 + (-2e × 0.29472) ×2 + (-2e × 0.29251) ×2] × 20.13716 ×10-10 / (1366.35 ×10-30)

= 1.6 × 10-19 × 2.2047 × 20.13716 / 1366.35 × 1020 C m-2

Table S2 Detection performance comparison between (Mpda)PbBr4 wafer and some recently reported 2D MHP X-ray detectors

| Compound | Electric field (V mm-1) | Sensitivity (µC Gy-1 cm-2) | Detection limit (nGy s-1) | Form | Direction | Refs |
| --- | --- | --- | --- | --- | --- | --- |
| (Mpda)PbBr4 | 0 | 483.6 | 15.5 | wafer | out-of-plane | This work |
|  | 1.67 | 705.4 | 18.6 | wafer |  |  |
|  | 3.33 | 1011.5 | 12.6 | wafer |  |  |
|  | 6.67 | 1112.1 | 10 | wafer |  |  |
|  | 13.33 | 1395.5 | 9.6 | wafer |  |  |
|  | 26.67 | 2285 | 7.2 | wafer |  |  |
| (F-PEA)3BiI6 | 100 | 52.6 | 30 | wafer | out-of-plane | [S3] |
| (PEA)2PbI4 | 50 | 28.1 | - | film | in-plane | [S4] |
| (HIS)2AgBiBr8 | 3.1 | 252.38 | 68.9 | single crystal | out-of-plane | [S5] |
| (NH4)3Bi2I9 | 6.5 | 803 | 55 | single crystal | out-of-plane | [S6] |
| (PEA)2PbBr4 | 100 | 1303.9 | 8.8 | single crystal | out-of-plane | [S7] |
| (HIS)2AgSbBr8 | 33.3 | 223 | 84.2 | single crystal | out-of-plane | [S8] |
| (Br-PEA)2PbI4 | 80 | 1003 | 36 | single crystal | in-plane | [S9] |
| (4ABA)PbI4 | 25 | 572 | 7.5 | single crystal | out-of-plane | [S10] |
| (Br-BA)2PbBr4 | 150 | 531.33 | 100 | single crystal | out-of-plane | [S11] |
| (o-F-PEA)2PbI4 | 1250 | 1724.5 | 460 | single crystal | in-plane | [S12] |
| (BA)2PbI4 | 10 | 148 | 241 | single crystal | out-of-plane | [S13] |
| (BA)2PbBr4 | 12.5 | 544.8 | 523.3 | wafer | out-of-plane | [S14] |
| (PA)2PbBr4 | 12.5 | 827.3 | 60 | wafer | out-of-plane |  |
| (PEA)2PbBr4 | 12.5 | 3416.4 | 27 | wafer | out-of-plane |  |
| (BDA)PbI4 | 310 | 242 | 430 | single crystal | out-of-plane | [S15] |
| EA4Pb3Br10 | 60 | 2228.9 | - | wafer | in-plane | [S16] |

*PEA = phenylethylamine, HIS = histamine, 4ABA = 4-aminobenzylamine, BA = butylamine, PA = propylamine, BDA = 1,4-butanediamine, EA = ethylamine.

Supplementary References

- S. You, P. Yu, J. Wu, Z.-K. Zhu, Q. Guan et al., Weak X-ray to visible lights detection enabled by a 2D multilayered lead iodide perovskite with iodine-substituted spacer. Adv. Sci. Weinheim Baden Wurttemberg Ger. 10(21), e2301149 (2023). https://doi.org/10.1002/advs.202301149

- C.-C. Fan, C.-D. Liu, B.-D. Liang, M.-L. Jin, T.-Y. Ju et al., A two-dimensional hybrid lead bromide ferroelectric semiconductor with an out-of-plane polarization. Inorg. Chem. 62(32), 12634–12638 (2023). https://doi.org/10.1021/acs.inorgchem.3c02057

- M. Li, H. Li, W. Li, B. Li, T. Lu et al., Oriented 2D perovskite wafers for anisotropic X-ray detection through a fast tableting strategy. Adv. Mater. 34(8), 2108020 (2022). https://doi.org/10.1002/adma.202108020

- F. Liao, L. Lei, X. Gan, P. Li, G. Yao, Flexible 2D perovskite film for dual-mode X-ray detection and imaging. IEEE Electron Device Lett. 45(9), 1610–1613 (2024). https://doi.org/10.1109/LED.2024.3424470

- Y. Zhou, L. Huang, M. Wu, F. Kuang, K. An et al., A two-dimensional lead-free double perovskite for self-powered and high performance X-ray detection. J. Mater. Chem. C 12(44), 18048–18057 (2024). https://doi.org/10.1039/d4tc03465a

- R. Zhuang, X. Wang, W. Ma, Y. Wu, X. Chen et al., Highly sensitive X-ray detector made of layered perovskite-like (NH4)3Bi2I9 single crystal with anisotropic response. Nat. Photonics 13(9), 602–608 (2019). https://doi.org/10.1038/s41566-019-0466-7

- B. Jia, D. Chu, Y. Hu, Z. Zhao, J. Pi et al., Reducing energy loss of 2D perovskite single crystal for stable and efficient X-ray detection by quenching the radioluminescence. Adv. Mater. 38(5), e03463 (2026). https://doi.org/10.1002/adma.202503463

- Q. Fan, H. Xu, S. You, Y. Ma, Y. Liu et al., Centimeter-sized single crystals of Dion-jacobson phase lead-free double perovskite for efficient X-ray detection. Small Weinheim Der Bergstrasse Ger. 19(34), e2301594 (2023). https://doi.org/10.1002/smll.202301594

- H. Zhong, S. You, J. Wu, Z.-K. Zhu, P. Yu et al., Multiple interlayer interactions enable highly stable X-ray detection in 2D hybrid perovskites. JACS Au 4(6), 2393–2402 (2024). https://doi.org/10.1021/jacsau.4c00345

- Q. Fan, Y. Ma, S. You, H. Xu, W. Guo et al., Dion–jacobson phase perovskite crystal assembled by π-conjugated aromatic spacer for X-ray detectors with an ultralow detection limit. Adv. Funct. Mater. 34(9), 2312395 (2024). https://doi.org/10.1002/adfm.202312395

- Q. Gu, K. Chen, X. Zhang, S. Wang, S. Wu et al., Butylammonium-based chiral 2D perovskite single crystals for efficient UV circularly polarized light differentiation and high-performance X-ray detection. ACS Appl. Mater. Interfaces 17(11), 17127–17134 (2025). https://doi.org/10.1021/acsami.5c01035

- B. Zhang, Z. Xu, C. Ma, H. Li, Y. Liu et al., First-principles calculation design for 2D perovskite to suppress ion migration for high-performance X-ray detection. Adv. Funct. Mater. 32(15), 2110392 (2022). https://doi.org/10.1002/adfm.202110392

- Yukta, J. Ghosh, M.A. Afroz, S. Alghamdi, P.J. Sellin et al., Efficient and highly stable X-ray detection and imaging using 2D (BA)2PbI4 perovskite single crystals. ACS Photonics 9(11), 3529–3539 (2022). https://doi.org/10.1021/acsphotonics.2c00776

- W. Wu, J. Zhang, C. Liu, J. Zhang, H. Lai et al., Spontaneous cooling enables high-quality perovskite wafers for high-sensitivity X-ray detectors with a low-detection limit. Adv. Sci. Weinheim Baden Wurttemberg Ger. 11(46), e2410303 (2024). https://doi.org/10.1002/advs.202410303

- Y. Shen, Y. Liu, H. Ye, Y. Zheng, Q. Wei et al., Centimeter-sized single crystal of two-dimensional halide perovskites incorporating straight-chain symmetric diammonium ion for X-ray detection. Angew. Chem. Int. Ed. 59(35), 14896–14902 (2020). https://doi.org/10.1002/anie.202004160

- J. Wu, Q. Yin, S. You, R. Li, C. Lin et al., Oriented perovskite ferroelectric wafers for sensitive self-driven X-ray detection. Nano Res. 19(7), 94908302 (2026). https://doi.org/10.26599/nr.2025.94908302